SUPPLEMENTARY INFORMATION (SI)

ESM_1. N2 Adsorption-desorption of Mg/Al LDH (a), Mg/Al-TiO2 (b), and Mg/Al-ZnO (c)

ESM_2. BET analysis of catalysts

| Adsorbent | Surface Area (m2/g) | Pore Size (nm), BJH | Pore Volume (cm3/g), BJH |
| --- | --- | --- | --- |
| Mg/Al-LDH | 8.963 | 6.225 | 0.028 |
| Mg/Al-TiO2 | 17.199 | 7.010 | 0.060 |
| Mg/Al-ZnO | 14.830 | 4.489 | 0.033 |

ESM_3. UV-Vis spectrum of oxidative desulfurization dibenzothiophene by Mg/Al and composites (50℃, 300 rpm, 0.25 g catalysts, n-hexane solvent)

ESM_4. Effect of catalyst dosage to oxidative desulfurization of dibenzothiophene by Mg/Al and composites (50℃, 300 rpm, 30 min, n-hexane solvent)

ESM_5. Effect of various temperatures on oxidative desulfurization of dibenzotiophene using Mg/Al and composite catalysts (30 min, 300 rpm, n-hexane solvent)

ESM_6. Effect of solvent on oxidative desulfurization of dibenzothiophene by Mg/Al and composite catalysts (50℃, 300 rpm, 30 min)

ESM_7. Reusability of Mg/Al and composites catalysts son oxidative desulfurization of dibenzothiophene (50℃, 300 rpm, 30 min, n-hexane solvent)

ESM_8. FTIR spectrum of Mg/Al-TiO2 (a) and Mg/Al-ZnO (b) before and after oxidative desulfurization of third cycle processes.