Supporting Information

# Evaluation of films mechanical properties prepared from Furcellaria lumbricalis and Gigartina skottsbergii seaweeds by PF-QNM methodology

# Ivan Šimkovica · Filip Gucmannb · Raniero Mendichic · Alberto Giacometti Schieronid · Daniele Piovanid · Edmund Dobročkab· Miloš Hricovínia

aInstitute of Chemistry, Slovak Academy of Sciences, 845 38 Bratislava, Slovakia

bInstitute of Electrical Engineering, Slovak Academy of Sciences, Dúbravská cesta 9, 84104 Bratislava, Slovakia

cProblem Solving, Innovation Support Complex Polymeric and Elastomeric Materials

Analysis, Molecular and Rheological Characterization Complex Polymers

Via Roma 7, 20067 Tribiano, Milan, Italy

dIstituto di Scienze e Tecnologie Chimiche "G. Natta", Via A. Corti 12, 20133 Milan, Italy

Correspondence: Ivan Šimkovic (e-mail: chemsimk@savba.sk); ORCID: 0000-0003-4107-1529

# Content

# Table S1. NMR data of observed carrageenans [ppm].

# Figure S1. Graphical abstract

# Table S1. NMR data of observed carrageenans [ppm].

Unit              H1/C1                   H2/C2          H3/C3           H4/C4             H5/C5            H6/C6

αG          5.39/102.54    3.65/74.41   3.97/76.17    3.84/74.11     3.84/74.11   3.78, 3.89/63.40

αG6S        5.33/102.60    3.58/74.40   3.93/76.12    3.79/79.14     3.71/75.57   4.32, 4.35/72.08

α-G        4.65/104.99    3.63/71.86   3.87/82.70    4.15/68.58     3.71/77.67   3.82/63.63

α-DA2S    5.24/94.77      3.57/74.54   3.97/76.08    3.62/80.15     3.94/72.95   4.23, 4.30/71.19

β-G         4.64/104.92    3.63/71.86    3.87/82.70    4.15/68.58     3.71/77.67    3.82/63.63

β-DA       5.10/97.10      4.14/72.21   4.54/81.60    4.63/80.33     4.67/79.13     4.06, 4.22/71.51

κ-G4S      4.66/104.80     3.63/71.86   3.99/80.74    4.85/76.29     3.71/77.67     3.82/63.63

κ-DA       5.11/97.10       4.09/72.55   4.53/81.60    3.63/80.65     4.67/79.13     4.18/69.60

ι-G4S        4.61/104.80     3.63/71.68   4.03/79.20     3.84/74.10    3.82/77.19     3.83/63.68

ι-DA2S    5.22/94.77       4.70/77.33   4.86/80.09     4.71/80.72   4.69/79.36  4.27, 4.12/75.00

θ-G2S      5.39/102.55     3.65/80.05  3.77/79.06     4.16/70.28  3.97/76.22    3.87/63.52

θ-DA2S     5.22/98.50       3.52/73.00  3.25/75.00     3.83/80.50  3.77/79.06    4.32/72.00

µ-G4S      4.49/106.18     3.42/72.37  3.65/80.05     3.97/76.22  3.28/77.15   3.95, 3.72/68.73

µ-D6S     4.98/100.70     4.16/70.28  3.52/72.57     3.61/80.90  3.91/73.14   3.76, 3.98/68.73

λ-G2S     4.72/105.86     4.50/79.88   3.97/76.22    4.28/66.47   3.74/75.27   3.77, 3.87/63.52

λ-D2S,6S   5.63/93.87       3.60/77.52  4.15/71.84     4.25/82.99   4.58/71.16  3.72, 4.12/70.34

ν-G4S     4.49/106.18     3.43/72.37  4.42/82.97     3.91/73.15    3.60/77.52  3.77, 3.87/63.52

ν-D2S,6S  4.98/100.70     4.66/78.21  4.16/70.28     4.25/82.99    4.16/70.28  4.12, 4.14/70.31

ξ-G2S     4.71/105.84     4.50/79.88   3.97/76.22    4.28/66.47    3.74/75.27  3.77, 3.87/63.52

ξ-D2S       5.23/94.77            -                   -                    -                 -               3.73, 4.26/70.31

Graphical abstract

Quantitative values of four studied quantities determined by AFM and PF-QNM techniques.