Supporting Information

All-Flexible Chronoepifluidic Nanoplasmonic Patch Allows Label-free Sweat Profiling

Jaehun Jeon1,2, Sangyeon Lee1, Seongok Chae3, Joo Hoon Lee4, Hanjin Kim1, Eun-Sil Yu1,2, Hamin Na1,2, Taejoon Kang4, Hyung-Soon Park3, Doheon Lee1, and Ki-Hun Jeong1,2,*

1 Department of Bio and Brain Engineering, Korea Advanced Institute of Science and Technology (KAIST), 291 Daehak-ro, Yuseong-gu, Daejeon 34141, Republic of Korea

2 KAIST Institute for Health Science and Technology (KIHST), KAIST, 291 Daehak-ro, Yuseong-gu, Daejeon, Republic of Korea, 305-701

3 Department of Mechanical Engineering, Korea Advanced Institute of Science and Technology (KAIST), 291 Daehak-ro, Yuseong-gu, Daejeon, 34141, Korea

4 Bionanotechnology Research Center, Korea Research Institute of Bioscience and Biotechnology (KRIBB), 125 Gwahak-ro, Yuseong-gu, Daejeon 34141, Republic of Korea

*kjeong@kaist.ac.kr

Figure S1. (a) Detailed micro and nanofabrication of the CEP-SERS patch. (b) optical images of the fabrication step 3, 4, 5 (Scale bar: 5 mm), 7 (Scale bar: 10 mm), and (c) an optical image of the fully fabricated SERS patch conformally attached to human skin (Scale bar: 60 mm).

Figure S2. (a) Absorption spectra and (b) SEM images before (blue) and after (red) low-temperature solid-state dewetting of Ag thin film on fluorocarbon-coated PDMS (Scale bar: 100 nm). The Ag film and fluorocarbon thickness are 10 nm and 2 nm, respectively.

Figure S3. (a) Absorption spectra and (b) optical images of the Ag nanoislands on fluorocarbon-coated PDMS. Each color represents different fluorocarbon thicknesses. (Scale bar: 5 mm).

Figure S4. (a) SERS spectra of 10 μM R6G (b) SERS noise spectra of fluorocarbon depending on fluorocarbon thicknesses. The gray bars represent the wavenumber of 1365 cm-1.

Figure S5. (a) Measured diameter, packing density, and (b) absorption spectra of Ag nanoisland on fluorocarbon-coated PDMS depending on Ag film thickness. The error bars represent one standard deviation from the mean.

Figure S6. SEM images (left), binary images (middle), and calculated E-field enhancement (right) of Ag nanoislands on fluorocarbon-coated PDMS fabricated by (a) 10 nm and (b) 12 nm repeated dewetting (Scale bar: 100nm).

Figure S7. SERS spectra of 1 μM R6G using SERS substrate fabricated by (a) different Ag film thickness, dewetting repetition, and (b) fluorocarbon (FC) coating. The gray bars represent the wavenumber of 1365 cm-1. (c) Comparison of SERS peak intensity from different nanofabrication conditions.

Figure S8. SERS spectra of R6G depending on different concentrations. The gray bars represent the wavenumber of 1365 cm-1.

Figure S9. SERS enhancement factor and fabrication uniformity of the CEP-SERS patch measured from 30 different points.

Figure S10. Optical images of vacuum-sealed CEP-SERS patch for on-body evaluation.

Figure S11. (a) The measured contact angle of PDMS and CEP-SERS patch. (b) Bursting pressure (BP) calculated by the Young-Laplace equation depending on channel widths and diverging angles. Each marker represents a specific CBV and its BP. The error bars represent one standard deviation from the mean.

Figure S12. Two-phase fluid dynamic analysis of chrono-sampling through capillary bursting valves.

Figure S13. (a) Schematic illustration of sequential sample injection setup. Optical images of (b) microfluidic sequential sampler with different chamber volumes and (c) sequential sampling using the CEP-SERS patch with 0.5 μL chamber volume (Scale bar: 5 mm).

Figure S14. Normalized fluid and bubble fraction depending on storage duration with and without Ag nanoisland on fluorocarbon and encapsulation (Scale bar: 5mm). Right optical images show the sample storage after 6 hours. The error bars represent one standard deviation from the mean.

Figure S15. SERS spectra of (a) uric acid, (b) lactate, and (c) tyrosine depending on different concentrations. The gray bars represent the main SERS peak of each metabolite.

Figure S16. (a) Composition of the artificial sweat solution. (b) Schematic illustration for sequential injection of the artificial sweat solution with different uric acid concentrations. SERS spectra from chrono-sampled solution with (c) sparse and (d) dense sampling intervals.

Figure S17. Schematic illustration of machine-learned metabolic quantification using an autoencoder with a logistic regression model. The autoencoder-based prediction model is trained to minimize the total loss function, including latent loss(L0), intra-class loss(L1), distance from the centroid (L2), and inter-class loss(L3).

Figure S18. SERS spectra of different concentration ratios between (a) lactate/tyrosine, (b) uric acid/lactate, and (c) tyrosine/uric acid. Each SERS spectrum is an average of 36 different measurements.

Figure S19. Examples of SERS spectra for (a) uric acid, (b) lactate, (c) tyrosine, and (d) glucose in different mixture solutions. (e) SERS spectra of mixture solutions with different combinations of metabolites. Each SERS spectrum is an average of 36 different measurements.

Figure S20. Two-dimensional latent scores of (a) uric acid, (b) lactate, and (c) tyrosine from measured SERS signals with different concentrations. Each color represents the different concentrations of the target metabolite in the mixture solution.

Figure S21. Evaluation of machine-learned quantification through 10 times repeated random sampling cross-validation for (a) uric acid, (b) lactate, and (c) tyrosine.

Figure S22. (a) Schematic illustration of SHAP feature importance calculation. (b) Raw spectra of the normalized SHAP feature importance of uric acid (red), lactate (blue), and tyrosine (green).

Figure S23. (a) Experimental protocols of the on-body evaluation. (b) Optical images of sweat collection using microtube (left) and assorted activities (right). The triangular markers represent the sweat collection during exercise for sensor validation.

Figure S24. SERS spectra of (a) human sweat depending on participants and (b) various metabolites in sweat.

Figure S25. SERS spectra of chrono-sampled sweat under (a) fasting condition and (b) purine-rich diet intake (Participant 1). Each SERS spectrum is an average of 7 different measurements.

Figure S26. SERS spectra of chrono-sampled sweat under (a) fasting condition and (b) purine-rich diet intake (Participant 2). Each SERS spectrum is an average of 7 different measurements.

Figure S27. SERS spectra of chrono-sampled sweat under (a) fasting condition and (b) purine-rich diet intake (Participant 3). Each SERS spectrum is an average of 7 different measurements.

Figure S28. SERS spectra of chrono-sampled sweat under (a) fasting condition and (b) purine-rich diet intake (Participant 4). Each SERS spectrum is an average of 7 different measurements.

Figure S29. Measured sweat rate depends on the participants and body parts.

Figure S30. Chronological profiling of lactate, uric acid, tyrosine, heart rate, oxygen (VO2), and carbon dioxide (VCO2) uptake under (a-f) fasting condition and (g-l) purine-rich diet intake (Participant 1). The error bars represent one standard deviation from the mean.

Figure S31. Chronological profiling of lactate, uric acid, tyrosine, heart rate, oxygen (VO2), and carbon dioxide (VCO2) uptake under (a-f) fasting condition and (g-l) purine-rich diet intake (Participant 2). The error bars represent one standard deviation from the mean.

Figure S32. Chronological profiling of lactate, uric acid, tyrosine, heart rate, oxygen (VO2), and carbon dioxide (VCO2) uptake under (a-f) fasting condition and (g-l) purine-rich diet intake (Participant 3). The error bars represent one standard deviation from the mean.

Figure S33. Chronological profiling of lactate, uric acid, tyrosine, heart rate, oxygen (VO2), and carbon dioxide (VCO2) uptake under (a-f) fasting condition and (g-l) purine-rich diet intake (Participant 4). The error bars represent one standard deviation from the mean.

|  | SERS substrate | Flexibility | Functional microfluidic compatibility | Label | Analytes |
| --- | --- | --- | --- | --- | --- |
| CEP-SERS patch | Ag nanoislands on fluorocarbon-coated PDMS | High | High | Label-free | Multiple metabolites - Uric acid - Lactate - Tyrosine |
| Y. Wang et al., Sci. Adv. (2021) [46] | Ag nanocube in hydrogel film | High | Not demonstrated (Low) | Label-free | Single drug - Nicotine |
| U. Mogera et al., Sci. Adv. (2022) [58] | Au nanorod on paper | High | Low | Label-free | Single metabolite - Uric acid |
| X. He et al., npj Flex. Elect. (2022) [54] | Ag nanomushroom on Si wafer | Mediocre | Mediocre (Simple assembly) | Label-free & probe molecule | Dual metabolites & pH - Urea - Lactate |
| J. Xiao et al., ACS Sens. (2023) [53] | Au nanomushroom on Si wafer | Mediocre | Mediocre (Simple assembly) | Label-free | Single drug - Acetaminophen |
| W. Yu et al., Biosens. & Bioelect. (2024) [48] | Core-shell Au nanorod on textile | High | Not demonstrated (Low) | SERS tag (Label) | Dual metabolites - Lactate - Glucose |
| Z. Chen et al., Lab Chip (2024) [52] | Ag nanowire on paper | High | Low | Label-free | Single metabolite - Uric acid |
| H. Ye et al., Nano Letters (2024) [53] | Au nanoparticle on PDMS | High | Mediocre (Simple assembly) | Label-free & probe molecule | Single metabolite & pH - Lactate |
| M. Hu et al., Biosens. & Bioelect(2024) [55] | Au @ Ag nanocubes on silk | High | Mediocre (Simple assembly) | Label-free | Dual metabolites - Creatinine - Uric acid |
| H. Zhang et al., Nano Letters (2024) [57] | Template printed Au nanowire on PDMS | High | Mediocre (Simple assembly) | Probe molecule | pH |
| G. Li et al., Nano Letters (2024) [60] | Au & Al2O3 trimers in hydrogel | High | Mediocre (Simple assembly) | Label-free | Dual metabolites - Lactate - Uric acid |

Table S1. Comparison of recent advances in wearable SERS patch for human sweat analysis. Previously reported wearable SERS patches still encounter several major challenges to accomplish precise sweat profiling: (1) Absence of an all-flexible SERS patch compatible with sophisticated functional microfluidic channels limits precise fluid control, restricting accurate quantification and time-resolved analysis. (2) The high molecular complexity of sweat hinders the multiplexed quantification of metabolites.