Hydrothermal deposition as a novel method for the preparation of Co-Mn mixed oxide catalysts supported on stainless steel meshes: application to VOC oxidation

Pavel Topkaa,*, Květuše Jirátová a, Michaela Dvořákováb, Jana Balabánováa, Martin Koštejna, František Kovandab

aInstitute of Chemical Process Fundamentals of the Czech Academy of Sciences, Rozvojová 135, 165 02 Prague, Czech Republic

bDepartment of Solid State Chemistry, University of Chemistry and Technology, Prague, Technická 5, 166 28 Prague, Czech Republic

Supplementary material

Fig. S1. Powder XRD pattern of commercial Co-Mn-Al mixed oxide catalyst (Com). O – Co-Mn-Al mixed oxide.

Table S1. Binding energies of core level electrons determined by XPS.

| Co/(Co+Mn)a | Co 2p3/2b | Mn 2p3/2c | O 1s | O 1s | O 1s |
| --- | --- | --- | --- | --- | --- |
| 0 | - | 641.4 | 529.6 | 531.6 | 533.3 |
| 0.2 | 779.9 | 641.2 | 529.6 | 531.4 | 533.2 |
| 0.4 | 779.9 | 641.2 | 529.6 | 531.3 | 532.8 |
| 0.5 | 779.9 | 641.2 | 529.6 | 531.5 | 533.2 |
| 0.6 | 779.8 | 641.1 | 529.6 | 531.5 | 532.9 |
| 0.8 | 779.8 | 641.2 | 529.6 | 531.2 | 532.5 |
| 1.0 | 779.7 | - | 529.6 | 531.4 | 533.1 |

a Nominal molar ratio

b Position of the peak corresponding to Co2+

c Position of the peak corresponding to Mn3+