Table1. Physicochemical characteristics of furfural

| Chemical formula | Molecular weight | Chemical structure |
| --- | --- | --- |
| C5H4O2 | 96.08 g/moL |  |

Table 6. Comparison of the adsorption of furfural onto various adsorbents

| Adsorbent material | Maximum removal (%) | Conditions | Disadvantages | Environmental Impacts | ref |
| --- | --- | --- | --- | --- | --- |
| Activated Carbon | 60 | pH = 5.9 Adsorbent dosage = 10 g/L Initial concentration = 50 mg/L Time = 60 min Temperature = 303 K | • High production cost: The production process of activated carbon (pyrolysis and activation) can be energy-intensive and costly. • Source of raw materials: The use of non-renewable resources or deforestation for obtaining raw materials (such as certain types of wood or coal) can have negative environmental effects. • Disposal issues: Spent activated carbon that has adsorbed pollutants requires proper waste management. Landfilling it can lead to the release of pollutants, and incineration produces CO2. • Lack of selectivity: It may also adsorb some desirable substances. •Expensive regeneration: Regeneration of saturated activated carbon can also be energy-intensive and costly | • Greenhouse gas emissions: Production (especially pyrolysis) and disposal (incineration) can lead to CO2 emissions. • Water pollution: Improper disposal of contaminated activated carbon can lead to pollutants leaching into groundwater. • Habitat destruction: Harvesting raw materials can lead to deforestation and habitat loss. | (18) |
| torrefied biomass | 60 | pH = 2 Adsorbent dosage = 250 g/L Initial concentration = 50 mg/L Time = 30 min | • Processing cost: The torrefaction process requires energy and specialized equipment, which can increase production costs. • Need for sustainable resource management: If biomass harvesting is not done sustainably, it can lead to deforestation and soil degradation. • Energy efficiency: Compared to fossil fuels, it may have lower energy efficiency. | • CO2 emissions: Although lower than fossil fuels, combustion still produces CO2. However, since biomass absorbs CO2 during growth, its carbon cycle is closer to neutral. • Air pollution: Combustion can release particulate matter and other pollutants. • Impact on biodiversity: Large-scale cultivation of energy crops can impact biodiversity. | (69) |
| MCM-48 | - | pH = 6 Adsorbent dosage = 0.1 g/L Initial concentration = 1000 mg/L Time = 1 h Temperature= 298 K | Synthesis cost: The synthesis of mesoporous materials like MCM-48 may involve the use of specific chemicals and controlled reaction conditions, which can increase costs. Use of solvents: The synthesis process often involves the use of solvents, which can have environmental impacts if not managed properly. Scalability: Large-scale production may be challenging | Energy consumption: Synthesis and processing can be energy-intensive. Chemical emissions: The release of solvents and other chemicals during production can lead to air and water pollution. Waste generation: The synthesis process may generate chemical waste that requires proper management. | (16) |
| nanoclay modified with nZVI | 62.6% | pH = 7 Adsorbent dosage = 8 g/L Initial concentration = 10 mg/L Time = 150 min Temperature = 25 ± 2°C | Potential nanotoxicity: nZVI nanoparticles can be toxic to some microorganisms and living organisms, although surface modification can reduce these effects. Nanoparticle stability and aggregation: The behaviour and stability of nanoparticles in different environments are complex, and they may aggregate. Environmental fate and transport: The transport of nanoparticles in soil and groundwater is not yet fully understood. | Soil and water contamination: Uncontrolled release of nanoparticles can lead to contamination. Ecological effects: Long-term effects on soil and aquatic ecosystems require further investigation. Toxicity to living organisms: Depending on the concentration and type of modification, it can be toxic to some organisms. | This study |
| synthesize zero valent iron nanoparticles (NZVI) | 87 | pH = 2 Adsorbent dosage = 0.5g/L Initial concentration=100 mg/L Time = 60 min Temperature = 298 K Speed = 200 rpm | High reactivity and oxidation: nZVI is highly reactive and easily oxidizes when exposed to air and water, reducing its effectiveness. Aggregation: Nanoparticles tend to aggregate, which reduces their active surface area. Potential toxicity: As mentioned for nanoclay modified with nZVI, there is potential toxicity to some living organisms. Environmental fate and persistence: Their behaviour in the environment is complex, and their persistence can be a concern. | Potential contamination: Release can lead to contamination. Ecological effects: Effects on microorganisms and food chains require careful investigation. Formation of by-products: The reaction of nZVI with pollutants may produce unwanted by-products. | (70) |
| Organobentonite | - | pH = 7 Adsorbent dose = 2 g/L Contact time = 6 h Temperature = 30 0C Initial ﬂuoride concentration = 100 mg/L | • Use of organic modifiers: The organic materials used to modify bentonite can be toxic or release volatile organic compounds (VOCs) during production or use. • Stability of organic materials: The organic modifiers may degrade over time, reducing the adsorbent's effectiveness. • Impact on soil properties: Large-scale use in the environment may affect the physical and chemical properties of the soil. | • Contamination with organic materials: The release of organic modifiers can lead to water and soil pollution. • Toxicity of organic materials: Some organic materials can be toxic to living organisms. • Waste generation: Disposal of saturated organobentonite requires proper management. | (21) |