Supplementary Information

for

Oral Delivery of Transferrin Coated Rivastigmine Microspheres for Alzheimer’s Disease Therapy

Omkar Khaire, Kailash Ahirwar, Ajit Singh, Rahul Shukla1* and S.J.S. Flora2*

1Department of Pharmaceutics, National Institute of Pharmaceutical Education and Research (NIPER) – Raebareli, Lucknow, 226002, India

Table 1S. Independent Parameters and Level Values

| Actual coded value | (A) PCL weight (mg) | (B) PVA conc. (%) | (C) Stirring rate (r.p.m) |
| --- | --- | --- | --- |
| 1 | 200 | 0.6 | 10000 |
| 0 | 150 | 0.4 | 9000 |
| -1 | 100 | 0.2 | 8000 |

Table 2S. ANOVA of calculated model for responses

| Parameters | Particle Size | Uniformity | EE% |
| --- | --- | --- | --- |
| Model |  |  |  |
| Sum of Squares | 0.4502 | 0.0833 | 106.5 |
| df | 9 | 9 | 6 |
| Mean Square | 0.05 | 0.0093 | 17.75 |
| F-value | 67.38 | 54.66 | 23.43 |
| p-value | 0.0001 | 0.0002 | 0.0001 |
| Lack of Fit |  |  |  |
| Sum of Squares | 0.0037 | 0.0007 | 4.59 |
| df | 3 | 3 | 6 |
| Mean Square | 0.0012 | 0.0002 | 0.7645 |
| F-value | 1.52 | 2.26 | 1.04 |
| p-value | 0.3421 | 0.3210 | 0.5663 |

Table 3S. Comparative evaluated data between predicted value and observed value

| Independent variable | Predicted value | Observed value | Residual value |
| --- | --- | --- | --- |
| Particle size | 3.054 | 3.261 | 0.207 |
| Uniformity | 0.266 | 0.275 | 0.009 |
| EE% | 86.51 | 87.72 | 1.21 |

Table 4S. Characteristic Peaks of drug, excipients, and formulation in FTIR Spectra

| Sample | Functional group | Wave number) |
| --- | --- | --- |
| RHT | -C=O Str (amide) | 1600-1630 |
|  | -C-O Str (alcohol) | 1050 |
|  | -C-N Str | 1000-1250 |
|  | -C-H Str | 2960-2850 |
| PVA | O-H Str | 3700-3500 |
|  | -C-H Str | 2960-2850 |
|  | -C-O Str (alcohol) | 1050 |
|  | -C-H (bending) | 1465 |
| PCL | O-H Str | 3700-3500 |
|  | -C-H Str | 2960-2850 |
|  | -C=O Str (ester) | 1750-1730 |
|  | -C-O Str | 1050 |
| Transferrin | -C=O Str (amide) | 1600-1630 |
|  | N-H Str | 3500-3300 |
|  | -C-H (bending) | 1465 |
| Physical mixture | -C=O Str (amide) | 1600-1630 |
|  | O-H Str | 3700-3500 |
|  | -C-H (bending) | 1465 |
|  | -C-N Str | 1000-1250 |
| Uncoated formulation | -C-H Str | 2960-2850 |
|  | -C-N Str | 1000-1250 |
|  | -C-O Str (alcohol) | 1050 |
| Coated formulation | N-H Str | 3500-3300 |
|  | -C-H (bending) | 1465 |
|  | -C-O Str (alcohol) | 1050 |

Table 5S. Regression coefficient (R2) values of release kinetic model for pH 1.2, 6.8, and 7.4

| Fitted Model | pH | R2 |  |  |
| --- | --- | --- | --- | --- |
|  |  | Free Drug | UC-MS | C-MS |
| Zero Order Model | 1.2 | 0.9831 | 0.9919 | 0.9945 |
| Higuchi Model | 6.8 | 0.9479 | 0.9713 | 0.9754 |
| Higuchi Model | 7.4 | 0.9592 | 0.9718 | 0.9895 |

Note: The n value for the Higuchi model was calculated to be 0.9895. The 0.9895 < n showed non-fickian drug release pattern from both uncoated and transferrin coated microsphere.