Computational Study on Aluminum Corrosion Inhibitive Potentials of Preferred Thiosemicarbazide Derivatives

Terngu T. Uzah 1 * Okon O. Ekpenyong2 Ijah S. Ioryue3 Azuka N. Amitaye4

1 Department of Chemistry, Federal University of Petroleum Resources, Effurun, Nigeria.

2Department of Pure and Applied Chemistry, University of Calabar, Calabar Nigeria

3Department of Biochemistry, Federal University of Technology, Ikot Abasi, Nigeria.

4Department of Chemistry, Nigeria Maritime University, Okerenkoko, Warri South-West, Nigeria

*Corresponding Author. Email: uzah2t@gmail.com

Abstract

Aluminum has been a primary metal relic of cultural history since ancient times. They are still widely used today in many different industrial domains. Aluminum, however, is susceptible to the corrosion process in harsh conditions. Numerous traditional protective inhibitors have been developed to counteract this harmful behavior. Sadly, these preventive inhibitors come with several major side effects, including high costs and negative impacts on the environment and human health. Density functional theory (DFT) evaluations were used to extensively examine the potentiality of the E)-2-(4-methylbenzylidene)hydrazinecarbothioamide (MBHC) and N-phenylhydeazinecarbothioamide (PHC): toward the corrosion inhibition of the aluminum surface. The sulfur and nitrogen atoms over the structures of the compounds under investigation were nucleophilic, as indicated by the electrostatic potential (ESP) analysis results. The molecular orbital theory results demonstrated the superior corrosion inhibitor preference of MBHC over PHC. After identifying the optimal MBHC − Al (111) and PHC − Al (111) complex configurations, Monte Carlo simulations were carried out. Remarkably, the MBHC demonstrated a wider range of competence in the corrosion inhibition process of Al (111) than the PHC, as demonstrated by the adsorption energy values of − 461.73 and −163.43 eV, respectively. These results offer a basis for the creation of environmentally friendly inhibitors that prevent corrosion on aluminum surfaces.

Keywords: adsorption energy; DFT; Potentials; Aluminum; inhibitor; Simulation

Introduction

In the crust of the globe, aluminum is the third most frequent metal overall and the fourth most prevalent in the crust specifically. After iron, aluminum is typically regarded as the second most significant metal. It has unique mechanical characteristics because of its low density (2.7 g cm-3), which is just about one-third that of mild steel. As a result, aluminum and its alloys offer a high strength-to-weight ratio. In addition, a wide range of metal machining processes can be readily applied to them, and they exhibit good electrical and thermal conductivity. Furthermore, aluminum and its alloys have been fully recycled and reused, meaning that the items made from recycled metal are similar to those that were made before recycling in terms of quality and attributes [1]. Because of its excellent strength-to-weight ratio and affordable price, aluminum and its alloys are widely used in aerospace, automotive, electrical parts, building, packaging, and chemical industries [2-4]. In non-aggressive conditions, an Al2O3 coating naturally forms on the alloy surface to preserve aluminum.[5] Because of its numerous flaws and pores, the oxide layer is rapidly dissolved by corrosive OH- or Cl- ions. However, because key alloy components like copper and magnesium are present, aluminum and its alloys are highly susceptible to localized corrosion in harsh conditions. This alloy's microstructure is rather complicated, and several phases with different compositions have been found [6]. Since an oxide layer forms on aluminum and prevents the metal from oxidizing further, aluminum has a high level of corrosion resistance in both aqueous solutions and the environment. However, in some conditions, such as acidic media, aluminum becomes extremely prone to corrosion. There are already several efficient protection techniques available, including surface coatings, organic inhibitor addition, anodic oxidation protection, and plasma electrolytic oxidation protection [7-9]. Inhibitors, which prevent corrosion on metal surfaces by forming a protective coating on them, are the most widely used and least expensive of them across a variety of industries. Products with an organic base are frequently used to prevent corrosion. Organic compounds with heteroatoms (N, S, and O) in a conjugated system exhibit excellent efficacy in preventing metal corrosion [10-12]. The effectiveness of corrosion inhibition has been precisely established by experimental research, however, the precise mechanism by which inhibitors contribute most to corrosion inhibition has not been thoroughly addressed. Costs and time for research are significant. These issues are bridged by the theoretical study, which is now backed by sufficient hardware and software. The electron density of the molecule determines the corrosion inhibition efficiency, and theoretical research can determine this density with high accuracy. When evaluating corrosion inhibition in a molecule, theoretical research is just as important as actual research. 
Questions concerning experimental results based on the interactions of organic inhibitors with metal surfaces can be addressed using quantum chemical computations [13,14]. The performance of each inhibitor concerning its structure and orientation, as well as the mechanism by which an inhibitor clings to metal surfaces, may be fully explained by the use of the methods of density functional theory and Monte Carlo simulation [15, 16]. The corrosion inhibition of E)-2-(4-methylbenzylidene)hydrazinecarbothioamide (MBHC) and N-phenylhydeazinecarbothioamide (PHC) (Fig.1): on Al (111) surfaces are studied in this work, along with the impacts of quantum parameters and the molecule's adsorption process.

Fig.1 The chemical structures of MBHC and PHC

2.1 Computational Investigations

2.1.1 DFT Study

Studies on corrosion inhibition commonly employ the density functional theory (DFT). When it comes to organic compounds' ability to suppress corrosion, the DFT approach provides an accurate description. Predicting the chemical properties of chemical species, such as the maximum occupied molecular orbital–lowest unoccupied molecular orbital (HOMO–LUMO), electron affinity (A), ionization potential (I), energy gap (ΔE), hardness (η), fraction of electrons transferred (ΔN), softness (σ), and electronegativity (χ), is the main goal of research on inhibitors. The following paper used theoretical calculations to anticipate the effectiveness of the Thiosemicarbazide derivatives E)-2-(4-methylbenzylidene)hydrazinecarbothioamide (MBHC) and N-phenylhydeazinecarbothioamide (PHC) (Fig.1). Employing the Gaussian 09W programming suite, the B3LYP technique coupled to 6-311G+ (d,p) basis sets were utilized to optimize all compounds geometrically. This approach is widely used in the research of organic corrosion inhibitors. Then, several relevant global and local variables of the molecule's electronic configuration were computed. The I, A, ΔE, ΔN, η, σ, χ, ELUMO, and EHOMO as well as maps of electrostatic potential were also computed [14,17].

A=ELUMO					(1)

I=EHOMO					(2)

ΔE=ELUMO-EHOMO 			(3)

η=(δ2EδN2)v=(δμδN)v=ELUMO-EHOMO 2 		(4)

σ=2(δNδμ)v(r)=1η=2ΔEELUMO-EHOMO  		(5)

χ=-(EHOMO+ELUMO )2				(6)

ΔN=χAl-χinh 2×ηAl-ηinh            			(7)

Where, χAl = 4.26 eV and  χinh= absolute electronegativities of the aluminum and inhibitor respectively. ηAl = 0 eV and ηinh = absolute hardness of the aluminum and inhibitor respectively.

2.1.2 Monte Carlo simulation.

The interactions between the chemical compounds and metal surface were theoretically studied by the Monte Carlo simulation The simulation was conducted in Material Studio 2020 (Biovia, USA) using COMPASS force-field (condensed phase), on the Al (111) surface (three dimensions to the slab model) under periodic boundary conditions. The energies and chemical adsorption mechanisms components were calculated using the Ewald and atom-based summations, or responsibly to the Adsorption Locator module, built-in Materials Studio 2020 which used Monte Carlo simulations to pinpoint the most stable arrangement of the adsorbates on the Al (111) surface is the most stable of the many aluminum surfaces [18, 19],

3.1	Results

3.1.1 DFT Results

Table 1 is a list of the calculated quantum chemical parameters. Given structures that are optimized HOMO and LUMO density distribution of PHC and MBHC, Fig.2 shows that PHC has fewer adsorption centers than MBHC, indicating that MBHC has a higher capacity for high-protective adsorption. As a result, the high EHOMO energy increases the inhibition performance by reflecting a greater connection between the molecule and the metal surface through the donor-acceptor process. [16, 20] MBHC can readily interchange electrons with the iron surface, as evidenced by its higher EHOMO value of −0.218 eV compared to PHC's −0.210 eV. On the other hand, the fact that MBHC has a lower ELUMO value indicates that it is an excellent inhibitor of electron acceptance and supports its superior performance (−0.018 eV) over PHC (−0.042 eV) [17, 21]. Better adsorption on aluminum surfaces is indicated by the narrower energy gap (ΔE) of MBHC (0.1493 eV) [22]. Further quantum chemical characteristics were derived, including ionization potential (I = −EHOMO), electron affinity (A = −ELUMO), global softness (σ), global hardness (η), electronegativity (χ), and number of electron transfer (ΔN). The literature claims that a molecule with a high (η) value is less reactive, whereas a high (χ) value indicates that the molecule may find it difficult to transfer its electrons to an acceptor [23, 24]. The findings in Table 1 demonstrate that MBHC has lower (η) and (χ) values than PHC, indicating that it is more reactive and can transfer electrons through donor-acceptor interactions with metal molecules. [25]. Within a group of inhibitors, the electron donation tendency is described by the charge transfer rate ΔN. According to Lukovits [24, 26], the efficiency of the inhibition increases as the electron donor capacity at the steel/electrolyte increases if ΔN < 3.6. Table 1 displayed ΔN values are all 3.6 lower than the original values. Therefore, the quantum chemical characteristics of MBHC performed better at its level of inhibition than the PHC inhibitor.

Table 1. The quantum chemical variables for MBHC and PHC inhibitors using the B3LYP/6-31G+ (d, p) basis set.

| C | ELUMO | EHOMO | ΔE | η | Σ | Χ | ∆NAl |
| --- | --- | --- | --- | --- | --- | --- | --- |
| MBHC | -0.0180 | -0.2178 | 0.1493 | 0.0747 | 13.40 | 0.143 | -20.66 |
| PHC | -0.0422 | -0.2095 | 0.1673 | 0.0837 | 11.95 | 0.0948 | -18.54 |

| Inhibitor | MBHC | PHC |
| --- | --- | --- |
| Optimized |  |  |
| HOMO |  |  |
| LUMO |  |  |

Fig.2 The frontier molecular orbital density distribution for MBHC and PHC investigated compounds (Optimized, HOMO, and LUMO)

3.1.2	Electrostatic Potential (ESP) Map

ESP map displays the three-dimensional charge distribution of the molecule (Fig.3). This map aids in the visualization of the molecule's variable charge areas, which helps forecast electrophilic and nucleophilic molecule-attack scenarios [27]. The highest positive region vulnerable to nucleophile assault is shown as blue in the ESP plot. On the other hand, the negative region that is vulnerable to electrophilic attack is shown in red. The MBHC and PHC sulfur and nitrogen atoms are found to have the highest electron density. Consequently, it is expected that these atoms will actively participate in the adsorption process on the Aluminium surface.

| Inhibitor | ESP maps | Surface contour |
| --- | --- | --- |
| MBHC |  |  |
| PHC |  |  |

Fig.3 ESP maps and surface contours illustration of the MBHC and PHC investigated

3.1.3	Monte Carlo simulation.

To reduce the amount of contact area between the metal surface and corrosion-causing materials (such as water, acidic, or alkaline media), molecules need to align their structures as closely as possible in parallel to the metal surface. Adsorption is the term for this process. Therefore, Monte Carlo simulation was applied to determine and identify the inhibitors under evaluation and their ability to adsorb onto the surface of Al (111). Fig.4 shows the optimal MBHC and PHC adsorption mode on the aluminum surface under study.

Table 2 displays the molecule under investigation's adsorption characteristics, which include total energy, rigid adsorption energy, adsorption energy, and deformation energy. We have previously defined these parameters [18, 24] in our previous work. The total rigid adsorption energy before and after an adsorbate's surface relaxation is known as the "adsorption energy," and it is the most significant energy characteristic in adsorption. Table 2 indicates that the inhibitor attaches to the surface of Al (111) spontaneously based on the negative value of the adsorption energies [19]. The differential adsorption energy (dEad/dNi), which is the energy needed or released to remove a portion of the adsorbate (i.e., desorption energy), is defined by assuming that the surface energy of Al is zero. The inhibitor's adsorption energy of -461.73 kcal mol-1 for MBHC and 163.43 kcal mol-1 for PHC and its desorption energy of --461.73 kcal mol-1 (MBHC) and –80.754 kcal mol-1 (PHC) indicate that the adsorption process is substantially preferred. The inhibitor preferentially adsorbs on the Al (111) surface with little to no competition because it adsorbs with significantly less energy, even in the presence of water (--4.28 kcal mol-1) [24, 28].

Table 2 Results and descriptors measured by the Monte Carlo simulation for adsorption of MBHC and PHC molecules on Al (111)

| Compound | dEad/dNi | Adsorption energy | Rigid adsorption energy | Deformation energy | Total energy |
| --- | --- | --- | --- | --- | --- |
| MBHC | -461.73 | -461.73 | -30.707 | -431.02 | -3.272 |
| PHC | -80.75 | -163.43 | -55.83 | -107.61 | -5.75 |
| Water | -4.281 | -8.297 | -7.346 | -0.950 | -7.346 |

| Inhibitor | Side view | Top view |
| --- | --- | --- |
| MBHC |  |  |
| PHC |  |  |

Fig.4 The most appropriate conformation for adsorption of the MBHC and PHC molecules on Al (111)

4. Conclusion

The corrosion inhibition potential of E)-2-(4-methylbenzylidene)hydrazinecarbothioamide (MBHC) and N-phenylhydeazinecarbothioamide (PHC) was analyzed and measured using density functional theory calculations employing the B3LYP/6-31G+ (d,p) basis set. This was done to determine whether these compounds had a potentially strong ability to inhibit corrosion in aluminum and its alloys. In contrast to PHC, MBHC has a lower electronegativity and ΔE, (0.1612 eV) values, which may be attributed to the presence of an aromatic ring and heteroatom in its structure, which demonstrated a stronger and mutual connection between the inhibitor and the metallic surface according to the results of the Density Functional Theory analysis: Furthermore, the results showed that MBHC had the largest ΔN value (0.258232 eV), indicating improved chemical stability and reactivity. In light of this, MBHC is more likely than PHC to react as an electron donor.de, which effectively inhibits the corrosion of alloys including aluminum. MBHC was predicted by Monte Carlo simulations to function as a more potent anti-corrosion agent than PHC, particularly in acidic environments.

Acknowledgments

The authors would like to acknowledge the Federal University of Petroleum Resources, Effurun for creating an enabling environment for this research work.

Funding

This research received no external funding.

Author contributions

The manuscript was written with contributions from all authors.

Declaration

Competing interests The authors declare no conflict of interest.

Data availability

The datasets generated during the current study are available from the corresponding author upon reasonable request.

References

- Olufumilayo OJ, Olakunle OJ. Corrosion inhibition of Aluminum alloy by chemical inhibitors: An overview. IOP Conference Series: Material Science and Engineering 2021, 1107, 012170. https://doi.org/10.1088/1757-899X/1/012170.

- Rouniya AK, Shandilya P. Fabrication and experimental investigation of magnetic field assisted powder mixed electrical discharge machining on machining of aluminum 6061 alloys, Proceeding of the Institution of Mechanical Engineer Part B Journal of Engineering Manufacturer, 2019, 233, 2283–2291.

- Becker M. Chromate-free chemical conversion coatings for aluminum alloys, Corrosion Review, 2019, 37, 321–342. https://doi.org/10.1515/corrrev-2019-0032

- Emadi M, Beheshti H, Heidari-Rarani M, Aboutalebi FH. Experimental study of collapse mode and crashworthiness response of tempered and annealed aluminum tubes under axial compression, Journal of Mechanical Science and Technology, 2019, 33, 2067–2074. http://dx.doi.org/10.1007/s12206-019-0410-2

- Arrousse N, Fernine Y, Al-Zaqri N, Boshaala A, Ech-chihbi E, Salim R, El Hajjaji F, Alami A, Ebn Touhamie M, Taleb M. Thiophene derivatives as corrosion inhibitors for 2024-T3 aluminum alloy in hydrochloric acid medium. RSC Advances, 2022, 12, 10321. DOI: 10.1039/d2ra00185c

- Liu Y, Li XL, Jin JF, Liu JA, Yan YY, Han ZW, Ren LQ. Anti-icing property of bioinspired microstructure superhydrophobic surfaces and heat transfer model, Applied Surface Science, 2017, 400, 498–505. https://doi.org/10.1016/j.apsusc.2016.12.219

- Gummanar N, Mokshanatha PB, Dyapur P, Yallappa GN. Organic corrosion inhibitors for aluminum-based alloys –A Review. Letters in Applied NanoBioScience. 2023, 12, 4, 170.  https://doi.org/10.33263/LIANBS124.170

- Markus B. Chromate-free chemical conversion coatings for aluminum alloys. Corrosion Review, 2019, 37, 32-39, https://doi.org/10.1515/corrrev-2019-0032.

- Yang W, Xu D, Chen J, Liu J, Jiang B. Characterization of self-sealing MAO ceramic coatings with green or black color on an Al alloy. RSC Advances 2017, 7, 1597-1605, https://doi.org/10.1039/C6RA25415B.

- Verma C, Olasunkanmi LO, Ebenso EE, Quraishi MA, Obot IB. Adsorption behavior of glucosamine-based, pyrimidine-fused heterocycles as green corrosion inhibitors for mild steel: Experimental and Theoretical Studies. The Journal of Physical Chemistry C, 2016, 120, 11598-11611, https://doi.org/10.1021/acs.jpcc.6b04429.

- Iroha NB, Akaranta O. Experimental and surface morphological study of corrosion inhibition of N80 carbon steel in HCl stimulated acidizing solution using gum exudate from Terminalia Mentaly. SN Applied Sciences 2020, 2, 1514, https://doi.org/10.1007/s42452-020-03296-8.

- Nkem B, Iroha NB, Maduelosi NJ. Corrosion inhibitive action and adsorption behavior of justicia secunda leaves extract as an eco‐friendly inhibitor for aluminum in acidic media. Biointerface Research in Applied Science. 11 (5), 2021, 13019 – 13030. https://doi.org/10.33263/BRIAC115.1301913030

- Ebenso EE, Verma C, Olasunkanmi LO, Akpan ED, Verma DK, Lgaz H, Quraishi M. A. Molecular modeling of compounds used for corrosion inhibition studies: a review. Physical Chemistry Chemical Physics, 2021, 23, 19987−20027. https://doi.org/10.1039/D1CP00244

- Verma DK, Aslam R, Aslam J, Quraishi MA, Ebenso EE, Verma C. Computational modeling: theoretical predictive tools for designing of potential organic corrosion inhibitors. Journal of Molecular Structures. 2021, 1236, 130294. https://doi.org/10.1016/j.molstruc.2021.130294

- Sulaiman KO, Onawole AT, Faye O, Shuaib DT. Understanding the corrosion inhibition of mild steel by selected green compounds using chemical quantum-based assessments and molecular dynamics simulations. Journal of Molecular Liquids 2019, 279, 342−350. http://dx.doi.org/10.1016/j.molliq.2019.01.136

- Hadisaputra S, Purwoko AA, Hakim A, Prasetyo N, Hamdiani S. Corrosion inhibition properties of phenyl phthalimide derivatives against carbon steel in the acidic medium: DFT, MP2, and Monte Carlo simulation studies. ACS Omega 2022, 7, 33054−33066. https://doi.org/10.1021/acsomega.2c03091

- Khabazi,, ME, Chermahini AN. DFT study on corrosion inhibition by tetrazole derivatives: investigation of the substitution effect. ACS Omega 2023, 8, 9978−9994. https://doi.org/10.1021/acsomega.2c07185

- Uzah TT, Mbonu IJ. Insight into synergistic corrosion inhibition of thiourea and ZnCl2 on mild steel: Experimental and theoretical Approaches. Journal of Chemistry Letters, 2023; 4, 211-221.  https://doi: 10.22034/jchemlett.2024.413932.1135

- Bourzi H, Oukhrib R, El Ibrahimi B, Oualid HA, Abdellaoui Y, Balkard B, El Issami S, Hilali, M, Bazzi L, Len C.  Furfural analogs as sustainable corrosion inhibitors—predictive efficiency using DFT and Monte Carlo simulations on the Cu (111), Fe (110), Al (111) and Sn (111) surfaces in acid media. Sustainability 2020, 12, 3304; doi:10.3390/su12083304

- Guo L, Obot IB, Zheng X, Shen X, Qiang Y, Kaya S, Kaya C. Theoretical insight into an empirical rule about organic corrosion inhibitors containing nitrogen, oxygen, and sulfur atoms, Applied Surface Science, 2017, 406, 301–306. http://dx.doi.org/10.1016/j.apsusc.2017.02.134

- Uzah TT, Mbonu JI. Enhancing the inhibition action of acetamide with iodide ions for mild steel corrosion in 0.5 M H2SO4 environment. Letters in Applied NanoBioScience. 2024, 13, 1-16, https://doi.org/10.33263/LIANBS131.049.

- Fouda AS, Etaiw SHE, Ibrahim AM, El-Hossianya AA.  Insights into using two novel supramolecular compounds as corrosion inhibitors for stainless steel in a chloride environment: experimental and theoretical investigation. RSC Advance, 2023, 13, 35305–35320. https://doi.org/10.1039/d3ra07397a

- Kaya S, Kaya C. A new method for calculation of molecular hardness: A theoretical study, Computational and theoretical chemistry 2015, 1060, 66. https://doi.org/10.1016/j.comptc.2015.03.004

- Uzah TT, Mbonu JI, Gber TE, Louis H. Synergistic effect of KI and urea on the corrosion protection of mild steel in 0.5 M H2SO4: Experimental and computational insights. Results in Chemistry, 2023, 5, 1-9. https://doi.org/10.1016/j.rechem.2023.100981

- Uzah TT. DFT and Monte Carlo simulation for the prediction of corrosion inhibitive efficacy of selected thiosemicarbazide derivatives on Al (111) and Cu (111) Surfaces in Acidic Media. Journal of Medical and Nanomaterial Chemistry. 2024, 6, 81-94, https://doi.org/10.48309/JMNC.2024.1.7

- Jabri Z, El Ibrahimi B, Jarmoni K, Sabir S, Misbahi K, Rodi YK, Mashrai A, Hökelek T, Mague JT, Sebbar NK, Essassi E.   New imidazo[4,5-b] pyridine derivatives: synthesis, crystal structures, Hirschfeld surface analysis, DFT computations, and Monte Carlo simulations. Journal of Chemical Technology and Metallurgy, 57, 3, 2022, 451- 463. https://doi.org/10.2174/0929867330666230426111650

- Thakur A, Kumar A. Computational insights into the corrosion inhibition potential of some pyridine derivatives: A DFT approach. European. Journal of Chemistry, 2023, 14(2), 246-253.  https://dx.doi.org/10.5155/eurjchem.14.2.246-253.2408

- Benzidia B, Barbouchi M, Hsissou R, Zouarhi M, Erramli H, Hajjaji N.  A combined experimental and theoretical study of green corrosion inhibition of bronze B66 in 3% NaCl solution by Aloe saponaria (syn. Aloe maculata) tannin extract. Current Research in Green and Sustainable Chemistry 2022, 5, 100299. https://doi.org/10.1016/j.crgsc.2022.100299