Supplementary information

Environmental friendly multi-step processing of efficient mixed-cation mixed halide perovskite solar cells from chemically bath deposited lead sulphide

Sahel Gozalzadeh1, Farzad Nasirpouri1,*, Sang Il Seok2

1Faculty of Materials Engineering, Sahand University of Technology, Tabriz 51335-1996, Iran

2School of Energy and Chemical Engineering, Ulsan National Institute of Science and Technology (UNIST), 50 UNIST-gil, Eonyang-eup, Ulju-gun, Ulsan 689-798, Republic of Korea

*-Corresponding author: nasirpouri@sut.ac.ir; f_nasirpouri@yahoo.com

Table S1. Representative of different water-based metal precursors for synthesizing perovskite film and fabricating PSC.

| Metal precursor | Processing route | PSC configuration | PCE(%) | Year/Ref |
| --- | --- | --- | --- | --- |
| Pb | Magnetron sputtering of Pb film Spin coating of MAI/IPA solution | FTO/ZnO/MAPbI3/spiro-OMeTAD/Au | 3.08 | 2016 16 |
| PbO | Electrodeposition of PbO Exposing in iodine vapors Spin coating MAI | FTO/mp-TiO2/MAPbI3/spiro-OMeTAD/Au | 12.5 | 2015 17 |
| PbO | Electrodeposition of PbO film Spin-coating a layer of MAI | FTO/mp-TiO2/MAPbI3/spiro-OMeTAD/Au | 14.59 | 2015 18 |
| PbO2 | Anodic ED of PbO2 Exposing PbO2 to an excess of HI vapor Exposing PbI2 to MAI vapor | - | - | 2016 19 |
| PbO2 | Electrodeposition of PbO2 Immersing in HI/ethanol solution Immersing PbI2 samples in MAI solution | FTO/bl-TiO2/mp-TiO2/MAPbI3/carbon electrode | 10.19 | 2015 20 |
| Pb(NO3)2 | Spin coating Spin coating MAI solution | FTO/mp-TiO2/MAPbI3/spiro-OMeTAD/Au | 13.7 | 2017 21 |
| Pb(NO3)2 | Spin coating Dipping in MAI solution | FTO/mp-TiO2/MAPbI3/spiro-OMeTAD/Ag | 13.7 | 2017 22 |
| Pb(NO3)2 | Spin coating Dipping in MAI solution | FTO/bl-TiO2/mp-TiO2/MAPbI3/spiro-OMeTAD/Au | 12.58 | 2015 23 |
| Pb(NO3)2 | Sequential dipping in Pb(NO3)2 and MAI solution | FTO/bl-TiO2/mp-TiO2/ZnO/ MAPbI3/spiro-OMeTAD/MoO3/Ag | 12.41 | 2018 24 |
| PbSe | Physical vapor deposition of PbSe Exposing to iodine vapor In situ closed-space vapor transport for conversion to MAPbI3 | - | - | 2019 25 |
| PbS | Atomic layer deposition of PbS Exposure to iodine gas Dipping in (MAI) solution | - | - | 2015 26 |
| PbS | Depositing PbS via rf-sputtering Exposure to iodide gas (I2) Dipping into MAI solution | - | - | 2018 27 |
| PbS | Chemical bath deposition of PbS Transforming to CH3NH3PbI3 by CVD process | FTO/C-TiO2/CH3NH3PbI3/Spiro-MeOTAD/Ag | 4.65 | 2016 28 |
| PbS | Electrodeposition of PbS Exposure to iodide gas (I2) Dipping into MAI solution | FTO/bl-TiO2/mp-TiO2/MAPbI3/spiro-OMeTAD/Au | 7.72 | 2021 29 |

Table S2. Thickness of PbS, PbI2 and perovskite layer versus immersion duration inside chemical bath.

| Immersion time | Thickness (nm) |  |  |
| --- | --- | --- | --- |
|  | PbS | PbI2 | perovskite |
| 30 | 60 | 130 | 320 |
| 60 | 158 | 310 | 600 |
| 90 | 200 | 400 | 800 |

Figure S1. Energy dispersive X-ray analysis (EDAX) of bright regions in perovskite structure. Table in the inset of Figure shows the atomic percentage of the constituent elements present in the sample.

Table S3. Photovoltaic parameters of FTO/bl-TiO2/mp-TiO2/FA-based perovskite /spiro-OMeTAD/Au solar cells chemically deposited PbS as the metal precursor by using three step method (i) chemical bath deposition of  PbS ii)iodination at 120°C iii) exposing to FAI/MACl/MABr solution)

|  | Voc | Jsc | FF | PCE |
| --- | --- | --- | --- | --- |
|  | 0.857 | 21.24 | 45.04 | 8.20 |
|  | 0.837 | 20.49 | 42.43 | 7.28 |
|  | 0.867 | 21.25 | 43.15 | 7.96 |
|  | 0.837 | 20.76 | 44.45 | 7.73 |
|  | 0.797 | 21.32 | 44.92 | 7.64 |
|  | 0.877 | 21.06 | 43.87 | 8.11 |
| avg. | 0.845333 | 21.02 | 43.97667 | 7.82 |
| stdev. | 0.028577 | 0.329059 | 1.032621 | 0.340646 |

Table S4. Photovoltaic parameters of FTO/bl-TiO2/mp-TiO2/FA-based perovskite /spiro-OMeTAD/Au solar cells chemically deposited PbS as the metal precursor by using three step method (i) chemical bath deposition of  PbS ii)iodination at 155°C iii) exposing to FAI/MACl/MABr solution)

|  | Voc | Jsc | FF | PCE |
| --- | --- | --- | --- | --- |
|  | 0.918 | 21.43 | 57.67 | 11.35 |
|  | 0.908 | 21.42 | 58.02 | 11.28 |
|  | 0.877 | 21.44 | 55.67 | 10.48 |
|  | 0.898 | 21.58 | 56.72 | 10.99 |
|  | 0.908 | 21.37 | 57.71 | 11.20 |
|  | 0.918 | 21.61 | 56.57 | 11.23 |
| avg. | 0.9045 | 21.475 | 57.06 | 11.08833 |
| stdev. | 0.015411 | 0.096488 | 0.894874 | 0.321709 |

Figure S2. SEM images of perovskite films obtained from spin coating of three different FAI:MACl:MABr solutions including a)70:10:10 mg in 1 ml IPA b)85:10:10 mg in 1 ml IPA and c)100:10:10 mg in 1 ml IPA on PbI2.