Table 2 Random variable parameters considered for Montecarlo simulations.

| Description | Variable | Distribution | μ | σ | Reference |
| --- | --- | --- | --- | --- | --- |
| Surface Chloride concentration (marine atmosphere)* | Acs | Normal | 2.57 | 0.36 | Shekar et al., 2018 |
|  | εcs | Normal | 0 | 0.41 | Shekar et al., 2018 |
| Surface Chloride concentration (deicing salts) | Cs,deicing | Lognormal | 0.1 | 0.01 | Shekar et al., 2018 |
| Critical chloride concentration | Ccr,deicing | Lognormal | 0.04 | 0.004 | Shekar et al., 2018 |
|  | Ccr,marine | Beta (min 0.2 max 2.0) | 0.6 | 0.15 | Nava et al., 2023 |
| Reference diffusion coefficient (cm2/y) | Dref,deicing | Lognormal | 1.29 | 0.129 | Shekar et al., 2018 |
|  | Dref,marine | Normal | 4.98 | 0.996 | Biondini et al., 2014 |
| Aging factor | a | Beta (min 0.0 max 1.0) | 0.3 | 0.12 | Biondini et al., 2014 |
| Model error | β | Uniform | 1.0 | 0.2 | Vu and Steward 2000 |
| Environmental factor (marine atmosphere) | ke | Gamma | 0.676 | 0.114 | Hu et al 2021 |
| Curing factor | kc | Gamma | 0.8 | 0.1 | Hu et al 2021 |

* Cs,marine=Acs+wbεcs