Supplementary Material

Manipulating growth of hyperfine CsPbBr3 particles by confinement in ZIF-8 and resultant stability of perovskite: selective trace-level Hg2+ detection

Lingyu Jiang1, Li Xiang1, Jianshe Tang1,2*

1 Department of Environmental and Energy Engineering, Anhui Jianzhu University, Ziyun Road 292, Hefei 230601, China

2 Anhui Provincial Key Laboratory of Environmental Pollution Control and Resource Reuse, Ziyun Road 292, Hefei 230601, China

CONTACT Prof. Jianshe Tang

E-mail: tjs28@126.com

Department of Environment and Energy Engineering, Anhui Jianzhu University, 230601, Hefei, People's Republic of China

Tel: +86-551-63828122

TableS1 Summary of TRPL decay parameters

| Sample | τ1(ns) | A1 | τ2(ns) | A2 |  | τave(ns) |
| --- | --- | --- | --- | --- | --- | --- |
| CsPbBr3 | 1.47 | 2676.17 | 7.39 | 491.26 | 4.31 |  |
| CsPbBr3/ZIF-8 | 2.37 | 1741.51 | 10.78 | 486.58 | 7.07 |  |
| CsPbBr3/ZIF-8+Hg2+ | 1.16 | 6872.48 | 6.03 | 627.27 | 2.52 |  |

Figure S1 XPS high resolution spectra of Zn 2p(a) Cs 3d (b), Pb 4f (c) and Br 3d (d) of CsPbBr3/ZIF-8

Figure S2 The impact of ZIF-8 dosage (a,b) and reaction temperature (c,d) on the fluorescence intensity of CsPbBr3/ZIF-8 during the synthesis process.

Figure S3(a) Fluorescence spectra of CsPbBr3 at various concentrations of Hg2+(10~5000nM). (b) Linear fitting curve of F/F0 of the fluorescence of CsPbBr3 and -lg(CHg2+).