The influence of the multi-level structure under high drawing on the preparation of high strength Lyocell fiber

Shiqiang Cui, Yang Zhang, Changjun Liu, Shanhao Lou,Yue Zhang*, Yumei Zhang *, Huaping Wang

(College of Materials Science and Engineering, Donghua University, State Key Laboratory for Modification of Chemical Fibers and Polymer Materials, Shanghai 201620, China)

* Correspondence to: Yumei Zhang, E-mail: zhangym@dhu.edu.cn; Yue Zhang, E-mail: zhangyue@dhu.edu.cn

Tensile measurements of different Lyocell fiber.

Figure S1. Tenacity-elongation curves of Lyocell fiber at different draw ratio.

One-dimensional WAXD profiles of Lyocell fiber

Figure S2. One-dimensional WAXD profiles of Lyocell fiber at different draw ratio.

Figure S3. A schematic diagram of WAXD peak fitting result of Lyocell fiber

One-dimensional SAXS profiles of Lyocell fiber

Figure S4. The Guinier plot of Lyocell fiber at different draw ratio.

Figure S5. The Ruland plot of Lyocell fiber at different draw ratio.