Supporting Information

Two-dimensional ferroelectric channel transistors integrating ultra-fast memory and neural computing

Shuiyuan Wang1, Lan Liu1, Lurong Gan1, Huawei Chen1, Xiang Hou1, Yi Ding1, Shunli Ma1, David Wei Zhang1, Peng Zhou1,*

1ASIC & System State Key Lab., School of Microelectronics, Fudan University, Shanghai 200433, China

* Correspondence should be addressed to Peng Zhou: pengzhou@fudan.edu.cn

- The schematic of fabricated 2D α-In2Se3 FeCTs process flow

Figure S1 shows the detailed preparation process of 2D α-In2Se3 FeCTs. First, Al2O3 is deposited on the substrate by ALD as the bottom dielectric layer, the bottom h-BN and 2D α-In2Se3 channel layer is prepared by mechanical exfoliation. Then PVA assists the transfer of h-BN as the top dielectric layer, wet-removes the PVA sacrificial layer, and then uses electron beam lithography to form the electrode pattern. It is worth mentioning that Al2O3 grown by ALD produces electrostatic doping to the α-In2Se3 channel,1 so the bottom h-BN is needed to optimize the interface. And the transferred top h-BN not only serves as a dielectric, but also provides passivation to the α-In2Se3 channel to isolate the influence of the ambient atmosphere.2-4 Finally, source-drain and top gates are deposited by electron beam evaporation, and a heavily doped silicon substrate is used as the global gate.

Figure S1. Schematic of fabricated process flow, including dielectric layer deposition, bottom h-BN mechanical exfoliation, α-In2Se3 channel layer and top h-BN dielectric layer transfer, transfer sacrificial layer removal and electrodes deposition.

- 2D FeCTs morphology and Raman characterization

Figure S2a characterizes the surface morphology of 2D FeCTs by AFM, where the height of the channel α-In2Se3, the top and bottom h-BN are about 40nm, 20nm, 20nm, respectively. Figure S2b shows the Raman spectrum of h-BN with a clear 1366cm-1 peak position, which is consistent with previous reports.2

FigureS2. 2D FeCTs surface morphology and Raman characterization. (a) AFM height error graph of 2D FeCT surface topography, indicating that the thickness of α-In2Se3, top and bottom h-BN is 40nm, 20nm, 20nm. (b) Raman characterization of h-BN, which shows a clear peak position at 1366cm-1.

- On-field PFM amplitude and phase hysteresis loops of the channel α-In2Se3

Figure S3a depicts the on-field PFM amplitude versus voltage bias hysteresis loop of the channel α-In2Se3 with three cycles. Figure S3b shows the on-field PFM phase versus voltage bias hysteresis loop of the channel α-In2Se3 with three cycles. Both the PFM amplitude and phase hysteresis loops show that the channel α-In2Se3 exhibits a clear ferroelectric polarization reversal effect under the external electric field.

FigureS3. (a) On-field PFM amplitude versus voltage bias hysteresis loop with three cycles. (b) On-field PFM phase versus voltage bias hysteresis loop with three cycles.

- α-In2Se3 ferroelectric hysteresis curve with varying scanning voltage and 2D FeCTs dynamic equilibrium energy band diagram

Figure S4 shows the energy band diagram of FeCTs in equilibrium, where 2D α-In2Se3, as the essence of a ferroelectric semiconductor, has mobile charges in addition to the polarization bound charges.1,5 Besides, band bending and polarization states are simultaneously modulated by top and global gates.

FigureS4. Equilibrium band diagram of 2D α-In2Se3 FeCTs. It is worth noting that 2D α-In2Se3, which is a ferroelectric semiconductor, has both mobile charges and polarization bound charges. And band bending and ferroelectric polarization are modulated by top and global gates.

- Output curves under varying VGG and VTG

Figure S5 shows the output curves under global and top gate. The output current under both GG and TG modulation increases with the accumulated gate bias. However, the drain current of GG modulation is relatively larger than that of TG, which may be due to the lower positive bias applied by TG (because of the top dielectric layer hBN may break down under a large forward bias) and the weaker tunability of TG than GG.

FigureS5. Output curves under varying VGG and VTG, Vds sweep is fixed from 0 to 1V. (a) Output curves under GG modulation, where GG is from -8 to 8V in 4V steps. (b) Output curves under TG modulation, where TG is from -8 to 0V in 2V steps.

- Memory LRS/HRS and dynamic erase/write characteristics

Figure S6 depicts the LRS and HRS under NVM basic erase and write operations, and the corresponding dynamic characteristics. Figure S6a shows the 2D α-In2Se3 FeCTs based NVM LRS and HRS implemented in sequence under the -6V GG erase and +6V GG write operations, with Vds of 0.1V and VTG of 0V, showing non-volatile data retention. Figure S6b shows the robust 10-cycle dynamic erase/write current response of FeCTs NVM, where the spike voltage is ±8V, Vds is 0.1V and VTG is 0V.

FigureS6. Memory LRS/HRS and dynamic erase/write characteristics. (a) The NVM LRS and HRS realized by VGG erase and write spikes, Vds is fixed at 0.1V and VTG is 0V. (b) The dynamic erase/write response of FeCTs NVM.

- Top gate transfer and minimal spike LTP/LTD curves

Figure S7a shows a typical TG transfer curve with Vds of 1V and VGG of 0V, where the red curve is the drain current and the black curve is the TG leakage current. The TG transfer curve of 2D α-In2Se3 FeCTs also shows a significant clockwise hysteresis memory window, similar to GG, and compared to the channel current, the leakage current is negligible, reflecting the excellent dielectric properties of TG hBN. Figure S7b exhibits the original voltage-current curve of progressive excitatory and inhibitory PSC modulation achieved with minimal spike voltage of ±0.5V. The red curve is PSC under LTP and LTD, sequentially, and the black curve is the corresponding VG spike. It is worth noting that the excitation and inhibition modulation with minimum spike voltage indicates the extremely low power consumption of 2D α-In2Se3 FeCTs for neural computing.6

FigureS7. Top gate transfer and minimal spike LTP/LTD curves. (a) TG transfer curve with Vds of 1V and VGG of 0V, which shows a significant clockwise hysteresis window and negligible leakage current. (b) Progressive excitatory and inhibitory PSC modulation achieved with minimal spike voltage of ±0.5V, which corresponds to LTP and LTD, respectively. The red curve is the modulated PSC under LTP and LTD, and the black curve is the corresponding VG spike.

- Paired pulse depression characteristics

Figure S8 describes the characteristics of PPD in neural computing. As the spike interval increases, PPD index gradually returns to 100%, showing the disappearance of the short-term inhibitory effect. The PSC response after paired pulses is shown in Figure S8a. And the PSC amplitude after first spike is recorded as A1, and the amplitude after second spike is recorded as A2, and when A2 is lower than A1, synaptic inhibition is simulated.7 Figure S8b shows the calculated PPD index as a function of interval time, which gradually refresh to 100% as the interval accumulates, which corresponds to a typical STP in neural computing.2,7

FigureS8. Paired pulse facilitation characteristics. (a) Typical PSC response to paired pulses. (b) PPF index as a function of interval time, which gradually refresh to 100% as the interval accumulates. And PPF index is calculated by A2/A1.

- Thermal dependence of VGG output and transfer curves

Figure S9a shows the output characteristics (Vds from -1 to 1V, VGG and VTG are fixed at 0V) as a function of thermal temperature (298~423K). As the temperature increases, the current climbs and a better ohmic contact is formed, which may be attributed to thermally affected channel ferroelectric polarization8 and defect healing.9,10 The thermal temperature-dependent transfer curves (VGG=-8~8V, Vds=1V) are shown in Figure S9b. Similarly, it still has clear memory windows, and the on-state current significantly increases to approximately the same value, while the off-state current gradually increases with increasing temperature, which shows flexible thermal temperature tunability.

FigureS9. Thermal dependence of VGG output and transfer curves. (a) Thermal temperature-dependent output characteristics, where Vds is from -1 to 1V, VGG and VTG are fixed at 0V. As the temperature increases, the current increases and a more symmetrical ohmic contact is formed, which is consistent with the optimization of contact and channel defects after annealing. (b) The transfer curves as a function of thermal temperature, with VGG from -8 to 8V and Vds of 1V. It still shows clear memory windows, and the on-state current increases significantly to an approximate value of 1μA, while the off-state current gradually climbs as the temperature increases.

- Thermal dependence of VGG transfer curves with varying sweeping range

Figures S10a, b depicts the thermal dependence of the transfer curves in the VGG range of -4 to 4V and -6 to 6V, respectively. Similar to Figure S9b, as the temperature increases from 298 to 373K, the on-state current increased significantly to an approximate value, while the off-state current gradually increased, and 2D α-In2Se3 FeCTs shows a varying memory window, reflecting flexible thermal temperature adjustability.

FigureS10. Thermal dependence of VGG transfer curves with varying sweeping range. (a) Thermal dependence of the transfer curve in the VGG range of -4 to 4V, where Vds is fixed at 1V and the thermal temperature is from 298 to 373K. (b) Vds and thermal temperature fixed, thermal-dependent transfer curve under -6 ~ 6V VGG sweep.

- Different VGG transfer curves under 323K and memory LRS/HRS thermal tunability

Figure S11a shows the transfer curves of VGG sweep range of -4 ~ 4V, -6 ~ 6V and -8 ~ 8V at 323K. As the VGG voltage increases, the hysteresis memory window expands, and the ON/OFF ratio can still reach ~103 at 323K. Figure S11b depicts the thermal temperature-adjustable LRS and HRS of 2D FeCTs NVM under ±4V erase and write spikes. As the thermal temperature increases, both LRS and HRS increase and gradually overlap, as shown by the red and blue arrows in Figure S11b, which is consistent with the raise of the switching coefficient under thermal operation, indicating the depolarization of α-In2Se3 channel ferroelectric and the electrothermal tunability of FeCTs NVM.11

FigureS11. Different VGG transfer curves under 323K and memory LRS/HRS thermal tunability. (a) The transfer curves of VGG sweep range of -4 ~ 4V, -6 ~ 6V and -8 ~ 8V at 323K, and Vds is fixed at 1V. (b) 2D FeCTs NVM thermally tunable LRS and HRS under ± 4V erase and write spikes, Vds is fixed at 1V. The evolution trend of LRS and HRS indicated by red and blue arrows implies ferroelectric channel depolarization and electrothermal adjustability.

- Flow chart of simulated Iris recognition and classification based on FeCTs fully connected neural network

Figure S12 shows the detailed flow chart of iris recognition and classification based on FeCTs simulated neural network, including loading the iris standard dataset, defining a fully connected network model, training the network, testing the network, and obtaining the weight matrix under the optimal accuracy. Subsequently, the device conductance mapping function SME is defined, the conductance is mapped to the optimal weight matrix, the new network after the conductance mapping is obtained, and the recognition and classification accuracy of the new network is retested.

FigureS12. Flow chart of iris classification based on FeCTs simulated neural network.

- SME with varying thermal and spike amplitudes to determine mapping coefficient

Figure S13a depicts the SME as a function of mapping coefficient at varying thermal temperatures. The optimal mapping coefficients λ at 323K, 373K, and 423K are 0.18, 0.28, and 0.9, respectively. Figure S13b shows the SME as a function of mapping coefficient with varying spike amplitudes at RT. And the optimal mapping coefficients λ for ±4V and ±0.5V spikes at RT are 8 and 12.5, respectively. Both thermal temperature and spike amplitudes have an effect on the mapping coefficient, due to the modulation of α-In2Se3 FeCTs channel polarization, which in turn affects SME.

FigureS13. SME with varying thermal and spike amplitudes to determine mapping coefficient. (a) SME as a function of mapping coefficient at varying thermal temperatures (323K, 373K, 423K). (b) SME as a function of mapping coefficient with varying spike amplitudes (±4V, ±0.5V) at RT.

- Weight distribution of conductance mapping with varying spike amplitude at RT

Figure S14 shows the weight distribution of conductance mapping with varying spike amplitudes at RT. Specifically, Figure S14a shows the network weight distribution after the α-In2Se3 FeCTs conductance mapping of ±4V spikes at RT, while Figure S14b exhibits the ±0.5V spikes mapped weight distribution.

FigureS14. Weight distribution of conductance mapping with varying spike amplitude at RT. (a) The network weight distribution after the FeCTs conductance mapping of ±4V spikes. (b) The weight distribution of FeCTs conductance mapping under ±0.5V spikes.

References:

1.	Si, M. et al. A ferroelectric semiconductor field-effect transistor. Nature Electronics 2, 580-586 (2019).

2.	Wang, S. et al. A Photoelectric-Stimulated MoS2 Transistor for Neuromorphic Engineering. Research 2019, 1618798 (2019).

3.	Lee, G.-H. et al. Highly stable, dual-gated MoS2 transistors encapsulated by hexagonal boron nitride with gate-controllable contact, resistance, and threshold voltage. ACS Nano 9, 7019-7026 (2015).

4.	Petrone, N. et al. Flexible graphene field-effect transistors encapsulated in hexagonal boron nitride. ACS Nano 9, 8953-8959 (2015).

5.	Cui, C. et al. Intercorrelated in-plane and out-of-plane ferroelectricity in ultrathin two-dimensional layered semiconductor In2Se3. Nano Lett. 18, 1253-1258 (2018).

6.	Van De Burgt, Y., Melianas, A., Keene, S. T., Malliaras, G. & Salleo, A. Organic electronics for neuromorphic computing. Nature Electronics 1, 386-397 (2018).

7.	Wang, S. et al. A MoS2/PTCDA hybrid heterojunction synapse with efficient photoelectric dual modulation and versatility. Adv. Mater. 31, 1806227 (2019).

8.	Xue, F. et al. Gate‐Tunable and Multidirection‐Switchable Memristive Phenomena in a Van Der Waals Ferroelectric. Adv. Mater. 31, 1901300 (2019).

9.	Jia, K. et al. Effects of defects and thermal treatment on the properties of graphene. Vacuu 116, 90-95 (2015).

10.	Xin, G. et al. Advanced phase change composite by thermally annealed defect-free graphene for thermal energy storage. ACS applied materials & interfaces 6, 15262-15271 (2014).

11.	Xue, F. et al. Gate‐Tunable and Multidirection‐Switchable Memristive Phenomena in a Van Der Waals Ferroelectric. Adv. Mater. 31, 1901300 (2019).