Supplementary Information

A Practical Inverse Design Approach for High-Entropy Catalysts with Generative AI

Donglai Zhou#1, Ruyu Yang#1, Zijin Jia#1, Yuhai Cai1, Luyuan Zhao1, Lulu Guo1, Guilin Ye1, Song Wang1, Linjiang Chen1,3, Daobin Liu1, Pieter E. S. Smith4, Yan Huang*1, Qing Zhu*1,2, Jun Jiang*1

1 Key Laboratory of Precision and Intelligent Chemistry, Hefei National Research Center for Physical Sciences at the Microscale, University of Science and Technology of China, Hefei, China, 230026

2 Institute of Intelligent Innovation, Henan Academy of Sciences, Zhengzhou, China, 451162

3 School of Chemistry and School of Computer Science, University of Birmingham, Birmingham, United Kingdom, B15 2TT

4 Hefei JiShu Quantum Technology Co., Ltd., Hefei 230026, China.

# These authors contributed equally to this work: D.Z., R.Y., Z.J.

*Corresponding authors. E-mails: hyan@ustc.edu.cn; qingzhu@ustc.edu.cn; jiangj1@ustc.edu.cn

Supplementary Table S1. A library of 462 senary metal-organic hybrid catalysts composed of Co, Ni, Cu, Mg, Cd, Zn, and 1,4-benzenedicarboxylic acid prepared, along with experimentally measured overpotentials at 10 mA/cm² (η10) for OER.

| Cat. No. | Synthetic formula |  |  |  |  |  | Potential@10 mA/cm2 (V vs. RHE) | η10 (mV) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Co | Ni | Cu | Mg | Cd | Zn |  |  |
| 1 | 0.08333 | 0.08333 | 0.08333 | 0.08333 | 0.08333 | 0.58333 | 1.6892 | 459.2 |
| 2 | 0.08333 | 0.08333 | 0.08333 | 0.08333 | 0.16667 | 0.5 | 1.6399 | 409.9 |
| 3 | 0.08333 | 0.08333 | 0.08333 | 0.08333 | 0.25 | 0.41667 | 1.6445 | 414.5 |
| 4 | 0.08333 | 0.08333 | 0.08333 | 0.08333 | 0.33333 | 0.33333 | 1.6604 | 430.4 |
| 5 | 0.08333 | 0.08333 | 0.08333 | 0.08333 | 0.41667 | 0.25 | 1.6185 | 388.5 |
| 6 | 0.08333 | 0.08333 | 0.08333 | 0.08333 | 0.5 | 0.16667 | 1.6402 | 410.2 |
| 7 | 0.08333 | 0.08333 | 0.08333 | 0.08333 | 0.58333 | 0.08333 | 1.6479 | 417.9 |
| 8 | 0.08333 | 0.08333 | 0.08333 | 0.16667 | 0.08333 | 0.5 | 1.6736 | 443.6 |
| 9 | 0.08333 | 0.08333 | 0.08333 | 0.16667 | 0.16667 | 0.41667 | 1.6589 | 428.9 |
| 10 | 0.08333 | 0.08333 | 0.08333 | 0.16667 | 0.25 | 0.33333 | 1.6688 | 438.8 |
| 11 | 0.08333 | 0.08333 | 0.08333 | 0.16667 | 0.33333 | 0.25 | 1.6386 | 408.6 |
| 12 | 0.08333 | 0.08333 | 0.08333 | 0.16667 | 0.41667 | 0.16667 | 1.6335 | 403.5 |
| 13 | 0.08333 | 0.08333 | 0.08333 | 0.16667 | 0.5 | 0.08333 | 1.6466 | 416.6 |
| 14 | 0.08333 | 0.08333 | 0.08333 | 0.25 | 0.08333 | 0.41667 | 1.6478 | 417.8 |
| 15 | 0.08333 | 0.08333 | 0.08333 | 0.25 | 0.16667 | 0.33333 | 1.6772 | 447.2 |
| 16 | 0.08333 | 0.08333 | 0.08333 | 0.25 | 0.25 | 0.25 | 1.675 | 445 |
| 17 | 0.08333 | 0.08333 | 0.08333 | 0.25 | 0.33333 | 0.16667 | 1.653 | 423 |
| 18 | 0.08333 | 0.08333 | 0.08333 | 0.25 | 0.41667 | 0.08333 | 1.6551 | 425.1 |
| 19 | 0.08333 | 0.08333 | 0.08333 | 0.33333 | 0.08333 | 0.33333 | 1.6813 | 451.3 |
| 20 | 0.08333 | 0.08333 | 0.08333 | 0.33333 | 0.16667 | 0.25 | 1.6708 | 440.8 |
| 21 | 0.08333 | 0.08333 | 0.08333 | 0.33333 | 0.25 | 0.16667 | 1.649 | 419 |
| 22 | 0.08333 | 0.08333 | 0.08333 | 0.33333 | 0.33333 | 0.08333 | 1.6735 | 443.5 |
| 23 | 0.08333 | 0.08333 | 0.08333 | 0.41667 | 0.08333 | 0.25 | 1.6888 | 458.8 |
| 24 | 0.08333 | 0.08333 | 0.08333 | 0.41667 | 0.16667 | 0.16667 | 1.664 | 434 |
| 25 | 0.08333 | 0.08333 | 0.08333 | 0.41667 | 0.25 | 0.08333 | 1.6549 | 424.9 |
| 26 | 0.08333 | 0.08333 | 0.08333 | 0.5 | 0.08333 | 0.16667 | 1.669 | 439 |
| 27 | 0.08333 | 0.08333 | 0.08333 | 0.5 | 0.16667 | 0.08333 | 1.6611 | 431.1 |
| 28 | 0.08333 | 0.08333 | 0.08333 | 0.58333 | 0.08333 | 0.08333 | 1.682 | 452 |
| 29 | 0.08333 | 0.08333 | 0.16667 | 0.08333 | 0.08333 | 0.5 | 1.6392 | 409.2 |
| 30 | 0.08333 | 0.08333 | 0.16667 | 0.08333 | 0.16667 | 0.41667 | 1.6425 | 412.5 |
| 31 | 0.08333 | 0.08333 | 0.16667 | 0.08333 | 0.25 | 0.33333 | 1.6499 | 419.9 |
| 32 | 0.08333 | 0.08333 | 0.16667 | 0.08333 | 0.33333 | 0.25 | 1.643 | 413 |
| 33 | 0.08333 | 0.08333 | 0.16667 | 0.08333 | 0.41667 | 0.16667 | 1.6162 | 386.2 |
| 34 | 0.08333 | 0.08333 | 0.16667 | 0.08333 | 0.5 | 0.08333 | 1.6543 | 424.3 |
| 35 | 0.08333 | 0.08333 | 0.16667 | 0.16667 | 0.08333 | 0.41667 | 1.6574 | 427.4 |
| 36 | 0.08333 | 0.08333 | 0.16667 | 0.16667 | 0.16667 | 0.33333 | 1.6581 | 428.1 |
| 37 | 0.08333 | 0.08333 | 0.16667 | 0.16667 | 0.25 | 0.25 | 1.6282 | 398.2 |
| 38 | 0.08333 | 0.08333 | 0.16667 | 0.16667 | 0.33333 | 0.16667 | 1.6328 | 402.8 |
| 39 | 0.08333 | 0.08333 | 0.16667 | 0.16667 | 0.41667 | 0.08333 | 1.6393 | 409.3 |
| 40 | 0.08333 | 0.08333 | 0.16667 | 0.25 | 0.08333 | 0.33333 | 1.6738 | 443.8 |
| 41 | 0.08333 | 0.08333 | 0.16667 | 0.25 | 0.16667 | 0.25 | 1.6583 | 428.3 |
| 42 | 0.08333 | 0.08333 | 0.16667 | 0.25 | 0.25 | 0.16667 | 1.647 | 417 |
| 43 | 0.08333 | 0.08333 | 0.16667 | 0.25 | 0.33333 | 0.08333 | 1.6445 | 414.5 |
| 44 | 0.08333 | 0.08333 | 0.16667 | 0.33333 | 0.08333 | 0.25 | 1.6616 | 431.6 |
| 45 | 0.08333 | 0.08333 | 0.16667 | 0.33333 | 0.16667 | 0.16667 | 1.6438 | 413.8 |
| 46 | 0.08333 | 0.08333 | 0.16667 | 0.33333 | 0.25 | 0.08333 | 1.6301 | 400.1 |
| 47 | 0.08333 | 0.08333 | 0.16667 | 0.41667 | 0.08333 | 0.16667 | 1.6563 | 426.3 |
| 48 | 0.08333 | 0.08333 | 0.16667 | 0.41667 | 0.16667 | 0.08333 | 1.668 | 438 |
| 49 | 0.08333 | 0.08333 | 0.16667 | 0.5 | 0.08333 | 0.08333 | 1.6626 | 432.6 |
| 50 | 0.08333 | 0.08333 | 0.25 | 0.08333 | 0.08333 | 0.41667 | 1.6579 | 427.9 |
| 51 | 0.08333 | 0.08333 | 0.25 | 0.08333 | 0.16667 | 0.33333 | 1.665 | 435 |
| 52 | 0.08333 | 0.08333 | 0.25 | 0.08333 | 0.25 | 0.25 | 1.6456 | 415.6 |
| 53 | 0.08333 | 0.08333 | 0.25 | 0.08333 | 0.33333 | 0.16667 | 1.6587 | 428.7 |
| 54 | 0.08333 | 0.08333 | 0.25 | 0.08333 | 0.41667 | 0.08333 | 1.6164 | 386.4 |
| 55 | 0.08333 | 0.08333 | 0.25 | 0.16667 | 0.08333 | 0.33333 | 1.6485 | 418.5 |
| 56 | 0.08333 | 0.08333 | 0.25 | 0.16667 | 0.16667 | 0.25 | 1.6435 | 413.5 |
| 57 | 0.08333 | 0.08333 | 0.25 | 0.16667 | 0.25 | 0.16667 | 1.6527 | 422.7 |
| 58 | 0.08333 | 0.08333 | 0.25 | 0.16667 | 0.33333 | 0.08333 | 1.612 | 382 |
| 59 | 0.08333 | 0.08333 | 0.25 | 0.25 | 0.08333 | 0.25 | 1.6416 | 411.6 |
| 60 | 0.08333 | 0.08333 | 0.25 | 0.25 | 0.16667 | 0.16667 | 1.6492 | 419.2 |
| 61 | 0.08333 | 0.08333 | 0.25 | 0.25 | 0.25 | 0.08333 | 1.6673 | 437.3 |
| 62 | 0.08333 | 0.08333 | 0.25 | 0.33333 | 0.08333 | 0.16667 | 1.6801 | 450.1 |
| 63 | 0.08333 | 0.08333 | 0.25 | 0.33333 | 0.16667 | 0.08333 | 1.659 | 429 |
| 64 | 0.08333 | 0.08333 | 0.25 | 0.41667 | 0.08333 | 0.08333 | 1.6711 | 441.1 |
| 65 | 0.08333 | 0.08333 | 0.33333 | 0.08333 | 0.08333 | 0.33333 | 1.6702 | 440.2 |
| 66 | 0.08333 | 0.08333 | 0.33333 | 0.08333 | 0.16667 | 0.25 | 1.6411 | 411.1 |
| 67 | 0.08333 | 0.08333 | 0.33333 | 0.08333 | 0.25 | 0.16667 | 1.6497 | 419.7 |
| 68 | 0.08333 | 0.08333 | 0.33333 | 0.08333 | 0.33333 | 0.08333 | 1.6325 | 402.5 |
| 69 | 0.08333 | 0.08333 | 0.33333 | 0.16667 | 0.08333 | 0.25 | 1.6529 | 422.9 |
| 70 | 0.08333 | 0.08333 | 0.33333 | 0.16667 | 0.16667 | 0.16667 | 1.6581 | 428.1 |
| 71 | 0.08333 | 0.08333 | 0.33333 | 0.16667 | 0.25 | 0.08333 | 1.6255 | 395.5 |
| 72 | 0.08333 | 0.08333 | 0.33333 | 0.25 | 0.08333 | 0.16667 | 1.6725 | 442.5 |
| 73 | 0.08333 | 0.08333 | 0.33333 | 0.25 | 0.16667 | 0.08333 | 1.6378 | 407.8 |
| 74 | 0.08333 | 0.08333 | 0.33333 | 0.33333 | 0.08333 | 0.08333 | 1.6735 | 443.5 |
| 75 | 0.08333 | 0.08333 | 0.41667 | 0.08333 | 0.08333 | 0.25 | 1.6474 | 417.4 |
| 76 | 0.08333 | 0.08333 | 0.41667 | 0.08333 | 0.16667 | 0.16667 | 1.631 | 401 |
| 77 | 0.08333 | 0.08333 | 0.41667 | 0.08333 | 0.25 | 0.08333 | 1.6254 | 395.4 |
| 78 | 0.08333 | 0.08333 | 0.41667 | 0.16667 | 0.08333 | 0.16667 | 1.6695 | 439.5 |
| 79 | 0.08333 | 0.08333 | 0.41667 | 0.16667 | 0.16667 | 0.08333 | 1.6346 | 404.6 |
| 80 | 0.08333 | 0.08333 | 0.41667 | 0.25 | 0.08333 | 0.08333 | 1.6463 | 416.3 |
| 81 | 0.08333 | 0.08333 | 0.5 | 0.08333 | 0.08333 | 0.16667 | 1.6157 | 385.7 |
| 82 | 0.08333 | 0.08333 | 0.5 | 0.08333 | 0.16667 | 0.08333 | 1.6423 | 412.3 |
| 83 | 0.08333 | 0.08333 | 0.5 | 0.16667 | 0.08333 | 0.08333 | 1.6269 | 396.9 |
| 84 | 0.08333 | 0.08333 | 0.58333 | 0.08333 | 0.08333 | 0.08333 | 1.614 | 384 |
| 85 | 0.08333 | 0.16667 | 0.08333 | 0.08333 | 0.08333 | 0.5 | 1.6317 | 401.7 |
| 86 | 0.08333 | 0.16667 | 0.08333 | 0.08333 | 0.16667 | 0.41667 | 1.6479 | 417.9 |
| 87 | 0.08333 | 0.16667 | 0.08333 | 0.08333 | 0.25 | 0.33333 | 1.6287 | 398.7 |
| 88 | 0.08333 | 0.16667 | 0.08333 | 0.08333 | 0.33333 | 0.25 | 1.6246 | 394.6 |
| 89 | 0.08333 | 0.16667 | 0.08333 | 0.08333 | 0.41667 | 0.16667 | 1.6197 | 389.7 |
| 90 | 0.08333 | 0.16667 | 0.08333 | 0.08333 | 0.5 | 0.08333 | 1.6378 | 407.8 |
| 91 | 0.08333 | 0.16667 | 0.08333 | 0.16667 | 0.08333 | 0.41667 | 1.6479 | 417.9 |
| 92 | 0.08333 | 0.16667 | 0.08333 | 0.16667 | 0.16667 | 0.33333 | 1.6354 | 405.4 |
| 93 | 0.08333 | 0.16667 | 0.08333 | 0.16667 | 0.25 | 0.25 | 1.6246 | 394.6 |
| 94 | 0.08333 | 0.16667 | 0.08333 | 0.16667 | 0.33333 | 0.16667 | 1.6253 | 395.3 |
| 95 | 0.08333 | 0.16667 | 0.08333 | 0.16667 | 0.41667 | 0.08333 | 1.6238 | 393.8 |
| 96 | 0.08333 | 0.16667 | 0.08333 | 0.25 | 0.08333 | 0.33333 | 1.6423 | 412.3 |
| 97 | 0.08333 | 0.16667 | 0.08333 | 0.25 | 0.16667 | 0.25 | 1.6387 | 408.7 |
| 98 | 0.08333 | 0.16667 | 0.08333 | 0.25 | 0.25 | 0.16667 | 1.6333 | 403.3 |
| 99 | 0.08333 | 0.16667 | 0.08333 | 0.25 | 0.33333 | 0.08333 | 1.6286 | 398.6 |
| 100 | 0.08333 | 0.16667 | 0.08333 | 0.33333 | 0.08333 | 0.25 | 1.6539 | 423.9 |
| 101 | 0.08333 | 0.16667 | 0.08333 | 0.33333 | 0.16667 | 0.16667 | 1.6799 | 449.9 |
| 102 | 0.08333 | 0.16667 | 0.08333 | 0.33333 | 0.25 | 0.08333 | 1.6656 | 435.6 |
| 103 | 0.08333 | 0.16667 | 0.08333 | 0.41667 | 0.08333 | 0.16667 | 1.6956 | 465.6 |
| 104 | 0.08333 | 0.16667 | 0.08333 | 0.41667 | 0.16667 | 0.08333 | 1.68 | 450 |
| 105 | 0.08333 | 0.16667 | 0.08333 | 0.5 | 0.08333 | 0.08333 | 1.6887 | 458.7 |
| 106 | 0.08333 | 0.16667 | 0.16667 | 0.08333 | 0.08333 | 0.41667 | 1.6552 | 425.2 |
| 107 | 0.08333 | 0.16667 | 0.16667 | 0.08333 | 0.16667 | 0.33333 | 1.6557 | 425.7 |
| 108 | 0.08333 | 0.16667 | 0.16667 | 0.08333 | 0.25 | 0.25 | 1.6485 | 418.5 |
| 109 | 0.08333 | 0.16667 | 0.16667 | 0.08333 | 0.33333 | 0.16667 | 1.6268 | 396.8 |
| 110 | 0.08333 | 0.16667 | 0.16667 | 0.08333 | 0.41667 | 0.08333 | 1.6314 | 401.4 |
| 111 | 0.08333 | 0.16667 | 0.16667 | 0.16667 | 0.08333 | 0.33333 | 1.6337 | 403.7 |
| 112 | 0.08333 | 0.16667 | 0.16667 | 0.16667 | 0.16667 | 0.25 | 1.658 | 428 |
| 113 | 0.08333 | 0.16667 | 0.16667 | 0.16667 | 0.25 | 0.16667 | 1.6467 | 416.7 |
| 114 | 0.08333 | 0.16667 | 0.16667 | 0.16667 | 0.33333 | 0.08333 | 1.633 | 403 |
| 115 | 0.08333 | 0.16667 | 0.16667 | 0.25 | 0.08333 | 0.25 | 1.657 | 427 |
| 116 | 0.08333 | 0.16667 | 0.16667 | 0.25 | 0.16667 | 0.16667 | 1.633 | 403 |
| 117 | 0.08333 | 0.16667 | 0.16667 | 0.25 | 0.25 | 0.08333 | 1.6338 | 403.8 |
| 118 | 0.08333 | 0.16667 | 0.16667 | 0.33333 | 0.08333 | 0.16667 | 1.6631 | 433.1 |
| 119 | 0.08333 | 0.16667 | 0.16667 | 0.33333 | 0.16667 | 0.08333 | 1.6635 | 433.5 |
| 120 | 0.08333 | 0.16667 | 0.16667 | 0.41667 | 0.08333 | 0.08333 | 1.6845 | 454.5 |
| 121 | 0.08333 | 0.16667 | 0.25 | 0.08333 | 0.08333 | 0.33333 | 1.6575 | 427.5 |
| 122 | 0.08333 | 0.16667 | 0.25 | 0.08333 | 0.16667 | 0.25 | 1.6235 | 393.5 |
| 123 | 0.08333 | 0.16667 | 0.25 | 0.08333 | 0.25 | 0.16667 | 1.6414 | 411.4 |
| 124 | 0.08333 | 0.16667 | 0.25 | 0.08333 | 0.33333 | 0.08333 | 1.6213 | 391.3 |
| 125 | 0.08333 | 0.16667 | 0.25 | 0.16667 | 0.08333 | 0.25 | 1.641 | 411 |
| 126 | 0.08333 | 0.16667 | 0.25 | 0.16667 | 0.16667 | 0.16667 | 1.6472 | 417.2 |
| 127 | 0.08333 | 0.16667 | 0.25 | 0.16667 | 0.25 | 0.08333 | 1.64 | 410 |
| 128 | 0.08333 | 0.16667 | 0.25 | 0.25 | 0.08333 | 0.16667 | 1.6738 | 443.8 |
| 129 | 0.08333 | 0.16667 | 0.25 | 0.25 | 0.16667 | 0.08333 | 1.6574 | 427.4 |
| 130 | 0.08333 | 0.16667 | 0.25 | 0.33333 | 0.08333 | 0.08333 | 1.675 | 445 |
| 131 | 0.08333 | 0.16667 | 0.33333 | 0.08333 | 0.08333 | 0.25 | 1.6337 | 403.7 |
| 132 | 0.08333 | 0.16667 | 0.33333 | 0.08333 | 0.16667 | 0.16667 | 1.6296 | 399.6 |
| 133 | 0.08333 | 0.16667 | 0.33333 | 0.08333 | 0.25 | 0.08333 | 1.611 | 381 |
| 134 | 0.08333 | 0.16667 | 0.33333 | 0.16667 | 0.08333 | 0.16667 | 1.654 | 424 |
| 135 | 0.08333 | 0.16667 | 0.33333 | 0.16667 | 0.16667 | 0.08333 | 1.6651 | 435.1 |
| 136 | 0.08333 | 0.16667 | 0.33333 | 0.25 | 0.08333 | 0.08333 | 1.6471 | 417.1 |
| 137 | 0.08333 | 0.16667 | 0.41667 | 0.08333 | 0.08333 | 0.16667 | 1.6321 | 402.1 |
| 138 | 0.08333 | 0.16667 | 0.41667 | 0.08333 | 0.16667 | 0.08333 | 1.6671 | 437.1 |
| 139 | 0.08333 | 0.16667 | 0.41667 | 0.16667 | 0.08333 | 0.08333 | 1.659 | 429 |
| 140 | 0.08333 | 0.16667 | 0.5 | 0.08333 | 0.08333 | 0.08333 | 1.6237 | 393.7 |
| 141 | 0.08333 | 0.25 | 0.08333 | 0.08333 | 0.08333 | 0.41667 | 1.6303 | 400.3 |
| 142 | 0.08333 | 0.25 | 0.08333 | 0.08333 | 0.16667 | 0.33333 | 1.6495 | 419.5 |
| 143 | 0.08333 | 0.25 | 0.08333 | 0.08333 | 0.25 | 0.25 | 1.6262 | 396.2 |
| 144 | 0.08333 | 0.25 | 0.08333 | 0.08333 | 0.33333 | 0.16667 | 1.618 | 388 |
| 145 | 0.08333 | 0.25 | 0.08333 | 0.08333 | 0.41667 | 0.08333 | 1.6087 | 378.7 |
| 146 | 0.08333 | 0.25 | 0.08333 | 0.16667 | 0.08333 | 0.33333 | 1.6107 | 380.7 |
| 147 | 0.08333 | 0.25 | 0.08333 | 0.16667 | 0.16667 | 0.25 | 1.675 | 445 |
| 148 | 0.08333 | 0.25 | 0.08333 | 0.16667 | 0.25 | 0.16667 | 1.6389 | 408.9 |
| 149 | 0.08333 | 0.25 | 0.08333 | 0.16667 | 0.33333 | 0.08333 | 1.638 | 408 |
| 150 | 0.08333 | 0.25 | 0.08333 | 0.25 | 0.08333 | 0.25 | 1.6416 | 411.6 |
| 151 | 0.08333 | 0.25 | 0.08333 | 0.25 | 0.16667 | 0.16667 | 1.6534 | 423.4 |
| 152 | 0.08333 | 0.25 | 0.08333 | 0.25 | 0.25 | 0.08333 | 1.6689 | 438.9 |
| 153 | 0.08333 | 0.25 | 0.08333 | 0.33333 | 0.08333 | 0.16667 | 1.6527 | 422.7 |
| 154 | 0.08333 | 0.25 | 0.08333 | 0.33333 | 0.16667 | 0.08333 | 1.6489 | 418.9 |
| 155 | 0.08333 | 0.25 | 0.08333 | 0.41667 | 0.08333 | 0.08333 | 1.6785 | 448.5 |
| 156 | 0.08333 | 0.25 | 0.16667 | 0.08333 | 0.08333 | 0.33333 | 1.6366 | 406.6 |
| 157 | 0.08333 | 0.25 | 0.16667 | 0.08333 | 0.16667 | 0.25 | 1.6159 | 385.9 |
| 158 | 0.08333 | 0.25 | 0.16667 | 0.08333 | 0.25 | 0.16667 | 1.6089 | 378.9 |
| 159 | 0.08333 | 0.25 | 0.16667 | 0.08333 | 0.33333 | 0.08333 | 1.6061 | 376.1 |
| 160 | 0.08333 | 0.25 | 0.16667 | 0.16667 | 0.08333 | 0.25 | 1.6348 | 404.8 |
| 161 | 0.08333 | 0.25 | 0.16667 | 0.16667 | 0.16667 | 0.16667 | 1.6297 | 399.7 |
| 162 | 0.08333 | 0.25 | 0.16667 | 0.16667 | 0.25 | 0.08333 | 1.6031 | 373.1 |
| 163 | 0.08333 | 0.25 | 0.16667 | 0.25 | 0.08333 | 0.16667 | 1.6431 | 413.1 |
| 164 | 0.08333 | 0.25 | 0.16667 | 0.25 | 0.16667 | 0.08333 | 1.6439 | 413.9 |
| 165 | 0.08333 | 0.25 | 0.16667 | 0.33333 | 0.08333 | 0.08333 | 1.6684 | 438.4 |
| 166 | 0.08333 | 0.25 | 0.25 | 0.08333 | 0.08333 | 0.25 | 1.6555 | 425.5 |
| 167 | 0.08333 | 0.25 | 0.25 | 0.08333 | 0.16667 | 0.16667 | 1.6061 | 376.1 |
| 168 | 0.08333 | 0.25 | 0.25 | 0.08333 | 0.25 | 0.08333 | 1.6445 | 414.5 |
| 169 | 0.08333 | 0.25 | 0.25 | 0.16667 | 0.08333 | 0.16667 | 1.6864 | 456.4 |
| 170 | 0.08333 | 0.25 | 0.25 | 0.16667 | 0.16667 | 0.08333 | 1.66 | 430 |
| 171 | 0.08333 | 0.25 | 0.25 | 0.25 | 0.08333 | 0.08333 | 1.6321 | 402.1 |
| 172 | 0.08333 | 0.25 | 0.33333 | 0.08333 | 0.08333 | 0.16667 | 1.6289 | 398.9 |
| 173 | 0.08333 | 0.25 | 0.33333 | 0.08333 | 0.16667 | 0.08333 | 1.6013 | 371.3 |
| 174 | 0.08333 | 0.25 | 0.33333 | 0.16667 | 0.08333 | 0.08333 | 1.6138 | 383.8 |
| 175 | 0.08333 | 0.25 | 0.41667 | 0.08333 | 0.08333 | 0.08333 | 1.6141 | 384.1 |
| 176 | 0.08333 | 0.33333 | 0.08333 | 0.08333 | 0.08333 | 0.33333 | 1.6731 | 443.1 |
| 177 | 0.08333 | 0.33333 | 0.08333 | 0.08333 | 0.16667 | 0.25 | 1.645 | 415 |
| 178 | 0.08333 | 0.33333 | 0.08333 | 0.08333 | 0.25 | 0.16667 | 1.6454 | 415.4 |
| 179 | 0.08333 | 0.33333 | 0.08333 | 0.08333 | 0.33333 | 0.08333 | 1.6611 | 431.1 |
| 180 | 0.08333 | 0.33333 | 0.08333 | 0.16667 | 0.08333 | 0.25 | 1.6526 | 422.6 |
| 181 | 0.08333 | 0.33333 | 0.08333 | 0.16667 | 0.16667 | 0.16667 | 1.6531 | 423.1 |
| 182 | 0.08333 | 0.33333 | 0.08333 | 0.16667 | 0.25 | 0.08333 | 1.6797 | 449.7 |
| 183 | 0.08333 | 0.33333 | 0.08333 | 0.25 | 0.08333 | 0.16667 | 1.6373 | 407.3 |
| 184 | 0.08333 | 0.33333 | 0.08333 | 0.25 | 0.16667 | 0.08333 | 1.6212 | 391.2 |
| 185 | 0.08333 | 0.33333 | 0.08333 | 0.33333 | 0.08333 | 0.08333 | 1.6416 | 411.6 |
| 186 | 0.08333 | 0.33333 | 0.16667 | 0.08333 | 0.08333 | 0.25 | 1.6596 | 429.6 |
| 187 | 0.08333 | 0.33333 | 0.16667 | 0.08333 | 0.16667 | 0.16667 | 1.6155 | 385.5 |
| 188 | 0.08333 | 0.33333 | 0.16667 | 0.08333 | 0.25 | 0.08333 | 1.6043 | 374.3 |
| 189 | 0.08333 | 0.33333 | 0.16667 | 0.16667 | 0.08333 | 0.16667 | 1.619 | 389 |
| 190 | 0.08333 | 0.33333 | 0.16667 | 0.16667 | 0.16667 | 0.08333 | 1.6181 | 388.1 |
| 191 | 0.08333 | 0.33333 | 0.16667 | 0.25 | 0.08333 | 0.08333 | 1.6339 | 403.9 |
| 192 | 0.08333 | 0.33333 | 0.25 | 0.08333 | 0.08333 | 0.16667 | 1.5907 | 360.7 |
| 193 | 0.08333 | 0.33333 | 0.25 | 0.08333 | 0.16667 | 0.08333 | 1.6172 | 387.2 |
| 194 | 0.08333 | 0.33333 | 0.25 | 0.16667 | 0.08333 | 0.08333 | 1.6092 | 379.2 |
| 195 | 0.08333 | 0.33333 | 0.33333 | 0.08333 | 0.08333 | 0.08333 | 1.5895 | 359.5 |
| 196 | 0.08333 | 0.41667 | 0.08333 | 0.08333 | 0.08333 | 0.25 | 1.6028 | 372.8 |
| 197 | 0.08333 | 0.41667 | 0.08333 | 0.08333 | 0.16667 | 0.16667 | 1.6056 | 375.6 |
| 198 | 0.08333 | 0.41667 | 0.08333 | 0.08333 | 0.25 | 0.08333 | 1.6435 | 413.5 |
| 199 | 0.08333 | 0.41667 | 0.08333 | 0.16667 | 0.08333 | 0.16667 | 1.6325 | 402.5 |
| 200 | 0.08333 | 0.41667 | 0.08333 | 0.16667 | 0.16667 | 0.08333 | 1.6298 | 399.8 |
| 201 | 0.08333 | 0.41667 | 0.08333 | 0.25 | 0.08333 | 0.08333 | 1.6415 | 411.5 |
| 202 | 0.08333 | 0.41667 | 0.16667 | 0.08333 | 0.08333 | 0.16667 | 1.6255 | 395.5 |
| 203 | 0.08333 | 0.41667 | 0.16667 | 0.08333 | 0.16667 | 0.08333 | 1.6241 | 394.1 |
| 204 | 0.08333 | 0.41667 | 0.16667 | 0.16667 | 0.08333 | 0.08333 | 1.6122 | 382.2 |
| 205 | 0.08333 | 0.41667 | 0.25 | 0.08333 | 0.08333 | 0.08333 | 1.6104 | 380.4 |
| 206 | 0.08333 | 0.5 | 0.08333 | 0.08333 | 0.08333 | 0.16667 | 1.6116 | 381.6 |
| 207 | 0.08333 | 0.5 | 0.08333 | 0.08333 | 0.16667 | 0.08333 | 1.6661 | 436.1 |
| 208 | 0.08333 | 0.5 | 0.08333 | 0.16667 | 0.08333 | 0.08333 | 1.6451 | 415.1 |
| 209 | 0.08333 | 0.5 | 0.16667 | 0.08333 | 0.08333 | 0.08333 | 1.6487 | 418.7 |
| 210 | 0.08333 | 0.58333 | 0.08333 | 0.08333 | 0.08333 | 0.08333 | 1.6483 | 418.3 |
| 211 | 0.16667 | 0.08333 | 0.08333 | 0.08333 | 0.08333 | 0.5 | 1.5995 | 369.5 |
| 212 | 0.16667 | 0.08333 | 0.08333 | 0.08333 | 0.16667 | 0.41667 | 1.6074 | 377.4 |
| 213 | 0.16667 | 0.08333 | 0.08333 | 0.08333 | 0.25 | 0.33333 | 1.6134 | 383.4 |
| 214 | 0.16667 | 0.08333 | 0.08333 | 0.08333 | 0.33333 | 0.25 | 1.6191 | 389.1 |
| 215 | 0.16667 | 0.08333 | 0.08333 | 0.08333 | 0.41667 | 0.16667 | 1.6033 | 373.3 |
| 216 | 0.16667 | 0.08333 | 0.08333 | 0.08333 | 0.5 | 0.08333 | 1.597 | 367 |
| 217 | 0.16667 | 0.08333 | 0.08333 | 0.16667 | 0.08333 | 0.41667 | 1.6076 | 377.6 |
| 218 | 0.16667 | 0.08333 | 0.08333 | 0.16667 | 0.16667 | 0.33333 | 1.6139 | 383.9 |
| 219 | 0.16667 | 0.08333 | 0.08333 | 0.16667 | 0.25 | 0.25 | 1.619 | 389 |
| 220 | 0.16667 | 0.08333 | 0.08333 | 0.16667 | 0.33333 | 0.16667 | 1.6083 | 378.3 |
| 221 | 0.16667 | 0.08333 | 0.08333 | 0.16667 | 0.41667 | 0.08333 | 1.6244 | 394.4 |
| 222 | 0.16667 | 0.08333 | 0.08333 | 0.25 | 0.08333 | 0.33333 | 1.6339 | 403.9 |
| 223 | 0.16667 | 0.08333 | 0.08333 | 0.25 | 0.16667 | 0.25 | 1.6164 | 386.4 |
| 224 | 0.16667 | 0.08333 | 0.08333 | 0.25 | 0.25 | 0.16667 | 1.616 | 386 |
| 225 | 0.16667 | 0.08333 | 0.08333 | 0.25 | 0.33333 | 0.08333 | 1.6372 | 407.2 |
| 226 | 0.16667 | 0.08333 | 0.08333 | 0.33333 | 0.08333 | 0.25 | 1.6217 | 391.7 |
| 227 | 0.16667 | 0.08333 | 0.08333 | 0.33333 | 0.16667 | 0.16667 | 1.64 | 410 |
| 228 | 0.16667 | 0.08333 | 0.08333 | 0.33333 | 0.25 | 0.08333 | 1.6173 | 387.3 |
| 229 | 0.16667 | 0.08333 | 0.08333 | 0.41667 | 0.08333 | 0.16667 | 1.6279 | 397.9 |
| 230 | 0.16667 | 0.08333 | 0.08333 | 0.41667 | 0.16667 | 0.08333 | 1.6414 | 411.4 |
| 231 | 0.16667 | 0.08333 | 0.08333 | 0.5 | 0.08333 | 0.08333 | 1.6245 | 394.5 |
| 232 | 0.16667 | 0.08333 | 0.16667 | 0.08333 | 0.08333 | 0.41667 | 1.5939 | 363.9 |
| 233 | 0.16667 | 0.08333 | 0.16667 | 0.08333 | 0.16667 | 0.33333 | 1.6012 | 371.2 |
| 234 | 0.16667 | 0.08333 | 0.16667 | 0.08333 | 0.25 | 0.25 | 1.5993 | 369.3 |
| 235 | 0.16667 | 0.08333 | 0.16667 | 0.08333 | 0.33333 | 0.16667 | 1.6059 | 375.9 |
| 236 | 0.16667 | 0.08333 | 0.16667 | 0.08333 | 0.41667 | 0.08333 | 1.5941 | 364.1 |
| 237 | 0.16667 | 0.08333 | 0.16667 | 0.16667 | 0.08333 | 0.33333 | 1.6005 | 370.5 |
| 238 | 0.16667 | 0.08333 | 0.16667 | 0.16667 | 0.16667 | 0.25 | 1.6155 | 385.5 |
| 239 | 0.16667 | 0.08333 | 0.16667 | 0.16667 | 0.25 | 0.16667 | 1.5822 | 352.2 |
| 240 | 0.16667 | 0.08333 | 0.16667 | 0.16667 | 0.33333 | 0.08333 | 1.613 | 383 |
| 241 | 0.16667 | 0.08333 | 0.16667 | 0.25 | 0.08333 | 0.25 | 1.617 | 387 |
| 242 | 0.16667 | 0.08333 | 0.16667 | 0.25 | 0.16667 | 0.16667 | 1.6101 | 380.1 |
| 243 | 0.16667 | 0.08333 | 0.16667 | 0.25 | 0.25 | 0.08333 | 1.6033 | 373.3 |
| 244 | 0.16667 | 0.08333 | 0.16667 | 0.33333 | 0.08333 | 0.16667 | 1.5975 | 367.5 |
| 245 | 0.16667 | 0.08333 | 0.16667 | 0.33333 | 0.16667 | 0.08333 | 1.5913 | 361.3 |
| 246 | 0.16667 | 0.08333 | 0.16667 | 0.41667 | 0.08333 | 0.08333 | 1.5939 | 363.9 |
| 247 | 0.16667 | 0.08333 | 0.25 | 0.08333 | 0.08333 | 0.33333 | 1.5986 | 368.6 |
| 248 | 0.16667 | 0.08333 | 0.25 | 0.08333 | 0.16667 | 0.25 | 1.6119 | 381.9 |
| 249 | 0.16667 | 0.08333 | 0.25 | 0.08333 | 0.25 | 0.16667 | 1.5935 | 363.5 |
| 250 | 0.16667 | 0.08333 | 0.25 | 0.08333 | 0.33333 | 0.08333 | 1.5942 | 364.2 |
| 251 | 0.16667 | 0.08333 | 0.25 | 0.16667 | 0.08333 | 0.25 | 1.5898 | 359.8 |
| 252 | 0.16667 | 0.08333 | 0.25 | 0.16667 | 0.16667 | 0.16667 | 1.6016 | 371.6 |
| 253 | 0.16667 | 0.08333 | 0.25 | 0.16667 | 0.25 | 0.08333 | 1.597 | 367 |
| 254 | 0.16667 | 0.08333 | 0.25 | 0.25 | 0.08333 | 0.16667 | 1.6097 | 379.7 |
| 255 | 0.16667 | 0.08333 | 0.25 | 0.25 | 0.16667 | 0.08333 | 1.604 | 374 |
| 256 | 0.16667 | 0.08333 | 0.25 | 0.33333 | 0.08333 | 0.08333 | 1.5962 | 366.2 |
| 257 | 0.16667 | 0.08333 | 0.33333 | 0.08333 | 0.08333 | 0.25 | 1.5884 | 358.4 |
| 258 | 0.16667 | 0.08333 | 0.33333 | 0.08333 | 0.16667 | 0.16667 | 1.5856 | 355.6 |
| 259 | 0.16667 | 0.08333 | 0.33333 | 0.08333 | 0.25 | 0.08333 | 1.5889 | 358.9 |
| 260 | 0.16667 | 0.08333 | 0.33333 | 0.16667 | 0.08333 | 0.16667 | 1.5956 | 365.6 |
| 261 | 0.16667 | 0.08333 | 0.33333 | 0.16667 | 0.16667 | 0.08333 | 1.5931 | 363.1 |
| 262 | 0.16667 | 0.08333 | 0.33333 | 0.25 | 0.08333 | 0.08333 | 1.5954 | 365.4 |
| 263 | 0.16667 | 0.08333 | 0.41667 | 0.08333 | 0.08333 | 0.16667 | 1.5914 | 361.4 |
| 264 | 0.16667 | 0.08333 | 0.41667 | 0.08333 | 0.16667 | 0.08333 | 1.5796 | 349.6 |
| 265 | 0.16667 | 0.08333 | 0.41667 | 0.16667 | 0.08333 | 0.08333 | 1.5845 | 354.5 |
| 266 | 0.16667 | 0.08333 | 0.5 | 0.08333 | 0.08333 | 0.08333 | 1.6307 | 400.7 |
| 267 | 0.16667 | 0.16667 | 0.08333 | 0.08333 | 0.08333 | 0.41667 | 1.6037 | 373.7 |
| 268 | 0.16667 | 0.16667 | 0.08333 | 0.08333 | 0.16667 | 0.33333 | 1.5961 | 366.1 |
| 269 | 0.16667 | 0.16667 | 0.08333 | 0.08333 | 0.25 | 0.25 | 1.6063 | 376.3 |
| 270 | 0.16667 | 0.16667 | 0.08333 | 0.08333 | 0.33333 | 0.16667 | 1.6045 | 374.5 |
| 271 | 0.16667 | 0.16667 | 0.08333 | 0.08333 | 0.41667 | 0.08333 | 1.5857 | 355.7 |
| 272 | 0.16667 | 0.16667 | 0.08333 | 0.16667 | 0.08333 | 0.33333 | 1.5998 | 369.8 |
| 273 | 0.16667 | 0.16667 | 0.08333 | 0.16667 | 0.16667 | 0.25 | 1.6184 | 388.4 |
| 274 | 0.16667 | 0.16667 | 0.08333 | 0.16667 | 0.25 | 0.16667 | 1.6098 | 379.8 |
| 275 | 0.16667 | 0.16667 | 0.08333 | 0.16667 | 0.33333 | 0.08333 | 1.606 | 376 |
| 276 | 0.16667 | 0.16667 | 0.08333 | 0.25 | 0.08333 | 0.25 | 1.6125 | 382.5 |
| 277 | 0.16667 | 0.16667 | 0.08333 | 0.25 | 0.16667 | 0.16667 | 1.6276 | 397.6 |
| 278 | 0.16667 | 0.16667 | 0.08333 | 0.25 | 0.25 | 0.08333 | 1.6207 | 390.7 |
| 279 | 0.16667 | 0.16667 | 0.08333 | 0.33333 | 0.08333 | 0.16667 | 1.6187 | 388.7 |
| 280 | 0.16667 | 0.16667 | 0.08333 | 0.33333 | 0.16667 | 0.08333 | 1.6213 | 391.3 |
| 281 | 0.16667 | 0.16667 | 0.08333 | 0.41667 | 0.08333 | 0.08333 | 1.6165 | 386.5 |
| 282 | 0.16667 | 0.16667 | 0.16667 | 0.08333 | 0.08333 | 0.33333 | 1.6052 | 375.2 |
| 283 | 0.16667 | 0.16667 | 0.16667 | 0.08333 | 0.16667 | 0.25 | 1.6006 | 370.6 |
| 284 | 0.16667 | 0.16667 | 0.16667 | 0.08333 | 0.25 | 0.16667 | 1.5972 | 367.2 |
| 285 | 0.16667 | 0.16667 | 0.16667 | 0.08333 | 0.33333 | 0.08333 | 1.5925 | 362.5 |
| 286 | 0.16667 | 0.16667 | 0.16667 | 0.16667 | 0.08333 | 0.25 | 1.6223 | 392.3 |
| 287 | 0.16667 | 0.16667 | 0.16667 | 0.16667 | 0.16667 | 0.16667 | 1.6135 | 383.5 |
| 288 | 0.16667 | 0.16667 | 0.16667 | 0.16667 | 0.25 | 0.08333 | 1.62 | 390 |
| 289 | 0.16667 | 0.16667 | 0.16667 | 0.25 | 0.08333 | 0.16667 | 1.5864 | 356.4 |
| 290 | 0.16667 | 0.16667 | 0.16667 | 0.25 | 0.16667 | 0.08333 | 1.607 | 377 |
| 291 | 0.16667 | 0.16667 | 0.16667 | 0.33333 | 0.08333 | 0.08333 | 1.6321 | 402.1 |
| 292 | 0.16667 | 0.16667 | 0.25 | 0.08333 | 0.08333 | 0.25 | 1.5976 | 367.6 |
| 293 | 0.16667 | 0.16667 | 0.25 | 0.08333 | 0.16667 | 0.16667 | 1.5984 | 368.4 |
| 294 | 0.16667 | 0.16667 | 0.25 | 0.08333 | 0.25 | 0.08333 | 1.6245 | 394.5 |
| 295 | 0.16667 | 0.16667 | 0.25 | 0.16667 | 0.08333 | 0.16667 | 1.615 | 385 |
| 296 | 0.16667 | 0.16667 | 0.25 | 0.16667 | 0.16667 | 0.08333 | 1.5959 | 365.9 |
| 297 | 0.16667 | 0.16667 | 0.25 | 0.25 | 0.08333 | 0.08333 | 1.6174 | 387.4 |
| 298 | 0.16667 | 0.16667 | 0.33333 | 0.08333 | 0.08333 | 0.16667 | 1.5936 | 363.6 |
| 299 | 0.16667 | 0.16667 | 0.33333 | 0.08333 | 0.16667 | 0.08333 | 1.5973 | 367.3 |
| 300 | 0.16667 | 0.16667 | 0.33333 | 0.16667 | 0.08333 | 0.08333 | 1.594 | 364 |
| 301 | 0.16667 | 0.16667 | 0.41667 | 0.08333 | 0.08333 | 0.08333 | 1.5786 | 348.6 |
| 302 | 0.16667 | 0.25 | 0.08333 | 0.08333 | 0.08333 | 0.33333 | 1.6135 | 383.5 |
| 303 | 0.16667 | 0.25 | 0.08333 | 0.08333 | 0.16667 | 0.25 | 1.6016 | 371.6 |
| 304 | 0.16667 | 0.25 | 0.08333 | 0.08333 | 0.25 | 0.16667 | 1.6 | 370 |
| 305 | 0.16667 | 0.25 | 0.08333 | 0.08333 | 0.33333 | 0.08333 | 1.61 | 380 |
| 306 | 0.16667 | 0.25 | 0.08333 | 0.16667 | 0.08333 | 0.25 | 1.6197 | 389.7 |
| 307 | 0.16667 | 0.25 | 0.08333 | 0.16667 | 0.16667 | 0.16667 | 1.6261 | 396.1 |
| 308 | 0.16667 | 0.25 | 0.08333 | 0.16667 | 0.25 | 0.08333 | 1.6105 | 380.5 |
| 309 | 0.16667 | 0.25 | 0.08333 | 0.25 | 0.08333 | 0.16667 | 1.6179 | 387.9 |
| 310 | 0.16667 | 0.25 | 0.08333 | 0.25 | 0.16667 | 0.08333 | 1.6196 | 389.6 |
| 311 | 0.16667 | 0.25 | 0.08333 | 0.33333 | 0.08333 | 0.08333 | 1.633 | 403 |
| 312 | 0.16667 | 0.25 | 0.16667 | 0.08333 | 0.08333 | 0.25 | 1.5947 | 364.7 |
| 313 | 0.16667 | 0.25 | 0.16667 | 0.08333 | 0.16667 | 0.16667 | 1.6121 | 382.1 |
| 314 | 0.16667 | 0.25 | 0.16667 | 0.08333 | 0.25 | 0.08333 | 1.585 | 355 |
| 315 | 0.16667 | 0.25 | 0.16667 | 0.16667 | 0.08333 | 0.16667 | 1.6079 | 377.9 |
| 316 | 0.16667 | 0.25 | 0.16667 | 0.16667 | 0.16667 | 0.08333 | 1.6289 | 398.9 |
| 317 | 0.16667 | 0.25 | 0.16667 | 0.25 | 0.08333 | 0.08333 | 1.6209 | 390.9 |
| 318 | 0.16667 | 0.25 | 0.25 | 0.08333 | 0.08333 | 0.16667 | 1.6213 | 391.3 |
| 319 | 0.16667 | 0.25 | 0.25 | 0.08333 | 0.16667 | 0.08333 | 1.5951 | 365.1 |
| 320 | 0.16667 | 0.25 | 0.25 | 0.16667 | 0.08333 | 0.08333 | 1.6113 | 381.3 |
| 321 | 0.16667 | 0.25 | 0.33333 | 0.08333 | 0.08333 | 0.08333 | 1.5968 | 366.8 |
| 322 | 0.16667 | 0.33333 | 0.08333 | 0.08333 | 0.08333 | 0.25 | 1.6041 | 374.1 |
| 323 | 0.16667 | 0.33333 | 0.08333 | 0.08333 | 0.16667 | 0.16667 | 1.593 | 363 |
| 324 | 0.16667 | 0.33333 | 0.08333 | 0.08333 | 0.25 | 0.08333 | 1.6156 | 385.6 |
| 325 | 0.16667 | 0.33333 | 0.08333 | 0.16667 | 0.08333 | 0.16667 | 1.5795 | 349.5 |
| 326 | 0.16667 | 0.33333 | 0.08333 | 0.16667 | 0.16667 | 0.08333 | 1.5991 | 369.1 |
| 327 | 0.16667 | 0.33333 | 0.08333 | 0.25 | 0.08333 | 0.08333 | 1.6044 | 374.4 |
| 328 | 0.16667 | 0.33333 | 0.16667 | 0.08333 | 0.08333 | 0.16667 | 1.613 | 383 |
| 329 | 0.16667 | 0.33333 | 0.16667 | 0.08333 | 0.16667 | 0.08333 | 1.6107 | 380.7 |
| 330 | 0.16667 | 0.33333 | 0.16667 | 0.16667 | 0.08333 | 0.08333 | 1.5964 | 366.4 |
| 331 | 0.16667 | 0.33333 | 0.25 | 0.08333 | 0.08333 | 0.08333 | 1.5711 | 341.1 |
| 332 | 0.16667 | 0.41667 | 0.08333 | 0.08333 | 0.08333 | 0.16667 | 1.6128 | 382.8 |
| 333 | 0.16667 | 0.41667 | 0.08333 | 0.08333 | 0.16667 | 0.08333 | 1.6119 | 381.9 |
| 334 | 0.16667 | 0.41667 | 0.08333 | 0.16667 | 0.08333 | 0.08333 | 1.5941 | 364.1 |
| 335 | 0.16667 | 0.41667 | 0.16667 | 0.08333 | 0.08333 | 0.08333 | 1.6087 | 378.7 |
| 336 | 0.16667 | 0.5 | 0.08333 | 0.08333 | 0.08333 | 0.08333 | 1.6141 | 384.1 |
| 337 | 0.25 | 0.08333 | 0.08333 | 0.08333 | 0.08333 | 0.41667 | 1.594 | 364 |
| 338 | 0.25 | 0.08333 | 0.08333 | 0.08333 | 0.16667 | 0.33333 | 1.6046 | 374.6 |
| 339 | 0.25 | 0.08333 | 0.08333 | 0.08333 | 0.25 | 0.25 | 1.6095 | 379.5 |
| 340 | 0.25 | 0.08333 | 0.08333 | 0.08333 | 0.33333 | 0.16667 | 1.5976 | 367.6 |
| 341 | 0.25 | 0.08333 | 0.08333 | 0.08333 | 0.41667 | 0.08333 | 1.6 | 370 |
| 342 | 0.25 | 0.08333 | 0.08333 | 0.16667 | 0.08333 | 0.33333 | 1.5913 | 361.3 |
| 343 | 0.25 | 0.08333 | 0.08333 | 0.16667 | 0.16667 | 0.25 | 1.572 | 342 |
| 344 | 0.25 | 0.08333 | 0.08333 | 0.16667 | 0.25 | 0.16667 | 1.5937 | 363.7 |
| 345 | 0.25 | 0.08333 | 0.08333 | 0.16667 | 0.33333 | 0.08333 | 1.6016 | 371.6 |
| 346 | 0.25 | 0.08333 | 0.08333 | 0.25 | 0.08333 | 0.25 | 1.598 | 368 |
| 347 | 0.25 | 0.08333 | 0.08333 | 0.25 | 0.16667 | 0.16667 | 1.5938 | 363.8 |
| 348 | 0.25 | 0.08333 | 0.08333 | 0.25 | 0.25 | 0.08333 | 1.5887 | 358.7 |
| 349 | 0.25 | 0.08333 | 0.08333 | 0.33333 | 0.08333 | 0.16667 | 1.5996 | 369.6 |
| 350 | 0.25 | 0.08333 | 0.08333 | 0.33333 | 0.16667 | 0.08333 | 1.5922 | 362.2 |
| 351 | 0.25 | 0.08333 | 0.08333 | 0.41667 | 0.08333 | 0.08333 | 1.5816 | 351.6 |
| 352 | 0.25 | 0.08333 | 0.16667 | 0.08333 | 0.08333 | 0.33333 | 1.6056 | 375.6 |
| 353 | 0.25 | 0.08333 | 0.16667 | 0.08333 | 0.16667 | 0.25 | 1.5906 | 360.6 |
| 354 | 0.25 | 0.08333 | 0.16667 | 0.08333 | 0.25 | 0.16667 | 1.5888 | 358.8 |
| 355 | 0.25 | 0.08333 | 0.16667 | 0.08333 | 0.33333 | 0.08333 | 1.5837 | 353.7 |
| 356 | 0.25 | 0.08333 | 0.16667 | 0.16667 | 0.08333 | 0.25 | 1.5907 | 360.7 |
| 357 | 0.25 | 0.08333 | 0.16667 | 0.16667 | 0.16667 | 0.16667 | 1.5866 | 356.6 |
| 358 | 0.25 | 0.08333 | 0.16667 | 0.16667 | 0.25 | 0.08333 | 1.581 | 351 |
| 359 | 0.25 | 0.08333 | 0.16667 | 0.25 | 0.08333 | 0.16667 | 1.5965 | 366.5 |
| 360 | 0.25 | 0.08333 | 0.16667 | 0.25 | 0.16667 | 0.08333 | 1.5696 | 339.6 |
| 361 | 0.25 | 0.08333 | 0.16667 | 0.33333 | 0.08333 | 0.08333 | 1.6068 | 376.8 |
| 362 | 0.25 | 0.08333 | 0.25 | 0.08333 | 0.08333 | 0.25 | 1.5851 | 355.1 |
| 363 | 0.25 | 0.08333 | 0.25 | 0.08333 | 0.16667 | 0.16667 | 1.5588 | 328.8 |
| 364 | 0.25 | 0.08333 | 0.25 | 0.08333 | 0.25 | 0.08333 | 1.5646 | 334.6 |
| 365 | 0.25 | 0.08333 | 0.25 | 0.16667 | 0.08333 | 0.16667 | 1.5865 | 356.5 |
| 366 | 0.25 | 0.08333 | 0.25 | 0.16667 | 0.16667 | 0.08333 | 1.5735 | 343.5 |
| 367 | 0.25 | 0.08333 | 0.25 | 0.25 | 0.08333 | 0.08333 | 1.5789 | 348.9 |
| 368 | 0.25 | 0.08333 | 0.33333 | 0.08333 | 0.08333 | 0.16667 | 1.593 | 363 |
| 369 | 0.25 | 0.08333 | 0.33333 | 0.08333 | 0.16667 | 0.08333 | 1.5838 | 353.8 |
| 370 | 0.25 | 0.08333 | 0.33333 | 0.16667 | 0.08333 | 0.08333 | 1.5706 | 340.6 |
| 371 | 0.25 | 0.08333 | 0.41667 | 0.08333 | 0.08333 | 0.08333 | 1.5708 | 340.8 |
| 372 | 0.25 | 0.16667 | 0.08333 | 0.08333 | 0.08333 | 0.33333 | 1.6277 | 397.7 |
| 373 | 0.25 | 0.16667 | 0.08333 | 0.08333 | 0.16667 | 0.25 | 1.6312 | 401.2 |
| 374 | 0.25 | 0.16667 | 0.08333 | 0.08333 | 0.25 | 0.16667 | 1.6063 | 376.3 |
| 375 | 0.25 | 0.16667 | 0.08333 | 0.08333 | 0.33333 | 0.08333 | 1.6006 | 370.6 |
| 376 | 0.25 | 0.16667 | 0.08333 | 0.16667 | 0.08333 | 0.25 | 1.603 | 373 |
| 377 | 0.25 | 0.16667 | 0.08333 | 0.16667 | 0.16667 | 0.16667 | 1.5943 | 364.3 |
| 378 | 0.25 | 0.16667 | 0.08333 | 0.16667 | 0.25 | 0.08333 | 1.6006 | 370.6 |
| 379 | 0.25 | 0.16667 | 0.08333 | 0.25 | 0.08333 | 0.16667 | 1.594 | 364 |
| 380 | 0.25 | 0.16667 | 0.08333 | 0.25 | 0.16667 | 0.08333 | 1.5885 | 358.5 |
| 381 | 0.25 | 0.16667 | 0.08333 | 0.33333 | 0.08333 | 0.08333 | 1.6047 | 374.7 |
| 382 | 0.25 | 0.16667 | 0.16667 | 0.08333 | 0.08333 | 0.25 | 1.5859 | 355.9 |
| 383 | 0.25 | 0.16667 | 0.16667 | 0.08333 | 0.16667 | 0.16667 | 1.5932 | 363.2 |
| 384 | 0.25 | 0.16667 | 0.16667 | 0.08333 | 0.25 | 0.08333 | 1.5803 | 350.3 |
| 385 | 0.25 | 0.16667 | 0.16667 | 0.16667 | 0.08333 | 0.16667 | 1.5916 | 361.6 |
| 386 | 0.25 | 0.16667 | 0.16667 | 0.16667 | 0.16667 | 0.08333 | 1.6 | 370 |
| 387 | 0.25 | 0.16667 | 0.16667 | 0.25 | 0.08333 | 0.08333 | 1.5874 | 357.4 |
| 388 | 0.25 | 0.16667 | 0.25 | 0.08333 | 0.08333 | 0.16667 | 1.5957 | 365.7 |
| 389 | 0.25 | 0.16667 | 0.25 | 0.08333 | 0.16667 | 0.08333 | 1.6026 | 372.6 |
| 390 | 0.25 | 0.16667 | 0.25 | 0.16667 | 0.08333 | 0.08333 | 1.584 | 354 |
| 391 | 0.25 | 0.16667 | 0.33333 | 0.08333 | 0.08333 | 0.08333 | 1.5558 | 325.8 |
| 392 | 0.25 | 0.25 | 0.08333 | 0.08333 | 0.08333 | 0.25 | 1.5943 | 364.3 |
| 393 | 0.25 | 0.25 | 0.08333 | 0.08333 | 0.16667 | 0.16667 | 1.5922 | 362.2 |
| 394 | 0.25 | 0.25 | 0.08333 | 0.08333 | 0.25 | 0.08333 | 1.5967 | 366.7 |
| 395 | 0.25 | 0.25 | 0.08333 | 0.16667 | 0.08333 | 0.16667 | 1.6005 | 370.5 |
| 396 | 0.25 | 0.25 | 0.08333 | 0.16667 | 0.16667 | 0.08333 | 1.5983 | 368.3 |
| 397 | 0.25 | 0.25 | 0.08333 | 0.25 | 0.08333 | 0.08333 | 1.5866 | 356.6 |
| 398 | 0.25 | 0.25 | 0.16667 | 0.08333 | 0.08333 | 0.16667 | 1.59 | 360 |
| 399 | 0.25 | 0.25 | 0.16667 | 0.08333 | 0.16667 | 0.08333 | 1.584 | 354 |
| 400 | 0.25 | 0.25 | 0.16667 | 0.16667 | 0.08333 | 0.08333 | 1.5844 | 354.4 |
| 401 | 0.25 | 0.25 | 0.25 | 0.08333 | 0.08333 | 0.08333 | 1.5665 | 336.5 |
| 402 | 0.25 | 0.33333 | 0.08333 | 0.08333 | 0.08333 | 0.16667 | 1.5831 | 353.1 |
| 403 | 0.25 | 0.33333 | 0.08333 | 0.08333 | 0.16667 | 0.08333 | 1.5997 | 369.7 |
| 404 | 0.25 | 0.33333 | 0.08333 | 0.16667 | 0.08333 | 0.08333 | 1.5863 | 356.3 |
| 405 | 0.25 | 0.33333 | 0.16667 | 0.08333 | 0.08333 | 0.08333 | 1.5888 | 358.8 |
| 406 | 0.25 | 0.41667 | 0.08333 | 0.08333 | 0.08333 | 0.08333 | 1.5803 | 350.3 |
| 407 | 0.33333 | 0.08333 | 0.08333 | 0.08333 | 0.08333 | 0.33333 | 1.5885 | 358.5 |
| 408 | 0.33333 | 0.08333 | 0.08333 | 0.08333 | 0.16667 | 0.25 | 1.5792 | 349.2 |
| 409 | 0.33333 | 0.08333 | 0.08333 | 0.08333 | 0.25 | 0.16667 | 1.5812 | 351.2 |
| 410 | 0.33333 | 0.08333 | 0.08333 | 0.08333 | 0.33333 | 0.08333 | 1.5788 | 348.8 |
| 411 | 0.33333 | 0.08333 | 0.08333 | 0.16667 | 0.08333 | 0.25 | 1.5847 | 354.7 |
| 412 | 0.33333 | 0.08333 | 0.08333 | 0.16667 | 0.16667 | 0.16667 | 1.5923 | 362.3 |
| 413 | 0.33333 | 0.08333 | 0.08333 | 0.16667 | 0.25 | 0.08333 | 1.582 | 352 |
| 414 | 0.33333 | 0.08333 | 0.08333 | 0.25 | 0.08333 | 0.16667 | 1.5871 | 357.1 |
| 415 | 0.33333 | 0.08333 | 0.08333 | 0.25 | 0.16667 | 0.08333 | 1.5932 | 363.2 |
| 416 | 0.33333 | 0.08333 | 0.08333 | 0.33333 | 0.08333 | 0.08333 | 1.5942 | 364.2 |
| 417 | 0.33333 | 0.08333 | 0.16667 | 0.08333 | 0.08333 | 0.25 | 1.5793 | 349.3 |
| 418 | 0.33333 | 0.08333 | 0.16667 | 0.08333 | 0.16667 | 0.16667 | 1.5804 | 350.4 |
| 419 | 0.33333 | 0.08333 | 0.16667 | 0.08333 | 0.25 | 0.08333 | 1.5891 | 359.1 |
| 420 | 0.33333 | 0.08333 | 0.16667 | 0.16667 | 0.08333 | 0.16667 | 1.5744 | 344.4 |
| 421 | 0.33333 | 0.08333 | 0.16667 | 0.16667 | 0.16667 | 0.08333 | 1.5878 | 357.8 |
| 422 | 0.33333 | 0.08333 | 0.16667 | 0.25 | 0.08333 | 0.08333 | 1.5773 | 347.3 |
| 423 | 0.33333 | 0.08333 | 0.25 | 0.08333 | 0.08333 | 0.16667 | 1.5682 | 338.2 |
| 424 | 0.33333 | 0.08333 | 0.25 | 0.08333 | 0.16667 | 0.08333 | 1.5791 | 349.1 |
| 425 | 0.33333 | 0.08333 | 0.25 | 0.16667 | 0.08333 | 0.08333 | 1.574 | 344 |
| 426 | 0.33333 | 0.08333 | 0.33333 | 0.08333 | 0.08333 | 0.08333 | 1.5764 | 346.4 |
| 427 | 0.33333 | 0.16667 | 0.08333 | 0.08333 | 0.08333 | 0.25 | 1.5927 | 362.7 |
| 428 | 0.33333 | 0.16667 | 0.08333 | 0.08333 | 0.16667 | 0.16667 | 1.5766 | 346.6 |
| 429 | 0.33333 | 0.16667 | 0.08333 | 0.08333 | 0.25 | 0.08333 | 1.5975 | 367.5 |
| 430 | 0.33333 | 0.16667 | 0.08333 | 0.16667 | 0.08333 | 0.16667 | 1.5986 | 368.6 |
| 431 | 0.33333 | 0.16667 | 0.08333 | 0.16667 | 0.16667 | 0.08333 | 1.5725 | 342.5 |
| 432 | 0.33333 | 0.16667 | 0.08333 | 0.25 | 0.08333 | 0.08333 | 1.5821 | 352.1 |
| 433 | 0.33333 | 0.16667 | 0.16667 | 0.08333 | 0.08333 | 0.16667 | 1.5743 | 344.3 |
| 434 | 0.33333 | 0.16667 | 0.16667 | 0.08333 | 0.16667 | 0.08333 | 1.5639 | 333.9 |
| 435 | 0.33333 | 0.16667 | 0.16667 | 0.16667 | 0.08333 | 0.08333 | 1.5691 | 339.1 |
| 436 | 0.33333 | 0.16667 | 0.25 | 0.08333 | 0.08333 | 0.08333 | 1.5632 | 333.2 |
| 437 | 0.33333 | 0.25 | 0.08333 | 0.08333 | 0.08333 | 0.16667 | 1.5624 | 332.4 |
| 438 | 0.33333 | 0.25 | 0.08333 | 0.08333 | 0.16667 | 0.08333 | 1.5879 | 357.9 |
| 439 | 0.33333 | 0.25 | 0.08333 | 0.16667 | 0.08333 | 0.08333 | 1.5874 | 357.4 |
| 440 | 0.33333 | 0.25 | 0.16667 | 0.08333 | 0.08333 | 0.08333 | 1.582 | 352 |
| 441 | 0.33333 | 0.33333 | 0.08333 | 0.08333 | 0.08333 | 0.08333 | 1.5852 | 355.2 |
| 442 | 0.41667 | 0.08333 | 0.08333 | 0.08333 | 0.08333 | 0.25 | 1.5858 | 355.8 |
| 443 | 0.41667 | 0.08333 | 0.08333 | 0.08333 | 0.16667 | 0.16667 | 1.5798 | 349.8 |
| 444 | 0.41667 | 0.08333 | 0.08333 | 0.08333 | 0.25 | 0.08333 | 1.567 | 337 |
| 445 | 0.41667 | 0.08333 | 0.08333 | 0.16667 | 0.08333 | 0.16667 | 1.5845 | 354.5 |
| 446 | 0.41667 | 0.08333 | 0.08333 | 0.16667 | 0.16667 | 0.08333 | 1.5743 | 344.3 |
| 447 | 0.41667 | 0.08333 | 0.08333 | 0.25 | 0.08333 | 0.08333 | 1.5855 | 355.5 |
| 448 | 0.41667 | 0.08333 | 0.16667 | 0.08333 | 0.08333 | 0.16667 | 1.5767 | 346.7 |
| 449 | 0.41667 | 0.08333 | 0.16667 | 0.08333 | 0.16667 | 0.08333 | 1.5747 | 344.7 |
| 450 | 0.41667 | 0.08333 | 0.16667 | 0.16667 | 0.08333 | 0.08333 | 1.5807 | 350.7 |
| 451 | 0.41667 | 0.08333 | 0.25 | 0.08333 | 0.08333 | 0.08333 | 1.5543 | 324.3 |
| 452 | 0.41667 | 0.16667 | 0.08333 | 0.08333 | 0.08333 | 0.16667 | 1.5894 | 359.4 |
| 453 | 0.41667 | 0.16667 | 0.08333 | 0.08333 | 0.16667 | 0.08333 | 1.5941 | 364.1 |
| 454 | 0.41667 | 0.16667 | 0.08333 | 0.16667 | 0.08333 | 0.08333 | 1.5828 | 352.8 |
| 455 | 0.41667 | 0.16667 | 0.16667 | 0.08333 | 0.08333 | 0.08333 | 1.5725 | 342.5 |
| 456 | 0.41667 | 0.25 | 0.08333 | 0.08333 | 0.08333 | 0.08333 | 1.5694 | 339.4 |
| 457 | 0.5 | 0.08333 | 0.08333 | 0.08333 | 0.08333 | 0.16667 | 1.5808 | 350.8 |
| 458 | 0.5 | 0.08333 | 0.08333 | 0.08333 | 0.16667 | 0.08333 | 1.5813 | 351.3 |
| 459 | 0.5 | 0.08333 | 0.08333 | 0.16667 | 0.08333 | 0.08333 | 1.5818 | 351.8 |
| 460 | 0.5 | 0.08333 | 0.16667 | 0.08333 | 0.08333 | 0.08333 | 1.5758 | 345.8 |
| 461 | 0.5 | 0.16667 | 0.08333 | 0.08333 | 0.08333 | 0.08333 | 1.5791 | 349.1 |
| 462 | 0.58333 | 0.08333 | 0.08333 | 0.08333 | 0.08333 | 0.08333 | 1.5837 | 353.7 |

Supplementary Table S2. Summary of the top 20 catalyst formulations predicted by SpecGen and their experimentally measured OER performance at 10 mA/cm².

| Cat. No. | Synthetic formula |  |  |  |  |  | Potential@10 mA/cm2 (V vs. RHE) | η10 (mV) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Co | Ni | Cu | Mg | Cd | Zn |  |  |
| 1 | 0.429593 | 0.113788 | 0.299182 | 0.040375 | 0.117062 | 0 | 1.5427 | 312.7 |
| 2 | 0.278453 | 0.130297 | 0.375048 | 0.028459 | 0.110748 | 0.076995 | 1.5398 | 309.8 |
| 3 | 0.233889 | 0.006294 | 0.417164 | 0.206321 | 0.136332 | 0 | 1.5521 | 322.1 |
| 4 | 0.227918 | 0.096763 | 0.191293 | 0.310761 | 0.140743 | 0.032522 | 1.5395 | 309.5 |
| 5 | 0.354431 | 0.044088 | 0.383341 | 0.069694 | 0.037643 | 0.110803 | 1.5709 | 340.9 |
| 6 | 0.240122 | 0.124119 | 0.490794 | 0.052902 | 0.041598 | 0.050464 | 1.5578 | 327.8 |
| 7 | 0.383386 | 0.029216 | 0.338549 | 0.241883 | 0.006966 | 0 | 1.5607 | 330.7 |
| 8 | 0.333932 | 0.108801 | 0.447896 | 0.096447 | 0.012923 | 0 | 1.5572 | 327.2 |
| 9 | 0.20159 | 0.092492 | 0.591005 | 0.105748 | 0 | 0.009166 | 1.5431 | 313.1 |
| 10 | 0.417451 | 0.005787 | 0.34112 | 0.13095 | 0.075295 | 0.029397 | 1.5223 | 292.3 |
| 11 | 0.204621 | 0.012808 | 0.342966 | 0.117014 | 0.1223 | 0.20029 | 1.5502 | 320.2 |
| 12 | 0.34895 | 0 | 0.24731 | 0.137717 | 0.113325 | 0.152698 | 1.5634 | 333.4 |
| 13 | 0.180125 | 0.215226 | 0.317918 | 0.054696 | 0.120048 | 0.111987 | 1.5723 | 342.3 |
| 14 | 0.411668 | 0.163669 | 0 | 0.075649 | 0.349014 | 0 | 1.5415 | 311.5 |
| 15 | 0.248242 | 0.07979 | 0.343541 | 0.166475 | 0.08879 | 0.073162 | 1.5568 | 326.8 |
| 16 | 0.269711 | 0.133135 | 0.331243 | 0.183442 | 0.082468 | 0 | 1.5572 | 327.2 |
| 17 | 0.317784 | 0.074374 | 0.493159 | 0 | 0.114683 | 0 | 1.5559 | 325.9 |
| 18 | 0.184427 | 0.31483 | 0.271342 | 0.099875 | 0.098735 | 0.030792 | 1.5741 | 344.1 |
| 19 | 0.246069 | 0.134868 | 0.388437 | 0.130266 | 0 | 0.100359 | 1.5832 | 353.2 |
| 20 | 0.162031 | 0.256435 | 0.337963 | 0.001164 | 0.054213 | 0.188193 | 1.5902 | 360.2 |

Supplementary Table S3. Predicted metal compositions and the corresponding S2P predicted catalytic performances for 20 randomly generated spectra using the VAE model and the S2C model.

| Cat. No. | Synthetic formula |  |  |  |  |  | Potential@10 mA/cm2 (V vs. RHE) | η10 (mV) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Co | Ni | Cu | Mg | Mn | Zn |  |  |
| 1 | 0.083664 | 0.192516 | 0.120434 | 0.130921 | 0.221782 | 0.250683 | 1.62543 | 395.43 |
| 2 | 0.104965 | 0.144921 | 0.240039 | 0.165926 | 0.144357 | 0.199792 | 1.65238 | 422.38 |
| 3 | 0.085047 | 0.149579 | 0.104232 | 0.321591 | 0.091574 | 0.247977 | 1.65286 | 422.86 |
| 4 | 0.083906 | 0.099876 | 0.154266 | 0.317227 | 0.21602 | 0.128705 | 1.63985 | 409.85 |
| 5 | 0.069772 | 0.129026 | 0.089359 | 0.231835 | 0.228337 | 0.251672 | 1.62895 | 398.95 |
| 6 | 0.134046 | 0.273188 | 0.222503 | 0.070222 | 0.090956 | 0.209084 | 1.61858 | 388.58 |
| 7 | 0.059531 | 0.061324 | 0.381616 | 0.259347 | 0.158872 | 0.079311 | 1.62996 | 399.96 |
| 8 | 0.082589 | 0.246164 | 0.26892 | 0.284079 | 0.118247 | 0 | 1.64055 | 410.55 |
| 9 | 0.120926 | 0.147138 | 0.329785 | 0.217809 | 0.182627 | 0.001714 | 1.59684 | 366.84 |
| 10 | 0.07278 | 0.135866 | 0.222313 | 0.332175 | 0.129223 | 0.107644 | 1.66529 | 435.29 |
| 11 | 0.036236 | 0.159356 | 0.074054 | 0.333284 | 0.353488 | 0.043582 | 1.65981 | 429.81 |
| 12 | 0.094321 | 0.114885 | 0.170099 | 0.395609 | 0.157402 | 0.067684 | 1.67524 | 445.24 |
| 13 | 0.080472 | 0.20921 | 0.273678 | 0.175374 | 0.075966 | 0.185301 | 1.68511 | 455.11 |
| 14 | 0.079725 | 0.229363 | 0.289096 | 0.24837 | 0.127623 | 0.025823 | 1.63282 | 402.82 |
| 15 | 0.040378 | 0.158388 | 0.140386 | 0.43762 | 0.15527 | 0.067959 | 1.67493 | 444.93 |
| 16 | 0.081034 | 0.142865 | 0.199849 | 0.35234 | 0.082113 | 0.141799 | 1.66382 | 433.82 |
| 17 | 0.118525 | 0.033514 | 0.243736 | 0.384257 | 0.080877 | 0.13909 | 1.68525 | 455.25 |
| 18 | 0.097563 | 0.142958 | 0.283518 | 0.306358 | 0.118437 | 0.051166 | 1.64646 | 416.46 |
| 19 | 0.071291 | 0.221154 | 0.148464 | 0.215178 | 0.21029 | 0.133622 | 1.63589 | 405.89 |
| 20 | 0.008291 | 0.104901 | 0.246859 | 0.487739 | 0.15221 | 0 | 1.65623 | 426.23 |

Supplementary Table S4. S2P predicted overpotential values of the best performing 20 catalyst compositions identified by the C2P model.

| Cat. No. | Synthetic formula |  |  |  |  |  | Potential@10 mA/cm2 (V vs. RHE) | η10 (mV) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Co | Ni | Cu | Mg | Mn | Zn |  |  |
| 1 | 0.46 | 0.02 | 0.46 | 0.02 | 0.02 | 0.02 | 1.57454 | 344.54 |
| 2 | 0.48 | 0.02 | 0.44 | 0.02 | 0.02 | 0.02 | 1.56868 | 338.68 |
| 3 | 0.5 | 0.02 | 0.42 | 0.02 | 0.02 | 0.02 | 1.58318 | 353.18 |
| 4 | 0.44 | 0.04 | 0.46 | 0.02 | 0.02 | 0.02 | 1.59117 | 361.17 |
| 5 | 0.46 | 0.04 | 0.44 | 0.02 | 0.02 | 0.02 | 1.59765 | 367.65 |
| 6 | 0.44 | 0.02 | 0.46 | 0.02 | 0.04 | 0.02 | 1.57439 | 344.39 |
| 7 | 0.48 | 0.04 | 0.42 | 0.02 | 0.02 | 0.02 | 1.58834 | 358.34 |
| 8 | 0.52 | 0.02 | 0.4 | 0.02 | 0.02 | 0.02 | 1.59572 | 365.72 |
| 9 | 0.46 | 0.02 | 0.44 | 0.02 | 0.04 | 0.02 | 1.57162 | 341.62 |
| 10 | 0.44 | 0.02 | 0.46 | 0.04 | 0.02 | 0.02 | 1.57028 | 340.28 |
| 11 | 0.48 | 0.02 | 0.42 | 0.02 | 0.04 | 0.02 | 1.59871 | 368.71 |
| 12 | 0.5 | 0.04 | 0.4 | 0.02 | 0.02 | 0.02 | 1.57655 | 346.55 |
| 13 | 0.46 | 0.02 | 0.44 | 0.02 | 0.02 | 0.04 | 1.58857 | 358.57 |
| 14 | 0.46 | 0.02 | 0.44 | 0.04 | 0.02 | 0.02 | 1.58885 | 358.85 |
| 15 | 0.5 | 0.02 | 0.4 | 0.02 | 0.04 | 0.02 | 1.58022 | 350.22 |
| 16 | 0.48 | 0.02 | 0.42 | 0.02 | 0.02 | 0.04 | 1.5745 | 344.51 |
| 17 | 0.44 | 0.06 | 0.44 | 0.02 | 0.02 | 0.02 | 1.57273 | 342.73 |
| 18 | 0.48 | 0.02 | 0.42 | 0.04 | 0.02 | 0.02 | 1.56807 | 338.07 |
| 19 | 0.42 | 0.04 | 0.46 | 0.02 | 0.04 | 0.02 | 1.56083 | 330.83 |
| 20 | 0.46 | 0.06 | 0.42 | 0.02 | 0.02 | 0.02 | 1.57067 | 340.67 |

Supplementary Fig. S1 The carbon paper-supported catalyst demonstrated excellent catalytic stability and repeatability for the OER test. Over 15 consecutive measurements, the average overpotential at 10 mA/cm² was found to be 1.589 V, with a maximum deviation of ±9 mV.

Supplementary Fig. S2 The robotic platform enabled high-throughput materials discovery with an average sample turnaround time of 78 minutes, compared to 20 hours for the manual operations.

Supplementary Fig. S3 XRD pattern of as-synthesized Exp-451.

Supplementary Note S1.

The VAE model aims to perform efficient approximate inference and learning with directed probabilistic models containing continuous latent variables or parameters, where the posterior distributions are intractable. The traditional variational Bayesian (VB) approach involves optimizing an approximation to this posterior. However, the common mean-field approach requires analytical solutions that are often intractable.1

Assume we have an i.i.d. dataset X = x(i)i=1N where each data point consists of continuous variables representing absorbance intensity at different wavelengths. These data points are assumed to be generated by a process involving an unobserved continuous random variable z. The goal is to perform optimization on the model parameters θ, and variational inference on the latent variables z to produce reasonable potential spectra.

The marginal likelihood is composed of a sum over the marginal likelihoods of individual data points log pθ(x(1), … ,x(N)) = i=1Nlog pθ(x(i)),which can each be rewritten as:

log pθ(x(i)) = DKL(qϕ(z|x(i))||pθ(z|x(i))) + L(θ,ϕ;x(i))

The first RHS term is the KL divergence of the approximate from the true posterior. Since this KL-divergence is non-negative, the second RHS term  L(θ,ϕ;x(i)) is called the (variational) lower bound on the marginal likelihood of data point i, and can be written as:

log pθ(x(i)) ≥ L(θ,ϕ;x(i)) = Eqϕ(z|x)[-log qϕ(z|x) + log pθ(x|z)]

L(θ,ϕ;x(i)) = -DKL(qϕ(z|x(i))||pθ(z)) + Eqϕ(z|x(i))[log pθ(x(i)|z)]

The challenge lies in maximizing L(θ,ϕ;x(i)) by adjusting the parameters ϕ and θ. However, the gradient of the loss function with respect to the parameters involves the sampling process. Since the distribution of z ~ qϕ(z|x(i)) is unknown, it is not possible to directly perform backpropagation through this sampling process.

To overcome this issue, the VAE model uses a parameterization stratagem. The key idea is to express the latent variable z as a deterministic variable z = gϕ(ϵ,x), where ϵ is an auxiliary variable with independent marginal distribution p(ϵ), and gϕ(⋅) is some vector-valued function parameterized by ϕ. This parameterization allows us to rewrite an expectation with respect to qϕ(z|x) so that the Monte Carlo estimate is differentiable with respect to ϕ.

In this case of the univariate Gaussian (z ~ p(z|x) = N(μ,σ2)), a valid reparameterization is z = μ + σϵ, where ϵ is an auxiliary noise variable ϵ ~ N(0,1).Therefore, EN(z;μ,σ2)[f(z)] = EN(ϵ;0,1)[f(μ + σϵ)] ≃ 1Ll=1Lf(μ + σϵ(l)) where ϵ(l) ~ N(0,1).

For the VAE model, a neural network is used as the probabilistic encoder qϕ(z|x) for the variational approximation to the posterior distribution of the generative model pθ(x,z). The parameters ϕ and θ are optimized jointly with the AEVB algorithm.

In our work, the prior over the latent variables is assumed to be the centered isotropic multivariate Gaussian distribution pθ(z) = N(z;0,I), with distribution parameters computed from z. Noting that the true posterior distribution pθ(z|x) is intractable, and there is much freedom in the form qϕ(z|x), the VAE model assumes the true posterior takes on an approximate Gaussian form with an approximately diagonal covariance. In this case, the variational approximate posterior can be modeled as a multivariate Gaussian with a diagonal covariance structure:

log qϕ(z|x(i)) = log N(z;μ(i),σ2(i)I)

The mean (μ(i)) and standard deviation (σ(i)) of the approximate posterior are the outputs of the encoding MLP. In other words, they are nonlinear functions of data point x(i) and the variational parameters ϕ.

To sample from the posterior distribution z(i,l) ~ qϕ(z|x(i)), the VAE model uses z(i,l) = gϕ(x(i),ϵ(l)) = μ(i) + σ(i)⊙ϵ(l) where ϵ(l) ~ N(0,I).In this model both pθ(z) (the prior) and qϕ(z|x) are Gaussian. Given this situation, we can get the reulting estimator for this model and data point x(i) is:

L(θ,ϕ;x(i)) ≃ 12j=1J(1 + log((σj(i))2) - (μj(i))2 - (σj(i))2) + 1Ll=1Llog pθ(x(i)|z(i,l))

where z(i,l) = μ(i) + σ(i)⊙ϵ(l) and ϵ(l) ~ N(0,I)

Supplementary Fig. S4 Comparison of experimentally measured UV-Vis-NIR spectra with those reconstructed from the VAE latent space.

Supplementary Fig. S5 (a, b) Digital images of the in situ electrochemical Raman spectroscopy setup for the detection of transient active species during the OER processes. (c,d) In-situ Raman spectra and corresponding contour plots of (c) the Exp-451 catalyst and (d) the SpecGen-optimized catalyst at various potentials.

Supplementary Fig. S6 Atomic-resolution HAADF-STEM imaging with EDS elemental mapping reveals the amorphous crystal structure of SpecGen-optimized catalyst. Inset shows a corresponding selected electron diffractogram.

Supplementary Fig. S7 Nyquist plots of the Exp-451 catalyst and the SpecGen-optimized catalyst.

Supplementary Fig. S8 Double layer capacitance of the Exp-451 catalyst and the SpecGen-optimized catalyst. Calculations were based on the linear regression of the current density differences at a non-Faradaic potential of E = 1.10 V vs. RHE (Δj = ja – jc), ja: anodic current, jc: cathodic current) vs. the scan rates.

Supplementary Fig. S9 Faradaic efficiencies (FEs) of SpecGen-optimized catalyst for OER in 1M KOH electrolyte at 10 and 50 mA/cm2.

Supplementary Table S5. A compositional table for a series of derivative metal-organic hybrid catalysts with the general formula (Co, Ni, Cu, Mg/Fe, Cd/Mn, Zn)-ligand. These catalysts were prepared by wet chemistry and can be classified into 4 groups based on variations in their metal compositions and organic ligands. Derivative Group A and B system maintain the original (Co, Ni, Cu, Mg, Cd, Zn) metal composition but possess different the organic ligands, 2-aminobenzene-1,4-dicarboxylic acid and 1,3,5-benzenetricarboxylic acid, respectively. Derivative Group C and D system maintain the 1,4-benzenedicarboxylic acid ligand but have different metal combinations, (Co, Ni, Cu, Fe, Cd, Zn) and (Co, Ni, Cu, Mg, Mn, Zn), respectively.

| Cat. No. | Synthetic formula |  |  |  |  |  | η10 (mV) |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Metal-1 (Co) | Metal-2 (Ni) | Metal-3 (Cu) | Metal-4 (Mg/Fe) | Metal-5 (Cd/Mn) | Metal-6 (Zn) | Derivative Group-A | Derivative Group-B | Derivative Group-C | Derivative Group-D |
| 1 | 0.1 | 0.1 | 0.1 | 0.1 | 0.1 | 0.5 | 393.5 | 404.1 | 342.4 | 400.1 |
| 2 | 0.1 | 0.1 | 0.1 | 0.1 | 0.2 | 0.4 | 381 | 445.3 | 359 | 390.7 |
| 3 | 0.1 | 0.1 | 0.1 | 0.1 | 0.3 | 0.3 | 384.1 | 402 | 334 | 420.3 |
| 4 | 0.1 | 0.1 | 0.1 | 0.1 | 0.4 | 0.2 | 374.8 | 419 | 354.6 | 423.3 |
| 5 | 0.1 | 0.1 | 0.1 | 0.1 | 0.5 | 0.1 | 423.3 | 419.1 | 385.3 | 440.2 |
| 6 | 0.1 | 0.1 | 0.1 | 0.2 | 0.1 | 0.4 | 398.5 | 430.6 | 337.3 | 416.2 |
| 7 | 0.1 | 0.1 | 0.1 | 0.2 | 0.2 | 0.3 | 403 | 414.5 | 369.9 | 432 |
| 8 | 0.1 | 0.1 | 0.1 | 0.2 | 0.3 | 0.2 | 397 | 420.8 | 420.8 | 474.3 |
| 9 | 0.1 | 0.1 | 0.1 | 0.2 | 0.4 | 0.1 | 381 | 418 | 345.1 | 441.8 |
| 10 | 0.1 | 0.1 | 0.1 | 0.3 | 0.1 | 0.3 | 408.6 | 453 | 347.9 | 445.7 |
| 11 | 0.1 | 0.1 | 0.1 | 0.3 | 0.2 | 0.2 | 391.9 | 428.8 | 374.7 | 506.6 |
| 12 | 0.1 | 0.1 | 0.1 | 0.3 | 0.3 | 0.1 | 372.3 | 429 | 338.2 | 433 |
| 13 | 0.1 | 0.1 | 0.1 | 0.4 | 0.1 | 0.2 | 411.8 | 424.6 | 359.2 | 431.5 |
| 14 | 0.1 | 0.1 | 0.1 | 0.4 | 0.2 | 0.1 | 396.1 | 441.3 | 383 | 433.4 |
| 15 | 0.1 | 0.1 | 0.1 | 0.5 | 0.1 | 0.1 | 437 | 443.6 | 330.6 | 444.3 |
| 16 | 0.1 | 0.1 | 0.2 | 0.1 | 0.1 | 0.4 | 386.8 | 392.1 | 341.9 | 402.3 |
| 17 | 0.1 | 0.1 | 0.2 | 0.1 | 0.2 | 0.3 | 357 | 396.7 | 410.8 | 429.8 |
| 18 | 0.1 | 0.1 | 0.2 | 0.1 | 0.3 | 0.2 | 355.2 | 396.7 | 344 | 416.3 |
| 19 | 0.1 | 0.1 | 0.2 | 0.1 | 0.4 | 0.1 | 340.6 | 396 | 373.6 | 454.7 |
| 20 | 0.1 | 0.1 | 0.2 | 0.2 | 0.1 | 0.3 | 384.4 | 419.2 | 369.2 | 421.7 |
| 21 | 0.1 | 0.1 | 0.2 | 0.2 | 0.2 | 0.2 | 412.7 | 499 | 334.8 | 424.8 |
| 22 | 0.1 | 0.1 | 0.2 | 0.2 | 0.3 | 0.1 | 373.8 | 447.7 | 369.5 | 409.7 |
| 23 | 0.1 | 0.1 | 0.2 | 0.3 | 0.1 | 0.2 | 430.1 | 422.9 | 385.7 | 447.8 |
| 24 | 0.1 | 0.1 | 0.2 | 0.3 | 0.2 | 0.1 | 396.5 | 423.5 | 331.3 | 425.2 |
| 25 | 0.1 | 0.1 | 0.2 | 0.4 | 0.1 | 0.1 | 433 | 429.7 | 355.7 | 431.2 |
| 26 | 0.1 | 0.1 | 0.3 | 0.1 | 0.1 | 0.3 | 414.1 | 452.9 | 341 | 387.6 |
| 27 | 0.1 | 0.1 | 0.3 | 0.1 | 0.2 | 0.2 | 400 | 478.3 | 352.7 | 408.5 |
| 28 | 0.1 | 0.1 | 0.3 | 0.1 | 0.3 | 0.1 | 384.2 | 411.7 | 371.6 | 402.9 |
| 29 | 0.1 | 0.1 | 0.3 | 0.2 | 0.1 | 0.2 | 426 | 460.8 | 344.4 | 450.5 |
| 30 | 0.1 | 0.1 | 0.3 | 0.2 | 0.2 | 0.1 | 418.1 | 459.4 | 326.2 | 400.6 |
| 31 | 0.1 | 0.1 | 0.3 | 0.3 | 0.1 | 0.1 | 428.3 | 362.7 | 339.6 | 419.2 |
| 32 | 0.1 | 0.1 | 0.4 | 0.1 | 0.1 | 0.2 | 373.3 | 452.5 | 343.4 | 368.5 |
| 33 | 0.1 | 0.1 | 0.4 | 0.1 | 0.2 | 0.1 | 366 | 428.5 | 342.4 | 394.4 |
| 34 | 0.1 | 0.1 | 0.4 | 0.2 | 0.1 | 0.1 | 384.5 | 448.3 | 343.8 | 392.1 |
| 35 | 0.1 | 0.1 | 0.5 | 0.1 | 0.1 | 0.1 | 369.6 | 434.9 | 335.6 | 389.9 |
| 36 | 0.1 | 0.2 | 0.1 | 0.1 | 0.1 | 0.4 | 407 | 466.1 | 301.2 | 413.1 |
| 37 | 0.1 | 0.2 | 0.1 | 0.1 | 0.2 | 0.3 | 420.4 | 463.9 | 300.8 | 394 |
| 38 | 0.1 | 0.2 | 0.1 | 0.1 | 0.3 | 0.2 | 387.1 | 457.5 | 334.2 | 410.6 |
| 39 | 0.1 | 0.2 | 0.1 | 0.1 | 0.4 | 0.1 | 383.2 | 442.6 | 446.6 | 419 |
| 40 | 0.1 | 0.2 | 0.1 | 0.2 | 0.1 | 0.3 | 433 | 467 | 334.9 | 429.3 |
| 41 | 0.1 | 0.2 | 0.1 | 0.2 | 0.2 | 0.2 | 419.5 | 431.2 | 340.2 | 429.9 |
| 42 | 0.1 | 0.2 | 0.1 | 0.2 | 0.3 | 0.1 | 416.3 | 456.9 | 347.6 | 467.3 |
| 43 | 0.1 | 0.2 | 0.1 | 0.3 | 0.1 | 0.2 | 428.2 | 445.1 | 340.9 | 459.5 |
| 44 | 0.1 | 0.2 | 0.1 | 0.3 | 0.2 | 0.1 | 423.1 | 464.5 | 373.1 | 409.6 |
| 45 | 0.1 | 0.2 | 0.1 | 0.4 | 0.1 | 0.1 | 454.8 | 456.3 | 389.5 | 417.7 |
| 46 | 0.1 | 0.2 | 0.2 | 0.1 | 0.1 | 0.3 | 433.8 | 438.5 | 346.5 | 410.4 |
| 47 | 0.1 | 0.2 | 0.2 | 0.1 | 0.2 | 0.2 | 397.1 | 409.7 | 348.4 | 389.3 |
| 48 | 0.1 | 0.2 | 0.2 | 0.1 | 0.3 | 0.1 | 395.7 | 446 | 358 | 437.7 |
| 49 | 0.1 | 0.2 | 0.2 | 0.2 | 0.1 | 0.2 | 506.2 | 379.7 | 326.2 | 341.2 |
| 50 | 0.1 | 0.2 | 0.2 | 0.2 | 0.2 | 0.1 | 398 | 426.9 | 351.1 | 425.5 |
| 51 | 0.1 | 0.2 | 0.2 | 0.3 | 0.1 | 0.1 | 400.6 | 449.7 | 350.3 | 435 |
| 52 | 0.1 | 0.2 | 0.3 | 0.1 | 0.1 | 0.2 | 375.7 | 424.9 | 351.5 | 399.3 |
| 53 | 0.1 | 0.2 | 0.3 | 0.1 | 0.2 | 0.1 | 419.6 | 412.7 | 330.2 | 367.5 |
| 54 | 0.1 | 0.2 | 0.3 | 0.2 | 0.1 | 0.1 | 373.4 | 394 | 335.6 | 430.2 |
| 55 | 0.1 | 0.2 | 0.4 | 0.1 | 0.1 | 0.1 | 370.4 | 424.1 | 365.6 | 445.1 |
| 56 | 0.1 | 0.3 | 0.1 | 0.1 | 0.1 | 0.3 | 413.8 | 460.1 | 331.3 | 429 |
| 57 | 0.1 | 0.3 | 0.1 | 0.1 | 0.2 | 0.2 | 406.8 | 442.6 | 297.9 | 417.6 |
| 58 | 0.1 | 0.3 | 0.1 | 0.1 | 0.3 | 0.1 | 414.3 | 445.6 | 322.2 | 439.2 |
| 59 | 0.1 | 0.3 | 0.1 | 0.2 | 0.1 | 0.2 | 456.9 | 431.3 | 294.7 | 458.9 |
| 60 | 0.1 | 0.3 | 0.1 | 0.2 | 0.2 | 0.1 | 414 | 454.8 | 303.1 | 424.7 |
| 61 | 0.1 | 0.3 | 0.1 | 0.3 | 0.1 | 0.1 | 455.5 | 449.9 | 289.9 | 447.5 |
| 62 | 0.1 | 0.3 | 0.2 | 0.1 | 0.1 | 0.2 | 413.8 | 429.5 | 264.5 | 399.1 |
| 63 | 0.1 | 0.3 | 0.2 | 0.1 | 0.2 | 0.1 | 382.5 | 425.2 | 297.6 | 463.3 |
| 64 | 0.1 | 0.3 | 0.2 | 0.2 | 0.1 | 0.1 | 403.2 | 421.6 | 303.2 | 442.2 |
| 65 | 0.1 | 0.3 | 0.3 | 0.1 | 0.1 | 0.1 | 362 | 451.6 | 300 | 410 |
| 66 | 0.1 | 0.4 | 0.1 | 0.1 | 0.1 | 0.2 | 419.3 | 446.6 | 375 | 411.7 |
| 67 | 0.1 | 0.4 | 0.1 | 0.1 | 0.2 | 0.1 | 490.9 | 448.3 | 382.2 | 462.4 |
| 68 | 0.1 | 0.4 | 0.1 | 0.2 | 0.1 | 0.1 | 422.8 | 439.7 | 325.3 | 465.2 |
| 69 | 0.1 | 0.4 | 0.2 | 0.1 | 0.1 | 0.1 | 396.5 | 405.4 | 305.5 | 425.2 |
| 70 | 0.1 | 0.5 | 0.1 | 0.1 | 0.1 | 0.1 | 406.5 | 431.8 | 341.6 | 462.6 |
| 71 | 0.2 | 0.1 | 0.1 | 0.1 | 0.1 | 0.4 | 384.1 | 429.7 | 309.2 | 371.1 |
| 72 | 0.2 | 0.1 | 0.1 | 0.1 | 0.2 | 0.3 | 382.7 | 420.5 | 317.7 | 382.4 |
| 73 | 0.2 | 0.1 | 0.1 | 0.1 | 0.3 | 0.2 | 357.9 | 400.7 | 301.4 | 396.6 |
| 74 | 0.2 | 0.1 | 0.1 | 0.1 | 0.4 | 0.1 | 408.1 | 419.8 | 308.4 | 400.4 |
| 75 | 0.2 | 0.1 | 0.1 | 0.2 | 0.1 | 0.3 | 383.5 | 429.7 | 299 | 382 |
| 76 | 0.2 | 0.1 | 0.1 | 0.2 | 0.2 | 0.2 | 413 | 472 | 340.9 | 385.4 |
| 77 | 0.2 | 0.1 | 0.1 | 0.2 | 0.3 | 0.1 | 344.1 | 390 | 351 | 397 |
| 78 | 0.2 | 0.1 | 0.1 | 0.3 | 0.1 | 0.2 | 350.2 | 426.8 | 338.7 | 392.9 |
| 79 | 0.2 | 0.1 | 0.1 | 0.3 | 0.2 | 0.1 | 386.6 | 437.5 | 309.6 | 394.3 |
| 80 | 0.2 | 0.1 | 0.1 | 0.4 | 0.1 | 0.1 | 395.6 | 420.2 | 326.9 | 398 |
| 81 | 0.2 | 0.1 | 0.2 | 0.1 | 0.1 | 0.3 | 370.9 | 398.2 | 346.8 | 367.3 |
| 82 | 0.2 | 0.1 | 0.2 | 0.1 | 0.2 | 0.2 | 361 | 393.8 | 350.6 | 383 |
| 83 | 0.2 | 0.1 | 0.2 | 0.1 | 0.3 | 0.1 | 348.1 | 420.2 | 350.3 | 382.2 |
| 84 | 0.2 | 0.1 | 0.2 | 0.2 | 0.1 | 0.2 | 366.1 | 425 | 333.9 | 416.2 |
| 85 | 0.2 | 0.1 | 0.2 | 0.2 | 0.2 | 0.1 | 357 | 389.5 | 339.2 | 359.5 |
| 86 | 0.2 | 0.1 | 0.2 | 0.3 | 0.1 | 0.1 | 406.4 | 399.3 | 337.1 | 389.9 |
| 87 | 0.2 | 0.1 | 0.3 | 0.1 | 0.1 | 0.2 | 364.3 | 369.5 | 409.1 | 331.1 |
| 88 | 0.2 | 0.1 | 0.3 | 0.1 | 0.2 | 0.1 | 374.7 | 349.2 | 356.5 | 370.2 |
| 89 | 0.2 | 0.1 | 0.3 | 0.2 | 0.1 | 0.1 | 369.2 | 380.5 | 321.4 | 366.5 |
| 90 | 0.2 | 0.1 | 0.4 | 0.1 | 0.1 | 0.1 | 391 | 363.8 | 344.2 | 354.2 |
| 91 | 0.2 | 0.2 | 0.1 | 0.1 | 0.1 | 0.3 | 421.8 | 398.6 | 402.7 | 371.7 |
| 92 | 0.2 | 0.2 | 0.1 | 0.1 | 0.2 | 0.2 | 374.7 | 440.3 | 339.9 | 391.2 |
| 93 | 0.2 | 0.2 | 0.1 | 0.1 | 0.3 | 0.1 | 368.8 | 409.7 | 330.3 | 385.8 |
| 94 | 0.2 | 0.2 | 0.1 | 0.2 | 0.1 | 0.2 | 384.2 | 421 | 374.5 | 374.5 |
| 95 | 0.2 | 0.2 | 0.1 | 0.2 | 0.2 | 0.1 | 378.5 | 421 | 345.8 | 374 |
| 96 | 0.2 | 0.2 | 0.1 | 0.3 | 0.1 | 0.1 | 420.7 | 429.8 | 291 | 391.2 |
| 97 | 0.2 | 0.2 | 0.2 | 0.1 | 0.1 | 0.2 | 368.8 | 397.3 | 337.6 | 361 |
| 98 | 0.2 | 0.2 | 0.2 | 0.1 | 0.2 | 0.1 | 371.2 | 391 | 345.1 | 386 |
| 99 | 0.2 | 0.2 | 0.2 | 0.2 | 0.1 | 0.1 | 378.4 | 388 | 327.3 | 395.5 |
| 100 | 0.2 | 0.2 | 0.3 | 0.1 | 0.1 | 0.1 | 350.3 | 347.6 | 347.6 | 365.4 |
| 101 | 0.2 | 0.3 | 0.1 | 0.1 | 0.1 | 0.2 | 549.8 | 463 | 327.6 | 395.8 |
| 102 | 0.2 | 0.3 | 0.1 | 0.1 | 0.2 | 0.1 | 352.5 | 446.2 | 340.8 | 397.3 |
| 103 | 0.2 | 0.3 | 0.1 | 0.2 | 0.1 | 0.1 | 418 | 407.8 | 338 | 372.7 |
| 104 | 0.2 | 0.3 | 0.2 | 0.1 | 0.1 | 0.1 | 559.1 | 383 | 325.5 | 378.5 |
| 105 | 0.2 | 0.4 | 0.1 | 0.1 | 0.1 | 0.1 | 419.1 | 428.8 | 337 | 412.6 |
| 106 | 0.3 | 0.1 | 0.1 | 0.1 | 0.1 | 0.3 | 353.3 | 389.3 | 387.3 | 349.4 |
| 107 | 0.3 | 0.1 | 0.1 | 0.1 | 0.2 | 0.2 | 545.8 | 408.1 | 333 | 362.8 |
| 108 | 0.3 | 0.1 | 0.1 | 0.1 | 0.3 | 0.1 | 559.8 | 421.4 | 324.4 | 384 |
| 109 | 0.3 | 0.1 | 0.1 | 0.2 | 0.1 | 0.2 | 400.1 | 387.4 | 326 | 362.8 |
| 110 | 0.3 | 0.1 | 0.1 | 0.2 | 0.2 | 0.1 | 388.8 | 402.8 | 334.1 | 352.9 |
| 111 | 0.3 | 0.1 | 0.1 | 0.3 | 0.1 | 0.1 | 377.6 | 385.1 | 341.8 | 425.3 |
| 112 | 0.3 | 0.1 | 0.2 | 0.1 | 0.1 | 0.2 | 339.8 | 377.5 | 308 | 359.2 |
| 113 | 0.3 | 0.1 | 0.2 | 0.1 | 0.2 | 0.1 | 318.1 | 389.7 | 339.8 | 364.9 |
| 114 | 0.3 | 0.1 | 0.2 | 0.2 | 0.1 | 0.1 | 343.8 | 367.3 | 308.7 | 342 |
| 115 | 0.3 | 0.1 | 0.3 | 0.1 | 0.1 | 0.1 | 321.9 | 358.6 | 334.4 | 351.3 |
| 116 | 0.3 | 0.2 | 0.1 | 0.1 | 0.1 | 0.2 | 349.2 | 403.9 | 297.1 | 347.1 |
| 117 | 0.3 | 0.2 | 0.1 | 0.1 | 0.2 | 0.1 | 352.5 | 340.4 | 337.2 | 373 |
| 118 | 0.3 | 0.2 | 0.1 | 0.2 | 0.1 | 0.1 | 364.7 | 364.2 | 376.2 | 370.5 |
| 119 | 0.3 | 0.2 | 0.2 | 0.1 | 0.1 | 0.1 | 340.9 | 348.9 | 332.6 | 336.7 |
| 120 | 0.3 | 0.3 | 0.1 | 0.1 | 0.1 | 0.1 | 367.3 | 361.9 | 305.5 | 394.8 |
| 121 | 0.4 | 0.1 | 0.1 | 0.1 | 0.1 | 0.2 | 361.4 | 370.1 | 350.6 | 363 |
| 122 | 0.4 | 0.1 | 0.1 | 0.1 | 0.2 | 0.1 | 363.4 | 364.4 | 315.7 | 356.9 |
| 123 | 0.4 | 0.1 | 0.1 | 0.2 | 0.1 | 0.1 | 363.8 | 357.7 | 333.2 | 361.7 |
| 124 | 0.4 | 0.1 | 0.2 | 0.1 | 0.1 | 0.1 | 347.5 | 366.2 | 318.1 | 334.5 |
| 125 | 0.4 | 0.2 | 0.1 | 0.1 | 0.1 | 0.1 | 347.7 | 374.8 | 323.4 | 377.5 |
| 126 | 0.5 | 0.1 | 0.1 | 0.1 | 0.1 | 0.1 | 297 | 348.4 | 363.9 | 364.6 |

Supplementary Fig. S10 Data-driven predictions of metal compositions from given spectral data using the S2C model for the Group-B derivative system.

Supplementary Fig. S11 Data-driven predictions of metal compositions from given spectral data using the S2C model for the Group-D derivative system.

Supplementary Fig. S12 (a) Predicted top 20 high-entropy catalysts of Group-B derivative system generated by the SpecGen model and experimentally measured overpotential at 10 mA/cm² by the AI-Chemist. (b) Kiviat diagram of metal compositions, (c) polarization curves at the sweep rate of 5 mV/s without iR correction and (d) Nyquist plots of EIS for the local best of the system and the optimal catalyst predicted by SpecGen model.

Supplementary Table S6. A summary of the predicted top 20 optimal catalyst formulations for Group-B derivative, as identified by SpecGen, which includes the predicted compositions of these catalysts and corresponding AI-chemist measured overpotentials at a current density of 10 mA/cm² (η10) during the OER process.

| Cat. No. | Synthetic formula |  |  |  |  |  | Potential@10 mA/cm2 (V vs. RHE) | η10 (mV) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Co | Ni | Cu | Mg | Cd | Zn |  |  |
| 1 | 0.31853 | 0.13637 | 0.23414 | 0.08654 | 0 | 0.22443 | 1.5534 | 323.403 |
| 2 | 0.19566 | 0.17702 | 0.27682 | 0.10659 | 0.08761 | 0.1563 | 1.58413 | 354.13 |
| 3 | 0.34336 | 0.02263 | 0.28275 | 0.2017 | 0 | 0.14956 | 1.55547 | 325.467 |
| 4 | 0.24069 | 0.14327 | 0.18361 | 0.06256 | 0.08629 | 0.28358 | 1.58286 | 352.857 |
| 5 | 0.34686 | 0.06884 | 0.25248 | 0.13058 | 0 | 0.20124 | 1.55757 | 327.568 |
| 6 | 0.16766 | 0.11558 | 0.31239 | 0.22501 | 0.00115 | 0.17821 | 1.59178 | 361.779 |
| 7 | 0.3134 | 0.05809 | 0.26159 | 0.10723 | 0 | 0.25969 | 1.55882 | 328.819 |
| 8 | 0.25903 | 0.15569 | 0.28736 | 0.09466 | 0 | 0.20325 | 1.58756 | 357.562 |
| 9 | 0.24225 | 0.12205 | 0.37393 | 0.07528 | 0 | 0.18649 | 1.55992 | 329.923 |
| 10 | 0.3824 | 0.06519 | 0.30496 | 0.02279 | 0 | 0.22467 | 1.57665 | 346.653 |
| 11 | 0.23018 | 0.00439 | 0.30433 | 0.29139 | 0 | 0.16971 | 1.58934 | 359.338 |
| 12 | 0.39876 | 0.06698 | 0.20386 | 0.14957 | 0 | 0.18082 | 1.55135 | 321.353 |
| 13 | 0.17999 | 0.16901 | 0.25265 | 0.19605 | 0.000824 | 0.20148 | 1.5798 | 349.796 |
| 14 | 0.25418 | 0.15088 | 0.08268 | 0.49582 | 0 | 0.01645 | 1.596 | 366 |
| 15 | 0.26931 | 0.09669 | 0.23217 | 0.24258 | 0 | 0.15925 | 1.57145 | 341.448 |
| 16 | 0.23779 | 0.08521 | 0.25308 | 0.23877 | 0 | 0.18515 | 1.58094 | 350.939 |
| 17 | 0.18372 | 0.08403 | 0.21865 | 0.16674 | 0.09029 | 0.25658 | 1.59054 | 360.542 |
| 18 | 0.13481 | 0.28281 | 0.25905 | 0.036 | 0.000793 | 0.28654 | 1.5498 | 319.796 |
| 19 | 0.21897 | 0.22238 | 0.29495 | 0.09841 | 0.04169 | 0.1236 | 1.55856 | 328.559 |
| 20 | 0.1483 | 0.19499 | 0.31552 | 0.22648 | 0.11406 | 0.000649 | 1.58272 | 352.724 |

Supplementary Fig. S13 (a) Predicted top 20 high-entropy catalysts of Group-D derivative system generated by the SpecGen model and experimentally measured overpotential at 10 mA/cm² by the AI-Chemist. (b) Kiviat diagram of metal compositions, (c) polarization curves at the sweep rate of 5 mV/s without iR correction and (d) Nyquist plots of EIS for the local best of the system and the optimal catalyst predicted by SpecGen model.

Supplementary Table S7. A summary of the predicted top 20 optimal catalyst formulations for Group-D derivative, as identified by SpecGen, which includes the predicted compositions of these catalysts and corresponding AI-chemist measured overpotentials at a current density of 10 mA/cm² (η10) during the OER process.

| Cat. No. | Synthetic formula |  |  |  |  |  | Potential@10 mA/cm2 (V vs. RHE) | η10 (mV) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Co | Ni | Cu | Mg | Mn | Zn |  |  |
| 1 | 0.22851 | 0.22312 | 0.24579 | 0.26436 | 0.02784 | 0.01038 | 1.55773 | 327.732 |
| 2 | 0.19137 | 0.15162 | 0.3001 | 0.26821 | 0.01532 | 0.07338 | 1.57082 | 340.823 |
| 3 | 0.25817 | 0.2431 | 0.37241 | 0 | 0.0584 | 0.06792 | 1.55286 | 322.863 |
| 4 | 0.21812 | 0.27459 | 0.2301 | 0 | 0.05966 | 0.21752 | 1.53889 | 308.894 |
| 5 | 0.25523 | 0.08799 | 0.39717 | 0.13798 | 0.05966 | 0.06198 | 1.54975 | 319.752 |
| 6 | 0.16713 | 0.20461 | 0.33679 | 0.27737 | 0 | 0.0141 | 1.60237 | 372.375 |
| 7 | 0.27173 | 0.12546 | 0.32491 | 0 | 0.10536 | 0.17253 | 1.55354 | 323.535 |
| 8 | 0.21047 | 0.25217 | 0.30548 | 0.1841 | 0.04639 | 0.00139 | 1.53026 | 293.286 |
| 9 | 0.12022 | 0.20813 | 0.45352 | 0.10762 | 0.05351 | 0.05701 | 1.57892 | 348.919 |
| 10 | 0.25647 | 0.10838 | 0.39921 | 0 | 0.12451 | 0.11142 | 1.54792 | 317.922 |
| 11 | 0.09606 | 0.27911 | 0.34103 | 0.03988 | 0.09416 | 0.14977 | 1.54983 | 319.828 |
| 12 | 0.23219 | 0.30044 | 0.39031 | 0 | 0.07707 | 0 | 1.536 | 306 |
| 13 | 0.21375 | 0.40214 | 0.18945 | 0 | 0.12066 | 0.074 | 1.54217 | 312.17 |
| 14 | 0.17848 | 0.43882 | 0 | 0.32605 | 0.05665 | 0 | 1.58832 | 358.323 |
| 15 | 0.11758 | 0.25045 | 0.20364 | 0.23831 | 0.06175 | 0.12828 | 1.57123 | 341.23 |
| 16 | 0.34381 | 0.29948 | 0.26418 | 0 | 0.08195 | 0.01058 | 1.52329 | 300.256 |
| 17 | 0.22022 | 0.11379 | 0.33617 | 0.25386 | 0.03198 | 0.043984 | 1.56719 | 337.19 |
| 18 | 0.17706 | 0.33236 | 0.27067 | 0.21296 | 0.00695 | 0 | 1.55457 | 324.569 |
| 19 | 0.20231 | 0.25635 | 0.32147 | 0.14314 | 0.04214 | 0.0346 | 1.54452 | 314.519 |
| 20 | 0.05732 | 0.33297 | 0.17257 | 0.16448 | 0.04473 | 0.22792 | 1.56392 | 333.92 |

Supplementary Fig. S14 Data-driven predictions of metal compositions from given spectral data using the S2C model for the Group-A derivative system.

Supplementary Fig. S15 Data-driven predictions of metal compositions from given spectral data using the S2C model for the Group-C derivative system.

Supplementary Fig. S16 (a) Predicted top 20 high-entropy catalysts of Group-A derivative system generated by the SpecGen model and experimentally measured overpotential at 10 mA/cm² by the AI-Chemist. (b) Kiviat diagram of metal compositions, (c) polarization curves at the sweep rate of 5 mV/s without iR correction and (d) Nyquist plots of EIS for the local best of the system and the optimal catalyst predicted by SpecGen model.

Supplementary Table S8. A summary of the predicted top 20 optimal catalyst formulations for Group-A derivative, as identified by SpecGen, which includes the predicted compositions of these catalysts and corresponding AI-chemist measured overpotentials at a current density of 10 mA/cm² (η10) during the OER process.

| Cat. No. | Synthetic formula |  |  |  |  |  | Potential@10 mA/cm2 (V vs. RHE) | η10 (mV) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Co | Ni | Cu | Mg | Cd | Zn |  |  |
| 1 | 0.26527 | 0.05092 | 0.20751 | 0.1842 | 0.16 | 0.1321 | 1.57666 | 346.66 |
| 2 | 0.15855 | 0.04296 | 0.28715 | 0.1252 | 0.31778 | 0.06836 | 1.60065 | 370.65 |
| 3 | 0.26976 | 0 | 0.29166 | 0.18558 | 0 | 0.25299 | 1.55811 | 328.11 |
| 4 | 0.24908 | 0.05508 | 0.11297 | 0.11317 | 0.33816 | 0.13154 | 1.60368 | 373.68 |
| 5 | 0.25005 | 0.03126 | 0.24754 | 0.19992 | 0.14619 | 0.12503 | 1.58614 | 356.14 |
| 6 | 0.18168 | 0.04204 | 0.33908 | 0.19908 | 0.17601 | 0.06212 | 1.59794 | 367.94 |
| 7 | 0.36219 | 0 | 0.16895 | 0.21795 | 0.06581 | 0.1851 | 1.61059 | 380.59 |
| 8 | 0.24959 | 0.06872 | 0.23981 | 0.17935 | 0.1246 | 0.13793 | 1.6088 | 378.8 |
| 9 | 0.19527 | 0.11016 | 0.46072 | 0.20669 | 0.02716 | 0 | 1.57081 | 340.81 |
| 10 | 0.39412 | 0 | 0.26977 | 0.19253 | 0 | 0.14358 | 1.59945 | 369.45 |
| 11 | 0.26446 | 0 | 0.31125 | 0.27956 | 0 | 0.14473 | 1.57777 | 347.77 |
| 12 | 0.38879 | 0 | 0.10478 | 0.17506 | 0 | 0.33137 | 1.6076 | 377.6 |
| 13 | 0.08513 | 0 | 0.2439 | 0.26475 | 0.16069 | 0.24552 | 1.65564 | 425.64 |
| 14 | 0.44782 | 0.13323 | 0 | 0.32153 | 0 | 0.09741 | 1.59566 | 365.66 |
| 15 | 0.22732 | 0 | 0.38792 | 0.24058 | 0 | 0.14419 | 1.59327 | 363.27 |
| 16 | 0.1694 | 0 | 0.27595 | 0.25146 | 0.19293 | 0.11025 | 1.59186 | 361.86 |
| 17 | 0.18077 | 0.06527 | 0.23095 | 0.15415 | 0.25283 | 0.11603 | 1.60524 | 375.24 |
| 18 | 0.17982 | 0.0541 | 0.30672 | 0.1466 | 0.19866 | 0.11409 | 1.58268 | 352.68 |
| 19 | 0.3179 | 0.04503 | 0.26993 | 0.17403 | 0.10342 | 0.08968 | 1.59012 | 360.12 |
| 20 | 0.14048 | 0 | 0.33382 | 0.20579 | 0.27943 | 0.04048 | 1.61552 | 385.52 |

Supplementary Fig. S17 (a) Predicted top 20 high-entropy catalysts of Group-C derivative system generated by the SpecGen model and experimentally measured overpotential at 10 mA/cm² by the AI-Chemist. (b) Kiviat diagram of metal compositions, (c) polarization curves at the sweep rate of 5 mV/s without iR correction and (d) Nyquist plots of EIS for the local best of the system and the optimal catalyst predicted by SpecGen model.

Supplementary Table S9. A summary of the predicted top 20 optimal catalyst formulations for Group-C derivative, as identified by SpecGen descriptors, which includes the predicted compositions of these catalysts and corresponding AI-chemist measured overpotentials at a current density of 10 mA/cm² (η10) during the OER process.

| Cat. No. | Synthetic formula |  |  |  |  |  | Potential@10 mA/cm2 (V vs. RHE) | η10 (mV) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Co | Ni | Cu | Fe | Cd | Zn |  |  |
| 1 | 0.31973 | 0.13471 | 0.12242 | 0.16727 | 0.12684 | 0.12904 | 1.51354 | 283.538 |
| 2 | 0.25284 | 0.14851 | 0.14978 | 0.1421 | 0.14299 | 0.16379 | 1.52377 | 293.771 |
| 3 | 0.27331 | 0.20254 | 0.1421 | 0.165 | 0.14839 | 0.06866 | 1.52346 | 293.457 |
| 4 | 0.26675 | 0.07492 | 0.11279 | 0.19147 | 0.1052 | 0.24887 | 1.53613 | 306.128 |
| 5 | 0.30259 | 0.15315 | 0.16008 | 0.13833 | 0.08814 | 0.15771 | 1.52369 | 293.688 |
| 6 | 0.22757 | 0.17552 | 0.19744 | 0.11635 | 0.14405 | 0.13907 | 1.52816 | 298.162 |
| 7 | 0.29572 | 0.12797 | 0.17078 | 0.14523 | 0.05386 | 0.20644 | 1.52295 | 292.948 |
| 8 | 0.25506 | 0.15931 | 0.16834 | 0.14223 | 0.11955 | 0.15552 | 1.52294 | 292.937 |
| 9 | 0.30436 | 0.10776 | 0.22576 | 0.12254 | 0.07635 | 0.16323 | 1.53113 | 301.126 |
| 10 | 0.43034 | 0.09884 | 0.17493 | 0.20642 | 0.05663 | 0.03284 | 1.5224 | 292.398 |
| 11 | 0.26377 | 0.11802 | 0.15234 | 0.18627 | 0.14305 | 0.13655 | 1.53212 | 302.122 |
| 12 | 0.39677 | 0.1277 | 0.10998 | 0.18801 | 0.09569 | 0.08185 | 1.51681 | 286.807 |
| 13 | 0.22326 | 0.241 | 0.10241 | 0.13519 | 0.1927 | 0.10543 | 1.54933 | 319.326 |
| 14 | 0.54876 | 0.14346 | 0.01014 | 0.06442 | 0.23322 | 0 | 1.57619 | 346.189 |
| 15 | 0.24045 | 0.194 | 0.14546 | 0.16478 | 0.1736 | 0.08171 | 1.53871 | 308.708 |
| 16 | 0.18572 | 0.21024 | 0.13349 | 0.11262 | 0.16959 | 0.18833 | 1.55354 | 323.536 |
| 17 | 0.25195 | 0.20117 | 0.1461 | 0.1529 | 0.11894 | 0.12894 | 1.53376 | 303.762 |
| 18 | 0.28018 | 0.12303 | 0.18259 | 0.16466 | 0.18487 | 0.06466 | 1.53725 | 307.248 |
| 19 | 0.25448 | 0.13013 | 0.20242 | 0.11535 | 0.10872 | 0.1889 | 1.53511 | 305.106 |
| 20 | 0.23969 | 0.22543 | 0.16354 | 0.13419 | 0.14848 | 0.08867 | 1.54401 | 314.006 |

References

1.	Kingma, D. P. Auto-encoding variational bayes. arXiv Prepr. arXiv1312.6114 (2013).