Electronic Supplementary material

Performance evaluation of novel M25 green concrete with GGBS, DRS and RCA material– A study employing response surface methodology

by

Prakash Chinnaiyan1*, Ananthkumar1 ,Bharath Krishnaa Anuradha Chandrasekar1, Malavika Sasi1 , Tejashwi Landu 1

Table S1: Regression Run Order

| Run order | GGBS % | DRS % | RCA % |
| --- | --- | --- | --- |
| 1 | 0 | 0 | 0 |
| 2 | 25 | 15 | 15 |
| 3 | 0 | 0 | 30 |
| 4 | 0 | 15 | 15 |
| 5 | 25 | 15 | 15 |
| 6 | 50 | 0 | 30 |
| 7 | 0 | 30 | 0 |
| 8 | 25 | 0 | 15 |
| 9 | 25 | 15 | 15 |
| 10 | 50 | 30 | 30 |
| 11 | 50 | 15 | 15 |
| 12 | 25 | 15 | 15 |
| 13 | 50 | 0 | 0 |
| 14 | 50 | 30 | 0 |
| 15 | 25 | 15 | 15 |
| 16 | 0 | 30 | 30 |
| 17 | 25 | 30 | 15 |
| 18 | 25 | 15 | 0 |
| 19 | 25 | 15 | 15 |
| 20 | 25 | 15 | 30 |

Table S2: Response Surface Regression: Slump (mm) versus GGBS, DRS, RCA

a. Coded Coefficients

| Term | Coef | SE Coef | T-Value | P-Value | VIF |
| --- | --- | --- | --- | --- | --- |
| Constant | 92.10 | 1.39 | 66.29 | 0.000 |  |
| GGBS | 3.70 | 1.39 | 2.66 | 0.019 | 1.00 |
| DRS | 12.60 | 1.39 | 9.07 | 0.000 | 1.00 |
| RCA | -16.40 | 1.39 | -11.80 | 0.000 | 1.00 |
| DRS*DRS | 2.70 | 1.96 | 1.37 | 0.191 | 1.00 |
| DRS*RCA | -9.88 | 1.55 | -6.36 | 0.000 | 1.00 |

b. Model Summary

| S | R-sq | R-sq(adj) | R-sq(pred) |
| --- | --- | --- | --- |
| 4.39379 | 95.09% | 93.33% | 89.56% |

c. Analysis of Variance

| Source | DF | Adj SS | Adj MS | F-Value | P-Value |
| --- | --- | --- | --- | --- | --- |
| Model | 5 | 5230.67 | 1046.13 | 54.19 | 0.000 |
| Linear | 3 | 4414.10 | 1471.37 | 76.22 | 0.000 |
| GGBS | 1 | 136.90 | 136.90 | 7.09 | 0.019 |
| DRS | 1 | 1587.60 | 1587.60 | 82.24 | 0.000 |
| RCA | 1 | 2689.60 | 2689.60 | 139.32 | 0.000 |
| Square | 1 | 36.45 | 36.45 | 1.89 | 0.191 |
| DRS*DRS | 1 | 36.45 | 36.45 | 1.89 | 0.191 |
| 2-Way Interaction | 1 | 780.13 | 780.13 | 40.41 | 0.000 |
| DRS*RCA | 1 | 780.13 | 780.13 | 40.41 | 0.000 |
| Error | 14 | 270.27 | 19.31 |  |  |
| Lack-of-Fit | 9 | 262.94 | 29.22 | 19.92 | 0.002 |
| Pure Error | 5 | 7.33 | 1.47 |  |  |
| Total | 19 | 5500.95 |  |  |  |

Table S3: Response Surface Regression: Compressive strength (N/mm^2) versus GGBS, DRS, RCA

a. Coded Coefficients

| Term | Coef | SE Coef | T-Value | P-Value | VIF |
| --- | --- | --- | --- | --- | --- |
| Constant | 29.237 | 0.592 | 49.35 | 0.000 |  |
| GGBS | 2.118 | 0.559 | 3.79 | 0.002 | 1.00 |
| DRS | 2.051 | 0.559 | 3.67 | 0.003 | 1.00 |
| RCA | -7.132 | 0.559 | -12.77 | 0.000 | 1.00 |
| GGBS*GGBS | 2.176 | 0.987 | 2.20 | 0.046 | 1.56 |
| RCA*RCA | -4.474 | 0.987 | -4.53 | 0.001 | 1.56 |
| GGBS*RCA | -1.500 | 0.625 | -2.40 | 0.032 | 1.00 |

b. Model Summary

| S | R-sq | R-sq(adj) | R-sq(pred) |
| --- | --- | --- | --- |
| 1.76637 | 94.36% | 91.76% | 80.41% |

c. Analysis of Variance

| Source | DF | Adj SS | Adj MS | F-Value | P-Value |
| --- | --- | --- | --- | --- | --- |
| Model | 6 | 678.930 | 113.155 | 36.27 | 0.000 |
| Linear | 3 | 595.579 | 198.526 | 63.63 | 0.000 |
| GGBS | 1 | 44.859 | 44.859 | 14.38 | 0.002 |
| DRS | 1 | 42.066 | 42.066 | 13.48 | 0.003 |
| RCA | 1 | 508.654 | 508.654 | 163.03 | 0.000 |
| Square | 2 | 65.350 | 32.675 | 10.47 | 0.002 |
| GGBS*GGBS | 1 | 15.150 | 15.150 | 4.86 | 0.046 |
| RCA*RCA | 1 | 64.057 | 64.057 | 20.53 | 0.001 |
| 2-Way Interaction | 1 | 18.000 | 18.000 | 5.77 | 0.032 |
| GGBS*RCA | 1 | 18.000 | 18.000 | 5.77 | 0.032 |
| Error | 13 | 40.561 | 3.120 |  |  |
| Lack-of-Fit | 8 | 39.876 | 4.985 | 36.41 | 0.001 |
| Pure Error | 5 | 0.685 | 0.137 |  |  |
| Total | 19 | 719.491 |  |  |  |

# Table S4 Response Surface Regression: Split Tensile Strength(N/mm^2) versus GGBS, DRS, RCA

a. Coded Coefficients

| Term | Coef | SE Coef | T-Value | P-Value | VIF |
| --- | --- | --- | --- | --- | --- |
| Constant | 3.6525 | 0.0241 | 151.83 | 0.000 |  |
| GGBS | 0.1730 | 0.0340 | 5.08 | 0.000 | 1.00 |
| DRS | 0.2050 | 0.0340 | 6.03 | 0.000 | 1.00 |
| RCA | -0.4100 | 0.0340 | -12.05 | 0.000 | 1.00 |
| GGBS*DRS | -0.1587 | 0.0380 | -4.17 | 0.001 | 1.00 |

b. Model Summary

| S | R-sq | R-sq(adj) | R-sq(pred) |
| --- | --- | --- | --- |
| 0.107586 | 93.75% | 92.08% | 89.74% |

c. Analysis of Variance

| Source | DF | Adj SS | Adj MS | F-Value | P-Value |
| --- | --- | --- | --- | --- | --- |
| Model | 4 | 2.60215 | 0.65054 | 56.20 | 0.000 |
| Linear | 3 | 2.40054 | 0.80018 | 69.13 | 0.000 |
| GGBS | 1 | 0.29929 | 0.29929 | 25.86 | 0.000 |
| DRS | 1 | 0.42025 | 0.42025 | 36.31 | 0.000 |
| RCA | 1 | 1.68100 | 1.68100 | 145.23 | 0.000 |
| 2-Way Interaction | 1 | 0.20161 | 0.20161 | 17.42 | 0.001 |
| GGBS*DRS | 1 | 0.20161 | 0.20161 | 17.42 | 0.001 |
| Error | 15 | 0.17362 | 0.01157 |  |  |
| Lack-of-Fit | 10 | 0.12007 | 0.01201 | 1.12 | 0.478 |
| Pure Error | 5 | 0.05355 | 0.01071 |  |  |
| Total | 19 | 2.77577 |  |  |  |

# Table S5: Response Surface Regression: Flexural strength(N/mm^2) versus GGBS, DRS, RCA

a. Coded Coefficients

| Term | Coef | SE Coef | T-Value | P-Value | VIF |
| --- | --- | --- | --- | --- | --- |
| Constant | 3.6209 | 0.0185 | 195.50 | 0.000 |  |
| GGBS | 0.1590 | 0.0175 | 9.11 | 0.000 | 1.00 |
| DRS | 0.1640 | 0.0175 | 9.39 | 0.000 | 1.00 |
| RCA | -0.2570 | 0.0175 | -14.72 | 0.000 | 1.00 |
| DRS*DRS | 0.0806 | 0.0309 | 2.61 | 0.022 | 1.56 |
| RCA*RCA | -0.0944 | 0.0309 | -3.06 | 0.009 | 1.56 |
| GGBS*RCA | 0.0350 | 0.0195 | 1.79 | 0.096 | 1.00 |

b. Model Summary

| S | R-sq | R-sq(adj) | R-sq(pred) |
| --- | --- | --- | --- |
| 0.0552190 | 96.86% | 95.41% | 91.22% |

c. Analysis of Variance

| Source | DF | Adj SS | Adj MS | F-Value | P-Value |
| --- | --- | --- | --- | --- | --- |
| Model | 6 | 1.22344 | 0.203907 | 66.87 | 0.000 |
| Linear | 3 | 1.18226 | 0.394087 | 129.25 | 0.000 |
| GGBS | 1 | 0.25281 | 0.252810 | 82.91 | 0.000 |
| DRS | 1 | 0.26896 | 0.268960 | 88.21 | 0.000 |
| RCA | 1 | 0.66049 | 0.660490 | 216.62 | 0.000 |
| Square | 2 | 0.03138 | 0.015691 | 5.15 | 0.023 |
| DRS*DRS | 1 | 0.02080 | 0.020801 | 6.82 | 0.022 |
| RCA*RCA | 1 | 0.02850 | 0.028501 | 9.35 | 0.009 |
| 2-Way Interaction | 1 | 0.00980 | 0.009800 | 3.21 | 0.096 |
| GGBS*RCA | 1 | 0.00980 | 0.009800 | 3.21 | 0.096 |
| Error | 13 | 0.03964 | 0.003049 |  |  |
| Lack-of-Fit | 8 | 0.03651 | 0.004563 | 7.28 | 0.021 |
| Pure Error | 5 | 0.00313 | 0.000627 |  |  |
| Total | 19 | 1.26308 |  |  |  |

Fig S1 Pareto chart of the standard effects (Compressive strength).

# Fig S2(a)  						  Fig S2(b)

# Fig S2(c)

# Fig S2 Contour plot of Compressive strength vs a) RCA, GGBS b) DRS, GGBS c) RCA,  DRS

Fig S3. Pareto chart of the standardized effects (Split Tensile strength).

# Fig S4 (a)       						Fig S4 (b)

# Fig S4 (c)

# Fig S4 Contour plot of Split tensile strength vs (a) DRS, GGBS, (b) RCA, GGBS, (c) RCA, DRS.

Fig S5 Pareto chart of the standard effects (Flexural strength).

# Fig S6 (a) 					                     Fig S6 (b)

# Fig S6 (c)

# Fig S6 Contour plot of Flexural strength vs (a)DRS, GGBS, (b)RCA, GGBS, (c)RCA, DRS