Tab. 1. BET characteristics of N-RSB before and after the reaction

|  | Specific surface area (m²·g-1 ) | Pore volume (m3·g-1) | Pore size (nm) |
| --- | --- | --- | --- |
| Before the reaction | 0.6906 | 0.002259 | 137.155 |
| After the reaction | 1.1595 | 0.006254 | 312.762 |