Table 1 Optimization of iron-catalyzed transfer hydrogenation of methyl benzoate.a

a Reaction conditions: methyl benzoate (1.0 mmol), H3N·BH3 (1.0 mmol), Fe1 (0.02 mmol), base (0.05 mmol), solvent (2 mL), and 6 h. b Conversions and Yields were determined via 1H NMR spectroscopy with an internal standard (xylene). c without Fe1.

Table 2 Catalytic transfer hydrogenation of esters using iron precatalyst 1.a

a Reaction conditions: substrate (1.0 mmol), H3N·BH3 (1.0 mmol), Fe1 (0.02 mmol), KOtBu (0.05 mmol), THF (2 mL), 60°C, and 12 h. b Isolated yields are given.

Table 3 Optimization of iron-catalyzed methanolysis of PET.a

a Reaction conditions: PET (1.0 mmol), H3N·BH3 (0.02 mmol), Fe1 (0.02 mmol), solvent (2 mL), (RT~80°C), and 12 h. b Isolated yields of DMT are given. c Without Fe1 and H3N·BH3.

Table 4. Hydrogenolysis of consumer polymer products using [Fe(NNHN)Cl2] and KOtBu.a

a Reaction conditions: The reactions were performed in a 250-mL steel autoclave within a 24 h reaction time at 120°C using x mol % Fe1 and y mol % KOtBu, 100 mL of THF, and a 20-bar constant hydrogen pressure.