Competing Orbital Magnetism and Superconductivity in electrostatically defined Josephson Junctions of Alternating Twisted Trilayer Graphene

Vishal Bhardwaj1, Lekshmi Rajagopal1, Lorenzo Arici1, Matan Bocarsly1, Alexey Ilin1, Gal Shavit5, Kenji Watanabe3, Takashi Taniguchi4, Yuval Oreg1, Tobias Holder6, Yuval Ronen1*

1Department of Condensed Matter Physics, Weizmann Institute of Science, Rehovot 7610001, Israel

3Research Center for Functional Materials, National Institute for Materials Science, Tsukuba 305-0044, Japan

4International Center for Materials Nanoarchitectonics, National Institute for Materials Science, Tsukuba 305-0044, Japan

5Department of Physics and Institute for Quantum Information and Matter, California Institute of Technology, Pasadena, California 91125, USA

6School of Physics and Astronomy, Tel Aviv University, Tel Aviv 69978, Israel

*yuval.ronen@weizmann.ac.il

- Stacking and fabrication of device

The stacks are prepared using flakes exfoliated on Si/SiO2 substrates. The dome shaped stamps are prepared using   polydimethylsiloxane (PDMS) and 6% (by weight) polycarbonate (PC) solution dissolved in chloroform. A big monolayer of graphene around 100×30um is identified using optical microscope and further confirm by analyzing 2D peak of Raman spectra (532nm laser of Witec Raman system). Raman 1064nm laser is used to cut the monolayer into 3 pieces of ~30um length. The hBNs are also exfoliated on Si/SiO2 and clean areas are identified using optical microscope. The stack is prepared using commercial transfer stage. The top hBN of thickness ~ 25nm is picked at 100° C by Z movement of the stamps. The first graphene layer is picked at 40° C also using Z movement of the stamp. The stage is rotated to around +1.45° and second layer is also picked at same parameters. Subsequently the stage is rotated to -1.45° and third layer is picked. The bottom hBN (~30nm) is picked at 50° C using Z movement of stamps, the stamp wavefront is moved away from stack area and the stage temperature is raised to 180° C to melt the PC with stack on chip. The stack is cleaned using chloroform to remove PC residues. The stack is annealed at 350° C for 2hr in vacuum furnace with base pressure of 5×10-8 Torr to release strain and remove any residues on top of stack. The flake thickness is measured, and the topography of stack is cleaned using Bruker AFM. See fig. S1 (a) for a 100X resolution picture of the stack before nanofabrication. The Jeol JBX 9300FS e-beam lithography is used to prepare Hall bar geometry. Double layer PMMA is used in every step of nano fabrication. In the first step, metal top gate is deposited with Cr (5nm) Au (20nm) using e-gun evaporator. In the second step, stack etching is performed using CHF3/O2 gas mixture in reactive ion etching machine. Metal bridges (Ti (25nm)/Au (250nm)) are prepared to avoid shorting of top gate leads to the graphene at the edges of stack. The edge contacts to the graphene are made by first etching stack using CHF3/O2 gas and subsequently depositing Cr (2nm)/ Au (65nm) metals on 15° angle using e-gun evaporator while rotating the sample holder. The final device consists of three Hall bar devices A, B and C. There are two Josephson junctions, first between device A and B of width ~200nm (JJ1) and second between device B and C of width ~100nm (JJ2).  See fig. S2 (b) for the image of the final device, after fabrication process.

The transport properties are measured in LD400 Bluefors dilution refrigerator. The fridge has thermo-coax lines and low pass RC and RF filters. It has 9-1-1 magnet with base temperature of 7mK. Standard 830SRS and 865SRS lock in amplifiers are used to measure transport properties. Femto DLPVA-101-F-D room temperature voltage amplifiers (1TΩ input impedance) are used before feeding signal to lock in amplifiers. Keithley 2400 voltage source meters are used for controlling voltages of gates.  For dV/dI characteristics, Yokogawa is used as dc source meter and lock in as AC source. The carrier density (n) and displacement field (D) are calculated using electrostatics equations n=εbε0Vbgedb + εtε0Vtgedt  and D=εbε0Vbgdb - εtε0Vtgdt  respectively. Here, ε0 is the dielectric constant of vacuum and is equal to  8.854×10-12 CV-1m-1, εtεb are the relative dielectric constant of the top (bottom) hBN ~ 3.9, dtdb are thickness of the top hBN (Si/SiO2 +bottom hBN) which we estimated to be 25 nm (285nm +30 nm), Vtg(Vbg) are the voltages of top (bottom) gates. The moiré super lattice carrier density (ns) for device A, B and C are 4.4×1012, 4.65×1012and  4.8×1012cm-2 respectively. The twist angles are estimated using equation ns=8θ2 /3 a2 (a=0.234nm) and are found to be 1.38°,1.41°, and 1.44° for A, B and C device, respectively.

Figure S1: (a) 100X zoomed optical image of the stack before nanofabrication. Color scale is 10um. (b) Optical image of the final devices after nanofabrication. The Josephson junctions, JJ1 and JJ2 have weak link of ~200nm and 100nm respectively. The width of the Hall bar is ~2mm, see the scale ~1mm.

- Transport characterization of hall bar devices:

When we dope, the electrons (holes) to the conduction (valence) bands of the TTG are distributed between the flat bands and ML Dirac cone. Most of the charge carriers are filled in the flat bands due to high density of state (DOS) and the rest goes to ML Dirac cone1,2.  The mini-Brillouin zone of TTG has four-fold degenerate bands with flavors K,K',↑, ↓. When we start doping electrons(holes) from v=0, all four flavors start filling the conduction (valence) bands equally, and hence a linear (unity) slope between Hall carrier density (nH) and v is expected in the vicinity of CNP3. At v=±1 (±3), the symmetry of four-fold degenerate bands breaks and out of four anyone (three) flavor is filled completely which result in resets towards zero. Similarly at v=±2, due to symmetry breaking of spin and valley isospin degenerate bands, two flavors of either spin or valley isospin are filled completely, and a reset is observed. At v=±4 all four flavors are filled and Fermi energy (EF) exits the flat bands and we observe reset toward zero again. This symmetry breaking of degenerate bands results in Chern insulator states at integer v, as seen in Landau fan diagrams of Rxx and Rxy at D=0V/nm (see extended Fig1).

We calculated the normalized Hall carrier density using equation vH =1(e*dRxydBz*ns)  ; (here, e is elementary charge, ns moiré superlattice density), the dRxydBz is calculated at low Bz range (-0.1T ≤Bz ≤0.1T) and high Bz range (-0.5T ≤Bz ≤0.5T) around Bz= 0T. The variation of quantity (vH-v) with v  shed light on the evolution of TTG DOS with varying EF4,5. Fig. S2 (a) and (b) shows the  (vH-v) vs v  plot for high B (red) and low B (blue) ranges at D=0V/nm and 0.6V/nm, respectively. The integer values of (vH-v) are expected at integer v corresponding to symmetry breaking and we observe this condition at v=+1, ±2, +3 and ±4, see red curve in fig. S2 (a). However, in addition to that a pronounced kink is observed in the vicinity of CNP towards hole doping and two small kinks are observed just before v=+2 and -2 as shown by black arrows in fig. S2 (a). These kinks are also associated with the symmetry breaking of flavors and presence of isospin ferromagnetic state5,6. The behavior of sample at high displacement field looks completely different, as seen in fig. S2 (b). The kinks near the CNP vanishes and strong van hove singularities are observed at v=±2 and v=±3, i.e. on the boundary of superconductivity region. This signifies the strengthening of superconductivity at high displacement field in 2≤ |v| ≤34. The Landau fan diagrams of  dRxydBz at high displacement fields (0.6V/nm) is shown in fig. S2(c)-(d) for devices A and C respectively. The jumps in Rxy around Bz=0 in both devices has vanished. An interesting note is that in Device C (θ=1.44°), v=3 becomes visible which is absent in device A (θ=1.38°).

Figure S2: The moiré filing factor (v) subtracted from renormalize Hall density vH=Bz /eρxyns vs v plots at low Bz (-0.1T ≤Bz ≤0.1T) and high Bz (-0.5T ≤Bz ≤0.5T) shown by blue and red colors, respectively at (a) D=0V/nm and (b) D=0.6V/nm. Landau level fan diagram of dRxydBz at D=0.6V/nm for device (c) A and (d) C.

Figure S3: The 2D plots of dRxydBz  for Bz vs D at fixed (a) v =-0.1 (device A), (b) v =0.5 (device A) (c) v=0.7 (device B) and (d) v=0.7 (device C).

The TTG band structure consist of flat bands of TBG at 2 times the twist angle and a bystander monolayer Dirac cone. The mirror symmetric configuration of TTG means the localization of wavefunction on top/bottom layers can be tuned by the application of displacement field. At D=0V/nm, flat bands and Dirac cone are decoupled, however with application of D the flat bands and Dirac cone start hybridizing. This hybridization can result in rich physics. Here we are utilizing the ML Dirac cone Landau levels and their hybridization as a probe to estimate the EF of flat bands1,2. We observe large value of dRxydBz near by Bz=0T due to orbital magnetism (OM) which disappear with the increase in hybridization (D).  The parabolic shaped curves in the figures represent the Landau levels (LLs) of monolayer graphene at constant Fermi energy (EF) defined by v. The most prominent feature is the upward curvature of these curves with increasing D, which results from the hybridization between the MLG Dirac cone and the flat bands1. As D, and therefore hybridization increases, the slope of the MLG Dirac cone, i.e. Fermi velocity, vF=dEdk decreases. Since  EF is fixed, the LLs appear at higher B. To quantify the change in the vF, we estimate Fermi energy EF by employing a single-particle equation for the MLG LLs spectrum, EF=sgn(Ln)vF√(2eħ |Ln |×B); where Ln is Landau level index, vF is Fermi velocity of the monolayer Dirac cone, e is the elementary charge, and ħ is reduced Planck’s constant.  We estimated EF~-8meV for LL1 and ~-9meV for LL2 at v ~-0.45 (see Fig 2 (a) main file) and EF~-4meV at v ~-0.10 we, see fig. S3(a). As we tune EF to electron doped v~0.70 we estimated EF~11meV for LL1 and EF~13meV for LL2, see Fig 2 (b) main file.  These values of EF at corresponding v matches exactly with the estimation made using squid on tip scanning experiments1. The upward curvature of LLs lines with D indicate the hybridization of monolayer Dirac cone with flat bands, with the increase in D the slope of dEdk decreases and hence vF decreases, since the EF is fixed the LLs are observed at higher Bz in higher D.  The estimated vF change at v=-0.10 and -0.45 is ~67% and 45% for D change from 0 to 0.5V/nm. At v=0.70 vF change by ~15% for D change from 0 to 0.25V/nm.

Fig. S4 (a) and (c) shows the Rxy jumps in forward and backward sweeping of magnetic field at v=-0.45 and v=0.7 respectively at D=0 V/nm. We note the absence of hysteresis in these plots, despite the presence of a clear jump. The corresponding Rxy-Bz sweeps at higher displacement, D=0.6 V/nm shows that these jumps have vanished, see fig. S4 (b) and (d). We explicitly show the dependence of Rxy jumps in 0o to 90o direction of the applied magnetic field (Bx2+Bz2) 1/2 for device B and C respectively in fig. S5 (a) and (b). The Rxy jumps are present in all devices but are most prominent in device A (main fig. 3 and extended fig. 2) and decreases as we move to twist angles closer to the magic angle. We characterize the SC in our near magic angle device, Device C. From Rxx-T plot of Device C, TC ~ 1.3 K estimated corresponding to the 90% drop in resistance, see fig. S6 (a). We show the linecuts of dV/dI characteristics of the JJ2 taken at BZ=0G, with configuration S|X|S, where S corresponds to v~2.7 and X corresponds to vj, which is varied from ~-3 to 2.5. We see asymmetricity in the dV/dI w.r.t Idc in vj close to the CNP, but this dies off at higher vj. See fig. S6(b).  Figure S6 (c) shows the temperature dependence of dV/dI characteristics across the JJ2 at vj=-0.45. The curve becomes approximately symmetric at 650mK.

Figure S4:  Line cuts of Rxy for Bz sweep directions -0.5T to 0.5T (black) and 0.5T to -0.5T (red) at (a) v = -0.45, D=0V/nm, (b) v = -0.45 and D=0.6V/nm; (c) v =0.70, D=0V/nm and  (b) v = 0.70and D=0.6V/nm for device A.

Figure S5: The Rxy  vs B=(Bx2+Bz2) 1/2 at varying θ between sample and B from 90o (blue) to 0o(red) in steps of 15o measured at 15mk for (a) device A and (b) device B.

Figure S6: (a) The Rxx-T plot of device C measured at Bz=0T, v=2.35 and D=0.42V/nm. (b) The dV/dI vs Idc characteristics for SC state tuned to v~2.7 across JJ2 and weak link tuned to different vj shown in figure legends. (c) Temperature dependence of dV/dI vs Idc characteristics vj ~-0.45 across JJ2.

We can switch between superconducting (SC) and non-SC states by alternating Idc between ±Ic- on the asymmetric curve of dV/dI at Bz=0 G. Fig. S7a shows the dVdI (Ω) characteristics measured by alternating between Ic- (dVdI=0 Ω) and -Ic-  every 20 seconds and plotted over time in the temperature range 20mK to 650mK. The resistance R in the non-SC state decreases with increasing temperature. We fitted the temperature dependence of R to a Curie Bloch law, viz. R=m(1-TTOM3)γ, and estimated m= 30.05±1.5Ω, γ ~0.24±0.05 and TOM3~650mK as seen in Fig. S7b. The exponent of Curie Bloch law is expected to contain information about the magnetic moments, for example for a magnetic state of 2D Ising nature a critical exponent of 0.125 is expected7,8 . However, in our case we measure the exponent 0.24±0.05 from resistance of the diode-like effect, 0.45±0.05 from the Rxy data and 0.6±0.2 from the asymmetry in critical currents. The scaling behaviors are consistent provided the resistance of diode effect is coupled to ~M2, Rxy to ~M3 and η to ~M4 9,10. However, we believe a microscopic picture is needed to clarify this point.

We show the Fraunhofer patterns in two e-h Josephson junction configurations, Fig. S7 (a) S`|OM|S`` and (b) S`|N|S`` in JJ2, here S` and S`` correspond to h and e side SC, respectively. We see that while S`|N|S`` (vL=-2.5, vj=1.8, vR~2.7 ) shows a clear Fraunhofer pattern with clear dips in interference, we do not see a clear pattern in S`|OM|S`` (vL=-2.4,  vj=0.5,  vR~2.7) . Moreover, the weak Fraunhofer is also slightly asymmetric about Idc=0, owing to the OM.

Figure S7: (a) ) The dVdI (Ω) characteristics of S|OM|S JJ measured at Bz=0 G while alternating Idc  between Ic- (dVdI=0 Ω, SC state) and  -Ic- (non-SC) after every 20 seconds in a temperature range of 20mK to 650mK. (b) Resistance of the non-SC state (R) calculated from Fig 4e and plotted as a function of temperature (black data points). The red line corresponds to fits of the Curie Bloch equation ΔR=m(1-TTOM3)γ. The error bars depict the standard deviations in R.

Figure S8: The Fraunhofer pattern measurements at (a) The S`|OM|S`` JJ configuration (BG=3.8V, TgL=-4.4, TgR=2.8)   the left side of JJ SC state tuned to vL~-2.5, right side SC vR~2.7 and weak link tuned vj~0.5. (b) The S`|N|S`` JJ configuration (BG=27.6V, TgL=-6.2, TgR=0.7) corresponding to hole side SC on left side (S`) vL~-2.4 and electron side SC on right side (S``) vR~2.7   of  the JJ with weak link tuned to vj~1.8.

- Transport characteristics of devices with 1.3o and 1.5o twist angles

Figure S9: The additional TTG devices with twist angles (a) 1.30 and (b) 1.50.

We stacked two other samples with twist angle 1.30o and 1.50o to explore OM in region above and below 1.40o regime, see fig. S8. Sample with 1.30o twist angle has top hBN~32nm and bottom hBN~55nm thickness. This sample has graphite as bottom gate. Sample with twist angle 1.50o has top hBN~60nm and bottom hBN~36 nm. This sample has two different Josephson junction devices, one has graphite as bottom gate and other has Si as bottom gate.

Fig. S9 (a) and (c) shows the Landau fan diagram of Rxx/▢ and Rxy respectively for sample 1.30o at D=0V/nm.  We observe correlated insulators at v=+2, ±4 only in this sample. Interestingly SC is observed only in electron side in this sample. Fig. S9 (b) and (d) shows the Landau Fan of Rxx and Rxy for sample with twist angle 1.50o, respectively at D=0V/nm. In this sample we observe Chern insulator states at v=±2, +3 and ±4. A wide pocket of SC is observed on electron doping side in comparison to hole doping. No jumps in Rxy are observed in both samples around Bz= 0.

Next, we analyzed the SC in both samples. Fig. S10 (a)-(c) shows the characterization of SC in sample with twist angle 1.30o. Fig. S10 (a) shows the temperature dependence (10mK to 1.2K) of dV/dI vs Idc characteristics. The TC  of ~1.0 K is estimated from the  Rxx/▢  vs T plot, corresponding to the 90% drop in resistance, see Fig. S10 (b). The Ginzburg Landau equation, Bc2=(φ0/2πξ2GL)(1-TTc) ,(where φ0=h/2e is superconducting flux quantum, ξGL is coherence length) is fitted to the temperature dependence of Bc2 taken at 90% drop in Rxx at that temperature, see fig. S10 (c). The upper critical field at 0K i.e Bc2 (0) ~ 0.13T is estimated from fitting which corresponds to ξGL ~50nm.  Fig. S10 (d) shows the Fraunhofer pattern measured in e-S| N |h-SC configuration of 1.50o device.

Figure S10: The Landau fan diagram (a) of Rxx/▢ for TTG with twist angle 1.30o and (b) of Rxx for TTG with 1.50o measured at D=0V/nm and 15mk.  The Landau fan diagram of Rxy (c) for 1.30o TTG device at 300mK and (d) for 1.50o TTG device at 15mK and D=0V/nm.

Figure S11: (a) IV characteristics of TTG device twist angle of 1.30 as the temperatures are varied from 10mK to 1.2K. (b)The  Rxx/▢ vs T curve for the same device with critical temperature Tc=1K. (c) The critical magnetic field Bc2 is plotted as a function of T/Tc and the Bc2 (0 K) is estimated to be approximately 0.13 T. (d) Fraunhofer pattern of e-h doped superconducting pockets for the device with twist angle 1.50.

References:

1. Bocarsly, M. et al. Imaging Coulomb interactions and migrating Dirac cones in twisted graphene by local quantum oscillations. arXiv (2024).

2. Shen, C. et al. Dirac spectroscopy of strongly correlated phases in twisted trilayer graphene. Nat. Mater. 22, 316–321 (2023).

3. Zondiner, U. et al. Cascade of phase transitions and Dirac revivals in magic-angle graphene. Nature 582, 203–208 (2020).

4. Hao, Z. et al. Electric field–tunable superconductivity in alternating-twist magic-angle trilayer graphene. Science 371, 1133–1138 (2021).

5. Saito, Y. et al. Isospin Pomeranchuk effect in twisted bilayer graphene. Nature 592, 220–224 (2021).

6. Xie, M. & MacDonald, A. H. Weak-Field Hall Resistivity and Spin-Valley Flavor Symmetry Breaking in Magic-Angle Twisted Bilayer Graphene. Phys. Rev. Lett. 127, 196401 (2021).

7. Moshe, M., Kogan, V. G. & Mints, R. G. Edge-type Josephson junctions in narrow thin-film strips. Phys Rev B 78, 020510 (2008).

8. Chen, S. et al. Current induced hidden states in Josephson junctions. Nat. Commun. 15, 8059 (2024).

9. Fei, Z. et al. Two-dimensional itinerant ferromagnetism in atomically thin Fe3GeTe2. Nat. Mater. 17, 778–782 (2018).

10. Li, Y. & Baberschke, K. Dimensional crossover in ultrathin Ni(111) films on W(110). Phys. Rev. Lett. 68, 1208–1211 (1992).