Supporting Information

Nucleation mechanism and growth behavior of nano-SiO2 arrays on plant fibers via sol-gel process

Xuan Liu*

Institute of Noise & Vibration, Naval University of Engineering, Wuhan 430033, China

Key Laboratory of Ship Vibration & Noise, Wuhan 430033, China

* Corresponding Author：

Email: m15724891216@163.com (X. Liu)

Measurements and characterizations

The contact angle of the fiber samples was tested by a surface tensiometer (Kruss100, Germany). The recorded value of contact angles (θ) was the average of more than 5 measurements. The surface energy (γf) representing the wettability of the fiber samples was calculated by the following equations [1-2]:

| γl1(1+cosθ1)=2γf p γl1 p +2γf d γl1 d | (1) |
| --- | --- |
| γl2(1+cosθ2)=2γf p γl2 p +2γf d γl2 d | (2) |
| γf=γf p + γf d | (3) |

where γf , γl1 (72.8 mN·m-1), γl2 (48.0 mN·m-1) are the surface energies of the fiber samples, distilled water and ethylene glycol, respectively. γf p, γl1 p (51.0 mN·m-1) and γl2 p (19.0 mN·m-1) are the polar components of the fiber samples, distilled water and ethylene glycol, respectively. γf d, γl1 d (21.8 mN·m-1) and γl2 d (29.0 mN·m-1) are the dispersion components of the fiber samples, distilled water and ethylene glycol, respectively. The deposition quality was evaluated by nano-deposition amount (m). The pre-dried fiber samples were weighed by an electronic balance (0.0001g precision) to obtain the weight before (m0) and after (m1) the deposition. The deposition amount of nano-SiO2 arrays was then calculated by the following equation:

| m(%)=m1-m0m0 | (4) |
| --- | --- |

Fig. S1. Photographs of reaction solutions under the various ammonia concentrations.

Fig. S2. Photographs of reaction solutions under the various TEOS concentrations.

Fig. S3. Photographs of reaction solutions under the various reaction times.

References

[1] Bai T, Wang D, Yan J, Cheng W, Cheng H, Shi SQ, Wang G, Han G (2021) Wetting mechanism and interfacial bonding performance of bamboo fiber reinforced epoxy resin composites. Compos Sci Technol 213:108951.

https://doi.org/10.1016/j.compscitech.2021.108951

[2] Lu K, Xie J, Li Z, Chen H, Huang X, Chen Z (2023) Wettability and anti-fouling performances of microground dental ceramics in relation to surface formation and contact angle compound model. Appl Surf Sci 635:157741.

https://doi.org/10.1016/j.apsusc.2023.15774