Supporting Information

Unexpectedly efficient ion desorption of graphene–based materials

Xinming Xia1,#, Feng Zhou2,#, Jing Xu1,#, Zhongteng Wang1, Jian Lan3, Yizhou Yang4, Yan Fan1, Zhikun Wang1, Wei Liu1, Junlang Chen1, Shangshen Feng1,3, Liang Chen1,* and Haiping Fang4,*

1Department of Optical Engineering, Zhejiang Prov Key Lab Carbon Cycling Forest Ecosy, College of Environmental and Resource Sciences, Zhejiang A&F University, Hangzhou 311300, China.

2Radiation Monitoring Technical Center of Ministry of Environmental Protection, State Environmental Protection Key Laboratory of Radiation monitoring, Key Laboratory of Radiation Monitoring of Zhejiang Province, Hangzhou 310012, China.

3College of Pharmaceutical Chemistry and Materials Engineering, Taizhou University, Taizhou, Zhejiang 317000, China.

4Department of Physics, East China University of Science and Technology, Shanghai, 200237, China.

#These authors contributed equally to this work

*Corresponding author. E-mail: fanghaiping@ecust.edu.cn (H.-P. F.); liangchen@zafu.edu.cn (L. C.)

Contents

PS1: Materials and methods	3

Preparation of GO	3

Preparation of M–GO	3

Characterization methods	4

PS2: The experimental operations and Correlation calculation equations	4

Adsorption and Desorption of Co2+, Mn2+, and Sr2+	4

Adsorption and Desorption of radioactive 60Co for enrichment	6

PS3: XRD patterns and Raman spectra for GO and M–GO	7

PS4: XPS spectra for GO and M–GO	7

PS5: Equilibrium adsorption capacity of M–GO for Co2+, Mn2+, Sr2+, and Al3+.	8

PS6: Ultraviolet (UV) absorption spectral experiments	9

References	10

PS1: Materials and methods

Preparation of GO

Graphene oxide (GO) was prepared from natural graphite powder using a modified Hummers methodS1. Graphite powders was concentrated in H2SO4 containing K2S2O8 and P2O5, and stirred continuously for several hours. Then the mixture was washed and filtered in deionized water (DI). After vacuum drying, pre–oxidized graphite was obtained. Pre–oxidized graphite was oxidized in concentrated H2SO4 and KMnO4, diluted with DI water and further oxidized with H2O2 (30%). Then, the product was centrifuged and washed using HCl aqueous solution and DI water. Finally, the GO was obtained and placed in water for further use.

Preparation of M–GO

Magnetite–graphene oxide (M–GO) was prepared through chemical co–precipitation of magnetic iron oxide nanoparticles by coating GO with Fe3+ and Fe2+ under alkaline conditionsS2, S3. Under 353K and N2 protection, an acidic mixed aqueous solution of 0.8g FeCl2·4H2O and 2.2g FeCl3·6H2O was slowly added into the solution containing 0.5g GO. At 358K, ammonia solution was quickly added to adjust pH to about 12 and the mixture was stirred vigorously for 60 min. Then, the suspension was cooled to room temperature. By magnetic separation, the solid phase was washed to neutral with DI water, after which it was washed with DI water and ethanol. Finally, M–GO was obtained and placed in water for further use.

Characterization methods

GO and M–GO were characterized using Raman spectroscopy, XRD, and XPS. The magnetic properties of M–GO were determined using a vibration magnetometer (VSM). The morphology of M–GO was characterized using TEM. The concentrations of the ions (Mn2+, Sr2+, Co2+, and Al3+) were determined using ICP–OES. The detailed parameters for all instrument characterization are as follows: Raman spectroscopy (horiba evolution), XRD (X' Pert Powder), XPS (Thermo Scientific K–Alpha), VSM (Quantum Design PPMS DynaCool), and TEM (JEOL JEM 2100).

PS2: The experimental operations and Correlation calculation equations

Adsorption and Desorption of Co2+, Mn2+, and Sr2+

In the adsorption and desorption kinetics study of Co2+, Mn2+, and Sr2+, the prepared M–GO (200 mg) was added to 200 mL solutions of 10 mg/L Co2+, Mn2+, and Sr2+, which were prepared using MnCl2·4H2O, SrCl2·6H2O, CoCl2·6H2O, and AlCl3·6H2O, respectively. Subsequently, these mixtures were stirred at 298 K for 125 min. A negligible volume of highly concentrated Al3+ solutions was subsequently added such that the concentration of Al3+ in the mixtures was 10 mg/L, followed by stirring at 298 K for another 125 min. At designated time intervals ranging from 0 to 250 min, 5 mL of the solution was taken each time for filtration separation and the measurements of residual ion concentration. The adsorption capacity (qt) at time t was calculated according to equation (1).

qt=C0-CtVm                                    (1)

Where C0 and Ct (mg/L) are the initial and t time concentrations of Co2+, Mn2+, Sr2+, or Al3+ in the mixed solution, respectively, V (L) is the total volume of the solution, and m (g) is the solid mass of the adsorbent in the aqueous mixture.

In the adsorption and desorption study of Co2+, Mn2+, Sr2+, and Al3+, the prepared M–GO (30 mg) was added to 30 mL solutions of 10 mg/L Co2+, Mn2+, Sr2+, and Al3+. These mixtures were shaken at 160 rpm for 1 h to reach adsorption equilibrium and thereafter separated through magnetic separation and filtration. The ions in the filtrates were determined using ICP–OES. The equilibrium adsorption capacity (qe, mg/g) of Co2+, Mn2+, Sr2+, or Al3+ were calculated from the concentration of initial and equilibrium solutions according to the following equations (2).

qe=C0-CeVm                                               (2)

Where C0 and Ce (mg/L) are the initial and equilibrium concentrations of Co2+, Mn2+，Sr2+, or Al3+ in the mixed solution during adsorption, respectively, V (L) is the total volume of the solution, and m (g) is the solid mass of the adsorbent in the aqueous mixture.

The mixture solutions containing 30 mg M–GO and 10 mg/L Co2+, Mn2+, and Sr2+ were shaken at 160 rpm and 298 K for 1 h, respectively, which is a continuation of the adsorption experiments. A negligible volume of Al3+ solution was thereafter added such that the concentration of Al3+ in each ion mixture ranged from 2 to 10 mg/L. After shaking for another 1 h, the mixtures were separated through magnetic separation and filtration, and the ions in the filtrates were determined using ICP–OES. The equilibrium adsorption capacity of Al3+ was calculated according to equation (2) during desorption. Meanwhile, desorption rate (D %) of Co2+, Mn2+, and Sr2+ were calculated according to equation (3).

D %=Ce'-CeC0-Ce×100%                            (3)

Where C0 and Ce (mg/L) are the initial and equilibrium concentrations of Co2+, Mn2+, or Sr2+ in the mixed solution during adsorption, respectively. Ce' (mg/L) is the equilibrium concentration of Co2+, Mn2+, or Sr2+ during desorption.

Adsorption and Desorption of radioactive 60Co for enrichment

The enrichment multiple (n) was calculated from the activity concentrations of the initial and desorbed solutions according to equation (4).

n=C3C1                                        (4)

Where C1 and C3 (Bq/L) are the activity concentrations of 60Co of initial and desorbed solution, respectively.

PS3: XRD patterns and Raman spectra for GO and M–GO

Fig. S1 (a) XRD pattern of GO and M–GO, and (b) Raman spectra (λ=532 nm) of GO and M–GO.

PS4: XPS spectra for GO and M–GO

Fig. S2 XPS spectra: (a) wide scan of GO and M–GO, (b) Fe2p spectra of GO and M–GO, (c) C1s spectra of GO, and (d) C1s spectra of M–GO.

PS5: Equilibrium adsorption capacity of M–GO for Co2+, Mn2+, Sr2+, and Al3+.

Fig. S3 Equilibrium adsorption capacity of M–GO for Co2+, Mn2+, Sr2+, and Al3+.

The experimental operation of equilibrium adsorption capacity of M–GO for Co2+, Mn2+, Sr2+, and Al3+ can be found in section PS2. As shown in Fig. S3, the equilibrium adsorption capacities of M–GO for Co2+, Mn2+, Sr2+, and Al3+ solutions were 6.0 ± 0.1, 4.2 ± 0.1, 5.8 ± 0.1, and 7.0 ± 0.3 mg/g, respectively, which is consistent with those of previous reportsS2–S4. This demonstrates the efficient ion removal effect of M–GO, indicating that the M–GO adsorbed ions can be conveniently separated from the aqueous solution through magnetic solid/liquid separation, consistent with previous reportsS5.

PS6: Ultraviolet (UV) absorption spectral experiments

The UV absorption spectra of GO and GO in CoCl2 and AlCl3 solution are showed in Fig. S3. The UV spectrum of GO at ~ 230 nm, which is assigned to a conjugate double bond of the aromatic group that easily generated π–π* transitionS6–S8. Compared with the UV intensity of GO in CoCl2 solution, the intensity of GO in AlCl3 solution markedly decreased, indicating that the conjugate double bonds of the aromatic group in GO are greatly affected in AlCl3 solution.

Fig. S4 UV absorption spectra of GO suspension (50 mg/L) mixed in a 1:1 ratio with 0.4 M CoCl2 and AlCl3 solutions (blue and red solid line) together with GO suspension in pure water (black solid line), and pure 0.4 M CoCl2 and AlCl3 salt solution (blue and red dashed line).

References

S1. Hummers, et al. Preparation of Graphitic Oxide. J. Am. Chem. Soc. 80, 1339 (1958).

S2.	Liu, M., Chen, C., Hu, J., Wu, X. & Wang, X. Synthesis of Magnetite/Graphene Oxide Composite and Application for Cobalt (II) Removal. J. Phys. Chem. C 115, 25234–25240 (2011).

S3.	Yan, H. et al. Rapid Removal and Separation of Iron (II) and Manganese (II) from Micropolluted Water Using Magnetic Graphene Oxide. ACS Appl. Mater. Interfaces 6, 9871–9880 (2014).

S4. Minitha, C. R. et al. Magnetite Nanoparticle Decorated Reduced Graphene Oxide Composite as an Efficient and Recoverable Adsorbent for the Removal of Cesium and Strontium Ions. Ind. Eng. Chem. Res. 57, 1225–1232 (2018).

S5.	Lingamdinne, L. P., Koduru, J. R. & Karri, R. R. A comprehensive review of applications of magnetic graphene oxide based nanocomposites for sustainable water purification. Journal of Environmental Management 231, 622–634 (2019).

S6. Shi, G. et al. Unexpectedly Enhanced Solubility of Aromatic Amino Acids and Peptides in an Aqueous Solution of Divalent Transition-Metal Cations. Phys. Rev. Lett. 117, 238102 (2016).

S7. Chuang, C. H. & Chen, Y. T. Raman scattering of L-tryptophan enhanced by surface plasmon of silver nanoparticles: vibrational assignment and structural determination. J. Raman Spectrosc. 40, 150-156 (2009).

S8. Yorita, H. et al. Evidence for the cation-π interaction between Cu2+ and tryptophan. J. Am. Chem. Soc. 130, 15266-15267 (2008).