Table 2: Compositional analysis of the raw and pre-treated sugarcane bagasse. The relative concentrations of lignin, cellulose, and hemicellulose were based on dry weight.

| Composition (%) | In natura | Pre-treated |
| --- | --- | --- |
| Cellulose | 36.7 ± 0.3 | 52.7 ± 0.3 |
| Hemicellulose | 20.5 ± 0.1 | 4.7 ± 0.0 |
| Lignin | 24.4 ± 0.0 | 20.9 ± 0.1 |
| Extractives | 4.8 ± 0.0 | 12.2 ± 0.2 |
| Ashes | 6.4 ± 0.3 | 8.8 ± 0.3 |