Supplementary Information

Broadband giant nonlinear response from electrically tunable polaritonic metasurfaces

Jeayeon Yu1, Seongjin Park1, Inyong Hwang1, Daeik Kim1, Frederic Demmerle2, Gerhard Boehm2, Markus-Christian Amann2, Mikhail A. Belkin2, and Jongwon Lee1*

1School of Electrical and Computer Engineering, Ulsan National Institute of Science and Technology (UNIST), Ulsan 44919, Republic of Korea

2Walter Schottky Institut, Technische Universität München, Am Coulombwall 4, Garching 85748, Germany

*Corresponding author. E-mail: jongwonlee@unist.ac.kr

1. Electrically tunable intersubband transitions in the MQW structure

Supplementary Fig. 1. Conduction band diagram of the coupled three-quantum-well unit structure under (a) +4V (+100 kV cm-1) and (b) -4V (-100 kV cm-1) applied on 400-nm-thick MQW layer. Eij and zij are IST energy and transition dipole moment elements between electron subband i and j. (c) Calculated IST energies under the different bias voltages.

| Voltage Bias Physical Parameters | -4V | -3V | -2V | -1V | 0V | 1V | 2V | 3V | 4V |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| E12 (meV) | 87.7 | 96.5 | 106 | 117 | 128 | 139 | 150 | 161 | 171 |
| E23 (meV) | 138 | 137 | 136 | 135 | 133 | 131 | 130 | 127 | 124 |
| E34 (meV) | 134 | 127 | 119 | 111 | 105 | 98.9 | 94.6 | 92.1 | 91.4 |
| z12 (nm) | 2.04 | 1.89 | 1.76 | 1.65 | 1.55 | 1.49 | 1.43 | 1.39 | 1.35 |
| z23 (nm) | 2.29 | 2.29 | 2.29 | 2.30 | 2.31 | 2.33 | 2.36 | 2.39 | 2.42 |
| z34 (nm) | 2.46 | 2.55 | 2.67 | 2.81 | 2.95 | 3.07 | 3.18 | 3.26 | 3.29 |
| z13 (nm) | 0.62 | 0.66 | 0.69 | 0.73 | 0.75 | 0.78 | 0.80 | 0.81 | 0.82 |
| z24 (nm) | 0.36 | 0.34 | 0.32 | 0.29 | 0.25 | 0.20 | 0.14 | 0.08 | 0.02 |

Supplementary Table 1. Calculated physical parameters of the MQW structure under the different bias voltages.

2. Intersubband absorption measurement

Supplementary Fig. 2. (a) Optical setup for the intersubband absorption measurement. TE (background) and TM (signal) polarized broadband IR light from the FTIR and the linear polarizer incident on the one side of the multipath sample piece polished both sides at an angle of 45 degrees. The IR signal passing through the sample was collected by the pair of ZnSe lenses and the MCT detector. (b) Intersubband absorption spectra measured by normalizing the TM signal to the TE background signal and subtracting the background absorption. (c) Real (black) and imaginary (red) part of the surface normal component of dielectric function .

From the intersubband absorption measurement result shown in Supplementary Fig. 2b, absorption coefficient spectra was extracted using the following formula [Ref. S1] where Lint = 1.654 μm is the MWQ interaction length of the multipath sample piece, ITM and ITE are the measured signal for TM and TE polarization, respectively. The imaginary part of the surface normal component of dielectric function can be expressed as a function of the absorption coefficient as;

(S1)

From the equation, we extracted the imaginary part of  using the absorption coefficient spectra from the intersubband absorption measurement. In a different way, the surface normal component of dielectric function  of the MQW structure can be modelled as following equation [Ref. S1];

(S2)

where is the averaged dielectric constant of the undoped semiconductor heterostrutures, and  are the averaged doping density at 1st and 2nd electron subband, respectively, e is the electron charge,  is the pump frequency, ,, and , are the transition energy, linewidth, and dipole moment, respectively, for the intersubband transitions between the electron subband i and j.  Using the averaged electron density at the 1st and 2nd electron subband, and , as fitting parameters, we compared the imaginary part of the from the two equations S1 and S2. The in-plane dielectric function of the MQW structure can be modelled as following equation;

(S3)

where  is the Drude relaxation time and we assumed free electron motion in the plane of semiconductor layer. The physical parameters measured and extracted from the above calculation are provided in the Methods in the main manuscript.

3. Metasurface fabrication processes

Supplementary Fig. 3. Metasurface fabrication processes.

4. Simulation and linear characterization of M1 and M3 metasurface

Supplementary Fig. 4. (a, b) Top view cross-section of the normalized Ez field enhancement distribution of the M1 metasurface at FF with x-polarized input E-field (a, ) and at SH frequency with y-polarized input E-field (b, ). The dimensions of the M1 meta-atom are: w1=240nm, w2=340nm, px=1230nm, py=1000nm, L=1040nm, and θ=57.6o. The Ez field enhancement was monitored at 100 nm below the top surface of the MQW layer. (c) Scanning electron microscopy image of the fabricated M1 metasurface. (d) Simulated (dashed curve) and measured (solid curve) linear reflection spectra of the metasurface for x- (black) and y-polarized (red) normal incident light.

Supplementary Fig. 5. (a, b) Top view cross-section of the normalized Ez field enhancement distribution of the M3 metasurface at FF with x-polarized input E-field (a, ) and at SH frequency with y-polarized input E-field (b, ). The dimensions of the M3 meta-atom are: w1=280nm, w2=400nm, px=1450nm, py=1200nm, L=1220nm, and θ=57.6o. The Ez field enhancement was monitored at 100 nm below the top surface of the MQW layer. (c) Scanning electron microscopy image of the fabricated M3 metasurface. (d) Simulated (dashed curve) and measured (solid curve) linear reflection spectra of the metasurface for x- (black) and y-polarized (red) normal incident light.

5. Simulation of electrically tunable linear reflection spectra near the pump wavelength

Supplementary Fig. 6. (a-c) Simulated reflection spectra of the three arrays of the meta-atom structures, M1 (a), M2 (b), and M3 (c) that are optimized to have plasmonic resonance at 10.5 μm, 9.8 μm, and 9.6 μm, respectively, under the x-polarized incident light and the DC bias voltage ranging from -6V to +2V with 1V step. For better display of the data, the reflection spectra at different bias voltages are offset from each other vertically by 0.3. In this simulation, IST energies calculated from the Poissson-Schrodinger solver were used.

6. Simulation and experiment of electrically tunable linear reflection spectra near SH wavelength

Supplementary Fig. 7. (a-c) Simulated reflection spectra of the three arrays of the meta-atom structures, M1 (a), M2 (b), and M3 (c), respectively, near SH wavelength under the y-polarized incident light and the DC bias voltage ranging from -6V to +2V with 1V step. For better display of the data, the reflection spectra at different bias voltages are offset from each other vertically by 0.3. In this simulation, IST energies calculated from the Poissson-Schrodinger solver were used.

Supplementary Fig. 8. (a-c) Experimentally measured reflection spectra of the three arrays of the meta-atom structures, M1 (a), M2 (b), and M3 (c), respectively, near SH wavelength under the y-polarized incident light and the DC bias voltage ranging from -4V to +4V with 1V step. For better display of the data, the reflection spectra at different bias voltages are offset from each other vertically by 0.15.

7. Electric characterization of the metasurface

Supplementary Fig. 9. Current-voltage characteristic of the metasurface.

For SHG signal modulation measurement shown in Fig. 6 in the main manuscript, the voltage range from -4V to -2V was used and corresponding average resistance of the device is 7.2 Ω. The dimension of the mesa structure containing the MQW layer with 400nm thickness (LMQW) is Amesa=200 μm × 200 μm and the dimension of the contact pad containing the SiN passivation layer with 400nm thickness (LSiN) is ASiN=200 μm × 200 μm. The averaged dielectric constant of the MQW and the SiN layer are and . The capacitance of the structure can be calculated as . The RC time constant of the device was and corresponding cut-off frequency was .

8. Simulation of SHG spectral peak tuning

Supplementary Fig. 10. 3D plot of simulated SHG conversion efficiency spectra normalized to their maximum value as a function of input pump wavenumber for different DC bias voltages from -6V to +2V with 2V step.

9. Modal overlap factor and band bending formation in z-direction

Supplementary Fig. 11. (a) integrated modal overlap factor over the surface of the meta-atom unit structure (SMQW, ) as a function of z-directional position in the MQW layer for the M2 metasurface at the pump wavelength of 9.8 μm and the SH wavelength of 4.9  μm. The modal overlap factor gradually decreases as away from the top surface of the MQW layer. (b, c) MQW conduction band bending formation in z-direction for +2V (b) and -2V (c) applied on the top metal contact with grounded bottom metal. The band bending mainly formed near the bottom and top region of the MQW layer for the applied positive and negative bias voltage, respectively.

10. SHG peak conversion efficiency for different bias voltage

Supplementary Fig. 12. (a-c) Experimentally measured SHG peak conversion efficiency for the three meta-atom structures, M1 (a), M2 (b), and M3 (c) as a function of the applied DC bias voltage from -4V to +4V with 1V step.

REFERENCES

S1. Capasso, F., Sirtori, C., and Cho, A. Y. Coupled-quantum-well semiconductors with giant electric-field tunable nonlinear-optical properties in the infrared. IEEE J. Quantum Electron. 30, 1313-1326 (1994).