Table S1. Major element content

| Depth/ m | percentage/ % |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Fe2O3 | SiO2 | S | CaO | Al2O3 | MgO | K2O | Na2O |
| 0 | 47.11 | 22.31 | 6.54 | 15.59 | 2.26 | 1.31 | 1.31 | 0.26 |
| -0.5 | 45.32 | 18.37 | 7.07 | 13.98 | 3.15 | 1.86 | 1.86 | 0.15 |
| -1 | 38.82 | 22.67 | 5.51 | 17.38 | 2.98 | 2.5 | 2.5 | 0.18 |
| -1.5 | 34.4 | 29.04 | 4.52 | 16.64 | 3.95 | 2.64 | 2.64 | 0.26 |
| -2 | 31.74 | 25.58 | 4.83 | 15.76 | 3.02 | 2.76 | 2.76 | 0.22 |
| -2.5 | 35.44 | 26.54 | 4.52 | 20.74 | 3.63 | 2.71 | 2.71 | 0.24 |
| -3 | 33.71 | 22.44 | 4.37 | 25.57 | 3.20 | 2.74 | 2.74 | 0.2 |
| -3.5 | 32.58 | 26.58 | 4.59 | 14.9 | 3.10 | 2.23 | 2.23 | 0.22 |
| -4 | 30.19 | 25.98 | 4.20 | 18.76 | 2.99 | 2.76 | 2.76 | 0.21 |
| -4.5 | 29.67 | 24.01 | 4.31 | 15.76 | 2.86 | 2.32 | 2.32 | 0.19 |
| -5 | 31.02 | 23.15 | 4.19 | 16.25 | 3.12 | 2.41 | 2.41 | 0.2 |

Table S2. Heavy mental content of tailings profile

| Depth/ m | mg·kg-1 |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Cu | Zn | Pb | Cr | Cd | Ni | As |  |
| 0 | 887.30 | 679.54 | 41.51 | 54.06 | 0.61 | 21.14 | 120.51 |  |
| -0.5 | 2135.21 | 827.30 | 66.88 | 57.13 | 0.57 | 61.70 | 112.68 |  |
| -1 | 2867.58 | 1036.87 | 101.89 | 49.50 | 0.66 | 46.69 | 115.56 |  |
| -1.5 | 2536.17 | 1095.58 | 78.53 | 38.92 | 0.79 | 43.79 | 86.20 |  |
| -2 | 1692.71 | 810.81 | 82.53 | 48.94 | 1.22 | 39.90 | 55.93 |  |
| -2.5 | 2273.40 | 656.42 | 67.24 | 55.25 | 1.51 | 41.71 | 61.24 |  |
| -3 | 1556.58 | 519.10 | 59.81 | 50.31 | 1.69 | 32.70 | 65.92 |  |
| -3.5 | 1659.77 | 789.57 | 62.40 | 51.58 | 2.10 | 44.78 | 66.71 |  |
| -4 | 1853.62 | 751.20 | 55.81 | 52.29 | 2.50 | 46.52 | 56.41 |  |
| -4.5 | 1596.11 | 698.71 | 72.92 | 53.61 | 1.81 | 52.31 | 61.50 |  |
| -5 | 1459.80 | 653.21 | 67.79 | 49.85 | 1.89 | 41.18 | 59.08 |  |
| Max | 2867.58 | 1095.58 | 101.89 | 57.13 | 2.50 | 61.70 | 120.51 |  |
| Min | 887.30 | 519.10 | 41.51 | 38.92 | 0.57 | 21.14 | 55.93 |  |
| Ave | 1865.30 | 774.39 | 68.85 | 51.04 | 1.39 | 42.95 | 78.34 |  |
| SD | 552.72 | 168.97 | 15.61 | 4.76 | 0.67 | 10.33 | 25.75 |  |
| GB15618—2018 | 50 | 200 | 70 | 150 | 0.3 | 60 | 40 |  |
| Soil background | 32.15 | 85.58 | 47.81 | 61 | 0.09 | 26.90 | 12.44 |  |

GB15618—2018：Soil pollution risk screening value of agricultural land

Table S3. XRD diffraction peak parameters

| Profile | Number | Phase | Chemical formula | 2-Theta (Distance、Height) |
| --- | --- | --- | --- | --- |
| Hardened layer | 1 | Gypsum | CaSO4·H2O | 11.590 (7.629, 4208); 20.681 (4.291, 638); 23.340 (3.808, 802); 29.052 (3.071, 801) |
|  | 2 | Quartz | SiO2 | 26.590 (3.350, 357) |
|  | 3 | Jarosite | KFe3(SO4)2(OH)6 | 33.311 (2.688, 194) |
|  | 4 | Muscovite | KAl2Si3AlO10(OH)2 | 40.639 (2.218, 93) |
|  | 5 | Sphalerite | (Fe, Zn)S | 47.809 (1.901, 126) |
| Loose layer | 1 | Gypsum | CaSO4·H2O | 11.614 (7.596, 228); 20.841 (4.259, 231); |
|  | 2 | Quartz | SiO2 | 26.651 (3.342, 1383); 50.161 (1.827, 156); 68.169 (1.375, 88) |
|  | 3 | Sphalerite | (Fe, Zn)S | 27.569 (3.233,266); |
|  | 4 | Feldspar | (K, Na, Ca)Al2Si2O8 | 29.790 (2.997, 196); |
|  | 5 | Jarosite | KFe3(SO4)2(OH)6 | 30.970 (2.885, 224) |
|  | 6 | Muscovite | KAl2Si3AlO10(OH)2 | 33.229 (2.694, 257); |
|  | 7 | Goethite | FeO(OH) | 36.539 (2.457, 126); |
|  | 8 | Pyrite | FeS2 | 39.471 (2.281, 98); |
|  | 9 | Calcite | CaCO3 | 47.569 (1.910, 79); 61.485 (1.507, 27); |
|  | 10 | Pyrrhotite | Fe(1-x)S | 57.132 (1.611, 98); |

Table S4. BCR sequential extraction procedures

| Step | Reagent | Tailing fraction |
| --- | --- | --- |
| F1 | Acetic acid CH3COOH (0.11 mol l-1), pH=2.85 | Exchangeable, water and acid-soluble |
| F2 | Hydroxyl ammonium chloride NH2OH·HCl (0.5 mol l−1), pH=1.5 | Reducible (e.g. iron/manganese oxides) |
| F3 | Hydrogen peroxide H2O2 (8.8 mol l−1) + ammonium acetate CH3COONH4 (1 mol l−1), pH=2 | Oxidizable (e.g. organic matter and sulphides) |
| F4 | HCl + HNO3 | Residual (non-silicate bound metals) |

Table S5. The content and extraction rate of HMs in representative composite tailing sample

| HMs |  | mg·kg-1 |  |  |  |  | extraction rate |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | F1 | F2 | F3 | F4 | Sum | Total HMs |  |
| Cu | 78.35 | 8.44 | 254.43 | 1534.76 | 1875.98 | 1897.35 | 98.87% |
| Zn | 42.58 | 163.9 | 50.06 | 338.84 | 595.38 | 652.14 | 91.30% |
| Pb | 0.61 | 12.77 | 3.69 | 37.8 | 54.87 | 60.69 | 90.41% |
| Cr | 0.25 | 5.64 | 0.44 | 39.98 | 46.31 | 50.22 | 92.21% |
| Cd | 0.66 | 0.3 | 0.13 | 0.98 | 2.07 | 1.89 | 109.52% |
| Ni | 3.94 | 6.99 | 3.2 | 22.67 | 36.8 | 40.21 | 91.52% |
| As | 0.07 | 0.39 | 0.31 | 107.95 | 108.72 | 99.87 | 108.86% |

Table S6. The TCLP content of HMs in representative composite tailing sample

| HMs | mg·L-1 |  |  |
| --- | --- | --- | --- |
|  | leaching content | Chinese regulation | USEPA regulation |
| Cu | 66.35 | 100 | - |
| Zn | 96.77 | 100 | 250 |
| Pb | 2.22 | 5 | 5 |
| Cr | 3.25 | 5 | 15 |
| Cd | 1.18 | 1 | 1 |
| Ni | 4.41 | 5 | - |
| As | 0.33 | 5 | 5 |