
Supplementary Materials for
Evaluating Interfacial Stability in Solid-State Pouch Cells Via Ultrasonic Imaging

Hanyu Huo1†, Kai Huang2,3,†, Wei Luo1*, Jintao Meng2, Liangyi Zhou2, Zhe Deng2,3, Jiayun Wen1, Yiming Dai1, Zhimei Huang2, Yue Shen2,3*, Xiangxin Guo4, Xiulei Ji5, Yunhui Huang2*
1Institute of New Energy for Vehicles, School of Materials Science and Engineering, Tongji University, Shanghai 201804, China

2State Key Laboratory of Material Processing and Die & Mould Technology, School of Materials Science and Engineering, Huazhong University of Science and Technology, Wuhan, Hubei 430074, China

3HUST- Wuxi Research Institute, Wuxi, Jiangsu 214000, China
4College of Physics, Qingdao University, Qingdao 266071, China

5Department of Chemistry, Oregon State University, Corvallis, OR, 97331-4003, USA
†These authors contributed equally to this work

* Corresponding authors.

Email address: weiluo@tongji.edu.cn; shenyue1213@hust.edu.cn; and huangyh@hust.edu.cn

[image: image13.png]a Blade casting b Hot pressing





Supplementary Fig. 1 Schematic images of the fabrication of electrolyte membranes by the (a) blade casting and (b) hot pressing.
[image: image2.png]4000

Y]

3000

Q)

2000

Z,,

1000

—«— PEO(LITFSI) ! b
—e—PLLZ@HP
-—— PLLZ@BG" ~£{ -
& = E
> ‘8 o
s 2
| -
0 1 1
0 1000 2000 3000 4000
z. (Q

PLLZ@BC
—m—PLLZ@HP

31 3.2

1000/T (K™)





Supplementary Fig. 2 (a) EIS spectra of the PEO(LiTFSI), PLLZ@HP, and PLLZ@BC at 25 oC. (b) Arrhenius plots of the PLLZ@HP and PLLZ@BC. Top-view SEM images of the (c) PLLZ@BC, and (d) PLLZ@HP. 

[image: image3.png]PLLZ@BC 1V

0.50

P-P Value:0.58 V

o

N

a
T

Intensity (V)
o
]
I |
?l

&
N
o
T

-0.50 . . . ,
64 66 68 70 72 74
ov Time of flight (us)





Supplementary Fig. 3 The ultrasonic transmission image of the PLLZ@BC and the ultrasonic wave at the position marked by the arrow.

[image: image4.png]1.5

1.0t

—e— After assembling
—o— After 0.5 h
—o— After 1.5 h

2.0

2.5




Supplementary Fig. 4 EIS spectra of the Li/PLLZ@HP/Li cell after different time. 

[image: image5.png]1E-4
1E-5

_ 1E6
1E7
1E-8
1E9
1E-10
1E-11
1E-12
1E-13

Current (A)

——He——H,——CH,
——CH,——CH,

4 _ 06
Time (h)

0.8

1.0




Supplementary Fig. 5 DEMS results for the Li/PLLZ@HP/Li cell without charge/discharge process.
[image: image6.png]0.2

2 0.1
(]
g oof
S-01f
-0.2
1E-9 ol
=S
e CH,
 1E-10 ~— ] '
E Hy
3
m
1E-11[ co.
S———— Y
1E_12 1 1 1 1
o 2 4 6 8 10

Time (h)




Supplementary Fig. 6 Voltage profile and corresponding DEMS results of the Li/PLLZ@HP/Li cell cycled at 0.1 mA cm-2 and 45 oC.
[image: image7.png]a 10 - - >
E 05 Li/PLLZ@HPI/Li, 0.2 mA cm Short circuit
S 0.0
s
©-0.5
>
1.0 1 1 1 1
0 100 200 300 400 500
Time (h)
b 1.0 Interfacial activation _
. Before cycling
S o5
% 0.0 !lﬂﬂﬂﬂﬂﬂ[lﬂﬂﬂﬂﬂﬂ[lﬂﬂﬂﬂ[
8
5 -0.5}
>
1.0 1 1 1 1
0 10 20 30 40 50
Time (h)
d Interfacial aging e
1.0 a Short circuit
Sosl
8
5-05
>
1.0 . .

100 110 120 '380 390
Time (h)

400




Supplementary Fig. 7 (a) Galvanostatic cycling performance of the Li/PLLZ@HP/Li cell at 0.2 mA cm-2 (0.1 mAh cm-2) at 45 oC. (b) Magnified image for 0-50 h. (c) The corresponding ultrasonic transmission images of the Li/PLLZ@HP/Li cell during the initial cycling. (d) Magnified image for 100-400 h. (e) The corresponding ultrasonic transmission images of the Li/PLLZ@HP/Li cell during the following cycling.
[image: image8.jpg]Before cycling After cycling

k & - 3 § e





Supplementary Fig. 8 Top-view SEM images of Li metal in Li/PLLZ@HP/Li cell (A) before and (B) after cycling. 

[image: image9.png]—38V
—4.4V
—5V

Transmittance (%)

2000 1800 1600 1400 1200
Wavenumber (cm™)




Supplementary Fig. 9 FTIR spectra of the PLLZ@HP at different voltages. 

[image: image10.png]Charge

Discharge

3.8V 4.0V 4.2V 4.2V (0.5 h)

& R

40V gy 100mV

ov

42V (1h)

*




Supplementary Fig. 10 Differential ultrasonic images of the LCO/PLLZ@HP/Li cell during the cycling at 0.1 C.
[image: image11.png]Q

(o2

Intensity (a.u.)

Co 2p F1s LiTFSI/PVDF c Cis oc | d
— LiF - —
El El - Ei
—A\_A s 3| _cf ocs H
z z z
@ i @ @
§ LITFSIPVDF | & o-c, §
£ E c-c .
C-Fy
804 800 796 792 788 784 780 776 696 692 688 684 680 206 292 288 284 280 538 536 534 532 530 528 526
Binding energy (eV) Binding energy (eV) Binding energy (eV) Binding energy (eV)




Supplementary Fig. 11 (A) Co 2p, (B) F 1 s, (C) C 1s, and (D) O 1s XPS spectra of LCO cathode before and after cycling.

XPS was carried out to compare the LCO cathode before and after cycling (Fig. S11). Co 2p spectra show no change of Co chemical valence during cycling up to 4.2 V. The peak at 688.6 eV in the F 1s spectrum corresponds to the Poly(vinylidene fluoride) (PVDF) binder and LiTFSI 1. A new peak of LiF at 684.8 eV is obtained after cycling, which could be attributed to the oxidation of LiTFSI at a high voltage. LiF with an ultralow ionic conductivity can hinder the Li+ transport in the LCO cathode, thus leading to the fast capacity decay. Three peaks at 284.3, 286.2, and 292.4 eV are obtained in the C 1s spectrum, which can be assigned to C-C, C-O, and CF3 in the pristine LCO cathode, respectively 2. The intensity of C-C peak decreases and a new peak of O-C=O at 288.1 eV occurs after cycling. The oxidation of PEO molecular skeleton is also confirmed by the O 1s spectrum.
[image: image12.png]H—C—H CH, CHs

85°C 2CN—C—— + N, ‘

N=C——C——N=—=N—C——CN
| A

CHs CH, CHs C





Supplementary Fig. 12 (a) Thermolysis equation of Azobisisobutyronitrile (AIBN) at 85 oC. Ultrasonic images before and after (b) 3 μL, and (c) 7 μL N2 generation in the pouch cells. 
36.65 mg AIBN was added into 5 mL methylpyrrolidone (NMP)/ethanol (1:1) solvent and stirred for 6 h, forming 0.0446 mol L-1 AIBN solution. Then, AIBN solution (3 μL and 7 μL) was dipped into the separator and vacuum dried at 50 oC for 1 h to remove the solvent. Pouch cells (4.5 cm×5 cm) were assembled with 2.8 mL liquid electrolyte and rested for 6 h. Ultrasonic imaging was carried out when the electrolyte was fully wetted the separator. Then, heating the pouch cells at 85 oC for 2 h, which leads to the decomposition of AIBN and releases N2 in the pouch cells (Supplementary Fig. 12a). The ultrasonic images were subsequently obtained for comparison.
As shown in Supplementary Fig. 12b, 3 μL N2 can be well reflected in the pouch cell as the green region. It is estimated that 6 μm void/gap is detectable by our ultrasonic equipment according to the gas area of 5 cm-2. When the gas amount increases to 7 μL, the ultrasonic signal further attenuates, leading to the blue color in the gas region (Supplementary Fig. 12c).

References

1
Qiu, J. et al. Enabling Stable Cycling of 4.2 V High‐Voltage All‐Solid‐State Batteries with PEO‐Based Solid Electrolyte. Adv. Funct. Mater. 30, 1909392, doi:10.1002/adfm.201909392 (2020).

2
Yang, X. et al. Determining the limiting factor of the electrochemical stability window for PEO-based solid polymer electrolytes: main chain or terminal –OH group? Energy & Environmental Science 13, 1318-1325, doi:10.1039/d0ee00342e (2020).



3

[image: image1]