Extended Data Fig. 1 Polymerization-induced 2D/3D self-assembly of hierarchical non-crosslinked meso-particles, intra-crosslinked meso-/microparticles, and intra-crosslinked meso-/nanofibrils.

Extended Data Fig. 2 Randomly 2D self-assembled high-order condensed solid states of nascent G1–4 powders. a: Long-period nanostructures characterized via 2D/1D-USAXS; b: Highly ordered condensed solid-states characterized via DSC.

Extended Data Fig. 3 Hierarchical transformations from high-order condensed solid-states to order melt and to disordered melt by annealing at temperatures between Tm and TO-D and above TO-D.

Extended Data Fig. 4 Morphologies of nascent G2–3 and G6 powders before and after vacuum annealing at 250 °C for 6–20 h. a: G2-3 powders: inter-coalescence after annealing, and transparent sheets are obtained; b: Morphologies before and after annealing nascent G6 powders containing high-content intrinsic nanofibrils (G6: only strong intra-coalescence after annealing, and an opaque sheet is obtained).

Extended Data Fig. 5 Characterization of the dynamic and static chain re-entanglements of G3-NPs and the influence of chain re-entanglements and relaxation on the tensile solid-state stress–strain properties, non-isothermal crystallization, melting properties and dual-shaped memory effects.

Extended Data Fig. 6 Hierarchical 2D-ordered and 2D-oriented nanofibrillar superstructures, preserved intrinsic nanofibrillar networks and the properties of the G1–2/4 Sheets.

Extended Data Fig. 7 Qualitative and quantitative 2D/1D-USAXS measurements of condensed-order solid-states from high-order condensed solid-states of nascent powders via self-nucleation and isothermal crystallization (Tp = 140 °C, 15 min; Tc = 128 °C, 3 h) and from inter-crosslinked order melts of pressed sheets (Tp = 142 °C, 15 min; Tp = 300 °C, 1–2 h; Tc = 128 °C for isothermal crystallization (IC), 3–23 h; Tc < 60 °C for quenched crystallization (Q) (TP: through-plane direction; IP: in-plane direction).

Extended Data Fig. 8 Hierarchical structure and properties. a: Melting behaviors of highly 2D-ordered nanofibrillar superstructures obtained via self-nucleation of G1–2 powders at 140 °C for 15 min and isothermal crystallization at 128 °C for 3 h; subsequent non-isothermal crystallization behaviors after annealing at 160 °C for 5 min; b: Fracture morphologies of bi-notched impact and tensile deformed G5 sheets containing high contents of intrinsic nanofibrils (Fig. S5); c: Melting behaviors of meso-superstructures and disordered condensed solid-states; d: Tensile and thermal properties; e: Characterization of crystal stems and their orientation via X-ray diffraction.

Extended Data Fig. 9 Non-isothermal crystallization and melting behaviors (a), tensile properties (b), and morphologies (c-e) of eplastomers containing dynamic 2D-ordered nanofibrillar networks and disordered 3D meso-/microgranules.

Extended Data Fig. 10 Shearing (a), internal mixing (a), compression molding (b, d), extrusion (c) and crystallization (d) procedures for UHMWPE and eplastomers.