Construction of The Heterojunction with Basic Bismuth Nitrates and CuCr-Cl-LDH for Enhanced Photocatalytic Degradation of Tetracycline Under Visible-light

Brazilian Journal of Chemical Engineering

Yin-Yan Dou1, Yan-Ming Shen*1, Jun-Hua Wen1, Lei Yang1

1Department of Chemical Engineering, Shenyang University of Chemical Technology, Shenyang, China

*Corresponding author, e-mail: sym6821@sina.com.cn

Text S1

Stability test for the photocatalyst

The BBN/LDH-2 photocatalyst was selected to test the stability of photocatalyst. After photocatalytic degradation of TC, the used photocatalyst particles were collected by filtration and separation, and washed with distillated water and ethanol for three times, then dried at 60 oC at vacuum for 12 h. The obtained photocatalyst particles were used for the next photcatalytic degradation test. The photocatalytic degradation condition was set as catalyst dosage of 0.5 g/L, TC concention of 20 mg/L.

Figures:

Fig.S1 EDS element maps and composition of sample BBN/LDH-2.

Fig. S2 N2 adsorption-desorption isotherms and pore size distribution curves of samples.

Fig. S3 Results of stability experiment

Fig. S4 The schematic diagram for photocatalytic reaction process on BBN/CuCr-Cl-LDH composite.

Tables:

Table S1 TOC degradation effects of different catalystsa

| Photocatalyst | TOC/mg·L-1 |  |
| --- | --- | --- |
|  | After adsorption | Irradiation time of 120 min |
| CuCr-Cl-LDH | 11.01 | 9.738 |
| BBN | 11.04 | 8.712 |
| BBN/LDH-1 | 8.210 | 2.703 |
| BBN/LDH-2 | 6.256 | 1.670 |
| BBN/LDH-3 | 6.465 | 1.877 |

a Note: TOC value of initial TC concentration was 11.57 mg·L-1.

Table S2 complete list of all acronyms used within the manuscript

| Full name | acronym |
| --- | --- |
| Basic Bismuth Nitrates | BBN |
| tetracycline | TC |
| advanced oxidation processes | AOPs |
| layered doubled hydroxides | LDHs |
| Isopropyl alcohol | IPA |
| p-benzoquinone | BQ |
| disodium ethylenediaminetetraacetic acid | EDTA-2Na |
| X-ray diffraction | XRD |
| scanning electron microscope | SEM |
| transmission electron microscope | TEM |
| energy dispersive spectrometer | EDS |
| UV-vis diffuse reflectance spectra | UV-vis DRS |
| X-ray photoelectron spectroscopy | XPS |
| electrochemical impedance spectroscopy | EIS |
| Mott-Schottky | MS |
| Total Organic Carbon | TOC |
| electron paramagnetic resonance | EPR |