Supplementary Material

Sensor with strong solid emission for fluorescence colormetric detection of 1,4 dioxane in Water and vapor based on the

Keto-Enol isomerisation

Jing Wang1, Zi-Ao Zong2, Shi-Fu Huang1, Mohd. Muddassir4, Zhi-Yong Xing1, Na-Na Li2,3,* Wen-Qiong Jiang5, 6,*

1Modern Industrial College of Biomedicine and Great Health, Youjiang Medical University for Nationalities, Baise 533000, China

2Key Laboratory of Research on Environment and Population Health in aluminium mining areas (Youjiang Medical University for Nationalities), Education Department of Guangxi Zhuang Autonomous Region, Baise, China

3Department of Chemistry, Xinzhou Normal University, Xinzhou, Shanxi 034000, PR China

4Department of Chemistry, College of Science, King Saud University, Riyadh 11451, Saudi Arabia

5Affiliated Hospital of Youjiang Medical University for Nationalities, Baise 533000 Guangxi, PR China

6Guangxi Key Laboratory for Biomedical Material Research, Baise 533000 Guangxi, PR China

*Correspondence: LMT13643562571@126.com (N.-N. Li); 2901058890@qq.com (Wen Qiong Jiang)

† These authors contributed equally to this work.

Materials and analysis.

1H NMR spectra were recorded on a Bruck AV-600 spectrometer in d6-DMSO. IR spectra were performed with a Perkin-Elmer IR spectrophotometer. Pgeneral TU-2550 UV-vis spectrophotometer and Perkin Elmer LS55 fluorescence spectrometer were employed to measure absorption and fluorescence spectra, respectively. Mass spectrum was acquired with an Agilent 6220 Quadruple LC/MS (Agilent Co, USA). Elemental analyses (C, H, N and S) were conducted with a 2400 model Perkin-Elmer analyzer.

For fluorescence measurements, excitation wavelength was 360 nm and the excitation and emission wavelength band passes were both set at 5 nm and 5 nm.

Fig. S1. 1H NMR (DMSO-d6, 600 MHz) spectra of BPCA.

Fig. S2. 13C NMR (DMSO-d6, 600 MHz) spectra of BPCA.

Fig. S3. ESI-MS spectrum of BPCA.

Fig. S4. The UV-vis spectrum of BPCA in 1, 4-dioxane.

Fig. S5. FT-IR spectra of BPCA, BPCA/1, 4-dioxane system.

Fig. S6. Plot of fluorescence intensity value at 435 nm in different content of 1, 4-dioxane. λex = 360 nm, slit: 5 nm/5 nm.

Determination of binding constants

Assuming a 1: n stoichiometry for interaction between BPCA and 1, 4-dioxane., the equilibrium is given by the following equation:

BPCA+n1, 4-dioxaneBPCA1, 4-dioxanen                                                                   (2)

The association constant, K, is therefore expressed as:

K=[BPCA1,4−Dioxn][BPCA][1,4−Diox]n=[BPCA1,4−Dioxn]([BPCA]0−1,4−Dioxn)([1,4−Diox]0−n[BPCA1,4−Dioxn])n

(3)

[BPCA1,4−Dioxn], [BPCA] and [1, 4-dioxane] represent the equilibrium concentrations of the complex, free BPCA, and free 1, 4-dioxane, respectively. [BPCA]0  and [1,4−Diox]0 are the initial concentrations of BPCA and 1, 4-dioxane, respectively. If [1,4−Diox]0≫[BPCA1,4−Dioxn], the Eq. (3) can be simplified as follows:

K=[BPCA1,4−Dioxn]([BPCA]0−1,4−Dioxn)[1,4−Diox]0n                                                  (4)

Then it can be transformed to:

K[1,4−Diox]0n=[BPCA1,4−Dioxn][BPCA]0−[BPCA1,4−Dioxn]                                           (5)

Fluorescence intensity is given by following equations:

F−FminFmax−F=[BPCA1,4−Dioxn][BPCA1,4−Dioxn]max−[BPCA1,4−Dioxn]=[BPCA1,4−Dioxn][BPCA]0−[BPCA1,4−Dioxn]                       (6)

Fmin is the fluorescence intensity of BPCA without cations, F is the fluorescence intensity of BPCA obtained with 1, 4-dioxane, Fmax is the fluorescence intensity of BPCA in the presence of excess amount of 1, 4-dioxane. In the presence of excess amount of 1, 4-dioxane, [BPCA1,4−Dioxn]max is almost equal to [BPCA]0. Using Eqs. (5) and (6), the following equation is given:

F−FminFmax−F=K[1,4−Diox]0n                                                      （7）

lgF−FminFmax−F =lgK+nlg[1,4−Diox]0                                             (8)

When assuming the 1:1 stoichiometry (n = 1), Eq. (1) is obtained.

lgF−FminFmax−F =lgK+lg[1,4−Diox]                                                (1)

Fig. S7. The non-linear fitting (fluorescent emission at 435 nm) of BPCA lg[(F-Fmin)/(Fmax-F)] = lgK+lg[1, 4-dioxane]. K is the association constant, Fmin is the fluorescence intensity of BPCA without any cations, F is the fluorescence intensity of BPCA obtained with 1, 4-dioxane, Fmax is the fluorescence intensity of BPCA in the presence of excess amount of 1, 4-dioxane.

Fig. S8. 1H NMR spectra of BPCA and BPCA/Diox system (DMSO-d6, 600 MHz).

Table S1 Probe BPCA for the determination of 1, 4-dioxane in water samples from tap and lake water

| Water samples studied | Amount of standard 1, 4-dioxane added (fw) | Total 1, 4-dioxane found (n=3) (μM) | Recovery of 1, 4-dioxane (n=3) added (%) | RSD (%) | Relative error （%） |
| --- | --- | --- | --- | --- | --- |
| Tap water | 2% | 2.11% | 105.50 | 2.20 | 2.75 |
|  | 3% | 3.03% | 101.00 | 0.50 | 2.17 |
|  | 4% | 4.21% | 105.25 | 3.57 | 0.63 |
|  | 5% | 5.12% | 104.20 | 1.50 | 1.82 |
|  | 6% | 6.15% | 102.50 | 2.56 | 3.12 |
|  | 7% | 6.98% | 99.71 | 0.20 | -2.63 |