# Tunable porosity in a hydrogel with extreme vibration damping properties

Graham J. Day1,2,3, Qicheng Zhang2, Chrystel D. L. Remillat2, Gianni Comandini2, Adam W. Perriman1,4 and Fabrizio Scarpa2

1 School of Cellular and Molecular Medicine, University of Bristol, BS8 1TD Bristol, UK

2 Bristol Composites Institute, School of Civil, Aerospace and Design Engineering (CADE), University of Bristol, Bristol BS8 1TR, UK

3 Centre for the Cellular Microenvironment, Division of Biomedical Engineering, James Watt School of Engineering, The Advance Research Centre, University of Glasgow, Glasgow G12 8QQ, UK

4 Research School of Chemistry and John Curtin School of Medical Research, Australian National University, Canberra ACT2601, Australia

# Supplementary figures

Supplementary figure S1. Chemical structures of the polymers used to make porous hydrogels. a Linear alginate polymer comprised of (1→4)-linked β-D-mannuronate (m) and α-L-guluronate (n), bound to monovalent sodium ions (Na+; blue spheres). b Guluronate chains of alginate cross-linked by divalent calcium ions (Ca2+; green spheres). c Structure of the triblock copolymer Poloxamer 407, comprised of hydrophilic polyethylene glycol (red boxes) and hydrophobic propylene glycol (orange box). a = 101 and b = 56.

Supplementary figure S2. Forming hydrogels for compression testing. a The mold used in dialysis to yield hydrogel discs 12 mm in diameter and 5 mm in height. b Optical images of the A1.25 hydrogel discs with increasing Poloxamer concentration. c–d Corresponding images of the A2.5 and A5 hydrogels, respectively. Yellow lines demarcate 1 cm.

Supplementary figure S3. Forming the hydrogels for dynamic mechanical characterisation. a–b Optical images of the mold used in dialysis to form hydrogel blocks 30×30×15 mm. c–d Images of the blocks.

Supplementary figure S4. Pore diameters of the A5 hydrogels. Average pore diameter and distribution measured from the cryo-EM micrographs. n = 290, error bars = SD. **** = p <0.0001.

Supplementary figure S5. Linearity of the dynamic mechanical analysis set-up. The dynamic modulus of A5–P0 (a; black), A5–P2.5 (b;blue), A5–P5 (c;green), and A5–P10 (d;red) at increasing acceleration rates under increasing degrees of pre-stress (increasing opacity).

Supplementary figure S6. Transmissibility factor amplitudes (a–d) and corresponding phase curves (e–h) of A5–P0 (black), A5–P2.5 (blue), A5–P5 (green), and A5–P10 (red). Increasing opacity corresponds to increasing pre-stress. This data is also displayed in Figure 5b, but re-plotted here per individual hydrogel composition.

Supplementary figure S7. Characterization of A5–P5 hydrogel using a dynamic mechanical analyzer (DMA) between 100–130 Hz. a Storage modulus. b Loss modulus. c Tan δ. Tests were done at 25 °C, with a pre-loading force of 0.001 N and oscillation amplitude of 10 µm.

# Supplementary tables

Supplementary table S1. The mass of alginate, Poloxamer 407, and water required to make 50 g gels for dialysis casting.

| Hydrogel | Alginate mass (g) | Poloxamer 407 mass (g) | Water mass (g) |
| --- | --- | --- | --- |
| A1.25–P0 | 0.625 | 0.0 | 49.375 |
| A1.25–P2.5 |  | 1.25 | 48.125 |
| A1.25–P5 |  | 2.5 | 46.875 |
| A1.25–P10 |  | 5.0 | 44.375 |
| A2.5–P0 | 1.25 | 0.0 | 48.75 |
| A2.5–P2.5 |  | 1.25 | 47.5 |
| A2.5–P5 |  | 2.5 | 46.25 |
| A2.5–P10 |  | 5.0 | 43.75 |
| A5–P0 | 2.5 | 0.0 | 47.5 |
| A5–P2.5 |  | 1.25 | 46.25 |
| A5–P5 |  | 2.5 | 45.0 |
| A5–P10 |  | 5.0 | 42.5 |

| Alginate (wt%) | Poloxamer (wt%) | C01 (kPa) | C10 (kPa) |
| --- | --- | --- | --- |
| 1.25 | 0.0 | 3.17 | -0.13 |
|  | 2.5 | 3.41 | 0.08 |
|  | 5.0 | 3.67 | -0.47 |
|  | 10.0 | 2.03 | 0.60 |
| 2.5 | 0.0 | 14.81 | -3.90 |
|  | 2.5 | 16.15 | -4.72 |
|  | 5.0 | 14.31 | -5.87 |
|  | 10.0 | 1.02 | -0.11 |
| 5.0 | 0.0 | 45.75 | -17.61 |
|  | 2.5 | 52.06 | -22.87 |
|  | 5.0 | 58.18 | -24.36 |
|  | 10.0 | 17.72 | -9.87 |

Supplementary table S2. Derived coefficients from the Mooney–Rivlin model of hyperelasticity.