Extended Figure 1: (a) The synergistic characteristics of the ionic biogel resulting from the combination of the gelatin-glycerol system with the PEDOT:PSS/ionic liquid. (b) The schematic phase-transition of ionic biogel.

Extended Figure 2: (a) The synergistic interplay of electrostatic interactions from PEDOT:PSS/EMIM-TFSI and hydrogen bonding from the gelatin-glycerol-salt matrix. (b) Raman spectroscopy and (c) Fourier-transform infrared spectroscopy (FTIR) of the ionic biogel at different temperatures. (d) Atomic force microscopy (AFM) of the phase-separated, porous ionic biogel. (f,g) Grazing-incidence wide-angle X-ray scattering (GIWAXS) patterns of ionic biogel at different temperatures. (h) Biocompatibility test of the ionic biogel using MCF-10A for 24 h and 48 h

Extended Figure 3: (a) Comparison in dynamic viscosity as a function of temperature between non-ionic and ionic biogel. (b) Variation of loss-tangent as a function of time during temperature ramp-up, ramp-down, and isothermal conditions. (c) Variation in the normalized viscosity from a ~3-month-old ionic biogel during repeated temperature cycles of ramp-up, ramp-down, and isothermal conditions. (d) Lap-shear adhesion test of the ionic biogel. (e) Water-vapour transmission rate (WVTR) of ionic biogel compared to open bottle. (f) Thermoelectric Voltage as a function of Temperature change from 0 to 8 K to determine the Seeback Coefficient.

Extended Figure 4: (a) Comparison in the skin contact impedance magnitude and phase between the ionic biogel and non-ionic biogel. (b) Comparison in the skin contact impedance magnitude and phase from the ionic biogel at different temperatures. (c) Comparison in electrochemical impedance spectroscopy (EIS) between the ionic biogel and normal biogel. (d) Variation of impedance (left) and capacitance (right) as a function of time over 8 days. (e) Characterisation of the charge injection capacity (CIC) of the ionic biogel electrodes with 5 mA current at 0.5 Hz to give a CIC of 100 mC/cm2. (f) Comparison in the transient voltage between different current amplitudes of 5 and 10 mA.

Extended Figure 5: (a) Scalp contact impedance magnitude and phase of the ionic biogel at C3 location. (b) Comparison in the frequency spectrum of alpha wave between closed and open eyes. (c) Power spectra of the beta wave for different loading weights. Power spectrogram showing event-related desynchronization (ERD) at Cz during (d) 1 kg and (e) 2 kg reps. (f) Power spectrogram showing ERD during sensory mechanical vibration at C3 locations.

Extended Figure 6: Schematic of the wearable electrical stimulator array placed on the arm.

Extended Figure 7: COMSOL simulation of the tip-shaped OECT with (a) temperature distribution profile, (b) velocity profile of the ionic biogel extrusion, and (c) ion concentration over the ionic biogel at the tip-shaped neural interface.