Supporting Information

Operando Unraveling Photothermal-Promoted Dynamic Active Sites Generation in Spinel NiFe2O4 for Oxygen Evolution

Likun Gao1,2,4, Xun Cui1,4, Zewei Wang1, Christopher D. Sewell1, Zili Li1, Shuang Liang1, Mingyue Zhang1, Jian Li2, Yingjie Hu3, Zhiqun Lin1*

1School of Materials Science and Engineering, Georgia Institute of Technology, Atlanta, GA 30332, USA

2Key Laboratory of Bio‐based Material Science and Technology of Ministry of Education, Northeast Forestry University, Harbin 150040, China

3Nanjing Key Laboratory of Advanced Functional Materials, Nanjing Xiaozhuang University, Nanjing 211171, China

4These authors contributed equally: Likun Gao, Xun Cui

* Corresponding Authors: Zhiqun Lin

E-mail: zhiqun.lin@mse.gatech.edu

Supplementary Table 1. Summary of molecular weights (MWs) of amphiphilic multi-arm star-like PAA-b-PSAN diblock copolymers, the corresponding sizes of PSAN-ligated NiFe2O4 nanoparticles (NFO NPs), and the length of outer PSAN chains.

| Samples | Mn, PtBAa | Mn, PtBA-b-PSANb | Mn, PAAc | Mn, PSANd | Dh of Star-like PAA-b-PSANe | NP Designation | NP size |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 76K | 162K | 5K | 8K | 8.4 ± 0.3 nm | NFO-3-8K | 3.3 ± 1.7 nm |
| 2 | 110K | 326K | 7K | 15K | 19.0 ± 0.7 nm | NFO-7-15K | 7.0 ± 1.8 nm |
| 3 | 203K | 637K | 15K | 21K | 28.8 ± 0.8 nm | NFO-12-21K | 12.0 ± 2.1 nm |
| 4 | 196K | 343K | 15K | 7K | 23.4 ± 0.5 nm | NFO-12-7K | 12.1 ± 2.5 nm |

Notes: aNumber average molecular weight (Mn) of star-like PtBA nanoreactor before hydrolysis determined by GPC in THF. bMn of star-like PtBA-PSAN nanoreactor before hydrolysis determined by GPC in THF. cMn of each PAA block calculated from the molecular weight difference between PtBA block (before hydrolysis) and PAA block (after hydrolysis). dMn of each PSAN block calculated from 1H NMR data. eHydrodynamic diameter Dh of star-like PAA-b-PSAN diblock copolymers in DMF measured by dynamic light scattering (DLS).

Supplementary Fig. 1 Histograms of the size distributions of randomly selected 50 nanoparticles from TEM images in Fig. 2. PSAN-ligated NFO NPs with diameters of (a) 3.3 ± 1.7 nm ligated by 8K PSAN chains (denoted NFO-3-8K), (b) 7.0 ± 1.8 nm ligated by 15K PSAN chains (denoted NFO-7-15K), (c) 12.0 ± 2.1 nm ligated by 21K PSAN chains (denoted NFO-12-21K), and (d) 12.1 ± 2.5 nm ligated by 7K PSAN chains (denoted NFO-12-7K).

Supplementary Fig. 2 Dynamic light scattering (DLS) measurements on unimolecular micelles of star-like PAA-b-PSAN diblock copolymers in DMF (i.e., samples in Supplementary Table 1). Star-like PAA-b-PSAN diblock copolymers with hydrodynamic diameter Dh of (a) 8.4 ± 0.3 nm (denoted Sample 1), (b) 19.0 ± 0.7 nm (denoted Sample 2), (c) 28.8 ± 0.8 nm (denoted Sample 3), and (d) 23.4 ± 0.5 nm (denoted Sample 4).

Supplementary Fig. 3 XRD pattern of PSAN-ligated NFO NPs.

Supplementary Fig. 4 HRTEM images of (a) NFO-3-8K, (b) NFO-7-15K, and (c) NFO-12-21K. The white circles are the guides to eyes.

Supplementary Fig. 5 TEM images of (a) carbon black, (b) PSAN-ligated NFO-12-7K NPs (after ethanol washing yet without subsequent drying) on carbon black, and (c) PSAN-ligated NFO-12-7K (after ethanol washing, followed by subsequent drying) on carbon black. The white dashed circle in (c) illustrates that the NPs deposited outside carbon black substrate (i.e., marked as no carbon black).

Supplementary Fig. 6 LSV curves of PSAN-ligated NFO-12-7K without drying (η20 = 329 mV) and NFO-12-7K with drying (η20 = 420 mV) for OER in 1.0 M KOH.

Supplementary Fig. 7 Cyclic voltammetry (CV) curves measured at different scan rates from 20 to 60 mV s-1 for (a) NFO-3-8K, (b) NFO-7-15K, (c) NFO-12-21K, and (d) NFO-12-7K.

Supplementary Fig. 8 Nyquist plots of PSAN-ligated NFO-3-8K, NFO-7-15K, NFO-12-21K and NFO-12-7K samples. The simple Randles circuit was used, containing a solution resistance (Rs), charge transfer resistance (Rct), and a constant-phase element (CPE) related to the double layer capacitance.

Supplementary Fig. 9 (a) O 1s, (b) Ni 2p and (b) Fe 2p XPS spectra of NFO-3-8K, NFO-7-15K, NFO-12-21K and NFO-12-7K.

Supplementary Fig. 10 Schematic diagrams illustrating the relationship between the PSAN chain length and the exposed active surface area for three representative PSAN-ligated NFO NPs samples (i.e., NFO-3-8K, NFO-12-21K and NFO-12-7K). The white-and-red balls represent OH‒ ions of electrolyte (i.e., KOH solution). A decreasing trend for the OH‒ ions to access the surface of NFO NPs is as follows: NFO-12-7K > NFO-12-21K > NFO-3-8K.

Supplementary Fig. 11 TEM images of (a) NFO NPs templated by star-like PAA only, and (b) NFO NPs formed without the use of any templates.

Supplementary Fig. 12 LSV curves of NFO NPs templated by star-like PAA (η20 = 390 mV; blue), NFO NPs synthesized without the use of template (η20 = 440 mV; green) and star-like PAA-b-PSAN template for the OER in 1.0 M KOH.

Supplementary Fig. 13 Schematic diagram illustrating the principle of electrophoretic deposition of NFO NPs (NFO-12-7K) from their DMF solution onto a nickel foam (NF). Specifically, 5 mg mL-1 of 5 mL PSAN-ligated NFO NPs DMF solution was transferred into a vial, and two pieces of nickel foams (1.0 cm × 5.0 cm) serving as substrates were inserted in parallel with a fixed gap of ~8 mm and then connected to a DC power supply. With increasing time, the NFO NPs in the solution moved toward the nickel foam and were assembled onto the nickel foam. Then, the as-prepared PSAN-ligated NFO NPs on nickel foam (denoted NFO/NF) were dried at 80 oC for 2 h.

Supplementary Fig. 14 SEM images of (a) bare nickel foam (NF), (b) NFO/NF prepared via electrophoretical deposition, and (c) NFO/NF prepared via direct immersion. The insets are the high-magnification SEM images. For direct immersion method (c), the NF substrate is directly immersed into NFO NPs DMF solution (5 mg mL-1) for 30 min, and then dried at 80 oC for 2 h.

Supplementary Fig. 15 UV–vis absorption spectra of the bare NF and NFO/NF electrodes, respectively.

Supplementary Fig. 16 The temperature evolution of 1.0 M KOH electrolyte, bare nickel foam (NF), and NFO/NF over a period of 360 s under exposure to NIR light (808 nm, 2.5 W cm-2) measured every 2 s using a digital IR-thermo camera.

Supplementary Fig. 17 Chronoamperometric responses of NFO/NF at 1.50 V vs. RHE.

Supplementary Fig. 18 (a-b) SEM images of NFO after a 12-h chronoamperometric stability test.

Supplementary Fig. 19 Photograph of the photoelectrochemical cell used for introducing photothermal effect to NFO/NF electrode during the electrocatalytic process. A photoelectrochemical cell with a typical three-electrode system in an O2-saturated 1.0 M KOH solution is irradiated with an 808 nm NIR light to render investigation into the photothermal-assisted electrocatalysis. The circulating water is used to ensure the temperature of electrolyte to be maintained at room temperature.

Supplementary Fig. 20 Tafel plots of NFO/NF electrodes in 1.0 M KOH without (at 25 °C; i.e., without NIR light irradiation) and with (at 45 °C; i.e., with NIR light irradiation) photothermal effect.

Supplementary Fig. 21 (a) Photothermal electrochemical activities of bare nickel foam (NF) toward OER, measured at different electrode temperatures induced by NIR light. Inset shows the decrease of overpotential at j = 20 mA cm-2 with the increase of temperature. (b) Tafel plots of NF in 1.0 M KOH without (at 25 °C; i.e., without NIR light irradiation) and with (at 45 °C; i.e., with NIR light irradiation) photothermal effect.

Supplementary Table 2. Summary on the properties of earth-abundant OER catalysts.

| Catalyst |  | Electrolyte | Overpotential @20 mA cm-2 (mV vs.RHE) | Overpotential @50 mA cm-2 (mV vs.RHE) | Overpotential @100 mA cm-2 (mV vs.RHE) | Tafel Slope (mV dec-1) | Ref. |
| --- | --- | --- | --- | --- | --- | --- | --- |
| NFO/NF without photothermal effect | 1.0 M KOH | 307 | 353 | 370 | 67 | This work |
| NFO/NF with photothermal effect (2.5 W cm-2 NIR light) | 1.0 M KOH | 272 | 297 | 309 | 43 | This work |
| Ni/Fe3O4@N-doped carbon nanorods/GC | 1.0 M KOH | ≈ 320 | ≈ 345 | ≈ 371 | 61 | [1] |
| Carbon-confined NiCo@NiCoO2 core@shell nanoparticles | 1.0 M KOH | 366 | ≈ 400 | ≈ 450 | 83.97 | [2] |
| ZnCo2O4/N-CNT/GC | 0.1 M KOH | ≈ 480 | -- | -- | 70.6 | [3] |
| Ni0.75V0.25-LDH/GC | 1.0 M KOH | ≈ 340 | ≈ 385 | -- | 50 | [4] |
| CoNi(OH)x nanotubes@Cu foil | 1.0 M KOH | ≈ 290 | ≈ 310 | ≈ 340 | 77 | [5] |
| Co2+/NiCoO2/CP | 1.0 M KOH | ≈ 290 | ≈ 320 | ≈ 360 | 56.9 | [6] |
| Ni(OH)2-CeO2@CP | 1.0 M KOH | ≈ 260 | ≈ 320 | ≈ 350 | 81.9 | [7] |
| Ultrathin Co3O4 nanomeshes/GC | 1.0 M KOH | ≈ 330 | ≈ 370 | 407 | 76 | [8] |
| Fe-V/NiO@NF | 1.0 M KOH | ≈ 230 | 271.1 | ≈ 340 | 55 | [9] |
| NiCo2O4@CP | 1.0 M NaOH | ≈ 400 | ≈ 440 | 463 | 74 | [10] |
| Ni/NiFe2O4-CNTs/GC | 1.0 M KOH | ≈ 350 | ≈ 390 | -- | 46.03 | [11] |
| NiFex/NiFe2O4/N-doped graphitic carbon/CP | 1.0 M KOH | ≈ 280 | ≈ 300 | ≈ 340 | 51.4 | [12] |
| V-doped Co3O4/GC | 1.0 M KOH | ≈ 320 | ≈ 350 | ≈ 370 | 53.3 | [13] |
| P-Ni0.5Fe@C/GC | 1.0 M KOH | ≈ 270 | ≈ 290 | ≈ 360 | 65 | [14] |
| Ni/NiO@NF without irradiation | 1.0 M KOH | ≈ 340 | ≈ 370 | ≈ 400 | 70 | [15] |
| Ni/NiO@NF with irradiation (300 W Xenon lamp) | 1.0 M KOH | ≈ 290 | ≈ 330 | ≈345 | 41 |  |
| Co3O4@NF without irradiation | 1.0 M KOH | ≈ 360 | ≈ 430 | ≈ 460 | 111.5 | [16] |
| Co3O4@NF with irradiation (5 W cm-2 NIR laser) | 1.0 M KOH | ≈ 280 | ≈ 325 | ≈ 340 | 74.6 |  |

Notes: GC is glassy carbon electrode; NF is nickel foam substrate; and CP is carbon paper substrate. The symbol @ refers to the catalyst directly grown on the substrate; the symbol / represents the catalyst dropped on the substrate; and the symbol ≈ means the value estimated from the curve in literature.

Supplementary Fig. 22 (a) Arrhenius plots for bare NF electrode, depicting semilogarithmic dependence of current densities j on inverse temperatures T at various overpotentials η. Five η are taken from 300 mV to 500 mV at an interval of 50 mV. (b) Activation energy Ea at the zero overpotential (η = 0) obtained through extrapolation to η = 0.

Supplementary Fig. 23 EIS response for the NFO/NF electrodes without (i.e., without NIR light irradiation, thus the temperature remains at 25 oC) and with (i.e., with NIR light irradiation that raises the temperature to 45 oC) photothermal effect.

Supplementary Fig. 24 EIS response for bare NF electrodes without (i.e., without NIR light irradiation, thus the temperature remains at 25 oC) and with (i.e., with NIR light irradiation that raises the temperature to 35 oC) photothermal effect.

Supplementary Fig. 25 The enlarged Ni oxidation peaks between 1.32 and 1.44 V vs. RHE (from Fig. 4c).

Supplementary Fig. 26 ex-situ XPS spectra for (a) Ni 2p and (b) Fe 2p of NFO/NF before and after photothermal-promoted OER tests.

Supplementary Fig. 27 ex-situ HRTEM images showing the surface regions for (a) as-prepared NFO NPs, and (b) NFO NPs after photothermal-promoted OER process and detached from NF for TEM imaging. The green and red regions represent original NFO and reconstructed oxyhydroxides surface (i.e., (Ni,Fe)oxyhydroxides), respectively.

Supplementary Fig. 28 (a) Raman spectra of bare NFO powder, NFO/NF and NFO/NF electrode under open circuit potential (OCP), respectively. (b) Close-up of the Raman shift between 100 and 400 cm-1 for the NFO/NF electrode under OCP.

Supplementary Fig. 29 Operando Raman spectra of NFO/NF electrode without invoking photothermal effect (i.e., no exposure to 808-nm NIR light for triggering photothermal heating) from open circuit potential (OCP) to 1.50 V vs. RHE in 1.0 M KOH.

Supplementary Fig. 30 Operando Raman spectra of NFO/NF electrode without (i.e., without 808-nm NIR light irradiation during OER) and with photothermal (i.e., with 808-nm NIR light irradiation during OER) effect at 1.50 V vs. RHE in 1.0 M KOH. ∆I1 and ∆I1′ represent the peak intensity difference between 554 cm-1 and 692 cm-1 for the spectra of NFO/NF without and with photothermal effect, respectively. Similarly, ∆I2 and ∆I2′ represent the peak intensity difference between 474 cm-1 and 692 cm-1 for the spectra of NFO/NF without and with photothermal effect, respectively. Obviously, much higher ∆I1′ and ∆I2′ are seen for NFO/NF with photothermal effect than those without photothermal effect (∆I1 and ∆I2).

Supplementary Table 3. Entropies Energy (T = 298.15K) and Zero Point Energy (eV) for gaseous and adsorbed molecules.

|  | ZPE (eV) | TS (eV) | ZPEa (eV) | TSb (eV) |
| --- | --- | --- | --- | --- |
| H2(g) | 0.345 | 0.40 | 0.35 | 0.40 |
| O2(g) | 0.134 | 0.63 | - | 0.63 |
| H2O(l) | 0.570 | 0.67 | 0.57 | 0.67 |
| O* | 0.061 | - | 0.06 | 0 |
| OH* | 0.369 | - | 0.37 | 0 |
| OOH* | 0.477 | - | 0.44 | 0 |

Note: a ZPE values from Ref. [17]. b TS values from Ref. [18].

Supplementary Table 4. Calculation results of ΔZPE ‒ TΔS (eV) for the corresponding steps.

|  | ΔZPE (eV) | TΔS (eV) | ΔZPE ‒ TΔS (eV) |
| --- | --- | --- | --- |
| Step Ⅰ | -0.030 | -0.470 | 0.440 |
| Step Ⅱ | -0.135 | 0.215 | -0.350 |
| Step Ⅲ | -0.015 | -0.470 | 0.455 |
| Step Ⅳ | - | - | - |

Note: Step Ⅰ to Step Ⅳ represent the proposed 4e OER process in Fig. 5c and Supplementary Fig. 32.

Supplementary Fig. 31 The model crystal structure for inverse spinel NiFe2O4, where green ball represents Ni, dark gray ball represents Fe, and red ball represents for O.

Supplementary Fig. 32 The proposed 4e-mechanism and optimized structures of the intermediates of NiFe2O4. The Ni ion (*Ni) in NiFe2O4 is active site.

Supplementary Fig. 33 Schematic illustration of proposed photothermal-assisted electrocatalytic OER mechanism of NFO/NF electrode under 808-nm NIR irradiation with (a) reduced activation energy and (b) promoted surface reconstruction. The silver substrate under NFO NPs represents NF. The orange balls correspond to NFO NPs that are capable of conducting photo-to-thermal conversion and thus in-situ generating heat. (a) In the case of photothermal-promoted OER system, localized heat due to NFO NPs under NIR irradiation would lower the activation energy of water splitting. (b) With photothermal effect, it significantly facilitates the surface reconstruction from inactive Ni2+ to active Ni3+, thus enabling OER reactivity.

Supplementary Note 1: Optimization of the electrocatalyst ink preparation

In contrast to PSAN-ligated NFO-12-7K NPs washed by ethanol yet without subsequent drying for preparing the electrocatalyst ink with carbon black, for PSAN-ligated NFO-12-7K NPs washed by ethanol and then dried, they were redispersed in DMF with sonication for 30 min, then mixed with carbon black to prepare the electrocatalyst ink. More NPs were found to reside outside carbon black substrate (marked with a white dashed circle; Supplementary Fig. 5c). Thus, the contact resistant between NPs electrocatalyst and carbon black is larger, resulting in a decreased OER performance as represented by a larger overpotential η20 of 420 mV at the current density of 20 mA cm-2 (Supplementary Fig. 6) for NFO-12-7K with the subsequent drying process prior to dissolution in DMF and mixing with carbon black (Supplementary Fig. 5c). Contrastively, a η20 of 329 mV (Supplementary Fig. 6) was found for NFO-12-7K without subsequent drying (Supplementary Fig. 5b).

Supplementary Note 2: X-ray photoelectron spectroscopy (XPS) studies

The chemical compositions and intrinsic deficiencies are studied by X-ray photoelectron spectroscopy (XPS). The presence of intrinsic oxygen vacancies can be introduced by altering the synthesis conditions, particularly at low temperature and oxygen-deficient environment.[19] Therefore, in the present study, the oxygen vacancies were introduced to as-prepared PSAN-ligated NFO NPs due to low temperature (250 oC) and oxygen-deficient environment (N2) used for the growth of NFO NPs. Interestingly, the number of oxygen vacancies can be augmented via adjusting the size and shape of nanomaterials, such as nanosheets and nanoparticles.[20, 21] For the O 1s, three peaks can be clearly distinguished (Supplementary Fig. 9a). Specifically, the peak at 530.1 eV is associated with the chemical bonding between oxygen atoms and metal atoms (i.e., Fe-O and Ni-O). The peak with a binding energy of 533.5 eV is due to the surface-adsorbed hydroxyl groups of H2O molecules. The peak at 531.5 eV can be assigned to the defect sites (i.e., oxygen vacancies),[22] further signifying the existence of oxygen vacancies in as-synthesized PSAN-ligated NFO NPs. Notably, the relative peak intensity of oxygen vacancies (531.5 eV) to that of metal-O (530.1 eV) in the O 1s region exhibited a significant increase from NFO-3-8K to NFO-12-7K, indicating that PSAN-ligated NFO NPs with the largest NP size (12 nm) and the shortest surface PSAN chains (MW = 7K) (i.e., NFO-12-7K) possessed more oxygen vacancies.

The XPS peaks in the Ni 2p, Fe 2p and O 1s regions of NFO-3-8K, NFO-7-15K, NFO-12-21K, and NFO-12-7K (Supplementary Fig. 9a-c) showed identical binding energies, revealing the same chemical composition for these samples, in good agreement with the XRD and HRTEM results. In the Ni 2p spectra (Supplementary Fig. 9a), the peaks at 855.7 eV and 857.4 eV can be assigned to Ni2+ and Ni3+, respectively.[1] The peaks at 710.3 and 711.8 eV in Fe 2p region are ascribed to Fe2+ and Fe3+, respectively (Supplementary Fig. 9b).[1] Therefore, the analysis of EIS results (Supplementary Fig. 8) was consistent with the XPS results, that is, NFO-12-7K with the richest oxygen vacancies, achieved the fastest electron transfer (smallest Rct).

Supplementary Note 3: OER performances of the control samples

Importantly, the use of star-like PAA-b-PASN diblock copolymers renders the templated synthesis of NFO NPs of desired sizes without aggregation. By contrast, NFO NPs templated by star-like PAA homopolymers and NFO NPs synthesized without the use of any templates show severe aggregations (Supplementary Fig. 11a and 11b, respectively) and thus poor dispersion in solvent. Accordingly, it is not surprising that these two types of NFO NPs present poor OER activity with overpotential (η20) of 390 mV and 440 mV at a current density of 20 mA cm-2, respectively (Supplementary Fig. 12) because of the aggregation of NPs. Moreover, the LSV curve of star-like PAA-b-PSAN templates only is also shown in Supplementary Fig. 12, signifying negligible effects of polymers (either PSAN or PAA) on OER performance.

Supplementary Note 4: Optimization of the NFO/NF electrode preparation

Significantly, compared with electrophoretical deposition (Supplementary Fig.14b), there are still partial NF surfaces exposed after NFO NPs deposition by direct immersion method, as clearly evident in the inset (Supplementary Fig. 14c). The electrophoretically-deposited NFO NPs show a uniform NP layer that fully covers the NF surface (inset; Supplementary Fig. 14b).

Supplementary Note 5: Optimized Structures of (Ni,Fe)OOH and NiFe2O4

(Ni,Fe)OOH. cif:

_cell_length_a                    9.7788

_cell_length_b                    5.6303

_cell_length_c                    7.3815

_cell_angle_alpha                 101.2150

_cell_angle_beta                  82.8245

_cell_angle_gamma                 90.4536

H1     O17     0.990   .     S

H2     O17     0.985   .     S

H3     O18     0.984   .     S

H4     O18     0.981   .     S

H5     O19     0.991   .     S

H6     O19     0.985   .     S

H7     O20     0.980   .     S

H8     O20     0.982   .     S

Ni1    O15     2.039   .     S

Ni1    O6      1.916   .     S

Ni1    O13     1.882   .     S

Ni1    O11     1.879   1_655 S

Ni1    O8      2.044   1_655 S

Ni1    O14     1.913   1_655 S

Ni2    O6      1.881   .     S

Ni2    O9      1.898   .     S

Ni2    O11     1.887   1_655 S

Ni2    O14     1.881   1_665 S

Ni2    O13     1.888   1_565 S

Ni2    O4      1.895   1_665 S

Ni3    O2      1.896   .     S

Ni3    O3      1.870   .     S

Ni3    O10     1.884   .     S

Ni3    O16     1.868   1_565 S

Ni3    O12     1.879   1_565 S

Ni3    O5      1.891   1_565 S

Ni4    O10     1.891   .     S

Ni4    O6      1.871   .     S

Ni4    O1      1.879   .     S

Ni4    O9      1.893   .     S

Ni4    O15     1.865   .     S

Ni4    O5      1.903   1_565 S

Ni5    O8      1.861   .     S

Ni5    O11     1.891   .     S

Ni5    O2      1.898   .     S

Ni5    O3      1.850   .     S

Ni5    O7      1.870   .     S

Ni5    O4      1.895   1_565 S

Ni6    O7      1.927   .     S

Ni6    O12     1.864   .     S

Ni6    O10     1.872   .     S

Ni6    O3      2.035   .     S

Ni6    O1      1.930   .     S

Ni6    O16     2.044   .     S

Ni7    O4      1.900   .     S

Ni7    O8      1.858   .     S

Ni7    O14     1.870   .     S

Ni7    O7      1.877   .     S

Ni7    O12     1.890   .     S

Ni7    O2      1.899   1_545 S

Ni8    O1      1.871   .     S

Ni8    O5      1.897   .     S

Ni8    O16     1.858   .     S

Ni8    O13     1.898   .     S

Ni8    O15     1.869   .     S

Ni8    O9      1.890   1_545 S

O2     Ni7     1.899   1_565 S

O4     Ni5     1.895   1_545 S

O4     Ni2     1.895   1_445 S

O5     Ni4     1.903   1_545 S

O5     Ni3     1.891   1_545 S

O8     Ni1     2.044   1_455 S

O9     Ni8     1.890   1_565 S

O11    Ni2     1.887   1_455 S

O11    Ni1     1.879   1_455 S

O12    Ni3     1.879   1_545 S

O13    Ni2     1.888   1_545 S

O14    Ni1     1.913   1_455 S

O14    Ni2     1.881   1_445 S

O16    Ni3     1.868   1_545 S

NiFe2O4. cif:

_cell_length_a                    8.3965

_cell_length_b                    8.3965

_cell_length_c                    8.3965

_cell_angle_alpha                 90.0000

_cell_angle_beta                  90.0000

_cell_angle_gamma                 90.0000

Fe1    O25     1.889   .     S

Fe1    O33     1.889   .     S

Fe1    O31     1.889   .     S

Fe1    O36     1.889   .     S

Fe2    O29     1.889   .     S

Fe2    O56     1.889   .     S

Fe2    O27     1.889   .     S

Fe2    O55     1.889   .     S

Fe3    O32     1.889   .     S

Fe3    O26     1.889   .     S

Fe3    O35     1.889   .     S

Fe3    O53     1.889   .     S

Fe4    O34     1.889   .     S

Fe4    O30     1.889   .     S

Fe4    O54     1.889   .     S

Fe4    O28     1.889   .     S

Fe5    O37     1.889   .     S

Fe5    O50     1.889   .     S

Fe5    O40     1.889   1_455 S

Fe5    O52     1.889   1_455 S

Fe6    O39     1.889   1_444 S

Fe6    O47     1.889   1_455 S

Fe6    O38     1.889   1_554 S

Fe6    O45     1.889   1_545 S

Fe7    O43     1.889   .     S

Fe7    O49     1.889   1_554 S

Fe7    O51     1.889   .     S

Fe7    O42     1.889   1_554 S

Fe8    O46     1.889   .     S

Fe8    O41     1.889   1_545 S

Fe8    O44     1.889   1_545 S

Fe8    O48     1.889   .     S

Fe9    O35     2.059   .     S

Fe9    O55     2.059   .     S

Fe9    O30     2.059   .     S

Fe9    O44     2.059   .     S

Fe9    O52     2.059   .     S

Fe9    O49     2.059   .     S

Ni10   O36     2.059   .     S

Ni10   O54     2.059   1_545 S

Ni10   O29     2.059   1_554 S

Ni10   O43     2.059   .     S

Ni10   O47     2.059   .     S

Ni10   O48     2.059   .     S

Ni11   O34     2.059   1_455 S

Ni11   O33     2.059   .     S

Ni11   O53     2.059   1_554 S

Ni11   O45     2.059   .     S

Ni11   O51     2.059   .     S

Ni11   O37     2.059   .     S

Ni12   O56     2.059   1_455 S

Ni12   O32     2.059   1_545 S

Ni12   O31     2.059   .     S

Ni12   O50     2.059   .     S

Ni12   O46     2.059   .     S

Ni12   O38     2.059   .     S

Ni13   O54     2.059   .     S

Ni13   O36     2.059   1_565 S

Ni13   O26     2.059   1_554 S

Ni13   O51     2.059   .     S

Ni13   O45     2.059   .     S

Ni13   O41     2.059   .     S

Ni14   O55     2.059   .     S

Ni14   O35     2.059   .     S

Ni14   O25     2.059   .     S

Ni14   O46     2.059   .     S

Ni14   O50     2.059   .     S

Ni14   O42     2.059   .     S

Fe15   O31     2.059   1_655 S

Fe15   O28     2.059   1_545 S

Fe15   O56     2.059   .     S

Fe15   O40     2.059   .     S

Fe15   O48     2.059   .     S

Fe15   O47     2.059   .     S

Fe16   O53     2.059   1_655 S

Fe16   O27     2.059   .     S

Fe16   O34     2.059   1_556 S

Fe16   O39     2.059   .     S

Fe16   O49     2.059   .     S

Fe16   O52     2.059   .     S

Fe17   O27     2.059   1_455 S

Fe17   O53     2.059   .     S

Fe17   O33     2.059   1_556 S

Fe17   O38     2.059   .     S

Fe17   O42     2.059   .     S

Fe17   O50     2.059   .     S

Ni18   O25     2.059   .     S

Ni18   O30     2.059   .     S

Ni18   O55     2.059   .     S

Ni18   O48     2.059   .     S

Ni18   O40     2.059   .     S

Ni18   O43     2.059   .     S

Fe19   O37     2.059   .     S

Fe19   O41     2.059   .     S

Fe19   O51     2.059   .     S

Fe19   O25     2.059   .     S

Fe19   O30     2.059   .     S

Fe19   O35     2.059   .     S

Fe20   O43     2.059   .     S

Fe20   O47     2.059   .     S

Fe20   O40     2.059   .     S

Fe20   O34     2.059   .     S

Fe20   O33     2.059   1_655 S

Fe20   O27     2.059   1_554 S

Ni21   O44     2.059   .     S

Ni21   O52     2.059   .     S

Ni21   O39     2.059   .     S

Ni21   O56     2.059   1_565 S

Ni21   O32     2.059   1_655 S

Ni21   O28     2.059   .     S

Fe22   O38     2.059   .     S

Fe22   O42     2.059   .     S

Fe22   O46     2.059   .     S

Fe22   O26     2.059   1_545 S

Fe22   O29     2.059   .     S

Fe22   O36     2.059   1_556 S

Fe23   O41     2.059   .     S

Fe23   O37     2.059   .     S

Fe23   O45     2.059   .     S

Fe23   O31     2.059   1_565 S

Fe23   O28     2.059   1_455 S

Fe23   O32     2.059   .     S

Ni24   O39     2.059   .     S

Ni24   O49     2.059   .     S

Ni24   O44     2.059   .     S

Ni24   O29     2.059   1_565 S

Ni24   O26     2.059   .     S

Ni24   O54     2.059   1_556 S

O26    Fe22    2.059   1_565 S

O26    Ni13    2.059   1_556 S

O27    Fe20    2.059   1_556 S

O27    Fe17    2.059   1_655 S

O28    Fe15    2.059   1_565 S

O28    Fe23    2.059   1_655 S

O29    Ni24    2.059   1_545 S

O29    Ni10    2.059   1_556 S

O31    Fe15    2.059   1_455 S

O31    Fe23    2.059   1_545 S

O32    Ni12    2.059   1_565 S

O32    Ni21    2.059   1_455 S

O33    Fe17    2.059   1_554 S

O33    Fe20    2.059   1_455 S

O34    Fe16    2.059   1_554 S

O34    Ni11    2.059   1_655 S

O36    Fe22    2.059   1_554 S

O36    Ni13    2.059   1_545 S

O38    Fe6     1.889   1_556 S

O39    Fe6     1.889   1_666 S

O40    Fe5     1.889   1_655 S

O41    Fe8     1.889   1_565 S

O42    Fe7     1.889   1_556 S

O44    Fe8     1.889   1_565 S

O45    Fe6     1.889   1_565 S

O47    Fe6     1.889   1_655 S

O49    Fe7     1.889   1_556 S

O52    Fe5     1.889   1_655 S

O53    Fe16    2.059   1_455 S

O53    Ni11    2.059   1_556 S

O54    Ni24    2.059   1_554 S

O54    Ni10    2.059   1_565 S

O56    Ni12    2.059   1_655 S

O56    Ni21    2.059   1_545 S

Supplementary Experimental Section

Materials. β-cyclodextrin (β-CD, Sigma-Aldrich) was dried at 80 °C under vacuum overnight prior to use. 2-Bromoisobutyryl bromide (98%), N,N,Nʹ,Nʹʹ,Nʹʹ-pentamethyldiethylene triamine (PMDETA, 99%), anhydrous 1-methyl-2-pyrrolidinone (NMP, 99.5%), triﬂuoroacetic acid (TFA, 99.9%), nickel acetate tetrahydrate (Ni(CH3COO)2·4H2O, Ni(OAc)2, 98.0%), iron(III) acetylacetonate (Fe(C5H7O2)3, Fe(AcAc)3, ≥ 99.0%), diphenyl ether (DPE, 99%), and butyl acrylate (BA, ≥99.0%) were purchased from Sigma-Aldrich, and used as received. CuBr (98%, Sigma-Aldrich) was stirred in acetic acid overnight, washed with ethanol and diethyl ether, respectively, and dried under vacuum. tBA (Sigma-Aldrich, 98.0%), acrylonitrile (AN, Aldrich, 99.0%), methyl ethyl ketone (MEK, Fisher Scientific, 99.9%) and N, N-dimethylformamide (DMF, Fisher Scientific, 99.9%) were dried over calcium hydride (CaH2) and distilled under reduced pressure prior to use. Styrene (St, Sigma-Aldrich, ≥99%) was washed with 10% NaOH aqueous solution and water successively, dried over anhydrous MgSO4 and CaH2 sequentially, and distilled under reduced pressure. All other reagents were purified by common purification procedures.

Synthesis of Multi-arm Star-Like Poly(tert-Butyl Acrylate) (PtBA) Terminated with Bromine End Groups (i.e., Star-like PtBA-Br). Heptakis[2,3,6-tri-O-(2-bromo-2-methylpropionyl)]-β-cyclodextrin (denoted 21Br-β-CD) was prepared according to previous work.[23, 24] Star-like PtBA was synthesized by atom transfer radical polymerization (ATRP) of tBA monomers (i.e., the first ATRP) in MEK using 21Br-β-CD as the macroinitiator. The polymerization of tBA monomers was carried out in an ampoule. In a typical process, an ampoule was loaded with CuBr, PMDETA, 21Br-β-CD, tBA, and methyl ethyl ketone (as solvent) (the molar ratio of tBA: Br of 21Br-β-CD macroinitiator: copper bromide: PMDETA = 800: 1: 1: 2; the volume ratio of monomer: solvent = 1:1), and was then degassed by three freeze-pump-thaw cycles in liquid nitrogen. The ampoule was sealed and dipped in an oil bath at 60 °C. After a certain desired polymerization time, the reaction was stopped by dipping the ampoule in liquid N2. The mixture was then diluted with THF, passed through a column of neutral alumina to remove the catalyst, and subsequently purified by fractional precipitation with methanol/water (v/v = 1/1) as the precipitator. The product was dried at 40 °C under vacuum for 2 d.

Synthesis of Multi-arm Star-Like Poly(tert-Butyl Acrylate)-block-Poly(Styrene-co-Acrylonitrile) (PtBA-b-PSAN) Diblock Copolymer. Star-like PtBA-b-PSAN was synthesized via ATRP of styrene-co-acrylonitrile copolymer (i.e., the second ATRP) using star-like PtBA as macroinitiator. In a typical process, star-like PtBA (1.0 g), CuBr (20.0 mg), PMDETA (50.0 µL), St (24.0 mL), and AN (6.0 mL) were mixed in an argon purged ampoule and degassed by three freeze-pump-thaw cycles. The polymerization was performed at 90 °C and quenched by dipping the ampoule in liquid N2 after a certain desired time. The crude product was diluted with THF and passed through a neutral alumina column to remove the catalyst and purified by fractional precipitation with methanol/water (v/v = 1/1) as the precipitator. The product, multi-arm, star-like PtBA-b-PSAN was dried at 40 °C under vacuum for 2 d.

Synthesis of Multi-arm Star-Like Poly(Acrylic Acid)-block-Poly(Styrene-co-Acrylonitrile) (PAA-b-PSAN) Diblock Copolymers. Star-like PAA-b-PSAN diblock copolymer via the hydrolysis of the tert-butyl ester groups of PtBA blocks in star-like PtBA-b-PSAN. Brieﬂy, star-like PtBA-b-PSAN was dissolved in CH2Cl2, followed by the addition of a 10-fold molar excess of TFA with respect to the amount of t-butyl groups in PtBA blocks. The reaction mixture was stirred at room temperature for 24 h. After hydrolysis, the resulting star-like PAA-b-PSAN diblock copolymer was gradually precipitated in CH2Cl2. The final product was washed with CH2Cl2, and thoroughly dried under vacuum at 40 °C.

Synthesis of PSAN-ligated NiFe2O4 Nanoparticles (PSAN-ligated NFO NPs). By capitalizing on star-like PAA-b-PSAN diblock copolymers as nanoreactors, PSAN-ligated NFO NPs were synthesized. In a typical procedure, star-like PAA-b-PSAN (10 mg) was dissolved in 0.2 mL DMF at room temperature, followed by the addition of 9 mL DPE. An appropriate amount of precursors (Ni(OAc)2 and Fe(AcAc)3) were added, where the molar ratio of acrylic acid (AA) units in PAA blocks to precursors was set at 1:10 in order to maximize the loading of precursors into the compartment containing PAA blocks. The mixture was stirred under N2 at 80 oC for 12 h to ensure that all precursors were well dissolved in DMF and the PAA blocks-containing compartment was fully loaded by precursors. Subsequently, 1 mL BA was added into the reaction system to swell the inner PAA chains as it is a good solvent for PAA yet poor solvent for PSAN. The reaction was then carried out at 250 oC. After reaction for 4 h, the resulting PSAN-ligated NFO NPs were collected by centrifugation and washed with ethanol several times to remove unreacted precursors and mixed solvent. For comparison, NFO NPs templated by star-like PAA homopolymers as well as NFO NPs without the use of any templates were also synthesized by a similar procedure and used as control samples.

Electrochemical Measurements. The OER activities of catalysts were measured in a three-electrode glass cell filled in 1.0 M KOH electrolyte on a Zennium PP211 electrochemical workstation using an Ag/AgCl electrode as the reference electrode, a carbon rod as the counter electrode, and the glassy carbon (GC, area, 0.19625 cm2) loaded with catalysts as the working electrode. The catalyst ink was prepared by dispersing 1 mL of the 5 mg mL-1 PSAN-ligated NFO NPs in DMF, 2 mg of carbon black and 80 µL Nafion solution (5 wt%) by sonication for 40 min to form a homogenous ink. Next, 20 µL of the ink was loaded onto GC working electrode. The ink was dried slowly in air until a uniform catalyst covered on the working electrode surface was formed.

The polarization curves were recorded at a scan rate of 10 mV s-1. All of the potentials in the LSV polarization curves were 95% iR-corrected with respect to the ohmic resistance of the solution, unless otherwise specified. The electrochemical impedance spectroscopy (EIS) tests were also performed at overpotential with a frequency loop from 100 mHz to 100 kHz by applying a sine wave with an amplitude of 5 mV. The measured impedance data were fitted to a simplified Randles circuit to extract the series and charge transfer resistances. The electrochemical active surface area (ECSA) of the electrocatalysts were estimated from the double-layer capacitance (Cdl), and cyclic voltammetry (CV) method was then employed to evaluate Cdl. Accordingly, a series of CV measurements were performed at various scan rates (20 mV s-1, 30 mV s-1, 40 mV s-1, 50 mV s-1, and 60 mV s-1) from 1.07 to 1.17 V vs. RHE range. The capacitance of each catalyst was estimated by Cdl = dq / dE = dj / dv. All the measured potentials were referred to RHE with the following equation:

E(RHE) = E(Ag/AgCl) + 0.197 V + 0.0592 × pH

Supplementary references

1.	Liu, G., et al. Encapsulation of Ni/Fe3O4 heterostructures inside onion-like N-doped carbon nanorods enables synergistic electrocatalysis for water oxidation. Nanoscale 10, 3997-4003 (2018).

2.	Xu, H., et al. Porous microrod arrays constructed by carbon‐confined NiCo@NiCoO2 core@shell nanoparticles as efficient electrocatalysts for oxygen evolution. Adv. Mater. 30, 1705442 (2018).

3.	Liu, Z. Q., et al. ZnCo2O4 quantum dots anchored on nitrogen‐doped carbon nanotubes as reversible oxygen reduction/evolution electrocatalysts. Adv. Mater. 28, 3777-3784 (2016).

4.	Fan, K., et al. Nickel–vanadium monolayer double hydroxide for efficient electrochemical water oxidation. Nat. Commun. 7, 1-9 (2016).

5.	Li, S., et al. Co–Ni‐based nanotubes/nanosheets as efficient water splitting electrocatalysts. Adv. Energy Mater. 6, 1501661 (2016).

6.	Jin, Y. Z., et al. Tuning spin state of rock‐salt‐based oxides by manipulation of crystallinity for efficient oxygen electrocatalysis. Adv. Energy Mater. 8, 1703469 (2018).

7.	Zhao, D., et al. Enhancing oxygen evolution electrocatalysis via the intimate hydroxide–oxide interface. ACS Nano 12, 6245-6251 (2018).

8.	Li, Y., et al. Ultrathin Co3O4 nanomeshes for the oxygen evolution reaction. ACS Catal. 8, 1913-1920 (2018).

9.	Zhu, Y. X., et al. An Fe–V@ NiO heterostructure electrocatalyst towards the oxygen evolution reaction. Nanoscale 12, 3803-3811 (2020).

10.	Li, J., et al. Boosted oxygen evolution reactivity by igniting double exchange interaction in spinel oxides. J. Am. Chem. Soc. 142, 50-54 (2019).

11.	Yu, X., et al. Hierarchical coupling effect in hollow Ni/NiFe2O4-CNTs microsphere via spray-drying for enhanced oxygen evolution electrocatalysis. Nano Res. 13, 437-446 (2020).

12.	Zhao, J., et al. Metal–organic-framework-derived porous 3D heterogeneous NiFex/NiFe2O4@NC nanoflowers as highly stable and efficient electrocatalysts for the oxygen-evolution reaction. J. Mater. Chem. A 7, 21338-21348 (2019).

13.	Wei, R., et al. Engineering surface structure of spinel oxides via high-valent vanadium doping for remarkably enhanced electrocatalytic oxygen evolution reaction. ACS Appl. Mater. Inter. 11, 33012-33021 (2019).

14.	Fan, A., et al. Phosphorus-doped FeNi alloys/NiFe2O4 imbedded in carbon network hollow bipyramid as efficient electrocatalysts for oxygen evolution reaction. ACS Sustain. Chem. Eng. 7, 2285-2295 (2018).

15.	Han, X., et al. Photogenerated carriers boost water splitting activity over transition-metal/semiconducting metal oxide bifunctional electrocatalysts. ACS Catal. 7, 6464-6470 (2017).

16.	Jin, B., et al. Promoting oxygen evolution reaction of Co‐based catalysts (Co3O4, CoS, CoP, and CoN) through photothermal effect. Small 15, 1903847 (2019).

17.	Bajdich, M., et al. Theoretical investigation of the activity of cobalt oxides for the electrochemical oxidation of water. J. Am. Chem. Soc. 135, 13521-13530 (2013).

18.	Liao, P., et al. Water oxidation on pure and doped hematite (0001) surfaces: Prediction of Co and Ni as effective dopants for electrocatalysis. J. Am. Chem. Soc. 134, 13296-13309 (2012).

19.	Zhao, Q., et al. Spinels: controlled preparation, oxygen reduction/evolution reaction application, and beyond. Chem. Rev. 117, 10121-10211 (2017).

20.	Cheng, F., et al. Enhancing electrocatalytic oxygen reduction on MnO2 with vacancies. Angew. Chem. Int. Edit. 125, 2534-2537 (2013).

21.	Yang, H., et al. Lateral-size-mediated efficient oxygen evolution reaction: insights into the atomically thin quantum dot structure of NiFe2O4. ACS Catal. 2017. 7(8): p. 5557-5567 (2017).

22.	Trotochaud, L., et al. Solution-cast metal oxide thin film electrocatalysts for oxygen evolution. J. Am. Chem. Soc. 134, 17253-17261 (2012).

23.	Cui, X., et al., Tailoring carrier dynamics in perovskite solar cells via precise dimension and architecture control and interfacial positioning of plasmonic nanoparticles. Energ. Environ. Sci. 13, 1743-1752 (2020).

24.	Pang, X., et al., A general and robust strategy for the synthesis of nearly monodisperse colloidal nanocrystals. Nat. Nanotechnol. 8, 426-431 (2013).

Table of Content