Table1– Experimental parameters with their levels.

| Factors |  | Fibers (%) | Lengths (mm) | NaOH(%) | Time(h) |
| --- | --- | --- | --- | --- | --- |
| Codes |  | A | B | C | D |
| Levels | Lower (-1) | 1 | 5 | 1 | 2 |
|  | Medium (0) | 3 | 10 | 3 | 8 |
|  | Higher (+1) | 5 | 15 | 5 | 14 |

Table 2- L29 experimental plan established using RSM method

| Run | Fiber fraction (%) | Fiber length (mm) | NaOH (%) | Immersion time (h) |
| --- | --- | --- | --- | --- |
| 1 | 3 | 5 | 3 | 2 |
| 2 | 3 | 10 | 3 | 8 |
| 3 | 5 | 10 | 3 | 2 |
| 4 | 1 | 5 | 3 | 8 |
| 5 | 5 | 10 | 1 | 8 |
| 6 | 1 | 10 | 3 | 2 |
| 7 | 5 | 10 | 3 | 14 |
| 8 | 3 | 10 | 3 | 8 |
| 9 | 3 | 15 | 1 | 8 |
| 10 | 5 | 10 | 5 | 8 |
| 11 | 5 | 15 | 3 | 8 |
| 12 | 1 | 10 | 1 | 8 |
| 13 | 3 | 10 | 3 | 8 |
| 14 | 3 | 10 | 3 | 8 |
| 15 | 3 | 10 | 3 | 8 |
| 16 | 3 | 15 | 5 | 8 |
| 17 | 3 | 10 | 5 | 2 |
| 18 | 3 | 5 | 3 | 14 |
| 19 | 3 | 5 | 5 | 8 |
| 20 | 3 | 15 | 3 | 2 |
| 21 | 3 | 10 | 1 | 14 |
| 22 | 3 | 5 | 1 | 8 |
| 23 | 1 | 10 | 5 | 8 |
| 24 | 1 | 15 | 3 | 8 |
| 25 | 3 | 15 | 3 | 14 |
| 26 | 1 | 10 | 3 | 14 |
| 27 | 3 | 10 | 5 | 14 |
| 28 | 5 | 5 | 3 | 8 |
| 29 | 3 | 10 | 1 | 2 |

Table 3 - Experimental design and response variables for bending and compression experiments utilizing RSM Box-Behnken L29

| Bending test |  |  |  |  | Compression test |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Run | Fiber fraction (%) | Fiber length (mm) | NaOH concentration (%) | Immersion time (h) | Flexural strength σf (MPa) |  |  | Flexural modulus Ef (GPa) |  | Compressive strength σc (MPa) |  | Compressive modulus Ec (GPa) |  |
|  |  |  |  |  |  |  | STD |  | STD |  | STD |  | STD |
| Reference | 0 | 0 | 0 | 0 | 4.00 | ±0.33 |  | 0.930 | ±0.06 | 21.01 | ±1.61 | 26.76 | ±5.09 |
| 1 | 3 | 5 | 3 | 2 | 3.47 | ±0.30 |  | 0.582 | ±0.25 | 23.87 | ±1.03 | 2.75 | ±0.15 |
| 2 | 3 | 10 | 3 | 8 | 2.92 | ±0.31 |  | 0.591 | ±0.19 | 14.92 | ±1.16 | 29.86 | ±4.77 |
| 3 | 5 | 10 | 3 | 2 | 1.97 | ±0.12 |  | 0.162 | ±0.02 | 29.52 | ±4.19 | 8.39 | ±5.41 |
| 4 | 1 | 5 | 3 | 8 | 4.98 | ±0.27 |  | 1.012 | ±0.24 | 33.75 | ±0.54 | 23.37 | ±6.92 |
| 5 | 5 | 10 | 1 | 8 | 2.13 | ±0.26 |  | 0.159 | ±0.03 | 24.33 | ±4.53 | 7.17 | ±4.24 |
| 6 | 1 | 10 | 3 | 2 | 5.00 | ±0.30 |  | 0.931 | ±0.03 | 27.89 | ±4.33 | 23.82 | ±5.66 |
| 7 | 5 | 10 | 3 | 14 | 2.11 | ±0.25 |  | 0.122 | ±0.09 | 16.67 | ±4.54 | 15.86 | ±7.24 |
| 8 | 3 | 10 | 3 | 8 | 2.92 | ±0.31 |  | 0.591 | ±0.19 | 14.92 | ±2.42 | 29.83 | ±9.55 |
| 9 | 3 | 15 | 1 | 8 | 2.80 | ±0.77 |  | 0.309 | ±0.02 | 24.26 | ±1.62 | 3.85 | ±0.54 |
| 10 | 5 | 10 | 5 | 8 | 2.29 | ±0.33 |  | 0.175 | ±0.01 | 22.22 | ±6.40 | 12.64 | ±5.31 |
| 11 | 5 | 15 | 3 | 8 | 2.10 | ±0.15 |  | 0.143 | ±0.02 | 28.22 | ±3.99 | 3.08 | ±0.17 |
| 12 | 1 | 10 | 1 | 8 | 5.39 | ±0.53 |  | 1.130 | ±0.22 | 34.94 | ±8.17 | 48.91 | ±10.35 |
| 13 | 3 | 10 | 3 | 8 | 2.92 | ±0.31 |  | 0.591 | ±0.19 | 14.92 | ±2.42 | 29.83 | ±9.55 |
| 14 | 3 | 10 | 3 | 8 | 2.92 | ±0.31 |  | 0.591 | ±0.19 | 14.92 | ±2.42 | 29.83 | ±9.55 |
| 15 | 3 | 10 | 3 | 8 | 2.92 | ±2.92 |  | 0.317 | ±0.59 | 14.92 | ±2.42 | 29.83 | ±9.55 |
| 16 | 3 | 15 | 5 | 8 | 3.81 | ±0.80 |  | 0.416 | ±0.01 | 18.04 | ±5.32 | 16.02 | ±6.89 |
| 17 | 3 | 10 | 5 | 2 | 2.52 | ±1.53 |  | 0.33 | ±0.07 | 19.97 | ±3.01 | 18.33 | ±8.50 |
| 18 | 3 | 5 | 3 | 14 | 4.00 | ±0.06 |  | 0.449 | ±0.21 | 24.34 | ±1.67 | 22.75 | ±9.08 |
| 19 | 3 | 5 | 5 | 8 | 2.54 | ±0.23 |  | 0.397 | ±0.14 | 22.40 | ±2.07 | 6.69 | ±1.90 |
| 20 | 3 | 15 | 3 | 2 | 3.25 | ±1.63 |  | 0.467 | ±0.30 | 28.58 | ±2.53 | 5.36 | ±0.69 |
| 21 | 3 | 10 | 1 | 14 | 3.92 | ±0.34 |  | 0.476 | ±0.13 | 20.21 | ±2.66 | 24.15 | ±9.17 |
| 22 | 3 | 5 | 1 | 8 | 5.28 | ±0.13 |  | 0.921 | ±0.22 | 27.68 | ±2.55 | 4.84 | ±0.64 |
| 23 | 1 | 10 | 5 | 8 | 4.27 | ±0.14 |  | 0.818 | ±0.21 | 22.73 | ±3.01 | 29.47 | ±3.24 |
| 24 | 1 | 15 | 3 | 8 | 4.50 | ±0.33 |  | 0.719 | ±0.22 | 23.57 | ±3.54 | 23.31 | ±4.86 |
| 25 | 3 | 15 | 3 | 14 | 3.43 | ±0.24 |  | 0.457 | ±0.06 | 18.06 | ±5.89 | 17.60 | ±7.12 |
| 26 | 1 | 10 | 3 | 14 | 4.34 | ±0.32 |  | 1.025 | ±0.12 | 31.17 | ±1.98 | 29.09 | ±2.34 |
| 27 | 3 | 10 | 5 | 14 | 2.97 | ±1.39 |  | 0.498 | ±0.05 | 20.08 | ±4.01 | 23.32 | ±7.00 |
| 28 | 5 | 5 | 3 | 8 | 2.10 | ±0.11 |  | 0.141 | ±0.09 | 22.40 | ±1.09 | 2.52 | ±0.11 |
| 29 | 3 | 10 | 1 | 2 | 4.18 | ±0.33 |  | 0.766 | ±0.01 | 29.60 | ±1.62 | 6.17 | ±1.81 |

Table 4 -Bending and compression responses for the various statistical models used

| Test Type | Source | Std. Dev. | R2 | Adjusted R2 | Predicted R2 | PRESS | Remarks |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Flexural strength σf | Linear | 0.5138 | 0.7886 | 0.7534 | 0.6859 | 9.41 |  |
|  | 2FI | 0.3373 | 0.9317 | 0.8937 | 0.8511 | 4.46 |  |
|  | Quadratic | 0.2170 | 0.9780 | 0.9560 | 0.8733 | 3.80 | Suggested |
|  | Cubic | 0.0999 | 0.9980 | 0.9907 | 0.7123 | 8.62 | Aliased |
| Flexural modulus Ef | Linear | 0.1105 | 0.8753 | 0.8545 | 0.8077 | 0.4522 |  |
|  | 2FI | 0.0685 | 0.9641 | 0.9442 | 0.8951 | 0.2467 |  |
|  | Quadratic | 0.0585 | 0.9797 | 0.9593 | 0.8828 | 0.2756 | Suggested |
|  | Cubic | 0.0212 | 0.9989 | 0.9947 | 0.8356 | 0.3865 | Aliased |
| Compressive strength σc | Linear | 5.38 | 0.2793 | 0.1591 | 0.0411 | 923.81 |  |
|  | 2FI | 5.20 | 0.4947 | 0.2139 | 0.0973 | 869.64 |  |
|  | Quadratic | 0.9553 | 0.9867 | 0.9735 | 0.9236 | 73.60 | Suggested |
|  | Cubic | 0.1611 | 0.9998 | 0.9992 | 0.9767 | 22.44 | Aliased |
| Compressive modulus Ec | Linear | 8.50 | 0.5478 | 0.4724 | 0.3782 | 2382.03 |  |
|  | 2FI | 9.32 | 0.5917 | 0.3648 | 0.0393 | 3680.71 |  |
|  | Quadratic | 1.95 | 0.9861 | 0.9722 | 0.9200 | 306.36 | Suggested |
|  | Cubic | 0.4250 | 0.9997 | 0.9987 | 0.9593 | 156.06 | Aliased |

Std. Dev.: Standard Deviation; PRESS: Predicted sum of squares.

Table 5 - ANOVA outcomes for the quadratic response surface model of the bending tests

| Test Type | Flexural strength |  |  |  |  |  | Flexural modulus |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Source | Sum of Squares | Df | Mean Square | F-value | P-value | Remark | Sum of Squares | df | Mean Square | F-value | P-value | Remark |
| Model | 29.31 | 14 | 2.09 | 44.47 | < 0.0001 | Significant | 2.30 | 14 | 0.1645 | 48.15 | < 0.0001 | Significant |
| A- Fiber fraction | 20.77 | 1 | 20.77 | 441.12 | < 0.0001 | Significant | 1.87 | 1 | 1.87 | 546.23 | < 0.0001 | Significant |
| B- Fiber length | 0.5154 | 1 | 0.5154 | 10.95 | 0.0052 | Significant | 0.0818 | 1 | 0.0818 | 23.95 | 0.0002 | Significant |
| C-NaOH concentration | 2.34 | 1 | 2.34 | 49.70 | < 0.0001 | Significant | 0.1058 | 1 | 0.1058 | 30.97 | < 0.0001 | Significant |
| D-Immersion time | 0.0122 | 1 | 0.0122 | 0.2583 | 0.6192 | No-significant | 0.0037 | 1 | 0.0037 | 1.09 | 0.3151 | No-significant |
| AB | 0.0557 | 1 | 0.0557 | 1.18 | 0.2951 | No-significant | 0.0218 | 1 | 0.0218 | 6.37 | 0.0244 | Significant |
| AC | 0.4083 | 1 | 0.4083 | 8.67 | 0.0106 | Significant | 0.0269 | 1 | 0.0269 | 7.87 | 0.0140 | Significant |
| AD | 0.1600 | 1 | 0.1600 | 3.40 | 0.0865 | No-significant | 0.0045 | 1 | 0.0045 | 1.31 | 0.2710 | No-significant |
| BC | 3.51 | 1 | 3.51 | 74.52 | < 0.0001 | Significant | 0.0995 | 1 | 0.0995 | 29.13 | < 0.0001 | Significant |
| BD | 0.0294 | 1 | 0.0294 | 0.6248 | 0.4425 | No-significant | 0.0038 | 1 | 0.0038 | 1.11 | 0.3106 | No-significant |
| CD | 0.1250 | 1 | 0.1250 | 2.65 | 0.1255 | No-significant | 0.0524 | 1 | 0.0524 | 15.34 | 0.0015 | Significant |
| A² | 0.2977 | 1 | 0.2977 | 6.32 | 0.0247 | Significant | 0.0001 | 1 | 0.0001 | 0.0244 | 0.8782 | No-significant |
| B² | 0.7906 | 1 | 0.7906 | 16.79 | 0.0011 | Significant | 0.0310 | 1 | 0.0310 | 9.06 | 0.0094 | Significant |
| C² | 0.7048 | 1 | 0.7048 | 14.97 | 0.0017 | Significant | 0.0030 | 1 | 0.0030 | 0.8638 | 0.3684 | No-significant |
| D² | 0.2847 | 1 | 0.2847 | 6.05 | 0.0276 | Significant | 0.0092 | 1 | 0.0092 | 2.68 | 0.1238 | No-significant |
| Residual | 0.6591 | 14 | 0.0471 |  |  |  | 0.0478 | 14 | 0.0034 |  |  |  |
| Lack of Fit | 0.6591 | 10 | 0.0659 |  |  |  | 0.0478 | 10 | 0.0048 |  |  |  |
| Pure Error | < 0.0001 | 4 | < 0.0001 |  |  |  | < 0.0001 | 4 | < 0.0001 |  |  |  |
| Cor Total | 29.97 | 28 |  |  |  |  | 2.35 | 28 |  |  |  |  |
| Fit Statistics | Std Dev = 0.217 |  |  | R² = 0.9780 |  |  | Std Dev = 0.585 |  |  | R²= 0.9797 |  |  |
|  | Mean = 3.38 |  |  | Adjusted R² = 0.9560 |  |  | Mean = 0.5366 |  |  | Adjusted R² = 0.9593 |  |  |
|  | C.V. % = 6.42 |  |  | Predicted R² = 0.8733 |  |  | C.V. % = 10.90 |  |  | Predicted R² = 0.8828 |  |  |
|  |  |  |  | Adeq Precision = 23.9933 |  |  |  |  |  | Adeq Precision = 24.5477 |  |  |

Table 6 - ANOVA outcomes for the quadratic response surface model of the compression tests

| Test Type | Compressive strength |  |  |  |  |  | Compressive modulus |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Source | Sum of Squares | Df | Mean Square | F-value | P-value | Remark | Sum of Squares | df | Mean Square | F-value | P-value | Remark |
| Model | 950.58 | 14 | 67.90 | 74.39 | < 0.0001 | Significant | 3777.96 | 14 | 269.85 | 71.03 | < 0.0001 | Significant |
| A- Fiber fraction | 78.43 | 1 | 78.43 | 85.94 | < 0.0001 | Significant | 1372.43 | 1 | 1372.43 | 361.25 | < 0.0001 | Significant |
| B- Fiber length | 15.63 | 1 | 15.63 | 17.13 | 0.0010 | Significant | 3.30 | 1 | 3.30 | 0.8684 | 0.3672 | No-significant |
| C-NaOH concentration | 105.33 | 1 | 105.33 | 115.41 | < 0.0001 | Significant | 81.08 | 1 | 81.08 | 21.34 | 0.0004 | Significant |
| D-Immersion time | 69.63 | 1 | 69.63 | 76.30 | < 0.0001 | Significant | 641.86 | 1 | 641.86 | 168.95 | < 0.0001 | Significant |
| AB | 63.96 | 1 | 63.96 | 70.08 | < 0.0001 | Significant | 0.0958 | 1 | 0.0958 | 0.0252 | 0.8761 | No-significant |
| AC | 25.52 | 1 | 25.52 | 27.96 | 0.0001 | Significant | 6.48 | 1 | 6.48 | 1.70 | 0.2127 | No-significant |
| AD | 65.04 | 1 | 65.04 | 71.27 | < 0.0001 | Significant | 77.59 | 1 | 77.59 | 20.42 | 0.0005 | Significant |
| BC | 0.2218 | 1 | 0.2218 | 0.2431 | 0.6296 | No-significant | 26.67 | 1 | 26.67 | 7.02 | 0.0191 | Significant |
| BD | 30.21 | 1 | 30.21 | 33.10 | < 0.0001 | Significant | 15.04 | 1 | 15.04 | 3.96 | 0.0665 | No-significant |
| CD | 22.56 | 1 | 22.56 | 24.72 | 0.0002 | Significant | 42.17 | 1 | 42.17 | 11.10 | 0.0049 | Significant |
| A² | 359.65 | 1 | 359.65 | 394.05 | < 0.0001 | Significant | 33.55 | 1 | 33.55 | 8.83 | 0.0101 | Significant |
| B² | 141.16 | 1 | 141.16 | 154.66 | < 0.0001 | Significant | 1309.59 | 1 | 1309.59 | 344.71 | < 0.0001 | Significant |
| C² | 82.90 | 1 | 82.90 | 90.83 | < 0.0001 | Significant | 416.06 | 1 | 416.06 | 109.52 | < 0.0001 | Significant |
| D² | 104.39 | 1 | 104.39 | 114.38 | < 0.0001 | Significant | 81.74 | 1 | 81.74 | 21.52 | 0.0004 | Significant |
| Residual | 12.78 | 14 | 0.9127 |  |  |  | 53.19 | 14 | 3.80 |  |  |  |
| Lack of Fit | 12.78 | 10 | 1.28 |  |  |  | 53.19 | 10 | 5.32 |  |  |  |
| Pure Error | < 0.0001 | 4 | < 0.0001 |  |  |  | < 0.0001 | 4 | < 0.0001 |  |  |  |
| Cor Total | 963.36 | 28 |  |  |  |  | 3831.15 | 28 |  |  |  |  |
| Fit Statistics | Std Dev = 0.9553 |  |  | R² = 0.9867 |  |  | Std Dev = 1.95 |  |  | R²= 0.9861 |  |  |
|  | Mean = 23.08 |  |  | Adjusted R² = 0.9735 |  |  | Mean = 18.23 |  |  | Adjusted R² = 0.9722 |  |  |
|  | C.V. % = 4.14 |  |  | Predicted R² = 0.9236 |  |  | C.V. % = 10.69 |  |  | Predicted R² = 0.9200 |  |  |
|  |  |  |  | Adeq Precision = 28.8290 |  |  |  |  |  | Adeq Precision = 31.7055 |  |  |

Table 7 - Interactions of the development parameters two by two for the Young’s modulus in bending.

|  | Factor A (%) | Factor B (mm) | Factor C (%) | Factor D(h) | Young’s Modulus (GPa) |
| --- | --- | --- | --- | --- | --- |
| Interaction 1 | 1 | - | 1 | - | 1.130 |
| Interaction 2 | 1 | 5 | - | - | 1.020 |
| Interaction 3 | - | - | 1 | 2 | 0.766 |
| Interaction 4 | - | 5 | 1 | - | 0,818 |

Table 8 - Ten optimal combinations of bio-mortar manufacturing parameters obtained with multi-objective optimization using the desirability function

| Number | Fiber fraction | Fiber length | NaOH | Immersion Time | Flexural strength | Flexural modulus | Compressive strength | Compressive modulus | Desirability |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 1.000 | 7.940 | 1.849 | 13.999 | 5.393 | 1.066 | 37.524 | 43.722 | 0.955 |
| 2 | 1.000 | 7.957 | 1.833 | 13.998 | 5.400 | 1.066 | 37.541 | 43.699 | 0.955 |
| 3 | 1.000 | 8.036 | 1.813 | 14.000 | 5.393 | 1.065 | 37.434 | 43.769 | 0.955 |
| 4 | 1.000 | 7.821 | 1.893 | 14.000 | 5.393 | 1.067 | 37.652 | 43.640 | 0.955 |
| 5 | 1.000 | 7.951 | 1.842 | 13.923 | 5.393 | 1.068 | 37.409 | 43.625 | 0.955 |
| 6 | 1.000 | 7.907 | 1.847 | 13.955 | 5.401 | 1.068 | 37.540 | 43.604 | 0.955 |
| 7 | 1.000 | 7.903 | 1.857 | 13.862 | 5.393 | 1.070 | 37.372 | 43.513 | 0.955 |
| 8 | 1.000 | 7.766 | 1.912 | 13.999 | 5.393 | 1.068 | 37.708 | 43.587 | 0.955 |
| 9 | 1.000 | 7.932 | 1.844 | 13.811 | 5.393 | 1.071 | 37.270 | 43.460 | 0.955 |
| 10 | 1.000 | 7.870 | 1.865 | 13.765 | 5.393 | 1.073 | 37.271 | 43.356 | 0.955 |