Supporting Information for

Bending Behavior and Directed Self-assembly of Rod-Coil Block Copolymers

Ling-Ying Shi,1,2 Sangho Lee,2 Qingyang Du,2 Rong Ran,1 Runze Liu,2 Caroline A. Ross*,2

1College of Polymer Science and Engineering, Sichuan University, Chengdu 610065, China

2Department of Materials Science and Engineering, Massachusetts Institute of Technology, 77 Massachusetts Avenue, Cambridge, Massachusetts 02139, United States

* To whom correspondence should be addressed. E-mail: caross@mit.edu

Contents

| Bending energy in a coil-coil block copolymer | S2-3 |
| --- | --- |
| Fig. S1. SEM images of oxidized PDMS nanopatterns formed in D4KM17K films on PS-brush and PDMS-brush functionalized silicon substrates, and the oxidized PDMS patterns of D4KM12K, D4KM21K, D4KM34K and D4KS7KM40K films on PDMS brush functionalized silicon substrates | S4 |
| Fig. S2. SEM images of oxidized PDMS nanopatterns formed in D4KM12K (a), D4KM17K (b), D4KM21K (c) and D4KM34K (d) block copolymers thin films with indication of the bending angle. | S5 |
| Fig. S3. SEM images of oxidized PDMS nanopatterns formed in D4KS7KM40K terpolymer thin films with indication of the bending angle. | S6 |
| Fig. S4. Phase diagrams of bending morphologies of D4KM12K (a), D4KM17K (b), D4KM21K (c) and D4KS7KM40K (d) in the plots of Lcp/L0 and Lcv/L0 as function of . (e,f) The length of segments (Lb) in the Y-junctions as a function of , and the curves of normalized Lb/L0 as function of . | S7 |
| Fig. S5. Low magnification SEM images of transverse cylinders of D4KM12K (a), D4KM21K (b), D4KM34K (c) and D4KS7KM40K (d) block copolymers in 100 nm deep topographic trenches with trench width 120 nm. | S8 |
| Fig. S6. Low magnification SEM images of transverse cylinders of D4KM12K (a), D4KM21K (b), D4KM34K (c) and D4KS7KM40K (d) block copolymers in 100 nm deep topographic trenches with trench width 120 nm. | S9 |
| Fig. S7. SEM images of transverse cylindrical patterns in 780 nm wide topographic trenches (a), in trenches with different bending angles (b), and in other geometrical patterned trenches (c-d). | S10 |
| Fig. S8. Low magnification SEM images of parallel cylinders of D4KM34K block copolymers in PDMS brush functionalized topographic trenches with width 120 nm. | S11 |
| Fig. S9. SEM images of thick films of D4KM21K templated by PS brush and PDMS brush functionalized topographic trenches. | S11 |
| Fig. S10. SEM images of D4KM21K vertical lamellae after two-step anneal in PS brush and PDMS brush functionalized topographic trenches. | S12 |
| Fig. S11. The preferred parallel orientation of cylinders of D4KM34K block copolymers in PDMS brush functionalized templates. | S12 |

Bending energy in a coil-coil block copolymer

To characterize the bends, we describe a bent cylinder as shown in Fig. S4a where L0 is the equilibrium cylinder-cylinder spacing, d is the diameter of the cylinder and  is the bending angle. The bent region forms an arc with width W and radius Rc = W/2cos(/2). The distance between neighboring bending center points Lcp and the gap between neighboring bends Lcv are given by Lcp=L0/sin(/2), and Lcp=(L0d)/sin(/2). Lcp values with bending angle 150, 120, 90, 60 and 30o are calculated to be 1.04L0, 1.15L0, 1.41L0, 2L0 and 3.86L0, respectively. This is illustrated in Fig. S4b-f, where the Lcp and Lcv are plotted vs. bend angle , using the line-space ratios and L0 values from Table 1. For the Y-junction, Fig. S4a, Lb represents the length of the segment protruding into the bend.

The bending energy for cylinders is given by:45,46

∆Gbend(L,Rc)=π2128∙kTNa2∙(L/2)4∙1Rc2

where k, T, a, and N, denote the Boltzmann constant, the temperature, the Kuhn step size, and the total number of Kuhn segments. The length L is the cylinder-cylinder distance at the center of bending region, i.e. Lcp, and Rc is the curvature of the bending region, both of which are functions of  : L=L0/sin(/2) and Rc=W/2cos(/2), where L0 is the equilibrium cylinder-cylinder distance and W is the bending boundary width as shown in Fig. 2b.42 The domain spacing for the relaxed chain, L0relaxed, is twice the end-to-end distance of a Gaussian chain, and following the Alexander-de Gennes formalism, that is L0relaxed = 2aN1/2.47 Thus, Na2 = (L0ralaxed/2)2. Considering that the chains are 10-40% stretched by microphase separation compared with the relaxed state, L0relaxed should be smaller than the microphase separated periodicity L0. In the case of 30% stretching, L0relaxed ≈0.7L0 and Na2 =(0.35L0)2. This yields a bending energy vs. bending angle:

∆Gbend=π262.7∙kT∙L02W2∙1-sinθ22sinθ24

To show the dependence of Gbend on the angle of the bend, Fig. S5 plots Gbend/kT per chain as a function of , where  = (L0/W)2. Gbend increased as the bending angle decreased, with dramatic increases below ~60˚, e.g. for  = 120o, 90o and 60o, Gbend = (0.07, 0.30 and 1.89)kT respectively. The width W of the bent region of cylinders also affects the energy, with Gbend ~ W-2.

Fig. S1. SEM images of oxidized PDMS nanopatterns formed in D4KM17K films on PS-brush and PDMS-brush functionalized silicon substrates (a-b), and the oxidized PDMS patterns of D4KM12K, D4KM21K, D4KM34K and D4KS7KM40K films on PDMS brush functionalized silicon substrates (c-f).

Fig. S2. SEM images of oxidized PDMS nanopatterns formed in D4KM12K (a), D4KM17K (b), D4KM21K (c) and D4KM34K (d) block copolymers thin films with the bending angle indicated. The yellow circles indicate the chevrons, the green circles indicate the Y-junctions and the light pink circles indicate the line segments, and the circles with bolder lines indicate the examples with critical bending angle around the bending morphology transition.

Fig. S3. SEM images of oxidized PDMS nanopatterns formed in D4KS7KM40K terpolymer thin films with the bending angle indicated.

Fig. S4. (a) Schematic illustrations of a model of bending morphology (i) and a comparison of straight cylinders, chevrons and Y-junctions (ii-iv). Phase diagrams of bending morphologies of D4KM12K (b), D4KM17K (c), D4KM21K (d), D4KM34K (e) and D4KS7KM40K (f) in the plots of Lcp/L0 and Lcv/L0 as function of . The length of segments (Lb) in the Y-junctions as a function of  (g).

Fig. S5. The plot of bending free energy per chain as function of , in which the constant  is (L0/W)2 and W is the bending boundary width.

Fig. S6. Low magnification SEM images of transverse cylinders of D4KM12K (a), D4KM21K (b), D4KM34K (c) and D4KS7KM40K (d) block copolymers in 100 nm deep, 120 nm wide topographic trenches.

Fig. S7. SEM images of transverse cylindrical patterns in 780 nm wide topographic trenches (a), in trenches with different bending angles (b), and in other geometrical patterned trenches (c-d). (Some breaks in the cylinders are attributed to overetching)

Fig. S8. Low magnification SEM images of parallel cylinders of D4KM34K block copolymers in PDMS brush functionalized topographic trenches with width 120 nm.

Fig. S9. SEM images of thick films of D4KM21K templated by PS brush and PDMS brush functionalized topographic trenches.

Fig. S10. SEM images of D4KM21K vertical lamellae after two-step anneal in PS brush (a) and PDMS (b) brush functionalized topographic trenches. Some regions of in-plane lamellae are visible in (b).

Fig. S11. The parallel orientation of cylinders of D4KM34K block copolymers in PDMS brush functionalized templates.