Mn-Atomic-Layered Antiphase Boundary Induced Robust Ferroelectricity in Transparent KNN-Based Lead-Free Film

Liqiang Xu,a Zhengyang Kong,a Beibei Zhu,a Xu Wang,a Kun Han,a Pingfan Chen,a Chao Li,e Wenbin Wu,b,d Fangzhou Yao,f* Ke Wang,c Zhen Huang,a,* and Feng Chenb,*

a Information Materials and Intelligent Sensing Laboratory of Anhui Province, Institutes of Physical Science and Information Technology, Anhui University, Hefei 230601, China

b Anhui Province Key Laboratory of Condensed Matter Physics at Extreme Condition, High Magnetic Field Laboratory, Chinese Academy of Sciences, Hefei, Anhui 230031, China

c State Key Laboratory of New Ceramics and Fine Processing, School of Materials Science and Engineering, Tsinghua University, Beijing 100084, China

d Hefei National Laboratory for Physical Sciences at the Microscale, University of Science and Technology of China, Hefei 230026, China

e School of Microelectronics and State Key Laboratory for Mechanical Behavior of Materials, Xi’an Jiaotong University, Xi’an, Shanxi, 710049, China

f Research Center for Advanced Functional Ceramics, Wuzhen Laboratory, Jiaxing 314500, China

*Corresponding authors.

E-mail addresses: yaofangzhou@xjtu.edu.cn (F.-Z. Yao), huangz@ahu.edu.cn (Z. Huang), and fchen@hmfl.ac.cn (F. Chen)

These authors contributed equally to this work.

Figure S1. (a) The XRD pattern and (b) the enlarged part around (200)pc peak of the KNNLT-M target.

Figure S2. The comparison of polarization of the present KNNLT-M films with the previously experimentally measured twice remnant polarization (2Pr) values in pure and doped KNN films from the year of 2007 to 2024.

Figure S3. (a) XPS survey spectra and high-resolution spectra around (b) K 2p, (c) Na 1s, (d) Nb 3d, (e) Ta 4f, (f) O 1s and (g) Mn 2p of KNNLT-M films grown on the LSSO-coated STO (001) substrate.

Figure S4. (a) Typical X-ray linear scans, (b) zoom-in view and (c) rocking curves around KNNLT-M (020), RSMs on the (d) STO (002) and (e) STO (103) reflections for KNNLT-M films grown on LSSO-coated STO (001) substrate.

Figure S5. (a - c) The change of the twice remnant polarization (2Pr), twice maximum polarization (2Pmax) and twice coercive electric field (2EC) with different test frequencies from 20 Hz to 1 gHz for KNNLT-M films grown on LSSO-coated STO (001) substrate.

Figure S6. (a-i) The comparative P-E hysteresis loops and (j-r) corresponding switching current curves at the same electrical field of 200 kV/cm, and (s) the enlarge view of the comparative loops for KNNLT-M films grown on LSSO-coated STO (001) substrate from 50 Hz to 10 kHz.

Figure S7. (a-d) The surface STEM images along the in-plane directions from low-magnification to atomic resolution for KNNLT-M films grown on LSSO-coated STO (001) substrate.

Figure S8. High-resolution (a) out-of-plane and (h) in-plane cross-sectional testing areas for elemental analysis. The corresponding EDS maps of Nb, Ta and O in the (b-d) out-of-plane and (f-h) in-plane test areas, respectively.

Figure S9. Temperature-dependent (a) dielectric constant and (b) dielectric loss measured at 1, 10 and 100 kHz for KNNLT-M films grown on LSSO-coated STO (001) substrate.