Table 1: Detailed size descriptions of the investigated PFMs. The degrees of polymerization (DP) are derived from NMR-conversion measurements, as described in the Supporting Information. Average molecular weight (Mn) and the ratio of LMA to NDAcrAm units are derived from the DP directly.

| Name | PFM A | PFM B | PFM C | PFM D | PFM E |
| --- | --- | --- | --- | --- | --- |
| d.p. LMA m | 42 | 42 | 375 | 375 | 375 |
| d.p. NDAcrAm n | 8 | 36 | 281 | 19 | 5 |
| Mn [kDa] | 13 | 20 | 162 | 100 | 97 |
| Functionalization [%] | 10 | 41 | 37 | 4 | 1 |
| Schematic Representation |  |  |  |  |  |