Supporting Information for:

Intrinsic Zero-Linear and Zero-Area Compressibility over an Ultra-Wide Pressure Range within a “Gear-Spring” Structure

Dequan Jiang1, Ting Wen1*, Huimin Song2, Zimin Jiang1, Chen Li1, Ke Liu1, Wenge Yang1, Ho-kwang Mao1 and Yonggang Wang1*

1Center for High Pressure Science and Technology Advanced Research (HPSTAR), Beijing 100094, China

2Center of Materials Science and Optoelectronics Engineering, University of Chinese Academy of Sciences, Beijing 100049, China

Emails: ting.wen@hpstar.ac.cn, yonggang.wang@hpstar.ac.cn

Content

Table S1 The cell parameters obtained from the high-pressure XRD patterns.

Fig. S1 Rietveld refinement of Li2Ti(IO3)6 under ambient pressure with the space group of P63, cell parameters a = b = 9.372 Å, c = 5.113 Å.

Fig. S2 The parallel manner of the lone pairs on I cations. The purple, red and green balls represent I, O and Ti atoms, respectively.

Fig. S3 The XRD patterns of the recovered sample and the sample at 0.7 GPa.

Fig. S4 The shifts of (210), (211), and (300) Bragg peaks under compression.

Fig. S5 The linear compressibilities calculated by the empirical function l = l0 + λ (p - pc)υ in the regions of (a) 0-8 GPa, (b) 8-18.9 GPa, (c) 18.9-40.2 GPa, and (d) 0-18.9 GPa.

Fig. S6 The linear and area compressibilities as a function of applied pressure calculated by the formula Kl = -Δl/lΔp, Ks = -Δs/sΔp.

Fig. S7 (a) High-pressure Raman spectra of Li2Ti(IO3)6 at selected pressures. (b) Pressure-dependence of the Raman peak positions in the wavenumber range of 400-850 cm-1.

Fig. S8 (a) The SHG intensity as a function of applied pressure. (b) The relative value of cell parameter c as a function of applied pressure.

Table S1. The cell parameters obtained from the high-pressure XRD patterns.

| P (GPa) | a (Å) | b (Å) | c (Å) |
| --- | --- | --- | --- |
| 0.7 | 9.353 | 9.353 | 5.019 |
| 1.7 | 9.33 | 9.33 | 4.977 |
| 2.4 | 9.313 | 9.313 | 4.933 |
| 3.2 | 9.302 | 9.302 | 4.891 |
| 4.1 | 9.288 | 9.288 | 4.842 |
| 5 | 9.279 | 9.279 | 4.8 |
| 6 | 9.265 | 9.265 | 4.755 |
| 7.1 | 9.259 | 9.259 | 4.696 |
| 8 | 9.259 | 9.259 | 4.632 |
| 9.2 | 9.261 | 9.261 | 4.548 |
| 10.6 | 9.267 | 9.267 | 4.48 |
| 12.1 | 9.281 | 9.281 | 4.386 |
| 13.6 | 9.295 | 9.295 | 4.285 |
| 15.4 | 9.326 | 9.326 | 4.161 |
| 16.7 | 9.346 | 9.346 | 4.081 |
| 17.8 | 9.378 | 9.378 | 3.983 |
| 18.9 | 9.395 | 9.395 | 3.921 |
| 20.1 | 9.394 | 9.394 | 3.856 |
| 22 | 9.384 | 9.384 | 3.813 |
| 24.6 | 9.367 | 9.367 | 3.762 |
| 26.1 | 9.352 | 9.352 | 3.721 |
| 28.4 | 9.336 | 9.336 | 3.693 |
| 31.9 | 9.324 | 9.324 | 3.679 |
| 34.6 | 9.311 | 9.311 | 3.666 |
| 36.6 | 9.293 | 9.293 | 3.653 |
| 38.5 | 9.29 | 9.29 | 3.652 |
| 40.2 | 9.281 | 9.281 | 3.646 |

Fig. S1 Rietveld refinement of Li2Ti(IO3)6 under ambient pressure with the space group of P63, cell parameters a = b = 9.372 Å, c = 5.113 Å.

Fig. S2 The parallel manner of the lone pairs on I cations. The brown, red and black balls represent I, O and Ti atoms, respectively.

Fig. S3 The XRD patterns of the recovered sample and the sample at 0.7 GPa.

Fig. S4 The shifts of (210), (211), and (300) Bragg peaks under compression.

Fig. S5 The linear compressibilities calculated by the empirical function l = l0 + λ (p - pc)υ in the regions of (a) 0-8 GPa, (b) 8-18.9 GPa, (c) 18.9-40.2 GPa, and (d) 0-18.9 GPa.

Fig. S6 The linear and area compressibilities as a function of applied pressure calculated by the formula Kl = -Δl/lΔp, Ks = -Δs/sΔp.

Fig. S7 (a) High-pressure Raman spectra of Li2Ti(IO3)6 at selected pressures. (b) Pressure-dependence of the Raman peak positions in the wavenumber range of 400-850 cm-1.

Fig. S8 (a) The SHG intensity as a function of applied pressure. (b) The relative value of cell parameter c as a function of applied pressure.