Synthesis of Finely Controllable Sizes of Au Nanoparticles on a Silica Template and Their Nanozyme Properties

Bomi Seong,1 Jaehi Kim,1 Wooyeon Kim,1 Sang Hun Lee,2 Xuan-Hung Pham,1* and Bong-Hyun Jun1,*

1 Department of Bioscience and Biotechnology, Konkuk University, Seoul 143-701, Republic of Korea. e-mail: iambomi33@konkuk.ac.kr (B.S.); susia45@gmail.com (J.K.)
2 Department of Chemical and Biological Engineering, Hanbat National University, Daejeon 34158, Korea; sanghunlee@hanbat.ac.kr (S.H.L)

Correspondence should be addressed to Xuan-Hung Pham: phamricky@gmail.com and Bong-Hyun Jun: bjun@konkuk.ac.kr

Figure S1. Absorption spectra of 0.1 mM TMB and 200 mM H2O2 in the presence SiO2@Au NPs fabricated in various concentrations of Au3+ precursor: (i) 0 μM, (ii) 50 μM, (iii) 100 μM, (iv) 150 μM, (v) 200 μM, and (vi) 300 μM Au3+.

Figure S2. The effects of TMB concentration in the range of 0 to 1.0 mM on the peroxidase-like activity of SiO2@Au in mixture of TMB and 200 mM H2O2.

Figure S3. The effects of H2O2 concentration in the range of 0 to 400 mM on the peroxidase-like activity of SiO2@Au in mixture of 0.6 mM TMB and H2O2.

Figure S4. (a) Effect of pH solution on the UV-Vis spectra of 0.6 mM TMB and 200 mM H2O2 in the presence of SiO2@Au at various pH conditions: (i) pH 3.0, (ii) pH 4.0, (iii) pH 5.0, (iv) pH 6.0, (v) pH 7.0, and (vi) pH 8.0

Figure S5. The effects of SiO2@Au amount in the range of 0 to 50 μg on the peroxidase-like activity of SiO2@Au in mixture of 0.6 mM TMB and 200 mM H2O2.