Table 1 Textural, surface chemical, and magnetic characteristics of CoF@NAC

Textural    characteristics                                              Surface chemical characteristics                                  __________________________________                 _________________________________

BET surface area (m2/g)   	       729                          Carboxylic (mEq/g)              0.5401

Total pore volume (cm3/g)            0.426                       Phenolic (mEq/g)                 0.0185

Micropore volume (cm3/g)            0.164                       Lactonic (mEq/g)                 0.5023

Mesopore volume (cm3/g)             0.262                      Total acidity (mEq/g)           1.0609

Microporosity (%)                        38.5                         Total basicity (mEq/g)          1.0717

Mesoporosity (%)                        61.5                          pHPZC                                    8.20

Average pore diameter (nm)         2.4

Table 2 Comparison of textural properties of CoF/NAC and some CoF-loaded carbonaceous materials reported in the literature

Materials                        SBET (m2/g)     VT (cm3/g)     Dp (nm)          References

CoF/NAC                       729                  0.426             2.4                  Present study

CoF/BC                          136                  0.273               -                   Wu et al. (2021)

CoF/AC                          269                  0.189             3.9                 Liang et al. (2019)

MWCNT/CoF                  72                  0.510            65                   Al-Musawi et al. (2022)

Commercial AC/CoF     463                  0.180              -                    Ai et al. (2010)

CoF/AC                          523                  0.432             3.1                Askari et al. (2023)

CoF/GO                            44                  0.242             7.6                Asadi et al. (2022)

CoF/AC                            79                  0.213              3.6               Karthikeyan et al. (2022)

†AC: activated carbon; CoF: CoFe2O4; GO: graphene oxide; BC: Biochar; MWCNT: multi-walled carbon nanotube

Table 3 Kinetic parameters for adsorption at different concentrations of MB and Pb(II) onto CoF@NAC

Models:        Pseudo-first-order                 Pseudo-second-order               Inta-particle diffusion

_____________________    ______________________    __________________

C0      Qe,exp    Qe,cal   k1x10-2  R2      Δq%       Qe,cal    k2 x10-3  R2      Δq%         kid           I          R2

MB

650    295.9    148.8   1.3   0.9941  5.71     300.0   2.8  0.9995  2.01         10.9   156.6    0.9905

700    315.5    150.7   1.5   0.9915  5.05     322.6   3.1  0.9989  1.55           8.9   185.4    0.9911

800    325.5    154.8   1.7   0.9734  4.42     333.3   3.4  0.9992  0.91           8.1   209.1    0.9981

Pb(II)

650    212.1    125.6   1.7  0.9876   5.15     222.2   3.54  0.9993  1.31          9.7    93.3    0.9896

700    222.2    126.6   1.9  0.9859   4.45     232.6   3.58  0.9991  0.84          9.9     99.3   0.9944

800    230.2    131.8   2.0  0.9885   3.39     238.1   5.25  0.9997  0.54          6.4   148.2   0.9897

† (C0: mg/L; Qe,exp: mg/g; Qe,cal: mg/g; k1: 1/min; k2: g/mg min); kid: mg/g min1/2; I: mg/g.

Table 4 Isotherm and thermodynamics parameters for MB and Pb(II) adsorptions onto CoF@NAC at different temperatures

Freundlich                             Langmuir                                            Thermodynamics

____________________     _____________________________   ________________

T (K)   KF   1/n      R2          Δq%        Qm    KLx10-3  R2        Δq%   RL         ∆Go       ∆Ho      ∆So

MB

293     3.1   0.73   0.7771   4.99         588      2.1    0.9598   1.64   0.586      -15.9    7.94   0.081

303     7.9   0.61   0.7387   4.13         625      2.4    0.9506   1.33   0.529      -16.7

313   12.8   0.55   0.7219   2.89         667      2.6    0.9733   0.98   0.494      -17.5

Pb(II)

293     9.3   0.54   0.7449   5.34          455     3.0    0.9746   1.56   0.099      -19.4   -42.4   -0.21

303   13.9   0.46   0.7762   4.88          400     3.6    0.9641   1.32   0.498      -17.1

313   17.9   0.41   0.7899   3.67          370     3.4    0.9501   1.21   0.535      -16.7

†T: K; KF: (mg/g)(L/mg)1/n; Qm: mg/g;  KL: L/mg;  ∆Go: kJ/mol ; ∆Ho:  kJ/mol;  ∆So: kJ/mol K.

Table 5 Comparison of maximum adsorption capacity of MB and Pb(II) of CoF@NAC with other magnetic composite adsorbents reported in the literature.

Adsorbent                                           Conditions                    Qm            References

(mg/g)

MB

Magnetic MWCN                             298 K, pH 7.0, 24 h        12        Gong et al. (2009)

Montmorillonite/CoFe2O4                318 K, pH 6.0, 40 min    98        Ai et al. (2011)

Fe3O4/chitosan/graphene oxide        303 K, pH 10, 50 min   181        Fan et al. (2012)

Magnetic peanut shell-AC               298 K, pH 6.5, 5 h        202        Wang (2018)

Magnetic green peas peels-BC        297 K, pH 7.0, 1 h        175       Rubangakene et al. (2023)

Magnetic AC/alginate                      298 K, pH 7.0, 50 h      476        Saning et al. (2024)

Magnetic asphalt-AC                       298 K, pH -,     6 h        710        Wang et al. (2023)

CoF@NAC                                      313 K, pH 5.5,  6 h        667       This study

Pb(II)

MnFe2O4@wild plant-BC               323 K, pH 5.0, 3 h           90        Fuat and Cumali (2021)

Magnetic AC/alginate                     298 K, pH 5.0, 30 h       164        Saning et al. (2024)

Chitosan/CoFe2O4                           303 K, pH 6.0, 50 min   228        Fan et al. (2017)

Magnetic graphene oxide/LDH       298 K, pH 6.0, 4 h        192         Huang et al. (2018)

Magnetic macadamia nutshell-BC  303 K, pH 6.0, 3 h        200         Zhou et al. (2024)

MnFe2O4-sludge-BC                       298 K pH 5.0,  6 h        174         Chen et al. (2021)

CoFe2O4@almond husk-AC           333 K, pH 5.0, 2 h            6         Yahya et al. (2020)

CoF@NAC                                      293 K, pH 5.1, 6 h       455         This study

†AC: Activated carbon; BC: Biochar: MWCN: multi-wall carbon nanotube; LDH: Layered double hydroxide