Supplementary Information

Valley Selectivity Manipulation via Interfacial Magnon-Exciton Interactions in TMD/CrSBr Antiferromagnetic van der Waals Heterostructures

Xilin Zhang1, Yaojie Zhu2, Ruixue Bai1, Runcheng Mao1, Zuowei Yan1, Xiaoshan Du1, Rui Zhou2, Yisen Tang2, Heng Li3, Zdenek Sofer3, Hui Ma*2 & Chongyun Jiang*1

1 College of Electronic Information and Optical Engineering, Nankai University, Tianjin 300350, China.
2 School of Physical Science and Technology, Tiangong University, Tianjin 300387, China.
3 Department of Inorganic Chemistry, University of Chemistry and Technology Prague, Technická 5, 166 28 Praha 6, Czech Republic.

*Email: jiang.chongyun@nankai.edu.cn;
*Email: mahui@tiangong.edu.cn.

Supplementary Note 1: Optical microscope images of three heterostructure samples.

Supplementary Note 2: Reduction of exciton emission caused by charge transfer in HS.

Supplementary Note 3: Exclusion of possible mechanisms contributing to the blueshift of X* and T*, as well as the emergence of M*.

Supplementary Note 4: Assignment of emission peaks in WSe2/SiO2 and WSe2/CrSBr (Sample 3).

Supplementary Note 5: Exciton VP in MoSe2/SiO2 and MoSe2/CrSBr (Sample 1) with σ+ excitation.

Supplementary Note 6: Exclusion of VP enhancement from other possible mechanisms.

Supplementary Note 7: Interfacial magnon-exciton interaction in the WSe2/CrSBr heterostructure.

Supplementary Note 8: Theoretical modeling of V-shaped variation of VP with magnetic field.

Supplementary Note 1: Optical microscope images of three heterostructure samples.

Figure S1. Optical microscope image of MoSe2/CrSBr (a), WSe2/CrSBr (b), WSe2/CrSBr and MoSe2/CrSBr (c) heterostructures, scale bar: 10 μm. The crystal axes of CrSBr are labeled in the figure.

Sample 1 refers to the MoSe2/CrSBr sample mentioned in the main text, while Sample 2 and 3 are additional WSe2/CrSBr samples. In the following text, we use X* or X to refer to excitonic states in HS or ML TMD, and M* to refer to complexes in the heterostructure.

Supplementary Note 2: Reduction of exciton emission caused by charge transfer in HS.

Figure S2. PL spectra of MoSe2/SiO2 and MoSe2/CrSBr (Sample 1) with the excitation wavelength of 715 nm.

Under the same excitation power and exposure time, the emission intensity of excitonic states in MoSe2/CrSBr is significantly reduced in contrast to that in MoSe2/SiO2 due to charge transfer.

Supplementary Note 3: Exclusion of possible mechanisms contributing to the blueshift of X* and T*, as well as the emergence of M*.

The contact between ML MoSe2 and CrSBr, along with laser irradiation, may lead to the following effects: interlayer charge transfer, a magnetic exchange field (MEF) induced by magnetic proximity effect (MPE) of CrSBr, and interlayer particle interactions. First, we can exclude the doping effect induced by the interlayer charge transfer as the source of the blueshift energy of X* and T*, and the emergence of M*. Doping has been demonstrated to have essentially no effect on the exciton peak energy in the MoSe2 monolayer1-4 and incredibly resulted in the creation of new peak M* with tens of meV shift away from the excitonic states. Furthermore, the type-III band alignment prevents the interlayer transfer of photogenerated carriers under laser irradiation5, allowing us to disregard the impact of photogenerated carrier transfer between MoSe2 and CrSBr. Next, the in-plane magnetization of CrSBr cannot result in so large blueshift energy of X* and T* and the appearance of M*. In-plane magnetic field enable dark excitons to brighten in ML MoSe2, with the reported blueshift energy of ~ 1.4 meV relative to bright excitons6. Even under an in-plane magnetic field of 30T, the energy shift between the bright excitons and brightened dark excitons is only ~ 3 meV6, insufficient to account for the ~ 16 meV blueshift. Thus, in-plane MEF also cannot be the origin of the blueshift for X* and T*, or responsible for the occurrence of M*.

Supplementary Note 4: Assignment of emission peaks in WSe2/SiO2 and WSe2/CrSBr (Sample 3).

Figure S3. PL spectra and fitting results of WSe2/SiO2 and WSe2/CrSBr (Sample 3), measured at 15 K using continuous-wave excitation of 670 nm. The emission peaks in WSe2/SiO2 and WSe2/CrSBr are marked in the figure.

Figure S4. Excitation power dependence and g-factor of excitonic states and complexes in WSe2/SiO2 and WSe2/CrSBr (Sample 3). (a, d) Excitation power dependence of the integrated PL intensity of excitonic states in WSe2/SiO2 (a) and WSe2/CrSBr (d). Solid curves show I ∝ Pα fitting, along with their α value. (b-c, e-f) Valley splitting of excitonic states in WSe2/SiO2 (b-c) and excitonic states and complexes in WSe2/CrSBr (e-f). Eσ⁺σ⁺(σ⁻σ⁻) represents co-polarized PL peak energy under σ+ (σ⁻) excitation. The solid lines represent linear fits results.

Table S1. Peak energy, α value and g-factor of excitonic states and complexes in WSe2/SiO2 and WSe2/CrSBr (Sample 3).

| WSe2/SiO2 (Sample 3) |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak |  |  | L | DR | D− | T | X |
| Peak energy (eV) |  |  | 1.663 | 1.684 | 1.696 | 1.715 | 1.745 |
| α value |  |  | 0.57 | 0.99 | 1.17 | 0.99 | 1.00 |
| g-factor |  |  | -5.60 | -7.79 | -8.92 | -3.27 | -3.54 |
| WSe2/CrSBr (Sample 3) |  |  |  |  |  |  |  |
| Peak | M* | P1* | P2* | DR* | D0* | T* | X* |
| Peak energy (eV) | 1.627 | 1.654 | 1.668 | 1.683 | 1.701 | 1.718 | 1.744 |
| α value | 0.98 | 1.15 | 1.21 | 0.98 | 1.12 | 1.04 | 1.00 |
| g-factor | -7.91 | -10.36 | -8.25 | -8.87 |  | -3.27 |  |

The emission peaks in WSe2/SiO2 and WSe2/CrSBr are fitted and shown in Figure S3, while Figure S4 presents their α value and g-factors. These results are summarized in Table S1. All peaks except for peak L produce linear dependence of PL intensity on power excitation, which excludes the possibility that they are biexcitons, localized excitons, or moiré excitons. In ML WSe2, the g-factor for intravalley dark exciton recombination is ~ -8, whereas the g-factor for intervalley dark exciton recombination is ~ -123,4. For WSe2/SiO2, L is identified as a localized state due to the sublinear dependence of its intensity on excitation power. Referring to previous studies3,4, in ML WSe2, the emission energy of positive trion and negative trion is ~ 20 meV and ~ 28 meV lower than that of excitons, respectively. Based on this, we infer that our WSe2/SiO2 sample is likely n-doped, and we assign T as negative trion. Furthermore, the g-factor of DR is close to -8, and its emission energy is ~61 meV lower than X4. Thus, we assign DR as the Γ5 phonon replica of the dark exciton. Since in ML WSe2, the emission energies of negative dark trion and dark exciton are ~ 54 meV and ~ 40 meV lower than that of exciton, corresponding to 1.691 eV and 1.705 eV, respectively, we suggest that D− (1.696 eV) is more likely to be a negative dark trion, while D0 cannot be distinguished from D− due to its weak intensity. The energy of D0 is expected to be 1.705 eV, which is ~ 21 meV higher than its phonon replica DR, corresponding to the energy of Γ5 phonon4.

We assign M* in the WSe2/CrSBr as the complex of D0 in ML WSe2 and magnon in CrSBr, based on experimental evidence that the g-factor of M* is similar to that of D0, and the energy difference between the M* and D0 emission (~78 meV) is comparable to the energy of two magnons (~90 meV)7,8. The slight energy deviation may be related to nonlinear effects of magnons9 (e.g., second harmonic generation), strain10, substrate, or magnon-exciton scattering. Additionally, we assign D0* as a dark exciton because its energy in WSe2/CrSBr is closer to that of D0 in WSe2/SiO2. The transition from D− to D0* may be associated with p-doping induced by interlayer charge transfer. The energy difference between M* and D0* is ~ 74 meV, which does not match the phonon energy in ML WSe2, indicating that M* is not a phonon replica. Furthermore, the energy differences between P1* and P2* with respect to D0* are ~ 47 meV11 and ~ 33 meV4, respectively, which we assign to phonon replicas of the intervalley and intravalley negative dark trion, respectively.

Supplementary Note 5: Exciton VP in MoSe2/SiO2 and MoSe2/CrSBr (Sample 1) with σ+ excitation.

Figure S5. Exciton VP in MoSe2/SiO2 and MoSe2/CrSBr (Sample 1) as a function out-of-plane magnetic field under σ+ excitation. The solid lines represent linear fits results.

As shown in Figure S5, the exciton VP in MoSe2/CrSBr at 0 T increases by ~ 16% compared to MoSe2/SiO2, excluding intervalley charge transfer as the origin of the VP enhancement (see Supplementary Note 6). Besides, VP of X and X* show obviously linear variations with the magnetic field, with X and X* showing similar rates of change, which is consistent with the main text.

Supplementary Note 6: Exclusion of VP enhancement from other possible mechanisms.

1. Out-of-plane MEF from MPE. Since CrSBr flake features an antiferromagnet with an in-plane magnetic order, this mechanism can be ruled out to introduce the VP enhancement.

2. In-plane MEF from MPE. The spin orientation of excitons in the K (-K) valley of ML TMD is out-of-plane, and an in-plane magnetic field is expected to induce Hanle precession12,13, reducing the VP, which contrary to our result. On the other hand, previous reports have shown that this mechanism primarily affects the VP of resident carriers13, whereas the VP of short-lived excitons in ML TMD remains unaffected in an in-plane magnetic field up to 9T12. In any case, an in-plane magnetic field cannot be a mechanism for increasing VP.

3. Intervalley charge transfer possibly induced by phonons. Before recombination, photoexcited electrons in the K valley might be scattered by phonons to the -K valley, where they can either bound with holes to form excitons in the -K valley or bound with excitons in the K valley to form trions3. This would reduce the VP of excitons while increasing the VP of trions, which contradicts our experimental results that that the VP of both X* and T* are enhanced (see Figure S5).

4. Improved on-resonance-excitation condition by the blueshift energy. An enhanced on-resonance excitation condition is made possible by the blueshift energy, which likely leads to an increase in VP since it may reduce the gap between the emission and the excitation. Thus, we conducted the polarized PL experiment in MoSe2/SiO2 with an excitation wavelength of 721 nm (excitation energy ~1.720 eV, ~14 meV lower than the excitation of 715 nm) and found that the VP is ~0% (see Figure S6). Thus, this potential mechanism is excluded.

Figure S6. The PL spectra of MoSe2/SiO2 (Sample 1) excited at 721 nm. σ-σ-(σ-σ+) represents co-and cross-polarization under σ- excitation.

Supplementary Note 7: Interfacial magnon-exciton interactions in the WSe2/CrSBr heterostructure.

Figure S7. Excitonic and valley properties of excitonic states in WSe2/CrSBr (Sample 2). (a) Excitation power dependence of the integrated PL intensity of M*, T*, and X* in WSe2/CrSBr. Solid curves are fitted with I ∝ Pα. Temperature dependence of trion (b) and exciton (c) peak energy in WSe2/SiO2 and WSe2/CrSBr. (d) Temperature dependence of energy blueshift between X* (T*) and X (T). (e) Temperature dependence of VP for X and X*. (f) VP of excitons (X, X*) as a function of out-of-plane magnetic field under σ+ (solid symbols) and σ- excitation (empty symbols) in WSe2/SiO2 and WSe2/CrSBr. Solid and dashed lines are linear fitting results.

As shown in Figure S7a, the emission intensity of M*, T*, and X* in the WSe2/CrSBr exhibits linear dependence on the excitation power. The temperature dependence of the trion and exciton emission energy in WSe2/SiO2 and WSe2/CrSBr are shown in Figures S7b and S7c, respectively. We observe a significant blueshift of the excitonic states in WSe2/CrSBr compared to that in WSe2/SiO2 below TN.  The blueshift energy are extracted and shown in Figure S7d. It exhibits a maximum at 70 K and keeps a constant (~ 2.5 meV) when the temperature is higher than the Néel temperature of CrSBr, which is attributes to the variation of dielectric environment. This result is in accordance with that observed in MoSe2/CrSBr. Figure S7e shows the temperature dependence of valley polarization in WSe2/SiO2 and WSe2/CrSBr. Enhanced VP is observed unless the temperature surpasses ~120 K, consistent with the results in MoSe2/CrSBr. Figure S7f displays the exciton valley polarization in WSe2/SiO2 and WSe2/CrSBr under different magnetic fields. At 0 T, the exciton VP of WSe2/SiO2 and WSe2/CrSBr under σ+ (σ-) excitation are ~ 26.5% (20.7%) and 56.7% (52.7%), respectively, showing enhanced VP in the heterostructure. In addition, the VP of X and X* exhibits the same rate of change (~0%/T) with the magnetic field, which is consistent with the main text.

Figure S8. Valley properties of exciton-magnon complexes (M*) in WSe2/CrSBr (Sample 3). (a) VP of M* dependence on out-of-plane magnetic field under σ+ and σ⁻ excitation. The solid lines represent guide lines. (b) VCCD of M* in WSe2/CrSBr (Sample 3) and MoSe2/CrSBr (Sample 3) dependence on out-of-plane magnetic field. Dashed black lines indicate ±Hs, and the solid red line is the guide line.

In WSe2/CrSBr, M* exhibits an asymmetric V-shaped dependence of VP on the magnetic field and an S-shaped dependence of VCCD on the magnetic field, consistent with the results in MoSe2/CrSBr.

Supplementary Note 8: Theoretical modeling of V-shaped variation of VP with magnetic field.

Figure S9. Schematic diagram of exciton decay dynamics with a four-level system under σ+ excitation. Scattering driven by electron-hole exchange interaction and Zeeman effect are involved.

We establish a model to explain the VP in the presence of an out-of-plane magnetic field by describing the exciton decay dynamics in ML TMD. As shown in Figure S9, we consider a four-level system, where state |0⟩ represents the ground state, states |1⟩ and |2⟩ correspond to excitonic states in the K and -K valleys, respectively, and state |3⟩ represents the excitation energy level. γ0 is the exciton decay rate, γ1 and γ2 are the valley conservation and valley flipping rates, respectively, γe is the exchange-driven intervalley scattering rate, and γ12 and γ21 are the Zeeman-driven intervalley scattering rates.

For σ+ excitation, assuming that photogenerated carriers are only produced in the K valley, we can write the rate equation for the population in K and -K valley:

dN1dt=N3γ1+N2γ21+γe-N1γ12+γe-N1γ0 
dN2dt=N3γ2-N2γ21+γe+N1γ12+γe-N2γ0,                            (S1)

where Ni is the population of the i-th state. The VP of K valley can be written as follows:

Pc=N1-N2N1+N2=P0∙γ0γ0+γ12+γ21+2γe+γ21-γ12γ0+γ12+γ21+2γe,                                 (S2)
where Pc is the VP of K valley, and P0 = (γ1-γ2)/(γ1+γ2) is the initial VP of the system.

At zero magnetic field, γ12 = γ21 = γl, Pc can be simplified to:

Pc=P0∙11+2(r0+r0')=P0∙11+2(τ0/τv),                                                       (S3)
where τ0 = 1/γ0 is the exciton decay time, and τv = 1/(γl + γe) is the intervalley relaxation time. The parameters r0 = γl/γ0 and r0' = γe(B=0)/γ0 represent the ratio of the Zeeman-driven and e-h exchange-driven valley depolarization rate to the exciton decay rate at zero field, respectively. When P0 remains constant, the VP at zero field depends on the competition between exciton recombination (τ0) and intervalley scattering (τv), i.e., the τ0/τv term or the r0 + r0' term.

When an out-of-plane magnetic field is applied, γ12, γ21, and γe take the following forms14,15:

γ12=r0γ0exp⁡(+β) 
γ21=r0γ0exp⁡(-β) 
γe=r0'γ011+(∆EΓ)2,                                                                                     (S4)

where ΔE = Eσ⁺σ⁺ - Eσ⁻σ⁻ = gμBB is valley Zeeman splitting, g is the g-factor, β = ΔE/(2kBT), kB is the Boltzmann constant, T is temperature, and Γ is the width parameter of exchange interaction. γe can be negligible when ΔE is much larger than Γ. Therefore, Eq. (S2) can be modified as:

Pc=P0-2r0∙sinh⁡(β)1+2r0∙cosh⁡(β)+2r0'∙11+(∆EΓ)2.                                                                   (S5)
We assume that P0 is independent of the magnetic field. By the model fitting to Figure 4b with Eq. (S5), we obtained P0 = 0.2012, g = -8.75, T = 15 K, r0 = 0.02, r0' = 0.85, and Γ = 1.5 meV. The relative smaller r0 and larger r0' at 0 T indicate that the valley depolarization mechanism is dominated by the electron-hole exchange interactions.

REFERENCES

1	Le, C. T. et al. Negative Valley Polarization of the Intralayer Exciton via One-Step Growth of H-Type Heterobilayer WS2/MoS2. ACS Nano 17, 2629-2638 (2023).

2	Jiang, Y., Chen, S., Zheng, W., Zheng, B. & Pan, A. Interlayer exciton formation, relaxation, and transport in TMD van der Waals heterostructures. Light: Science & Applications 10, 72 (2021).

3	He, M. et al. Valley phonons and exciton complexes in a monolayer semiconductor. Nature Communications 11, 618 (2020).

4	Yang, M. et al. Relaxation and darkening of excitonic complexes in electrostatically doped monolayer WSe2: Roles of exciton-electron and trion-electron interactions. Physical Review B 105, 085302 (2022).

5	Lee, J. et al. Modulation of Junction Modes in SnSe2/MoTe2 Broken-Gap van der Waals Heterostructure for Multifunctional Devices. Nano Letters 20, 2370-2377 (2020).

6	Robert, C. et al. Measurement of the spin-forbidden dark excitons in MoS2 and MoSe2 monolayers. Nature Communications 11, 4037 (2020).

7	Scheie, A. et al. Spin Waves and Magnetic Exchange Hamiltonian in CrSBr. Advanced Science 9, 2202467 (2022).

8	Pawbake, A. et al. Magneto-Optical Sensing of the Pressure Driven Magnetic Ground States in Bulk CrSBr. Nano Letters 23, 9587-9593 (2023).

9	Diederich, G. M. et al. Exciton Dressing by Extreme Nonlinear Magnons in a Layered Semiconductor. Preprint at https://arxiv.org/abs/2411.14943 (2024).

10	Esteras, D. L., Rybakov, A., Ruiz, A. M. & Baldoví, J. J. Magnon Straintronics in the 2D van der Waals Ferromagnet CrSBr from First-Principles. Nano Letters 22, 8771-8778 (2022).

11	Li, Z. et al. Phonon-exciton Interactions in WSe2 under a quantizing magnetic field. Nature Communications 11, 3104 (2020).

12	Sallen, G. et al. Robust optical emission polarization in MoS2 monolayers through selective valley excitation. Physical Review B 86, 081301 (2012).

13	Yang, L. et al. Long-lived nanosecond spin relaxation and spin coherence of electrons in monolayer MoS2 and WS2. Nature Physics 11, 830-834 (2015).

14	Neumann, A. et al. Opto-valleytronic imaging of atomically thin semiconductors. Nature Nanotechnology 12, 329-334 (2017).

15	Surrente, A. et al. Intervalley Scattering of Interlayer Excitons in a MoS2/MoSe2/MoS2 Heterostructure in High Magnetic Field. Nano Letters 18, 3994-4000 (2018).