- Laboratory scale above the pack/out of pack aluminide coating system has been established.

- Additively manufactured Inco 939 samples have been coated successfully via this set-up.

- The fixed process parameters have been shared for conforming coatings in terms of industrial quality standards.

- Yttrium incorporation has been achieved by modification of powder mixture. %2 Y2O3 addition in the expense of Al2O3 to the pack mixture has resulted with yttrium incorporation in the additive layer just above the interdiffusion zone (IDZ)

- Platinum aluminide coatings with double phase structure have resulted regardless of platinum diffusion heat treatment. However, continues PtAl2 phase has been eliminated thanks to platinum dilution.