Appendix

Appendix 1: Saturation solubility of nanocrystals formulations

| Formulation | Fold Increment in Solubility (mean ± SD) |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | Curcumin |  |  | Piperine |  |  |
|  | 0.1N HCI | PBS | dH2O | 0.1N HCI | PBS | dH2O |
| FNC1 | 22.78 ± 0.0629 b,c,d,e,f,g,h,i | 47.78 ± 0.06299 b,c,d,e,f,g,h,i | 63.45 ± 0.3088 b,c,d,e,f,g,i | 4.53 ± 0.1052 b,c,d,e,f,h,i | 1.051 ± 0.1191 c,d,e,g,h,i | 5.048 ± 0.4684 b,c,d,e,f,g,h,i |
| FNC2 | 54.10 ± 0.069 a,c,d,e,g,h,i | 86.02 ± 0.1561 a,c,d,e,f,h,i | 83.38 ± 0.1017 a,c,e,f,g,h,i | 2.90 ± 0.03821 a,c,d,e,f,g,h,i | 1.088 ± 0.2840 a,c,d,e,g,h,i | 3.89 ± 0.02933 a,c,d,e,g,h,i |
| FNC3 | 1.67 ± 0.1191 a,b,d,e,g,h | 7.33 ± 0.06186 a,b,d,e,g,h | 7.33 ± 0.02062 a,b,d,e,g,h | 1.91 ± 0.1504 a,b,e,f,g | 0.51 ± 0.02236 a,b,d,f,g,h,i | 2.45 ± 0.06708 a,b,d,f,h,i |
| FNC4 | 19.78 ± 0.1666 a,b,c,e,f,g,h,i | 19.78 ± 0.07806 a,b,c,e,f,g,h,i | 77.56 ± 0.1242 a,c,e,f,g,h,i | 2.45 ± 0.1085 a,b,e,f,g,h,i | 0.54 ± 0.09747 a,b,c,e,f,g,h,i | 2.97 ± 0.08979 a,b,c,e,f,g,h,i |
| FNC5 | 51.89 ± 0.1208 a,c,d,e,g,h,i | 17.67 ± 1.202 a,b,c,d,f,i | 53.44 ± 0.07806 a,b,c,d,f,g,h,i | 2.00 ± 0.007746 a,b,c,d,f,g,h,i | 0.74 ± 0.03377 a,b,d,f,g,h,i | 2.49 ± 0.004473 a,b,d,f,g,h,i |
| FNC6 | 2.45 ± 0.01191 a,b,d,e,g,h | 0.667 ± 0 a,b,d,e,g,h | 2.89 ± 0.1192 a,b,d,e,g,h | 2.96 ± 0.1121 a,b,c,d,g,h,i | 0.82 ± 0.1291 a,c,d,e,g,h,i | 3.60 ± 0.2082 a,c,d,e,g,h,i |
| FNC7 | 10.89 ± 0.05189 a,b,c,d,e,f,h,i | 25.14 ± 0.0333 a,c,d,f,h,i | 51.11 ± 0.03149 a,b,c,d,f,h,i | 1.21 ± 0.02049 b,c,d,e,f,h,i | 0.27 ± 0.01183 a,b,c,d,e,f,i | 2.46 ± 0.06017 a,b,d,f,h,i |
| FNC8 | 39.67 ± 0.06186 a,b,c,d,e,f,g,i | 20.11 ± 1.262 a,b,c,d,f,i | 66.44 ± 0.01190 b,c,d,e,f,g,i | 1.31 ± 0.03873 a,b,c,d,e,f,g,i | 0.44 ± 0.03975 a,b,c,d,e,f,i | 1.95 ± 0.01613 a,b,c,d,e,f,g,i |
| FNC9 | 7.33 ± 0 a,b,d,e,g,h | 0.67 ± 0.01806 a,b,d,e,g,h | 9.56 ± 0.1190 a,b,d,e,g,h | 1.41 ± 0.06309 a,b,d,e,f,g,h | 0.42 ± 0.08934 a,b,c,d,e,f,g | 1.58 ± 0.07029 a,b,c,d,e,f,g,h |

HCI, Hydrochloric Acid; PBS, Phosphate Buffer Saline; dH2O, Distilled Water

Samples were analyzed using ANOVA Dunnett’s C statistical test. SD, standard deviation (n=3). FNC1, nanocrystal containing curcumin and piperine; aP<0.05 vs. FNC1; bP<0.05 vs. FNC2; cP<0.05 vs. FNC3; dP<0.05 vs. FNC4; eP<0.05 vs. FNC5; fP<0.05 vs. FNC6; gP<0.05 vs. FNC7; hP<0.05 vs. FNC8; iP<0.05 vs. FNC

Appendix 2: Stability test of optimized FNC1

|  | Particle Size (nm) |  |  | PDI |  |  | Zeta Potential (mV) |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | 4°C | 25°C | 40°C | 4°C | 25°C | 40°C | 4°C | 25°C | 40°C |
| Day 0 | 116.63 ± 2.131 | 116.63 ± 2.131 | 113.63 ± 0.709 | 0.1338 ± 0.0005 | 0.1339 ± 0.0004 | 0.1339 ± 0.0005 | -25.43 ± 1.515 | -25.43 ± 1.515 | -25.43 ± 1.515 |
| Day 3 | 115.57 ± 2.616 | 116.10 ± 0.497 | 113.90 ± 0.721 | 0.1340 ± 0.0004 | 0.1342 ± 0.0006 | 0.1341 ± 0.003 | -26.30 ± 1.143 | -24.70 ± 0.787 | -22.17 ± 1.966 |
| Day 7 | 118.63 ± 3.432 | 115.40 ± 0.816 | 113.57 ± 1.111 | 0.1342 ± 0.0004 | 0.1338 ± 0.002 | 0.1342 ± 0.001 | -25.07 ± 1.778 | -26.60 ± 0.216 | -22.83 ± 0.992 |
| Day 14 | 116.09 ± 1.836 | 114.30 ± 0.374 | 115.87 ± 0.519 | 0.1338 ± 0.00089 | 0.1332 ± 0.001 | 0.1337 ± 0.0009 | -28.07 ± 0.591 | -26.57 ± 1.471 | -22.73 ± 1.931 |
| Day 30 | 118.57 ± 0.556 | 115.67 ± 0.125 | 115.81 ± 2.38 | 0.1336 ± 0.0008 | 0.1336 ± 0.001 | 0.1337 ± 0.0008 | -28.43 ± 0.339 | -25.87 ± 0.169 | -23.83 ± 1.804 |

Appendix 3: Cumulative release of optimized nanocrystal containing curcumin and piperine 1

| Time (h) | Cumulative Release Profile (%) (mean ± SD) |  |  |  |
| --- | --- | --- | --- | --- |
|  | Pure Curcumin | FNC1 Curcumin | Pure Piperine | FNC1 Piperine |
| 0.5 | 1.63 ± 0.06969 | 11.21 ± 0.4464 | 1.60 ± 0.1425 | 8.19 ± 0.06695 |
| 1 | 2.28 ± 0.1317 | 23.20 ± 0 | 4.47 ± 0.2365 | 16.81 ± 0.04810 |
| 2 | 3.20 ± 0.1674 | 32.19 ± 0.3366 | 8.84 ± 0.2939 | 24.88 ± 0.1048 |
| 4 | 4.85 ± 0.2085 | 39.77 ± 0.6696 | 14.21 ± 0.4007 | 31.77 ± 0.2836 |
| 6 | 6.68 ± 0.2066 | 47.35 ± 0.3866 | 20.16 ± 0.4174 | 40.64 ± 0.3119 |
| 8 | 8.55 ± 0.2522 | 56.34 ± 0.6696 | 28.39 ± 0.4738 | 52.24 ± 0.5454 |
| 24 | 9.29 ± 0.2933 | 65.18 ± 0.9729 | 39.81 ± 0.5267 | 61.34 ± 0.4625 |
| 48 | 9.77 ± 0.2933 | 71.49 ± 1.3939 | 53.16 ± 0.6801 | 73.43 ± 0.6268 |
| 72 | 10.24 ± 0.2934 | 78.91 ± 1.7856 | 67.96 ± 0.6293 | 84.50 ± 0.6955 |

FNC1 Curcumin denoted the curcumin measured separately from piperine

FNC1 Piperine denoted the piperine measured separately from curcumin

FNC, Nanocrystal containing Curcumin and Piperine; SD, Standard Deviation