Extended Data Fig. 1 Order-to-disorder melt transformation and crystal polymorphism in the PP1/5OBC alloy and -nucleated iPP1. a: Order-to-disorder melt transformation in PP/5OBC and iPP1 via the content of in situ generated -form crystals versus distinct annealing temperatures; b: Crysal polymorphism in PP1/5OBC alloy and -nucleated iPP1; c: Irreversible order-to-disorder melt transformation in PP1/5OBC via sequential annealing and subsequent crystallization procedure (SA-SC); d: Reversible transformation from homogeneous order melt to heterogeneous order melt in -nucleated iPP1 via the SA–SCM procedure.

Extended Data Fig. 2 Nanoscale multiphase morphology of the cryo-fractured PP1/5OBC alloy.

Extended Data Fig. 3 Tensile toughness of PP/PE alloys, PP/PE blends and PP1-2 homopolymers with distinct crystal polymorphism (crystal polymorphism wq/I  and mq/I are controlled by water-quenching (wq), mold-quenching (mq) and isothermal crystallization at a Tc of 126 °C for 30 min from disordered and ordered melts, respectively; PE1: high viscosity PP1/PE alloys of 67PP1/3N/5OBC/25HDPE1-2 and 50HDPE1/5OBC/3N/42PP1; O: only compatibilized and mold-quenched 70PP1/5OBC/25HDPE blend; B: only -nucleated and isothermal crystallized 70PP1/5OBC/25HDPE blend; PE2: high-melt-flow PP2/PE alloys of 67PP2/3N/5OBC/25HDPE1-2; PP/5O: self-toughened PP1/5OBC alloy from ordered melt; PP1: -nucleated high-viscosity PP1 homopolymer from ordered melt, compared with non-nucleated PP1 with wq/I-form crystals; PP2: -nucleated high-melt-flow PP2 homopolymer).

Extended Data Fig. 4 Crystal polymorphism and tensile stress–strain properties of PP/PE alloys and blends. a: Crystal polymorphism of batch internal-mixer-compounded (BC) and continuous extrusion-compounded (EC) 67PP1/4N/5OBC/25HDPE1 alloys (BPOH) followed by isothermal crystallization (IC) and quenching in water (wq) and mold (mq); b: Scalable tensile ultra-ductility of BPOH from an ordered melt and tensile brittleness of BPOH from a disordered melt; c: Unscalable tensile ductility of only compatibilized POH and -nucleated BPH blends; d: Crystal polymorphism of BPOH alloy and BPH and POH blends (IC: isothermal crystallization at a Tc of 126 °C for 30 min; Q: quenching in the mold).

Extended Data Fig. 5 High-impact strength of high viscosity extrusion grade BPOH alloys, reactor multiphase polypropylene  alloys (rHIPP1-2), elastomer-toughened polypropylene (eHIPP1-3; 1: EPR; 2: POE; 3: OBC) and compatibilized high-viscosity PP/PE and PE/PP blends in the literature (C1: traditional OBC; C2: propylene-based di-block copolymer; C3: high-performance OBC; Y1: mass content of ethylene/propylene elastomers in the reactor alloys or compatibilizers in the blends; Y2: melt flow index of the reactor alloys or continuous phase in the blends) .

Extended Data Fig. 6 Multilayered multiphase morphology of the injection molded 50PE1/5OBC/3N/42PP1 alloy (white S: surface layer; yellow S: sheared layer; c: core layers).

Extended Data Fig. 7 Crystal polymorphism of -nucleated high-melt-flow PP2 homopolymer, synergistically toughened high-melt-flow PP2/PE alloys and high-viscosity extrusion grade PP1/PE alloys via compression molding and subsequent isothermal crystallization (115 °C) and mold-quenching (33/42 °C).

Extended Data Fig. 8 Multilayered crystal polymorphisms (Left: -nucleated isotactic polypropylene homopolymer (injection molded and isothermal crystallized iPP2, high-melt-flow grade); Middle: Injection molded and isothermal crystallized 67PP2/4N/5OBC/25HDPE1 alloy; Right: Injection molded and mold-quenched 67PP2/4N/5OBC/25HDPE1 alloy).

Extended Data Fig. 9 High-impact strength of high-melt-flow injection-grade BPOH alloys, reactor multiphase polypropylene alloys (rHIPP3-6) and compatibilized high-melt-flow PP/PE blends in the literature (C4: propylene/ ethylene random copolymer; Y1: mass content of ethylene/propylene elastomers in the reactor alloys or compatibilizers in the blends; Y2: melt-flow index of the reactor alloys or continuous phase in the blends).