Figure 1. (A): QCM-D data of MMT/PLL-CHX film build-up, frequency shifts and dissipations of overtone n=3 were presented. (B): Film thickness versis layer pairs calculated by Qsoft. (C): The variation of Zeta-potentials of (MMT/PLL-CHX)10 during LBL coating process. (D): SEM images of (MMT/PLL-CHX)10 silicon wafer.

Figure 2. CHX release in (A) different concentration of CMS solution and (B) different concentration of S. aureus.

Figure 3. ZOI measurement of (MMT/PLL-CHX)10 multilayer films after deposited in A-C: 0.01M PBS, 105 CFU/mL of S. aureus and 106 CFU/mL of S. aureus. D-E: Changes of ZOI and thickness.

Figure 4. ZOI measurement of (MMT/PLL-CHX)10 multilayer films after deposited in A-D: 0.01M PBS, 100 U/mL of CMS solution, 120 U/mL of CMS solution and 160 U/mL of CMS solution. E-F: Changes of ZOI and thickness.

Figure 5. In vitro antimicrobial assays. (A) bacterial inhibition rate assays. (B) protein leakage experiment.

Figure 6. CCK-8 assay for cellular viability.

Figure 7. Changes in WBC count, CRP, IL-1 and IL-8 levels of rats with different group.

Figure 8. X-ray results after 6 weeks of modeling, A-C: unmodified group, (MMT/PLL-CHX)10 group, SHAM group.

J: X-ray score with different group. Bacteriological examination in Kirschner wires, D-F: unmodified group, (MMT/PLL-CHX)10 group, SHAM group. K: bacteria recovered from implanted K-wire. Fluorescent microscopy images of live staining of S. aureus adhesions on G-I: unmodified group, (MMT/PLL-CHX)10 group, SHAM group.

Figure 9. (A) 6 weeks after modeling, micro-CT 3D images of the bone specimens. New bone formation around the Kirschner wires. (B) bone mineral density (BMD). (C) trabecular bone number (Tb.N). (D) percent bone volume (BV/TV). (E) connectivitydensity (Conn.D). (F) trabecularthickness (Tb.Th). (G) trabecular separation (Tb.Sp).

Figure 10. The tibia specimens bending test with different group. (A) the Maximum load. (B) the Resilience. (C) the Resilience stiffness.

Figure 11. Bone tissue HE staining and Masson trichrome, respectively: (A,D) unmodified group, (B,E) (MMT/PLL-CHX)10 group and (C,F) SHAM group.