Supporting Information

Structured illumination flowmetry

Haichun Liu1, Jerker Widengren1

1Department of Applied Physics, KTH Royal Institute of Technology, S-106 91, Stockholm, Sweden

Section 1: Er-Ho upconversion emission mechanism

Figure S1. Model of electronic states and their major transitions in NIR-II NaErF4:Ho@NaYF4 core-shell UCNPs excited at ~1500 nm. GSA, ESA, CR and ET denote ground state absorption, excited state absorption, cross-relaxation and energy transfer, respectively. Emission at ~1180 nm indicated by a red line.

Following the electronic state model for generation of upconversion emission of NaErF4:Ho@NaYF4 core-shell UCNPs (at 1180 nm from Ho3+ ions) under excitation of 1500 nm light, as is depicted in Figure S1, the upconversion processes can be modeled using the following set of rate equations:

Er3+(4I15/2): dn1dt=-σGSAIexc(t) hvexcn1+n3τ3+n4τ4+n5τ5+n6τ6+ c1n2n3+ c2n2n4+ wET1n2n7+wET2n3n7 +wET3n6n7+wET5n5n7	                                                                                      (S1)

Er3+(4I13/2): dn2dt=σGSAIexc(t)hvexcn1-σESA1Iexc(t)hvexcn2+β3n3- c1n2n3- c2n2n4- wET1n2n7 (S2)

Er3+(4I11/2): dn3dt=-σESA2Iexc(t)hvexcn3-β3n3+β4n4-n3τ3- c1n2n3 -wET2n3n7	               (S3)

Er3+(4I9/2): dn4dt=σESA1Iexc(t)hvexcn2-σESA3Iexc(t)hvexcn4- c2n2n4-n4τ4-β4n4+β5n5                    (S4)

Er3+(4F9/2): dn5dt=σESA2Iexc(t)hvexcn3+ c1n2n3-n5τ5-β5n5+β6n6+wET4n6n8-wET5n5n7   (S5)

Er3+(4S3/2 /2H11/2): dn6dt=σESA3Iexc(t)hvexcn4+ c2n2n4-β6n6-n6τ6 -wET3n6n7	-wET4n6n8      (S6)

Ho3+(5I8): dn7dt=n9τ9+n13τ13+n12τ12- c3n7n13- wET1n2n7-wET2n3n7-wET3n6n7-wET5n5n7

(S7)

Ho3+(5I7): dn8dt=β9n9+ c3n7n13+wET1n2n7-wET4n6n8	                                                 (S8)

Ho3+(5I6): dn9dt=-β9n9+β10n10-n9τ9+wET2n3n7+wET4n6n8 	                                     (S9)

Ho3+(5I5): dn10dt=-β10n10+β11n11                                                                                      (S10)

Ho3+(5I4): dn11dt=c3n7n13-β11n11+β12n12                                                                       (S11)

Ho3+(5F5): dn12dt= wET5n5n7-n12τ12-β12n12+β13n13                                                          (S12)

Ho3+(5F4 /2S2): dn13dt=wET3n6n7- c3n7n13-β13n13-n13τ13                                                (S13)

Here, ni (i=1 to 6) represent the populations of Er3+ ions in the 4I15/2, 4I13/2, 4I11/2, 4I9/2, 4F9/2, 2H11/2/4S3/2 states, respectively, and nj (j=7 to 13) denote the populations of Ho3+ ions in the 5I8, 5I7, 5I6, 5I5, 5I4, 5F5, 5F4/2S2 states, respectively. τi (i=2, 3, 4, 5, 6, 8, 9, 10, 11, 12, 13) represent the radiative decay lifetimes of the 4I13/2, 4I11/2, 4I9/2, 4F9/2, 2H11/2/4S3/2 states of Er3+ and the 5I7, 5I6, 5I5, 5I4, 5F5, 5F4/2S2 states of Ho3+, respectively. βi (i=3, 4, 5, 6, 9, 10, 11, 12, 13) represents the non-radiative decay rates of the 4I11/2, 4I9/2, 4F9/2, 2H11/2/4S3/2 states of Er3+ and the 5I6, 5I5, 5I4, 5F5, 5F4/2S2 states of Ho3+, respectively. wETi (i=1 to 5) denote the coefficients of the interionic energy transfer processes: 4I13/2 (Er3+) + 5I8 (Ho3+)→4I15/2 (Er3+) + 5I7 (Ho3+), 4I11/2 (Er3+) + 5I8 (Ho3+)→4I15/2 (Er3+) + 5I6 (Ho3+), 2H11/2/4S3/2 (Er3+) + 5I8 (Ho3+)→4I15/2 (Er3+) + 5F4/2S2 (Ho3+), 2H11/2/4S3/2 (Er3+) + 5I7 (Ho3+)→4F9/2 (Er3+) + 5I6 (Ho3+), 5I8 (Ho3+) + 4F9/2 (Er3+)→5F7 (Ho3+) + 4I15/2 (Er3+), respectively. σGSA denotes the absorption cross-section for the ground-state absorption process of Er3+: 4I15/2→4I13/2 at 1500 nm. Iexc(t) is the excitation intensity function at 1500 nm. h is the Planck’s constant. vexc is the frequency of excitation photon at 1500 nm. σESA1, σESA2, and σESA3 denote the absorption cross-sections for the excited state absorption processes 4I13/2→4I9/2, 4I11/2→4F9/2, 4I9/2→2H11/2/4S3/2, respectively, of Er3+ at ~1500 nm. ci (i=1 to 3) denote the coefficients of the cross-relaxation processes: 4I13/2 (Er3+) + 4I11/2 (Er3+)→4I15/2(Er3+) + 4F9/2 (Er3+), 4I13/2 (Er3+) + 4I9/2 (Er3+)→4I15/2(Er3+) + 2H11/2/4S3/2 (Er3+), 5I8 (Ho3+) + 5F4/2S2 (Ho3+)→5I4 (Ho3+) + 5I7 (Ho3+), respectively.

Table S1 Values of key photophysical parameters used in the simulations of the Er3+/Ho3+ co-doped UCNP photodynamics

| σGSA(cm2) |  | σESA1(cm2) |  | σESA2(cm2) |  | σESA3(cm2) | wET1(cm3s-1) | wET2(cm3s-1) | wET3 (cm3s-1) | wET4(cm3s-1) | wET5(cm3s-1) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 8×10-21 | 8×10-20 |  | 4×10-20 |  | 8×10-20 |  | 1.8×10-16 | 1.8×10-16 | 1.8×10-16 | 1.8×10-16 | 1.8×10-16 |
| β3(s-1) | β4(s-1) |  | β5(s-1) |  | β6(s-1) |  | β9(s-1) | β10(s-1) | β11(s-1) | β12(s-1) | β13(s-1) |
| 5×102 | 5×104 |  | 2×104 |  | 8×103 |  | 8×103 | 1×104 | 2×104 | 3×104 | 3×104 |
| τ2(μs) | τ3(μs) |  | τ4(μs) |  | τ5(μs) |  | τ6(μs) | τ8(μs) | τ9(μs) | τ10(μs) | τ11(μs) |
| 7.5×103 | 1×103 |  | 200 |  | 200 |  | 100 | 7.5×103 | 1×103 | 50 | 50 |
| τ12(μs) | τ13(μs) |  | c1(cm3s-1) |  | c2(cm3s-1) |  | c3(cm3s-1) |  |  |  |  |
| 150 | 100 |  | 3×10-18 |  | 3×10-18 |  | 3×10-18 |  |  |  |  |

Figure S2 Temporal UCL response (from a NaErF4:Ho@NaYF4 core-shell UCNP) to a sinusoidally modulated excitation intensity.

Figure S3 Excitation pattern, Iexc(x) (orange), providing a structured illumination, and the resulting UCL pattern, IUCL(x) (blue), from UCNPs (NaErF4:Ho@NaYF4 core-shell UCNPs) as they flow along a channel at a constant velocity (vc=2 mm/s). A phase shift between Iexc(x) and IUCL(x) can be clearly noticed.