Supplementary Materials for

Oxidation-CO2 leaching of spent LiFePO4 for lithium extraction and impurity control

Zhiming Yan1,*, You Wu2, Zepeng Lv3, Shiying Qin4, Mingrui Yang1, Anwar Sattar5, Zushu Li1,**

1, Advanced Materials Manufacturing Centre, WMG, University of Warwick, Coventry, CV4 7AL, UK

2, Sustainable Materials and Manufacturing Group, WMG, University of Warwick, Coventry, CV4 7AL, UK

3, Zhongyuan Critical Metals Laboratory, Zhengzhou University, 450001 Zhengzhou, Henan, PR China

4, Department of Materials, Design and Manufacturing Engineering, University of Liverpool, Liverpool, L69 3BX, UK

5, Recyclus Group, London, W1S 3PW, UK

Corresponding author:

*Zhiming Yan, Zhiming.yan@warwick.ac.uk

**Zushu Li, z.li.19@warwick.ac.uk

Figure S1. The on-site photos of using H2O2-CO2 leaching strategy to recycle the spent LiFePO4.

Figure S2. The SEM images of powder: (a) before leaching; (b) after CO2-H2O2 leaching.

Figure S3. (a) The leachate of LFP without and with impurities. (b) The leachate of LFP with individual impurities. (c) The leachate with impurities after different temperature treatments.

Figure S4. The XRD pattern of the obtained high-purity Li2CO3 product.

Figure S5. The flowchart of H2SO4-H2O2 and CO2-H2O2 strategies used in the environmental and economic analysis.

Figure S6. The mass flow of the CO2-H2O2 strategies used in the environmental and economic analysis. 1000kg of spent LFP as input (data shown in Table S4)

Table S1 Reagents and equipment used in the experiments.

| Reagents | Purity | Company | Country |
| --- | --- | --- | --- |
| LiFePO4 | 99.9% (battery grade) | PI-KEM | UK |
| H2O2 | 32.00% in H2O | Merck Life Science Ltd. | UK |
| CO2 | 99.9% | BOC gas | UK |
| Al foil/Cu foil | 99.95% (battery grade) | Thermo Scientific | UK |
| LiOH | 99.9% | Sigma-Aldrich | USA |
| CaO | 99.0% | Sigma-Aldrich | USA |
| Equipment | Model | Company | Country |
| Water bath | Optima T100 | Grant Instrument | UK |
| pH meter | Seven2Go | METTLER TOLEDO™ | USA |
| ICP-OES | 5110 ICP-OES | Agilent Technologies | USA |
| XRD | Aeris | Malvern Panalytical | UK |
| SEM | JEOL 7800F | JEOL | Japan |
| TEM | Talos F200x | FEI | USA |
| XPS | ESCALAB 250Xi | Thermo Scientific ( VG Scientific ) | USA |
| Pressure reactor | Model 4748 Vessels | Parr Instrument | USA |
| Oil bath | RCT Hotplate Stirrer | IKA | UK |
| Electrochemical Workstation | QL355TP Power Supply | AIM-TTI Instruments | UK |

Table S2. The ICP analysis of the solution, mg/L.

| Concentration, mg/L | Al | Cu | Fe | Li | P | Ca | pH |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Pure LFP leaching at 25 ℃ | 0 | 0 | 325.65 | 2154.30 | 225.45 | / | 7.32 |
| LFP with impurities leaching at 25 ℃ | 3.03 | 95.19 | 60.12 | 2129.25 | 70.14 | / | 7.48 |
| LFP with impurities leachate treated with 2g/L LiOH | / | 72.72 | 4.04 | 2712.71 | 68.68 | / | 9.89 |
| LFP with impurities leachate treated with 4g/L LiOH | / | 58.58 | 2.02 | 3273.27 | 64.64 |  | 10.85 |
| LFP with impurities leachate treated with 10g/L CaO | / | 35.35 | 3.03 | 2122.12 | 35.35 | 56.56 | 10.18 |
| LFP with impurities leachate treated with 20g/L CaO | / | 24.24 | 2.02 | 2118.6 | 20.20 | 59.59 | 12.50 |
| LFP with impurities leachate treated at 100℃ | / | 57.57 | 7.07 | 2117.97 | 74.74 | / | 8.99 |
| LFP with impurities leachate treated at 125 ℃ | / | 54.54 | 4.04 | 2099.18 | 72.72 | / | 9.19 |
| LFP with impurities leachate treated at 150 ℃ | / | 56.56 | 3.03 | 2022.00 | 46.46 | / | 9.28 |
| LFP with impurities leachate treated at 175 ℃ | / | 29.29 | 1.01 | 1900.10 | 4.04 | / | 9.48 |

Table S3. The ICP analysis of the Li2CO3 products after impurities removal

|  | Element | Li | Fe | P | Cu | Al | Ca | Mg |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Test 1 | Concentration, mg/L | 2531.89 | 0.17 | 3.32 | 0.39 | nd | 1.069 | nd |
|  | Content, wt.% | 18.755% | 0.001% | 0.025% | 0.003% | / | 0.008% | / |
| Test 2 | Concentration, mg/L | 3567.79 | 0.67 | 4.61 | 0.828 | nd | 1.427 | nd |
|  | Content, wt.% | 18.680% | 0.004% | 0.024% | 0.004% | / | 0.007% | / |
| Test 3 | Concentration, mg/L | 4155.92 | 0.38 | 4.54 | 0.567 | nd | 1.116 | nd |
|  | Content, wt.% | 18.720% | 0.002% | 0.020% | 0.003% | / | 0.005% | / |

nd: The element(s) measured are not present at the detection limit.

During the measurements, three samples (sample 1: 135mg, sample2: 191mg; sample 3: 222mg) are dissolved in 10 ml of 5M/L HNO3 then diluted for ICP-OES analysis.

Purity is defined as the ICP measured value of Li divided by the theoretical one.

For Li2CO3, theoretically Li content is 6.941/(6.941*2+12+16*3)=18.789%;

The purity of the final Li2CO3 product is defined as follows:

Purity of Li2CO3=measured Li content theoretical Li content

Then the Li2CO3 purity of samples 1-3 is 99.82%, 99.42%, 99.63%, respectively.

By calculating the mean and standard deviation, we can see that the purity of the sample is around 99.62%, and the error is within ±0.16%.

Table S4. The mass balance table of the CO2-H2O2 strategies used in the environmental and economic analysis. 1000kg of spent LFP packs as input.

| Materials | Materials | Weight, kg | Materials | Materials | Weight, kg |
| --- | --- | --- | --- | --- | --- |
| LFP battery pack | Cathod powder | 298.00 | Black Mass | Residue | 440.73 |
| LFP battery pack | Anode powder | 153.00 | Black Mass | Leachate | 15.37 |
| LFP battery pack | Binder | 9.00 | Water | Leachate | 2406.35 |
| LFP battery pack | Copper | 82.00 | H2O2 (30%) | Leachate | 424.50 |
| LFP battery pack | Aluminum | 121.00 | CO2 | Leachate | 121.78 |
| LFP battery pack | Steel | 179.00 | H2O2 (30%) | Released oxygen | 45.60 |
| LFP battery pack | Electrolyte | 81.00 | Residue | Carbon | 145.35 |
| LFP battery pack | Plastic | 19.00 | Residue | FePO4 | 270.56 |
| LFP battery pack | Others | 58.00 | Residue | Impurities | 24.72 |
| Cathod powder | Black mass | 283.10 | Leachate | Preciptation | 13.88 |
| Anode powder | Black mass | 145.35 | Leachate | Recovered Cu | 0.39 |
| Binder | Black mass | 8.55 | Leachate | Purified solution | 2953.73 |
| Copper | Black mass | 4.10 | Purified solution | Recycled Water | 2854.50 |
| Aluminum | Black mass | 6.05 | Purified solution | Battery Li2CO3 | 62.20 |
| Steel | Black mass | 8.95 | Purified solution | Decomposed CO2 | 37.03 |
| Cathod powder | Other recycling sector | 14.90 |  |  |  |
| Anode powder | Other recycling sector | 7.65 |  |  |  |
| Binder | Other recycling sector | 0.45 |  |  |  |
| Copper | Other recycling sector | 77.90 |  |  |  |
| Aluminum | Other recycling sector | 114.95 |  |  |  |
| Steel | Other recycling sector | 170.05 |  |  |  |
| Electrolyte | Other recycling sector | 81.00 |  |  |  |
| Plastic | Other recycling sector | 19.00 |  |  |  |
| Others | Other recycling sector | 58.00 |  |  |  |

Table S5 Materials Required for Recycling 1 kg of Spent LFP Battery Packs Using H2SO4-H2O2 and CO2-H2O2 strategies.

| Reagent (kg/kg spent pack) | H2SO4-H2O2 | CO2-H2O2 |
| --- | --- | --- |
| Carbon Dioxide | - | 0.122 |
| Hydrogen Peroxide | 0.477 | 0.127 |
| Sodium Hydroxide (NaOH) | 0.015 | - |
| Sulfuric Acid (H2SO4) | 0.122 | - |
| Soda Ash (Na2CO3) | 0.122 | - |

Table S6 Energy Input and Water Consumption for Recycling 1 kg of Spent LFP Battery Packs Using H2SO4-H2O2 and CO2-H2O2 strategies.

| Energy and Water | H2SO4-H2O2 | CO2-H2O2 |
| --- | --- | --- |
| Diesel (MJ) | 0.60 | 0.60 |
| Natural gas (MJ) | 2.50 | 2.50 |
| Electricity (MJ) | 0.13 | 0.30 |
| Water consumption (L/kg) | 2.20 | 1.39 |

Table S7 Equipment Selection for H2SO4-H2O2 and CO2-H2O2 strategies.

| Equipment unites | H2SO4-H2O2 | CO2-H2O2 |
| --- | --- | --- |
| Conveyor | 5 | 5 |
| Crusher | 1 | 1 |
| Calciner | 1 | 1 |
| Gas treatment | 1 | 1 |
| Wet granulator | 1 | 1 |
| Density separator | 1 | 1 |
| Crystallizer | - | 1 |
| Leaching tank | 1 | 1 |
| Filter press | 4 | 3 |
| Precipitation tank | 2 | 1 |
| Pump | - | 1 |
| Mixing tank | 1 | 1 |
| Dryer | 1 | 1 |
| Wheel loader | 1 | 1 |
| Water treatment | 4 | 1 |
| Screen, vibrating | - | 1 |
| Electrowinning cell | - | 1 |
| Heat treatment furnace | - | 1 |

Table S8 Life-Cycle Assessment Results for H2SO4-H2O2 and CO2-H2O2 strategies.

| Cost per kg feedstock processed | H2SO4-H2O2 | CO2-H2O2 |
| --- | --- | --- |
|  | $ 1.23 | $ 1.02 |
| Energy use in MJ per kg feedstock processed |  |  |
| Total Energy | 6.915 | 6.303 |
| Fossil fuels | 6.535 | 5.944 |
| Coal | 3.155 | 2.834 |
| Natural gas | 5.38 | 5.128 |
| Petroleum | 3.2 | 3.183 |
| Water use in gallon | 1.2 | 0.8 |
| Total Emissions in g per kg feedstock processed |  |  |
| VOC | 0.108 | 0.102 |
| CO | 0.439 | 0.425 |
| NOx | 0.911 | 0.908 |
| PM10 | 0.058 | 0.05 |
| PM2.5 | 0.05 | 0.046 |
| SOx | 0.206 | 0.118 |
| BC | 0.02 | 0.021 |
| OC | 0.012 | 0.012 |
| CH4 | 1.077 | 0.986 |
| N2O | 0.011 | 0.01 |
| CO2 | 569 | 523 |
| CO2 (w/ C in VOC & CO) | 570 | 524 |
| GHGs | 605 | 557 |
| Revenue per kg feedstock processed | $ 1.63 | $ 1.66 |
| Profit | 0.40 | 0.64 |

Table S9 Annual Cost Details for Different Recycling Plants with a Throughput of 50,000 Tons of LFP Spent Battery Packs

|  | H2SO4-H2O2 | CO2-H2O2 |
| --- | --- | --- |
| I. Fixed capital investment | $85,121,948 | $84,036,622 |
| A. Inside battery limits (ISBL) plant cost | $45,157,532 | $46,480,432 |
| Purchased Equipment | $14,111,729 | $18,592,173 |
| Equipment erection | $7,055,864 | $11,155,304 |
| Piping | $8,467,037 | $3,718,435 |
| Instumentation and control | $4,233,519 | $3,718,435 |
| Electrical | $2,822,346 | $2,788,826 |
| Civil | $4,233,519 | $3,718,435 |
| Structures and buildings | $2,822,346 | $1,859,217 |
| Lagging and paint | $1,411,173 | $929,609 |
| B. Offsite battery limits (OSBL) cost | $18,063,013 | $18,592,173 |
| C. Design and Engineering Cost | $15,805,136 | $13,014,521 |
| D. Contingency | $6,096,267 | $5,949,495 |
| II. Working Capital | $4,232,040 | $3,819,336 |
| III. Total Capital Investment | $89,353,989 | $87,855,958 |
| IV. Cash cost of production (CCOP), $/year | $25,020,915 | $20,073,712 |
| A. Variable costs of production (VCOP) | $12,971,337 | $8,102,087 |
| Raw Materials | $10,414,836 | $4,793,002 |
| Utilities | $800,562 | $1,990,972 |
| Consumables | $312,445 | $143,790 |
| Effluent disposal | $1,235,197 | $1,078,462 |
| Packaging and shipping | $208,297 | $95,860 |
| B. Fixed costs of production (FCOP), $/year | $12,049,578 | $11,971,625 |
| Labor costs | $3,456,000 | $3,456,000 |
| Operating labour | $1,843,200 | $1,843,200 |
| Supervision and management | $460,800 | $460,800 |
| Direct salary overhead | $1,152,000 | $1,152,000 |
| Maintenance | $2,257,877 | $2,324,022 |
| Property taxes and insurance | $632,205 | $650,726 |
| Rent of land and/or buildings | $1,264,411 | $1,301,452 |
| General plant overhead | $3,164,216 | $3,074,765 |
| R&D costs | $529,075 | $543,591 |
| Selling and marketing costs | $388,741 | $284,774 |
| General and administrative (G&A) costs | $2,246,400 | $2,246,400 |
| Allocated environmental charges | $632,205 | $650,726 |
| Running license fees and royalty payments | $388,741 | $284,774 |
| Capital charges | $253,922 | $229,160 |
| Interest on fixed capital | $- | $- |
| Interest on working capital | $253,922 | $229,160 |
| V. Annualized Capital Cost (ACC), $/year | $13,853,205 | $8,403,662 |
| VI. Total Cost of Production (TCOP), $/year | $38,874,120 | $28,477,374 |

Table S10 Mass Proportion, Recycling Yield, and Price of Recycled Materials in Spent LFP Battery Packs

| Main component in a pack | Price $/kg [1] | Composition | Recycling yield |
| --- | --- | --- | --- |
| LiFePO4 | 6.10 [2] | 29.80% | 95.0% |
| Li2CO3 | 13.38 [3] | / | / |
| Graphite | 2.07 [4] | 15.30% | 95.0% |
| Copper | 6.67 [5] | 8.20% | 95.5% |
| Aluminum | 1.54 [6] | 12.10% | 95.0% |
| Plastic | 0.25 [7] | 1.90% | 95.0% |

[1] GBP to USD exchange rate: 1.26; RMB to USD exchange rate: 0.14.

[2] https://www.100ppi.com/vane/detail-1312.html, 20/05/2024.

[3] https://carboncredits.com/why-lithium-prices-are-plunging-and-what-to-expect/, 20/05/2024.

[4] https://hq.smm.cn/h5/graphite-price, 20/05/2024.

[5] https://scraplocal.co.uk/scrap-metal-prices, 20/05/2024.

[6] https://scraplocal.co.uk/scrap-metal-prices, 20/05/2024.

[7] https://blog.recycleduklimited.com/current-plastic-recycling-prices, 20/05/2024.