Supporting information Achieving Highly Anisotropic Three-Dimensional, Lightweight, and Versatile Conductive Wood-Graphene Composite

Li Wang1,2,†, Xiao Tao Zhang3,4,†, Xi Ming Wang1,4,†, Zhang Jing Chen5, Yu Kun Ren6,

Sun Guo Wang7, Zhe Wang1, Li Li Li1, Jian Fang Yu1,*, Qin He1, Li Hong Yao1, Yi Nan Hao1, Li Jun Ding3, Qi Li1, Hua Qiong Duo1, WHITE Marshall5

(1. College of Material Science and Art Design, Inner Mongolia Agricultural University, Hohhot, China. 2. Analysis and Testing Center, Inner Mongolia University of Science & Technology, Baotou, China. 3. College of Science, Inner Mongolia Agricultural University, Hohhot, China. 4.Inner Mongolia Key Laboratory of Sandy Shrubs Fibrosis and Energy Development and Utilization, Hohhot, China. 5.Department of Sustainable Biomaterials, Virginia Polytechnic Institute and State University, Blacksburg, VA, USA. 6. Bioimaging Research, Sanofi Global R&D, Framingham, MA,USA. 7. Sungro Bioresource & Bioenergy Technologies Corp, Alberta, Canada.)

*Correspondence should be addressed to Jian Fang Yu.

Email: yjf_112@163.com

† Contributed equally to this paper.

(a)

(b)

(c)

(d)

(e)

(f)

(g)

(a)

(b)

(c)

(d)

(e)

(f)

(g)

Figure S1. SEM images of prepared GO from various graphite meshes. a, 100 mesh, b, 325 mesh, c, 1200 mesh, d, 4000 mesh, e, 8000 mesh, f, lateral size distribution of synthesized GO based on graphite mesh, and g, C:O ratio in the synthesized GO based on graphite mesh.

(a)

(b)

(c)

(d)

(a)

(b)

(c)

(d)

Figure S2. Optimizing the preparation influencing factors. a, Effects of GO concentration. b, Effects of AA concentration. c, Effects of reaction time. d, Effects of reaction temperature.

As the pore distribution in cross section is the most developed, we obtained the optimum process of conductive wood. From Figure S2, the variation of surface resistivity was higher than volume resistivity. With the increase of concentration of GO (Figure S2a) and AA (Figure S2b), both the surface resistivity and volume resistivity were all decreased at first, and then maintained a stable trend.

It can be seen from Figure S2 that when GO and AA concentration were both 5 mg/mL, reaction time was 4 h, and reaction temperature was 100 oC, the surface resistivity and volume resistivity reached the minimum values, 120.0 Ω·cm and 36.7 Ω·cm, respectively. This is probably due to an excessive dose of GO may accumulate a lot on the surface of the sample, seriously decreased the carrier mobilities of AA which led to lose the reducing ability of AA.

(a)

(b)

(c)

(a)

(b)

(c)

Figure S3. Higher magnification SEM images in the cross-section orientation. a, natural wood. b, GO/wood. and c, conductive wood.

Figure S4. XPS survey scan of natural wood and conductive wood.

(a)

(b)

(a)

(b)

Figure S5. TGA curves of natural wood and conductive wood. a, Thermogravimetric analysis results of natural wood and conductive wood. b, derivative weight % against temperature for natural wood and conductive wood.

Video.mp4 (Submitted online as Video.mp4)

Video S1  Demonstration of conductive effect in 3D directions of conductive wood.

Table S1. The surface properties of natural wood, conductive wood and GO.

| Sample | Total Intrusion Volume (mL·g-1) | Total Pore Area (m2·g-1) | Median Pore Volume (nm) | Median Pore Diameter (Area), nm | Average Pore Diameter (nm) | Bulk Density at 0.44 psia (g·mL-1) | Apparent (skeletal) Density, g·mL-1 | Porosity (%) | Stem Volume Used(%) | BET surface area (m2·g-1) | Pore size (nm) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Natural wood | 1.7696 | 12.7 | 2782.9 | 37.1 | 442.6 | 0.4125 | 1.1315 | 61.3928 | 45 | 2.1242 | 12.2399 |
| Conductive wood | 1.4053 | 4.187 | 12953.8 | 1048.3 | 1690.5 | 0.4369 | 1.528 | 73.0018 | 55 | 1.2273 | 15.6441 |
| GO | ─ | ─ | ─ | ─ | ─ | ─ | ─ | ─ | ─ | 131.29 | 23.911 |

Table S1 presented the surface characteristics of natural wood and conductive wood. Total intrusion volume and total pore area of natural wood is larger than that of conductive wood. The slight increase in apparent (skeletal) density implied a uniform distribution of thin layers of rGO in wood channels. Average pore diameter and porosity of natural wood was also higher than conductive wood (Figure. 3a). Significantly increase of median pore diameter revealed that rGO largely distributed in mesopores and partial macropores, such as cell lumens and pit voids.

Table S2. Summary of the carrier type, Hall coefficient, carrier density, carrier concentration, and resistivity of conductive wood in cross-section, radial section, and tangential section orientation.

| Sample name | Cross section | Radial section | Tangential section |
| --- | --- | --- | --- |
| Carrier type | n | n | n |
| Hall coefficient (cm3·C-1) | -9110.8 | -31044.7 | -43034.5 |
| Carrier density (cm2·Vs-1) | 247.8 | 52.4 | 13.3 |
| Carrier concentration (1013 vm4) | 6.86 | 2.01 | 1.45 |
| Resistivity (Ω·cm) | 36.7 | 591.4 | 3231.3 |

Table S3. Summary of reported literatures on conductive wood in recent years.

| Composite | Technique | Properties | Reference |
| --- | --- | --- | --- |
| Hierachical porous graphene/wood using CO2 laser scribing | CO2 laser scribing | Non-anisotropic properties. For steam generation | Adv. Mater., 2017, 29, 1702211 |
| Surface coated graphene | Drop- casting aqueous GO solution(0.3 wt%) on the surface of the radially cut wood and set aside for the GO solution to dry naturally. | Surface coating only. For steam generation | ACS Appl. Mater. Interfaces, 2017, 9, 7675-7681 |
| Wood cellulose and graphene oxide fibers | Wet spinning of the GO-NFC hybrid microfiber | Conductivity along one direction | NPG Asia Materials, 2015, 7, e150 |
| Mesoporous Wood-derived Carbon | Obtained wood slabs were transferred into a tube furnace and stabilized at 260 oC for 8h in air before further carbonized at 1000 oC under flowing argon for 2h. | Thin electrode of Imm thickness. Used in Na-ion battery | Adv. Energy Mater., 2016, 6, 1600377 |
| Chemically Crushed Wood Cellulose Fiber | Preparation of paper from wood pulp. Subsequently the paper was stabilized at 240 oC for 8h before being further carbonized at 1000 oC under argon for 2h. | Carbonization of wood fiber paper. Used as Na-ion battery electrode | ACS Appl. Mater. Interfaces, 2015, 7, 23291-23269 |
| Carbonized Mesoporous Wood Fiber | Preparation of paper from wood pulp. Wood fiber electrode was transfered into a tube furnace and stabilized at 240 oC for 8h before being further carbonized at 1000 oC under argon for 2h. | Carbonization of wood fiber paper. Used as Li-S battery electrode | ACS Appl. Mater. Interfaces, 2017, 9, 14801-14807 |
| Fexible Wood Transverse Section Slice and Reduced Grahene Oxide | WTSSs were immersed in aqueous GO dispersions 1 mg mL-1 for 5min and dried naturally at room temperature. Reduction with hydraine hydrate. | Wood used was 180 μm in thickness. Used as solidstate supercapactior | Electron. Mater. Lett., 2015, 11(4), 505-543 |
| Microfiber of Graphene Oxide Templated Carbonization of Nanofibrillated Cellulose | Prepared via extrusion of gel. The heating process performed at a temperature ramped from room temperature to 400 oC with a heating rate of 30oC/h, then further increase to 1000oC with a heating rate of 200oC/h. After that, the samples are held for 2h under 1000oC | Fiber-like product. Used in Li-ion battery | Adv. Funct. Mater., 2014, 24, 7366-7372 |
| Mesoporous, Three-Dimensional Wood Membrane | The wood slices were immersed in the PdCl2solution and heated for 12h at 80oC to obtain the Pd NPs/wood membrane | Wood thickness was 0.1mm. Used of expensive precusor Pd. Used as water treatment | ASC Nano 2017, 11, 4275-4282 |
| Wood-Derived Carbon Composite Monoliths | Wood cork was heated to 600oC and maintained at this temperature for 1h, then heated to 1000oC, and held st this temperature for 3h | Mechanical property was not improved (3.28 MPa at density of 0.151g/cm3 | ACS Appl. Mater. Interfaces, 2017, 9, 25, 21371-21381 |
| Highly anisotropic, multichannel wood carbon with optimized heteroatom doping | The wood slices were impregnated with trithiocyanuric acid were transferred into a tube furnace for stabilization at 150 oC for 3h before further carbonized at 950oC for 2h under N2 flowing with ramp rate of 3 oC min-1. | Mechanical properties was not investigated. Tremendous volume shrinkage after calcination | Carbon, 2018, 130, 532-543 |
| Lightweight anisotropic foams based on nanocellulose and graphene oxide | Defibrillation process on soft wood pulp | 180kPa with 90% strain. Light weight foam using cellulose fiber and graphene oxide | Nature Nanotechnology, 2015, 10, 277-283 |
| Laser-Induced Graphene from Wood Impregnated with Metal Salts | Cedar monolith was scibed by a 10.6μm CO2 Laser under Ar atmosphere at ambient temperature and pressure. | Surface conductive. Use of high power laser to induce graphene. Used as eletrocatalyst | ACS Appl. Nano Mater., 2018, 1, 5053-5061 |