Supplementary Information

Optical spin readout of a silicon color center in the telecom L-band

Shuyu Wen,1,2,3 Gregor Pieplow,4 Junchun Yang,1,5 Kambiz Jamshidi,5 Manfred Helm,1,5 Jun-Wei Luo,2,3 Tim Schröder,4 Shengqiang Zhou,1* & Yonder Berencén1**

1Helmholtz-Zentrum Dresden-Rossendorf, Institute of Ion Beam Physics and Materials Research, Bautzner Landstrasse 400, 01328 Dresden, Germany

2State Key Laboratory of Superlattices and Microstructures, Institute of Semiconductors, Chinese Academy of Sciences, Beijing 100083, China

3Center of Materials Science and Optoelectronics Engineering, University of Chinese Academy of Sciences, Beijing 100049, China

4Humboldt-Universität zu Berlin, Department of Physics, 12489 Berlin, Germany

5Technische Universität Dresden, 01062 Dresden, Germany

Corresponding authors: s.zhou@hzdr.de* y.berencen@hzdr.de**

Supplementary Figure S1 | Temperature and excitation power dependence of the photoluminescence (PL) spectra of an ensemble of C centers in silicon. a, Temperature-dependent PL measurement of the C center emission line under 57 mW of 1064 nm laser excitation. The PL signal from the C center is fully quenched above 45 K. b, Near-linear relationship between 1/temperature and the PL intensity of the C0 line. c, Laser power-dependent PL measurement at 20 K. d, Near-linear relationship between the excitation laser power and the PL intensity of the C0 line.

Supplementary Figure S2 | Line shape comparison between PL and RF-modulated PL of the C center in silicon. Comparison of the photoluminescence (PL) spectrum (black) and the differential PL signal ΔPL = PLRF-ON - PLRF-OFF (magenta) under 965 MHz RF excitation and 1064 nm laser excitation. Both the C₀ and C₁ emission lines exhibit optically detected magnetic resonance (ODMR).