Supplementary Information for

Digital Techniques Assisted in Tailoring Electrode Structure to Optimize Electrode Kinetics

Heng Huang1, Zhifu Zhou2, Wei-Tao Wu3, Lei Wei4, Chengzhi Hu1, Jiaxuan Ma1,

Linsong Gao5, Yang Li1, Yubai Li1*, Yongchen Song1*

1. Key Laboratory of Ocean Energy Utilization and Energy Conservation of Ministry of Education, Dalian University of Technology, Dalian 116023, China

2. State Key Laboratory of Multiphase Flow in Power Engineering, Xi'an Jiaotong University, Xi'an 710049, China

3. School of Mechanical Engineering, Nanjing University of Science and Technology, Nanjing 210094, China

4. Department of Mechanical and Energy Engineering, Southern University of Science and Technology, Shenzhen 518055, China

5. School of Mechanical Engineering and Mechanics, Xiangtan University, Xiangtan 411105, China

*Corresponding author: liyubai2021@126.com, songyc@dlut.edu.cn

Fig.S1. CT image segmentation based on full width at half maxima method (FWHM). (a) and (b) Grayscale variations along paths crossing AM and Pore segments. The inset in (b) depicts AM particle sizes across different grayscale ranges. (c) and (d) show regions segmented using the watershed algorithm and FWHM method. Both methods yield nearly identical results.

Fig. S2. Schematic of (a) particle model construction. (b) CBD addition.

Fig. S3. SOL distribution of the electrodes at the end moment of discharge. (a) 30 m-LP-LC, (b) 30 m-LP-HC, (c) 30 m-SP-LC, (d) 30 m-SP-HC, (e) 80 m-LP-LC, (f) 80 m-LP-HC, (g) 80 m-SP-LC, (h) 80 m-SP-HC.

Fig. S4. SOL evolution inside single particles. SOL and SOL gradient distribution of D90 particles along the particle size within the (a-b) 30 m and (c-d) 80 m. (e) Spatial distribution of particle SOL.

Fig. S5. Competitive analysis of SPD and EPD in 80 m-HC. (a), (c), (e), and (g) respectively show the distribution of activation overpotential, equilibrium lithiation potential, solid-phase potential, and liquid-phase potential of 80 m-LP-HC. (b), (d), (f), and (h) respectively show the distribution of activation overpotential, equilibrium lithiation potential, solid-phase potential, and liquid-phase potential of 80 m-SP-HC.

Fig. S6. Results validation of the electrochemical model based on 3D microstructure analysis. (a) Verification of the voltage profile for 30 µm-LP-LC. (b) Validation of the ability of the model to predict the rate performance of different electrode structures using the same input parameters.

Symbols in Fig. S6b represent experimental results measured by Lu et al. [1] and Boyce et al. [2].Dotted lines represent model predictions. The AM_LH _Uncal. data is used to validate the 30 µm-LP-LC; the AM_S1.5 24%_Cal. data is used to validate the 80 µm-SP-HC; and the AM_L2 22.5%_Cal. data is used to validate the 80 µm-LP-HC. Electrodes with porosities of 0.25 and 0.22 are used to validate the 30 µm-LP-LC and the 80 µm-LP-HC, respectively.

Fig. S7. Effects of laser perforation on the physical parameters of (a) large-particle and (b) small-particle electrodes. Mass distribution on (c) patterned and (d) pristine electrodes at 5C.

Fig. S8. Rate capacity of patterned electrodes. Specific capacity of (a) LP and (c) SP before and after patterning. Area capacity of (a) LP and (c) before and after patterning.

Fig. S9. Dynamic evolution of reaction fronts on electrodes. (a) Laser_SP, (b) Laser_LP.

Fig. S10. SOL distribution of initial electrodes with different LP fractions at 3C and 50% DOD. (a) 25%, (b) 50%, (c) 75%. Variation of liquid-phase parameters in the direction of the electrode thickness at the moment of discharge completion. (d) 25%, (e) 75%.

Fig. S11. Comparison of results obtained using the 3D microstructure model and the P2D model for the P0% case. (a) Voltage, (b) SOL, (c) SOL on electrode thickness.

Fig. S12. Heat generation rate and temperature rise curves of P50% at 1C and 25°C for different heat transfer conditions.

Nomenclature

| Variables | Descriptions |
| --- | --- |
| Js | Solid lithium diffusion flux, mol·m-2·s-1 |
| Jp | Current density in the solid phase, A·m-2 |
| Jl | Current density in the electrolyte, A·m-2 |
| Je | Lithium ion diffusion flux in the electrolyte, mol·m-2·s-1 |
| Ce | Lithium ion concentration in the electrolyte, mol·m-3 |
| Ce,0 | Initial lithium ion concentration in the electrolyte, mol·m-3 |
| cs | Solid lithium concentration in the particles, mol·m-3 |
| cs,max | Maximum Solid lithium concentration in the particles, mol·m-3 |
| SOLmin | Initial state of lithiation in the particles |
| SOLmax | Maximum state of lithiation in the particles |
| k | Reaction rate constant, A·m-2.5·mol-1.5 |
| i | Charge exchange current density, A·m-2 |
| ED | Activation energy of solid phase diffusion, kJ·mol-1 |
| Ei | Activation energy of exchange current density, kJ·mol-1 |
| t+ | Transference number of cations |
|  | Pore tortuosity |
| Ac | Cross-sectional area of electrode, m2 |
| VAM | Volume of active material, m3 |
|  | Charge transfer coefficient |
| ct | Overpotential, V |
| T | Operating temperature, K |
| Tinit | Initial electrode temperature, K |
| T∞ | Ambient temperature, K |
| F | Faraday constant, C·mol-1 |
| R | Universal gas constant, J·mol-1·K-1 |
| Uocv | Open circuit voltage, V |
| Ds | Solid phase diffusion coefficient, m2·s-1 |
| Crate | Discharge rate of electrode, h |
| dU/dT | Entropy heat coefficient of active material, V/K |
| s | Solid phase potential, V |
| e | Liquid phase potential, V |
| s | Electrical conductivity of Solid phase, S·m-1 |
| e | Electrical conductivity of Liquid phase, S·m-1 |
| De | Liquid phase diffusion coefficient, m2·s-1 |
| s | Volume fraction of active material |
| l | Porosity of electrode |
| t | Porosity of lumped pore |
| s | Active specific surface area, m-1 |
| seff | Effective electrical conductivity of solid phase, S·m-1 |

Electrochemical model

| Active surface |  |  |
| --- | --- | --- |
| Butler-Volmer equation |  | (1) |
| Interfacial exchange current density |  | (2) |
| Overpotential |  | (3) |
| Particles |  |  |
| Charge conservation |  | (4) |
| Ohm’s law |  | (5) |
| Fick’s second law |  | (6) |
| Fick’s first law |  | (7) |
| Electrolyte |  |  |
| Charge conservation |  | (8) |
| Electrolyte current flux |  | (9) |
| Fick’s second law |  | (10) |
| Electrolyte species flux |  | (11) |

Heat generation model

| Interface source |  |  |
| --- | --- | --- |
| Active heat |  | (12) |
| Reversible heat |  | (13) |
| Volume source |  |  |
| Joule heat of solid phase |  | (14) |
| Joule heat of liquid phase |  | (15) |
| Multi-field coupling |  |  |
| Temperature equation |  | (16) |
| Arrhenius equation |  | (17) |

Boundary conditions

| Current collector/Eletrode | ; |
| --- | --- |
| Separator/Electrode | ; ; |
| Particle/Electrolyte | ; ; ; |

n is directed towards the interior of the domain.

Table.S1. Input parameters.

| Parameter | Value |
| --- | --- |
| Ds / m2·s-1 | Lu et al. [3] |
| s,AM / S·m-1 | 1.039×10-3 [4] |
| s,CBD / S·m-1 | 375 [5] |
| cs,max / mol·m-3 | 32000 |
| t | From Table.S2 |
| SOLmin | 0.2 |
| SOLmax | 1 |
| k / A·m-2.5·mol-1.5 | 5.06 ×10-6 [6] |
| Ce,0 / mol·m-3 | 700 |
|  | 0.5 |
| t+ | 0.38 |
| De / m2·s-1 | Valoen et al. [7] |
| e / S·m-1 | Valoen et al. [7] |
| ED / kJ·mol-1 | 20 [8] |
| Ei / kJ·mol-1 | 30 [8] |
| dU/dT / V·K-1 | Zhao et al. [9] |
| Uocv / V | Lu et al. [1] |
| Tinit / K | 298; 263 & 273 for Section 2.4 |
| R / J·mol-1·K-1 | 8.314 |
| F / C·mol-1 | 96485 |

Table.S2. Parameters of electrodes.

|  | s (%) | l (%) | t (%) | s (m-1) |  | seff (S·m-1) |
| --- | --- | --- | --- | --- | --- | --- |
| 30 m -LP-LD | 53.99 | 37.83 | 82.22 | 0.78 | 2.31 | 0.91 |
| 80 m-LD-LP | 55.24 |  | 84.52 | 0.73 |  |  |
| 30 m-LD-SP | 52.53 |  | 79.69 | 1.50 | 2.34 | 0.516 |
| 80 m-LD-SP | 53.16 |  | 80.76 | 1.50 |  |  |
| 30 m-HD-LP | 53.99 | 20.81 | 43.86 | 0.31 | 7.16 | 47.68 |
| 80 m-HD-LP | 55.22 |  | 46.47 | 0.29 |  |  |
| 30 m-HD-SP | 52.32 |  | 43.64 | 0.80 | 11.6 | 38.18 |
| 80 m-HD-SP | 53.32 |  | 44.42 | 0.79 |  |  |

Supplement Note 1. Computational fluid dynamics simulations of mass diffusion and electron transport

The tortuosity reflects the resistance of Li+ transport in the pore structure, which can be evaluated by solving the concentration equation in the pore phase. Specifically, the material in the pore is driven by a constant concentration difference across the opposing surfaces and satisfies the following equation:

here, D represents the intrinsic diffusion coefficient, assumed to be 1. By solving for the material flux on the surface (Je), the tortuosity parameter of the pore structure is determined.

where ΔCe represents the concentration difference between opposite faces, and L is the Euler length for mass transfer.

The method for determining effective electrical conductivity is similar. Electrons in the solid phase conduct under a constant potential difference, governed by the following equation:

here, σs represents the solid-phase conductivity, it is 1.039×10-3 S·m-1 in the active material and 375 S·m-1 in CBD. The effective conductivity is calculated by averaging the in-plane electronic flux (Jp):

In the above equation, Δs represents the potential difference between opposing surfaces.

Supplement Note 2. Modelling instructions for tortuosity-particle gradation electrodes

In practice, tortuosity-particle gradation electrode (TG) can be fabricated through layered coating techniques. In this work, a random packing program is used to simulate the preparation of TG electrodes, allowing for subsequent electrochemical-thermal simulations, which can save substantial time, financial resources, and effort. The positioning of different particle layers is crucial for simulating TG electrodes, and this can be determined by the ratio of large to small particles. The electrode thickness can be calculated using the following formula:

where, V represents the volume of the electrode, ms is the mass of the electrode, ρs is the theoretical density of NCM622, εs is the volume fraction of the electrode material particles, and A is the cross-sectional area of the electrode.

Assuming that the manufacturing process does not cause the electrode particle size to significantly impact the structure, the proportion of the electrode thickness occupied by particles across different layers is solely related to the electrode mass. Given that both ρs and ​εs are fixed values, it can be inferred: LLP/LSP = VLP/VSP = mLP/mSP. It should also be noted that, to investigate the effects of particle size and tortuosity strategies, this work assumes the same CBD fraction for layers with different particle sizes. The formula is derived based on the specific gravity of the AM:

here, w represents the weight fraction of the active material in the electrode, while ρ(w) denotes the density of the solid mixture as a function of w.

Since the electrode materials in different layers only differ in particle size, with weight fractions remaining consistent, it can be inferred that LLP/LSP = VLP/VSP = mLP/mSP. Thus, in this work, layered electrodes with varying proportions of large particles are obtained by applying constraints on the volume fraction and thickness. Subsequently, TG electrodes are obtained through laser perforation using specific parameters.

Supplement Note 3. Description of the symmetric model

The complex mesh structure required by 3D microstructural models demands significant computational resources. This study utilizes the symmetry of the electrode model to extract a quarter model, thereby avoiding excessive computational load. This approach assumes a zero gradient in material properties across the symmetry planes and applies periodic boundary conditions to define ion and electron fluxes at the outer wall of the pore channels. It is worth noting that no carbon black and binder domain (CBD) is distributed within the pore channels, which are treated as part of the separator. A gradient of diffusion resistance may develop where these channels contact the electrode pores (which contain CBD), leading to notable variations in ion concentration and potential. However, these accumulations arise from changes in diffusion resistance rather than model defects, and similar results are observed in other simulations [10, 11]. To confirm this, a full structural model (shown in Fig. 13a) is constructed by periodically mirroring the model used in this work. The results of the periodic model are then compared with those of the symmetry model. The voltage curve in Fig. 13b shows no significant difference between the two, while Fig. 13c, displaying the liquid-phase potential and ion flux paths, indicates a consistent electric field distribution.

Fig. S13. Description of the symmetric model. (a) Construction of the symmetric model and the full model structure. (b) Comparison of the results between the two models. (c) Ionic potential distribution near the pore channels and the direction of conduction in both models.

References

[1].X. Lu, S.R. Daemi, A. Bertei, M.D. Kok, K.B. O’Regan, L. Rasha, J. Park, G. Hinds, E. Kendrick, D.J. Brett, Microstructural evolution of battery electrodes during calendering, Joule, 4 (2020) 2746-2768.

[2].A.M. Boyce, X. Lu, D.J.L. Brett, P.R. Shearing, Exploring the influence of porosity and thickness on lithium-ion battery electrodes using an image-based model, Journal of Power Sources, 542 (2022) 231779.

[3].X. Lu, A. Bertei, D.P. Finegan, C. Tan, S.R. Daemi, J.S. Weaving, K.B. O’Regan, T.M. Heenan, G. Hinds, E. Kendrick, 3D microstructure design of lithium-ion battery electrodes assisted by X-ray nano-computed tomography and modelling, Nature communications, 11 (2020) 2079.

[4].M. Park, X. Zhang, M. Chung, G.B. Less, A.M. Sastry, A review of conduction phenomena in Li-ion batteries, Journal of power sources, 195 (2010) 7904-7929.

[5].G. Liu, H. Zheng, S. Kim, Y. Deng, A. Minor, X. Song, V.S. Battaglia, Effects of various conductive additive and polymeric binder contents on the performance of a lithium-ion composite cathode, Journal of The Electrochemical Society, 155 (2008) A887.

[6].T. Danner, M. Singh, S. Hein, J. Kaiser, H. Hahn, A. Latz, Thick electrodes for Li-ion batteries: A model based analysis, Journal of Power Sources, 334 (2016) 191-201.

[7].L.O. Valøen, J.N. Reimers, Transport properties of LiPF6-based Li-ion battery electrolytes, Journal of The Electrochemical Society, 152 (2005) A882.

[8].Y. Ji, Y. Zhang, C.-Y. Wang, Li-ion cell operation at low temperatures, Journal of The Electrochemical Society, 160 (2013) A636.

[9].W. Zhao, M. Rohde, I.U. Mohsin, C. Ziebert, H.J. Seifert, Heat generation in NMC622 coin cells during electrochemical cycling: Separation of reversible and irreversible heat effects, Batteries, 6 (2020) 55.

[10].V. De Lauri, L. Krumbein, S. Hein, B. Prifling, V. Schmidt, T. Danner, A. Latz, Beneficial Effects of Three-Dimensional Structured Electrodes for the Fast Charging of Lithium-Ion Batteries, ACS Applied Energy Materials, 4 (2021) 13847-13859.

[11].V. Goel, K.-H. Chen, N.P. Dasgupta, K. Thornton, Optimization of laser-patterned electrode architectures for fast charging of Li-ion batteries using simulations parameterized by machine learning, Energy Storage Materials, 57 (2023) 44-58.