Supplementary Material for

Magnetostrictive Phononic Frequency Combs

Guanqi Ye, Ruitong Sun, Junning Zhao, and Fusheng Ma*

Key Laboratory of State Manipulation and Advanced Materials in Provincial Universities, Institute of Physics Frontiers and Interdisciplinary Sciences, School of Physics and Technology, Nanjing Normal University, Nanjing 210046, China

*Email: phymafs@njnu.edu.cn

Table of Contents

S1. Characterization of mechanical mode

S2. Higher harmonic PFCs

S3. Evolution of IHCs

S4. Tunability of comb tooth spacing for HIHCs

S5. Calculated evolution of HIHCs

S6. Analytical solution of IHCs

S1. Characterization of mechanical mode

For the amorphous ribbon Metglas, the fundamental mechanical mode f0 is expressed as1:

,								(S1)

where L, E, σ, and ρ are the length, Young's modulus, Poisson's ratio, and density. In our simulation2, the parameters are: L = 15 mm, E = 140 GPa, σ = 0.45, ρ = 6800 kg/m3. Fig. S1a shows the comparison of experimental and simulated results, which exhibits a resonance at 150.4 kHz corresponding to fundamental mechanical mode. The Eq. (S1) can be approximated as f0 = 2.25×106/L, where f0 is in Hz and L is in mm, the experimental and simulated f0 as shown in Fig. S1b. Therefore, Metglas with the sizes from mm to cm scale can be used to generate switchable PFCs in MHz to Hz region.

Fig. S1. a Experimentally measured S11 spectrum (blue line) and simulated resonant response spectrum (red line) of the magneto-mechanical macroresonator. Inset shows the fundamental mechanical mode at 150 kHz with normalized stress magnitude: red represents the maximum value and blue represents the minimum value. b f0 as a function of the length of the resonator. Blue dots are experimentally measured results for Hdc around 10 Oe, green line is the calculated results by Eq. (S1), and the red star is the length used in the main text. Yellow background represents the acoustic frequency range from 20 to 20000 Hz.

S2. Higher harmonic PFCs

The higher harmonic IHCs and HIHCs are also observed in the experiment with Hdc = 14.3 Oe, fp = 150 kHz, Vp = 17 V, and fs = 200 Hz.

Fig. S2. Meaured Vin(f) spectra for modes a M1 and d M2. b and e Zoom-in view on IHCs at l = 1, 2, 3, 4, and 5. c and f Zoom-in view on HIHCs at n = 1, 2, 3, 4, and 5.

The IHCs can be described in the manner of lfp ± mfs (l, m = 1, 2, 3, …), while the HIHCs can be described in the manner of (2n - 1) fp/2 ± mfs (m = 1, 2, 3, …, mode M1) and (2n - 1) fp/2 +fs/2 ± mfs (mode M2). Figs. S2a and d show the Vin(f) spectra in the frequency range from 0 to 765 kHz for modes M1 and M2 with Vs = 240 and 300 mV, respectively. Up to five distinct harmonics are observed. Figs. S2b and e show the zoom-in view of IHCs at fp and higher harmonics lfp (l = 2, 3, 4, 5). Figs. S2c and f show a zoom-in view of IHCs near (2n - 1) fp/2 (n= 1, 2, 3, 4, 5). It can be found that the amplitude of the comb teeth decreases with the order of harmonics. The higher harmonic HIHCs switch half a tooth spacing.

S3. Evolution of IHCs

The formation and evolution of IHCs are independent of the period-doubling bifurcation of fp. Fig. S3 shows the formation and evolution of IHCs via three-wave mixing. The spacing of the comb tooth is 200 Hz corresponding to modulating pumping frequency fs. For Vs = 750 mV, the bandwidth can approach 20 kHz with the number of comb teeth exceeding 100.

Fig. S3. a Color plot of measured Vin(f) spectra on the plane of frequency and modulating pumping amplitude Vs for bias magnetic field Hdc = 14.3 Oe, NR pumping amplitude Vp = 20 V, and NR pumping frequency fp = 150 kHz, where Δ = f - fp. b Typical spectra extracted from a. Each curve is shifted 60 dB apart.

S4. Tunability of comb tooth spacing for HIHCs

For HIHCs, the spacing of the comb tooth can be manipulated from 10 Hz to 5000 Hz via the detuning of the modulating pumping frequency.

Fig. S4. The upper and lower limits of comb tooth spacing for HIHCs with Vp = 150 kHz and Hdc = 14.3 Oe. The blue line corresponds to mode M1 (fp/2 ± mfs), and the red line corresponds to mode M2 (fp/2 + fs ± mfs). The comb tooth spacing is a 20 Hz, b 10 Hz, c 4 kHz, and d 5 kHz. The maximum tooth spacing is limited by the nonlinear dynamics of the system and the minimum tooth spacing is limited by the instrument resolution.

S5. Calculated evolution of HIHCs

We perform numerical simulations based on the modified duffing equation as Eq. (2). The simulation parameters are: γ = 7 × 103, f0 = 150.4 kHz, fp = 150 kHz, β = 4 × 1022, Ap = 1.8 × 107, fs = 200 Hz, and A0 = 1 × 107. The color plot of vibration spectra is calculated by increasing modulating pumping amplitude As from 0 to 1 × 1012 with a step size of 1 × 1010 as shown in Fig. S5a. It can be seen that the combs switch several times with the intensity of the modulating pumping Vs. We extract the amplitudes of three comb teeth (Δ = - 0.1, 0, and 0.1 kHz) as shown in Fig. S5b. The results show that the HIHC switches eight times with increasing As from 0 to 1 × 1012.

Fig. S5. a Color plot of calculated spectra in the form of Δ = f - fp/2 as a function of As. b Variation of teeth intensity as a function of As for the first three teeth, corresponding to Δ = - 0.1, 0, and 0.1 kHz in a.

S6. Analytical solution of IHCs

To understand the formation of IHCs, multiple-scale method3,4 is used to solve the modulated Duffing equation

, 			(S2)

where x is displacement, t is time, γ is damping, β is nonlinear coefficient, f0 is eigenfrequency of mechanical mode, Ap is driving amplitude, fp is driving frequency, A0 is bias magnetical force, and Ascos(2πfst) is the modulated linear stiffness.

Setting β = A0 = 0, fp = f0 and using the following variables: τ = 2πf0t, ωs = fs/f0, , , and , the Eq. (S2) can be simplified to

.						(S3)

For ωs → 0, an approximation to the solution of Eq. (S3) is assumed to be

,			(S4)

where τ0 = ε0τ and τn = εnτ are fast time scale and n-order slow time scale, respectively, ε is much less than 1. The time derivatives can be written as

,		(S5)

.				(S6)

Substituting Eqs. (S4), (S5), and (S6) into Eq. (S3), and using the following variables: , , and . Then, equating the same order of ε.

For order ε0:

. 								(S7)

The solution of Eq. (S7) is

, 								(S8)

which represents the forced vibration mode fp of the system.

For order ε1:

.			(S9)

Substituting Eq. (S8) into Eq. (S9), we get

.	(S10)

The resonance terms should be 0 as:

.

In this case, the Eq. (S10) can be simplified to

.				(S11)

The solution of Eq. (S11) is

.					(S12)

The (S12) indicates the generation of comb tooth for f = fp ± fs

For order ε2:

.		(S13)

Substituting Eqs. (S8) and (S12) into Eq. (S13), the solution is

,					(S14)

which indicates the generation of comb tooth for f = fp ± 2fs.

References

1	Landau, L. D. & Lifshitz, E. M. Theory of Elasticity. (Butterworths-Heinemann, 1995).

2	RF Module User’s Guide, COMSOL Multiphysics® v. 6.0. COMSOL AB, Stockholm (Sweden, 2021).

3	Nayfeh, A. H. Perturbation Methods. (John Wiley Sons, New Jersey, 2008).

4	Wang, X. et al. Frequency comb in a parametrically modulated micro-resonator. Acta. Mech. Sin. 38, 521596 (2022).