Remediation of steel processing and dishware enameling wastewater using ammonium carbonate-modified kaolinite clay

John Augustine Lawal *, Ezekiel Oluyemi Odebunmi 2 Folahan Amoo Adekola 3 and Omolola Titilayo Odeyemi 4

1 Department of Chemical Sciences, Achievers University, Owo, Ondo State, Nigeria

2 Department of Chemistry, University of Ilorin, Ilorin, Kwara State, Nigeria

3 Department of Industrial Chemistry, University of Ilorin, Ilorin, Kwara State, Nigeria

4 Department of Chemistry, Kwara State University, Malete, Nigeria

Corresponding author: lawal.ja@achievers.edu.ng

Table S1	Calculation of water quality index (WQI) of steel processing wastewater before adsorption on ACK

| Parameter |  | Observed value(Vi) | Standard value (Vd) | 1/ Sv | Unit weight (Wi) | Quality rating (Qr) | WiQr |
| --- | --- | --- | --- | --- | --- | --- | --- |
| pH |  | 1.3 | 6.5 | 0.153846 | 0.209074 | 1140 | 238.3441 |
| Cond. (µs/cm) |  | 10203 | 300 | 0.003333 | 0.00453 | 34.01 | 0.154063 |
| TSS (mg/L) |  | 40 | 500 | 0.002 | 0.002393 | 0.08 | 0.000191 |
| TDS (mg/L) |  | 1225 | 500 | 0.002 | 0.002393 | 2.45 | 0.005862 |
| DO (mg/L) |  | 4.68 | 5 | 0.2 | 0.239278 | 103.3333 | 24.72543 |
| BOD (mg/L) |  | 119 | 30 | 0.2 | 0.239278 | 2380 | 569.4826 |
| COD (mg/L) |  | 121 | 60 | 0.1 | 0.119639 | 1210 | 144.7634 |
| Cl- (mg/L) |  | 1768 | 250 | 0.004 | 0.004786 | 707.2 | 3.384354 |
| SO42- (mg/L) |  | 307 | 250 | 0.004 | 0.004786 | 122.8 | 0.587668 |
| Surfact. (mg/L) |  | 6.5 | 15 | 0.066667 | 0.079759 | 43.33333 | 3.456244 |
|  |  |  |  |  | i=110Wi=0.905916 |  | i=110WiQr=984.904 |
| WQI = i=110WiQr/i=110Wi = 1087.19 |  |  |  |  |  |  |  |
| Fe | 309 |  | 1 | 1 | 0.007486 | 30900 | 231.3174 |
| Zn | 40.4 |  | 4 | 0.25 | 0.001872 | 1010 | 1.890215 |
| Pb | 20.5 |  | 0.01 | 100 | 0.7486 | 205000 | 153463 |
| Cr | 10.9 |  | 0.05 | 20 | 0.14972 | 21800 | 3263.896 |
|  |  |  |  |  | i=110Wi= 0.907678 |  | i=110WiQr= 156960.1 |
| MPI = i=110WiQr/i=110Wi = 172925 |  |  |  |  |  |  |  |

Table S2	Calculation of water quality Index (WQI) of processing wastewater after adsorption on ACK

| Parameter |  | Observed value(Vo) | Standard value (Sv) | 1/ Sv | Unit weight (Wi) | Quality rating (Qr) | WiQr |
| --- | --- | --- | --- | --- | --- | --- | --- |
| pH |  | 5.85 | 6.5 | 0.153846 | 0.209074 | 230 | 48.08697 |
| Cond. (µs/cm) |  | 187 | 300 | 0.003333 | 0.00453 | 0.623333 | 0.002824 |
| TSS (mg/L) |  | 4 | 500 | 0.002 | 0.002393 | 0.008 | 1.91E-05 |
| TDS (mg/L) |  | 16 | 500 | 0.002 | 0.002393 | 0.032 | 7.66E-05 |
| DO (mg/L) |  | 7.24 | 5 | 0.2 | 0.239278 | 76.66667 | 18.34468 |
| BOD (mg/L) |  | 8 | 30 | 0.2 | 0.239278 | 160 | 38.28454 |
| COD (mg/L) |  | 20 | 60 | 0.1 | 0.119639 | 200 | 23.92784 |
| Cl- (mg/L) |  | 184 | 250 | 0.004 | 0.004786 | 73.6 | 0.352218 |
| SO42- (mg/L) |  | 86 | 250 | 0.004 | 0.004786 | 34.4 | 0.164624 |
| Surfact. (mg/L) |  | 0.25 | 15 | 0.066667 | 0.079759 | 1.666667 | 0.132932 |
|  |  |  |  |  | i=110Wi=0.905916 |  | i=110WiQr=129.2967 |
| WQI = i=110WiQr/i=110Wi = 142.7248 |  |  |  |  |  |  |  |
| Fe | 0.02 |  | 1 | 1 | 0.007486 | 2 | 0.014972 |
| Zn | 0.02 |  | 4 | 0.25 | 0.001872 | 0.5 | 0.000936 |
| Pb | 0 |  | 0.01 | 100 | 0.7486 | 0 | 0 |
| Cr | 0.02 |  | 0.05 | 20 | 0.14972 | 40 | 5.9888 |
|  |  |  |  |  | i=110Wi= 0.907678 |  | i=110WiQr= 6.004708 |
| MPI = i=110WiQr/i=110Wi = 6.615 |  |  |  |  |  |  |  |

Table S3	Calculation of water quality index (WQI) of dishware enameling wastewater before and after adsorption on ACK

| Parameter | Observed value(Vo) | Standard value (Sv) | 1/ Sv | Unit weight (Wi) | Quality rating (Qr) | WiQr |
| --- | --- | --- | --- | --- | --- | --- |
| Before adsorption |  |  |  |  |  |  |
| pH | 3.42 | 6.5 | 0.153846 | 0.088629 | 716 | 63.4583 |
| Cond. (µs/cm) | 908 | 300 | 0.003333 | 0.00192 | 3.026667 | 0.005812 |
| TSS (mg/L) | 130 | 500 | 0.002 | 0.002393 | 0.26 | 0.000622 |
| TDS (mg/L) | 126 | 500 | 0.002 | 0.002393 | 0.252 | 0.000603 |
| DO (mg/L) | 6.96 | 5 | 0.2 | 0.239278 | 79.58333 | 19.04257 |
| BOD (mg/L) | 78 | 30 | 0.2 | 0.239278 | 1560 | 373.2743 |
| COD (mg/L) | 267 | 60 | 0.1 | 0.119639 | 2670 | 319.4367 |
| Cl- (mg/L) | 49 | 250 | 0.004 | 0.004786 | 19.6 | 0.093797 |
| SO42- (mg/L) | 1300 | 250 | 0.004 | 0.004786 | 520 | 2.488495 |
| Surfact. (mg/L) | 5 | 15 | 0.066667 | 0.079759 | 33.33333 | 2.658649 |
| Fe | 80 | 1 | 1 | 1.196392 | 8000 | 9571.136 |
|  |  |  |  | i=110Wi=1.979253 |  | i=110WiQr=10351.6 |
| WQI = i=110WiQr/i=110Wi = 5230.05 |  |  |  |  |  |  |
| After adsorption |  |  |  |  |  |  |
| pH | 6.68 | 6.5 | 0.153846 | 0.088629 | 64 | 5.67225 |
| Cond. (µs/cm) | 59 | 300 | 0.003333 | 0.00192 | 0.196667 | 0.000378 |
| TSS (mg/L) | 7.5 | 500 | 0.002 | 0.002393 | 0.015 | 3.59E-05 |
| TDS (mg/L) | 12 | 500 | 0.002 | 0.002393 | 0.024 | 5.74E-05 |
| DO (mg/L) | 7.05 | 5 | 0.2 | 0.239278 | 78.64583 | 18.81825 |
| BOD (mg/L) | 13 | 30 | 0.2 | 0.239278 | 260 | 62.21238 |
| COD (mg/L) | 22 | 60 | 0.1 | 0.119639 | 220 | 26.32062 |
| Cl- (mg/L) | 17 | 250 | 0.004 | 0.004786 | 6.8 | 0.032542 |
| SO42- (mg/L) | 162 | 250 | 0.004 | 0.004786 | 64.8 | 0.310105 |
| Surfact. (mg/L) | 1.2 | 15 | 0.066667 | 0.079759 | 8 | 0.638076 |
| Fe | 0.24 | 1 | 1 | 1.196392 | 24 | 28.71341 |
|  |  |  |  | i=110Wi=1.979253 |  | i=110WiQr=142.718 |
| WQI = i=110WiQr/i=110Wi = 72.11 |  |  |  |  |  |  |