Supporting Information

Breaking the adverse correlation between thermal stability and electrical insulation in polymer dielectrics by rearranging the donor and acceptor units

Yuting Wan1, Hang Luo1*, Zhongna Yan2, Shuyi Shen1, Jiajun Peng1, Xiaona Li1, Guanghu He1, Dou Zhang1*, Jun-Wei Zha3*

1 State Key Laboratory of Powder Metallurgy, Central South University, Changsha 410083, Hunan Province, P. R. China

2. School of Energy and Power Engineering, Changsha University of Science and Technology, Changsha, Hunan, 410114, P. R. China

3. School of Chemistry and Biological Engineering, University of Science and Technology Beijing, Beijing 100083, P. R. China

E-mail: hangluo@csu.edu.cn, dzhang@csu.edu.cn, zhajw@ustb.edu.cn

The hopping conduction model1, 2

The hopping conduction mechanism is characterized by trapped charge carriers “hopping” from one trap to another within dielectric films, similar to the tunneling effect. The equation of the hopping conduction is expressed as,

J=2nqλv*exp⁡(-EaKBT)sinh⁡(λqE2kBT)

Where n represents the carrier concentration, q denotes the charge of the carrier, λ stands for the hopping distance, v is the attempt-to-escape frequency, Ea is the activation energy of hopping conductance, KB is the Boltzmann constant, T is the absolute temperature, and E is the applied electric field. As A=2nqλv exp⁡(-EaKBT) and B=λqE2kBT, the above equation can be simplified to J=Asinh(BE), where λ can be calculated from the parameters B. A higher correlation coefficient, R², indicates a stronger relationship with the hopping conduction model, while a smaller hopping distance suggests a deeper charge trap depth and a higher charge trap density in dielectric.

Two-parameter Weibull statistic3

Dielectric breakdown property is analyzed using a two-parameter Weibull statistic given by,

PE=1-exp⁡[-(EEb)β]

where, PE represents the cumulative probability of electric failure, E denotes the tested breakdown field, Eb stands for the characteristic breakdown strength of dielectrics corresponding to a cumulative breakdown probability of 63%, and β is a shape parameter related to the scatter of the measured data. A higher value of β indicates improved dielectric reliability.

Figure S1. 1H NMR spectra of a) PEI and b) TPEI polymer precursors.

Figure S2. a) UV-vis spectra and b) Gel contents of TPEI with uncross-linking network (TPEIu) and TPEI.

Figure S3. Surface morphology of PEI and TPEI films observed using an atomic force microscope (AFM).

Figure S4. The cross-sectional SEM views of PEI and TPEI films.

Figure S5. Electrostatic potential distributions and corresponding area percentages for a) PEI and b) TPEI within each electrostatic potential interval. Here, surface areas with |ESP| >10 kcal mol−1 are defined as strong electrostatic interaction areas.

Figure S6. XPS spectra of a) full spectrum, b) O 1s spectrum and c) C 1s spectrum of TPEI and TPEIu samples.

Figure S7. XRD curves of PEI and TPEI films.

Figure S8. Leakage current density of polymer films as a function of electric field at 250 °C.

Figure S9. Unipolar D-E loops of a) PEI, b) 1CH3-PEI, c)2CH3-PEI, e) TPEI measured at 150 ℃.

Figure S10. Unipolar D-E loops of a) PEI, b) 1CH3-PEI, c)2CH3-PEI, e) TPEI measured at 200 ℃.

Figure S11. Weibull distribution data for PEI, 1CH3-PEI, 2CH3-PEI and TPEI at a) 150 ℃ and b) 200 ℃.

Figure S12. Discharged energy density and efficiency for PEI, 1CH3-PEI, 2CH3-PEI and TPEI at a) 150 ℃ and b) 200 ℃.

Figure S13. Unipolar D-E loops of a) BOPP, b) PEI-PSU, c)Kapton, e) FPE measured at 200 ℃.

Figure S14. Unipolar D-E loops of a) TPEI, b) PEI-PSU, c)Kapton, e) FPE measured at 200 ℃.

Figure S15. Unipolar D-E loops of a) TPEI, b) PEI-PSU, c)Kapton, e) FPE measured at 250 ℃.

Figure S16. Discharged energy density and efficiency of TPEI, Kapton, FPE, PEI-PSU at 150 ℃ and BOPP at 120 ℃.

Figure S17. a) Discharged energy density and efficiency of TPEI film as a function of cycle number at 200 ℃. b) Fast discharge testing of TPEI (200 ℃) and BOPP (120 ℃) at 200 MV m-1 and 20 kΩ.

References

1.	Chiu F-C, Lee C-Y, Pan T-M. Current conduction mechanisms in Pr2O3 /oxynitride laminated gate dielectrics. J Appl Phys 105,  (2009).

2.	Chiu F-C. A review on conduction mechanisms in dielectric films. Adv Mater Sci Eng 2014, 1-18 (2014).

3.	Yuan C, et al. Polymer/molecular semiconductor all-organic composites for high-temperature dielectric energy storage. Nat Commun 11,  (2020).