Table 6 Summary of the effect of processing parameters on IMC and joint strength in Ti/Al laser welded joints

| Material and thickness (mm) | Laser welding process parameters |  |  |  | Results |  |  | Refs. |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Joint configuration | Power (W) | Welding speed (mm/s) | Offset (mm) | IMC types and thickness（μm） | IMC Morphology | Joint strength |  |
| Ti6Al4V -6061 Al 2 mm Al-12Si | Butt joint | A: 1600 B: 1900 C: 2200 D: 2500 | 8.33 | - | Ti(Al, Si)3、 Ti5Si3、Ti7Al5Si12 Max 12.00 Min 0.22 | Cellular-shape Serrated-shape Club-shape. | A: 156 MPa B: 241 MPa C: 220 MPa D: 185 MPa | [100] |
| Ti6Al4V-1050 Al 1.2 mm | Butt joint | A: 800/800 B: 800/800 C: 1000/600 | 7.5 | Al side A: 0.4 B: 0.4 C: 0.6 | TiAl3 Max 16.50 Min 1.73 | Lamellar-shaped Serrated-shape Club-shape | A: 139 MPa B: 117 MPa C: 93 MPa | [73] |
| Ti6Al4V-5052 Al 1 mm/1.5 mm | Lap joint (Ti on top) | 1200-2300 | - | - | TiAl2 TiAl3 Unknown | Acicular-shape | Max 2500N Min 490N | [101] |
| Ti6Al4V -6061 Al 2 mm Al-12Si | Butt joint | 1500-3000 | 41.67 | - | TiAl2 TiAl3 Max 1.00 | Lamellar-shaped | Max 213 MPa Min 138 MPa | [19] |
| Ti6Al4V -5754 Al 2 mm | Butt joint | A: 6000 B: 5000 C: 4000 | A: 200 B: 133 C: 88 | - | TiAl TiAl3 Ti3Al Unknown | Lamellar-shaped Island-shaped | A: 158 N/mm B: 166 N/mm C: 220 N/mm | [104] |
| Ti6Al4V -5A06 Al 1.5 mm | Butt joint | 1080-1280 | 8-11 | Al side 0.3-0.7 | TiAl TiAl2 TiAl3 Ti3Al Max 2.79 | Serrated-shaped Lamellar-shaped | Max 183 MPa | [105] |
| pure titanium-1050 Al 0.3 mm | Lap joint (A: Al on top B: Ti on top) | 1000 | 833.33 | - | TiAl2 TiAl3 Unknown | Dendrite- shaped Particle-shaped | Unknown | [106] |
| Ti6Al4V -5754 Al 2 mm/3 mm | Butt joint | 1200 | A: 16.67 B: 33.33 | Ti side 0.1 | TiAl TiAl2 TiAl3 Ti3Al Unknown | Lamellar-shaped Particle-shaped | A: 210 N/mm2 B: 290 N/mm2 | [107] |
| Pure Ti-2024 Al 1 mm | Lap joint (Ti on top) | 2500 | A: 120 B: 150 | - | TiAl3 Unknown | Unreported | A: 105-120 MPa B: 80-95 MPa | [16] |
| T40-5757 Al 1.5 mm | Butt joint | 1500 | A: 41.67 B: 50.00 | Ti side A: 0.75 B: 0.5 | TiAl3 1.00 | Lamellar-shaped | Max 191 MPa | [108] |
| Ti6Al4V -6061 Al 2 mm | Butt joint | 1550 | 41.67 | Ti side 0.3 | TiAl3 Ti3Al Unknown | Club-shape Lamellar-shaped | 167.9 MPa | [109] |
| TA15-5A06 Al 3 mm | Butt joint | 1500 | 25 | Ti side 0.1-0.7 | TiAl TiAl3 Ti3Al 1.0 | Unreported | Max 181 MPa | [110] |
| Ti6Al4V -5754 Al 2 mm | Butt joint | A: 6000 B: 4000 C: 5000 | A: 200 B: 107 C: 110 | Ti side 0.2 | TiAl TiAl2 TiAl3 Unknown | Dendrite- shaped Lamellar-shaped | A: 167 N/mm B: 159 N/mm C: 120 N/mm | [104] |
| Ti6Al4V -5754 Al 2 mm | Butt joint | A: 6000 B: 6000 C: 5000 | A: 200 B: 160 C: 110 | Al side 0.2 | TiAl Unknown | Lamellar-shaped | A: 155 N/mm B: 204 N/mm C: 203 N/mm | [104] |

Table 7 Summary of the effect of treatment on Ti/Al laser welded joints and comparison of joint strength

| Material and thickness (mm) | Laser welding process parameters |  |  |  | Treatment and process parameters | IMC | Joint strength |  | Refs. |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Joint configuration | Power (W) | Welding speed (mm/s) | Offset (mm) |  |  | Before treatment (Max) | After treatment (Max) |  |
| Ti6Al4V -2024 Al 2 mm | Butt joint | 3500 | 70 | Al side 0.7 | Pulsed laser preprocessing Power:120 W Laser speed: 6 mm/s Frequency: 30 kHz | TiAl TiAl3 Ti3Al thickness reduced from 6.12 μm to 1.62 μm | 186 MPa | 259 MPa | [117] |
| Ti6Al4V -5754 Al 2 mm/3 mm | Butt joint | 1200 | A: 16.67 B: 33.33 | Ti side 0.1 | Heat treatments Temperature: 350℃/450℃ Time: 168 h/336 h | TiAl TiAl2 TiAl3 Ti3Al | 290 N/mm2 | 280 N/mm2 | [107] |
| Ti6Al4V -6061 Al 2 mm | Butt joint | 1500 | 41.67 | Ti side 0.1-0.3 | Heat treatment Temperature: 530℃ Time: 2h | TiAl TiAl3 Ti3Al | 178 MPa | 86 MPa | [121] |

Table 8 Summary of the effect of Interlayer on Ti/Al laser welded joints and comparison of joint strength

| Material and thickness (mm) | Interlayer | Laser welding process parameters |  |  |  | IMC |  | Joint strength |  | Refs. |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Joint configuration | Power (W) | Welding speed (mm/s) | Offset (mm) |  | Before adding (Max) |  | After adding (Max) |  |
| Ti6Al4V -5A06 Al 1.5 mm/2 mm | 0.1-0.3 mm AlSi12 foil | Lap joint (Ti on top) | 1200 | 14 | - | TiAl TiAl3 Ti3Al | 1721 N |  | 2405 N | [122] |
| Ti6Al4V -5A06 Al 2 mm | Al–Cu–La fillers | Butt joint (Y Bevels) | Unreported | 1.25 | - | TiAl3 Ti2Al20La | Unreported |  | 270 MPa | [123] |
| Ti6Al4V -5A06 Al 2 mm | Al–Cu–Zr fillers | Butt joint (V Bevels) | Unreported | 1.25 | Ti side 2 | TiAl3 L-(Ti,Zr)Al3 H-(Ti,Zr)Al3 | Unreported |  | 284 MPa | [124] |
| Ti6Al4V -6082 Al 1 mm | CoNiCuNb0.5V1.5 filler | Lap joint (Ti on top) | 660 | 10 | - | VAl3 | Unreported |  | 190 MPa | [125] |
| Ti6Al4V -5052 Al 1 mm | 0.05 mm Zn foil AlSi12 | Lap joint (Al on top) | Unreported | 3.33 | - | TiAl3 TiZn16 | Unreported |  | 180 MPa | [127] |
| Ti6Al4V -Al1Mg0.9Si 3 mm | 0.4/0.7 mm Nb plate | Butt joint | 1000-2500 | 8.33-33.33 | - | TiAl3 NbAl3 | 33 MPa |  | 127 MPa | [53] |
| Ti6Al4V -6082 Al 1 mm | 0.2 mm Nb plate | Butt joint | 3200 | 3.33 | Al side 0.7 | NbAl3 Nb2Al | Unreported |  | 288.97 MPa | [128] |
| Ti6Al4V -6061 Al 2 mm | 0.14 mm Pure tungsten mesh (Diameter of the tungsten wire: 58 μm, the mesh diameter: 100 μm.) | Lap joint (Al on top) | 4000 | 3.33-6.66 | - | Al3(Ti, W) (Al, Si)3Ti | 2830 N |  | 4300 N | [131] |
| TA2-5150 Al 2 mm | Unreported Pure silver mesh (Diameter of silver wires: 40 μm, the mesh diameter: 80 μm) | Lap joint (Al on top) | A: 3300 B: 3500 C: 3700 | 3.33 | - | TiAl3 MgAg MgAgAl | 147.7 MPa |  | 171.4 MPa | [136] |
| Ti6Al4V -6061 Al 2 mm | 0.3 mm | Lap joint (Al on top) | 4000 | 3.33-10 | - | TiAl3 | 3200 N |  | 4505N | [137] |

The interlayer, upo